## Slide 1
M.G. Pellegriti1, A. Musumarra1,2, C. Massimi3, N. Patronis4, J. Balibrea5
R. Mucciola6, M. Spelta7, D. Papanikolau4
1INFN-Sezione di Catania
2Università di Catania
3Università di Bologna and INFN-Sezione di Bologna
4University of Ioannina
5ISIC-Valencia
6INFN-Sezione di Bari
7Università di Trieste
Rivelatori a stilbene per reazioni (n,g) e (n,n’)
d,p
S t i l
Notes: Good evening
Thanks to the organizer of the workshop for the invitation

## Slide 2
Outlook
Motivation for developing the prototype:
- Study of the d-stilbene active target TaraT for the n-n scattering length LoI
- A new detector to replace C6D6 for n-g
- n-n’ measurements
Stilbene scintillators developed at INFN-Sezione di Catania
The Stilbene–D12 developed for TARAT, LLNL crystal tested with SiPM at Demokritos in 2021 and at CERN
The d-Stil prototype, INRAD Crystal
The p-stil detectors (n. 4) INRAD ScintinelTM crystals
Issues arisen in performing an INFN indipendent analysis and pulse shape analysis on the last tests @ n_TOF
New stilbene crystal provider found !!
n. 4 p-stil detectors (n. 4) PROTEUS crystals assembly and test ongoing @ INFN CT
n_TOF Meeting Collaborazione Italiana, Trieste, 9-10 Novembre 2023

## Slide 3
“Big” C6D6 Liquid scintillators
Large & segmented C6D6
Solid organic scintillators
Read-outs/Power supplies
Solid
Higher density
No Chemical hazard
n/g discrimination
Compact array of small C6D6
Motivation for developing the prototype

## Slide 4
Stilbene characteristics
Linear response in energy
n_TOF Meeting Collaborazione Italiana, Trieste, 9-10 Novembre 2023
g / n discrimination

## Slide 5
Stilbene scintillators developed @ INFN-Sezione di Catania
Name | Crystal | Producer | Dimension | Sensor | INTC-LoI | Spokes
TARAT | deuterated | LLNL | 26 x 23 x 11 mm3 | n. 4 SiPM | INTC-I-220 | Massimi, Musumarra Patronis
d-stil | protonated | INRAD | 31.75mmx 10mm | PMT |  | Massimi, Musumarra Patronis
p-stil (n. 4) | protonated | INRAD-ScintinelTM | 1inchx1inch | PMT | INTC-I-254 | Musumarra Balibrea
p-stil (n.4) | protonated | PROTEUS | 1inchx1inch | PMT |  | 
n_TOF Meeting Collaborazione Italiana, Trieste, 9-10 Novembre 2023
Brand new !!

## Slide 6
 | 2020 |  | 2021 |  | 2022 |  | 2023 | 
 | 1sem | 2sem | 1sem | 2sem | 1sem | 2sem | 1sem | 2sem
TARAT Stilbene D12 SiPM – LoI CERN n-n scattering lenght: Cristian, Agatino, Nikolas |  |  |  |  |  |  |  | 
Crystal Procurement: Nikolas from N. Zaitseva @ LLNL |  |  |  |  |  |  |  | 
Active Target Development: Agatino |  |  |  |  |  |  |  | 
Test @ Demokritos: Agatino, Cristian + test @ CERN |  |  | Demokritis | EAR2-EAR! |  |  |  | 
Analysis of Demokritos data: Cristian, Agatino, Maria Grazia |  |  |  |  |  |  |  | 
Geant4 Simulations: Cristian, Riccardo – D break-up M.G. |  |  |  |  |  |  |  | 
Draft on Demokritos data: Cristian, Nikolas, Agatino, Maria Grazia |  |  |  |  |  |  |  | 
d-stil (INRAD)  protonato |  |  |  |  |  |  |  | 
Crystal Procurement: Nikolas from INRAD for n-n LoI |  |  |  |  |  |  |  | 
Development-Assembly: Agatino |  |  |  |  |  |  |  | 
Test @ CERN: Agatino, Nikolas |  |  |  |  |  |  |  | 
Analysis: Javi, Cristian, Riccardo |  |  |  |  |  |  |  | 
p-stil (INRAD- ScintinelTM) n.4 |  |  |  |  |  |  |  | 
Procurement - Assemblaggio: INFN CT |  |  |  |  |  |  |  | 
CERN LoI: Agatino, Javi and test@CERN: Agatino, Javi, Cristian |  |  |  |  |  |  |  | 
Analysis: Javi, Cristian, Michele |  |  |  |  |  |  |  | 
p-stil (new provider - PROTEUS) n. 4 |  |  |  |  |  |  |  | 
Procurement – Assemblaggio: INFN CT |  |  |  |  |  |  |  | 
Test: gamma source @ INFN CT |  |  |  |  |  |  |  | 
Analisi: Dimitris (Erasmus Training student ) |  |  |  |  |  |  |  | 
Activities timeline

## Slide 7
d-Stilbene
2 HAMAMATSU 6x6
2 AdvanSid 4x4
TaraT test run at NCSR Demokritos (Athens) June 2021
thanks to
Natalia P. Zaitseva
LLNL
26 x 23 x 11 mm3
) -)) + (1-⍴) *() -)))
Signal parametrization
n_TOF Meeting Collaborazione Italiana, Trieste, 9-10 Novembre 2023

## Slide 8: Neutron gate
Fast/Slow analysis
AVANSID 1
Integral of Fit function
QFAST
QTOT
QFAST/QTOT
QTOT
AVANSID 1
QTOT
----FIT
----No FIT
N_TOF Collaboration Meeting, Edinburgh, 13-14 December 2022
Ebeam=15MeV
Windows from leading-edge: 25 ns for QFAST and 430 ns for QTOT
Draft to be finished and submitted at the begininng of 2024!
SIMULATION by Riccardo
Detector response conv. must be included

## Slide 9
3.5 cm
HAMAMATSU R1924A
Sens-Tech PS1807
Ultra compact active base
with DC-DC converter
no HV needed
n_TOF Meeting Collaborazione Italiana, Trieste, 9-10 Novembre 2023
d-stil prototype

## Slide 10
N_TOF Collaboration Meeting, Edinburgh, 13-14 December 2022
First test @ EAR2 – June 2022

## Slide 11
By Javi Balibrea
Analysis
ToF spectras for DSTI and STED have similar shape
ToF spectra normalized to saturated resonance
n_TOF Meeting Collaborazione Italiana, Trieste, 9-10 Novembre 2023

## Slide 12
By Riccardo Mucciola
New setup HV=600 V
Second test during Mo(n,g) measurement in EAR2
n_TOF Meeting Collaborazione Italiana, Trieste, 9-10 Novembre 2023

## Slide 13
1”x 1” 4 cylindrical INRAD p-stilbene detectors +
1 d-stilbene assembled in carbon fiber housing
137Cs
N_TOF Collaboration Meeting, Edinburgh, 13-14 December 2022
The p-stil detectors (n. 4) INRAD ScintinelTM crystals

## Slide 14
n_TOF Meeting Collaborazione Italiana, Trieste, 9-10 Novembre 2023
LoI for stilbene detector development @ n_TOF – April 2023

## Slide 15
Legnaro C6D6
LLNL d-stilbene
EAR2 proposed set-up - May 2023

## Slide 16
n_TOF Meeting Collaborazione Italiana, Trieste, 9-10 Novembre 2023
EAR2 May 2023 set-up

## Slide 17
Detector | Rise time [ns] | Pulse width [ns]
L6D6 | 8 | 40
sTED | 4.4 | 24
DSTI-1 | 3 | 23
DSTI-2 | 3.3 | 19
PSTI | 4.4 | 24
Rise time: 10%-->90%
Pulse Width: 10% →10%
Average pulse shape calculated from 88Y calibration source
LLN –ISIC
1stINRAD
2ndINRAD
3.8-3.9ns
by Dimitris Papanikolau
Catania-October 2023
by Javi Balibrea – talk n_TOF coll. meeting May 2023
Detectors’ pulse shape analysis (only ɣ)

## Slide 18
All linear Energy calibrated!
Small crystals→ Low threshold
Deposited energy calibration
by Javi Balibrea – talk n_TOF coll. meeting May 2023

## Slide 19
197Au(n,ɣ) saturated resonance to establish relative efficiency between detectors
197Au(n,ɣ) saturated resonance
by Javi Balibrea – talk n_TOF coll. meeting May 2023

## Slide 20
Empty subtracted C low intensity pulses
2x106
3x106
4x106
7x106
by Javi Balibrea – n_TOF coll. meeting May 2023
Carbon target
n_TOF Meeting Collaborazione Italiana, Trieste, 9-10 Novembre 2023
-agreement of PSTI-90 with STED
-angular distribution effects shown by PSTI-135!
-still no pulse shape analysis still provided
-need of an INFN independent analysis to evaluate
the performance of the detectors with respect to
Spanish group analysis (very fast and efficient)
-limit in neutron discrimination for future n.n’ exp.

## Slide 21
Fast/slow analysis on AmBe source file (test EAR2 – May 2023)
by Michele Spelta
n_TOF Meeting Collaborazione Italiana, Trieste, 9-10 Novembre 2023

## Slide 22
n_TOF Meeting Collaborazione Italiana, Trieste, 9-10 Novembre 2023
Open issues on analysis of stilbene test
-agreement of PSTI-90 with STED!
-angular distribution effects already shown by PSTI-135!
-still no pulse shape analysis provided to perform n/g discrimination for background subtraction
or n, n’ measurements
-need for an independent analysis to evaluate the performance of the detectors

## Slide 23
New stilbene crystals from PROTEUS: first tests October 2023
by Dimitris Papanikolau
n_TOF Meeting Collaborazione Italiana, Trieste, 9-10 Novembre 2023

## Slide 24
New stilbene crystals from PROTEUS: first tests October 2023
by Dimitris Papanikolau
n_TOF Meeting Collaborazione Italiana, Trieste, 9-10 Novembre 2023
Agreement between INRAD and PROTEUS Crystal concerning the shape of deposited energy obtained by 60Co or 137Cs
n/g pulse shape analysis to be tested with AmBe

## Slide 25
n_TOF Meeting Collaborazione Italiana, Trieste, 9-10 Novembre 2023
Conclusions
p-stilbene are new promising detectors to replace C6D6 for n-g and to perform n-n’ measurements
N. 4 INRAD + n.4 PROTEUS modules soon avaliable
TO DO:
To finish the analisyis of the n.4 INRAD crystal (June test in EAR2): estimate background and signal characterization, in particular to check pulse shape analysis
Assembly and Characterize the new p-stil detectors (n. 4) PROTEUS crystals (new provider!!)
- BUT no new proposal or LoI can be supported in EAR2 or EAR1 before finishing the present analysis!