## Slide 1
Possible use of LaBr3 scintillators for (n,xn) reactions at n_TOF
Paolo Finocchiaro

## Slide 2
A short historical recall
proposed in May 2016
basically rejected with the statement:
"LaBr3 was tested and cannot be used at n_TOF"

## Slide 3
Material | BaF2 |  | LaBr3(Ce)
Density (g/cc) | 4.88 |  | 5.1
< Z > | 24.7 |  | 40.5
Light yield (photons/MeV) | 10000 | 2000 | 70000
Decay time (ns) | 620 | 0.6 | 30
Emission Peak (nm) | 310 | 220 | 375
Hygroscopic | NO |  | YES
Main features of LaBr3 as compared to BaF2
NUMEN LaBr3 detector samples

## Slide 4
High rate NUMEN test (active PMT base)
LaBr3
SiB
Detection of 473 keV gamma from n+10B in coincidence with the alpha
AmBe 1.5·106 n/s emitted
59 keV gamma from Am (34 GBq)
4.4 MeV gamma from 9Be(a,n)
2.2 MeV gamma from H(n,g)D
1.47 MeV
0.84 MeV
0.473 MeV
SiB = Silicon + 10B

## Slide 5
SiB spectrum, simulated and measured
High rate NUMEN test
free run
free run

## Slide 6
High rate NUMEN test
coincidence run
coincidence run
473 keV
coincidence scatter plot
473 keV

## Slide 7
Energy calibration
quite linear at low HV
non-linearity at high HV and/or high rate
may need a better active base

## Slide 8
287ns
En = 350 MeV
sample waveform from a preliminary test at n_TOF