## Slide 1: Pulsed laser melting as a tool for crystal bending in crystalline light source application
D. De Salvador1,2, F. Sgarbossa1,2, D. Valzani 1,2. G. Maggioni1,2 , C.Carraro1,2, E. Napolitani1,2
1 Dipartimento di Fisica e Astronomia, Università di Padova, Via Marzolo 8, I-35131 Padova, Italy davide.desalvador@unipd.it
2 National Institute for Nuclear Physics INFN, Laboratori Nazionali di Legnaro, Viale dell’Università 2, 35020 Legnaro, Italy
Semiconductor and Advanced Crystals group

## Slide 2
LNL-INFN

## Slide 3
Ge applications
g-Ray detectors
Plasmonic molecular sensors
Lasers
Nanoelectronics
Channeling
Photovoltaic/ThermoPV
D. De Salvador
Notes: Germanium is one of the most studied semiconductor materials nowadays. In particular, there are already in commerce some germanium based device, but there are a lot of studies to implement Ge in others application. All of these application requires a high doping concentration and shallow junction; for these reason our research group try to develop new germanium doping methods.
thanks to its very good optical and electrical properties and also thanks to its compatibility with silicon technology.
The new technological request from all these application fields has some common ground and one of the most important is the needs of developing new doping methods, in order to have high doping concentration and shallow junction.
Moreover, Ge has the most high hole mobility of all semiconductors materials and also an higher electron mobility respect to silicon, making Ge the most interesting material for Complementary MOS devices, the units of all our electronical devices like computer, smartphones and all cpu based devices.

## Slide 4
Ge application
g-Ray detectors
Plasmonic molecular sensors
Lasers
Nanoelectronics
Highest-z crystals with no dislocation
Photovoltaic ThermoPV
D. De Salvador
Channeling

## Slide 5: Ge channeling for 400GeV Protons
De Salvador et al.
De Salvador et al.

## Slide 6: 850MeV electrons, deflection and radiations with bent crystals at MAMI
Sytov et al. Eur. Phys. J. C (2017) 77:901
Bandiera et al. Eur. Phys. J. C (2021) 81:284

## Slide 7
Doping issues - applications
g-Ray detectors
Plasmonic molecular sensors
Lasers
Nanoelectronics
D. De Salvador
Photovoltaic cells
High doping
Strain control
High purity
Channeling

## Slide 8: PLM – Pulsed Laser Melting technique
KrF Laser at DFA:
248 nm, ~1 J/cm2, 22 ns pulses
22ns
David Sands, DOI: 10.5772/28736
5x5 mm homogeneous spot

## Slide 9: Melting regime
David Sands, DOI: 10.5772/28736
When laser energy density is high enough melting temperature Tm is exceeded, melting occurs.
Tm
Fast liquid phase epitaxy

## Slide 10: Melting regime
David Sands, DOI: 10.5772/28736
Fast liquid phase epitaxy
Tm
Tm
Impurities fast diffuse in the liquid
If an impurity source in placed on the sample surface:
T
c

## Slide 11: Impurity diffusion and incorporation
Tm
Tm
If an impurity source in placed on the sample surface:
Impurities fast diffuse in the liquid
Impurities incorporate under non equilibrium conditions during fast regrowth
]
T
c
T
c

## Slide 12
Sb incorporation in Ge (100) by PLM
13 at%
Carraro et al. Appl. Surf. Sci 509 145229 (2020).
Electrical activation
Carraro et al. Appl. Surf. Sci 509 145229 (2020).

## Slide 13
n-type
exp.
exp.
Sb incorporation in germanium by PLM
Electrical activation
Carraro et al. Appl. Surf. Sci 509 145229 (2020).

## Slide 14
Sb strain in Germanium
Strain defects

## Slide 15: Substrate bending–Stoney formula for perfect epitaxial layers
For a pseudomorphic film with elastic properties similar to the bulk:

## Slide 16: PLM strain optimization
Multi-parametric optimization:
  Orientation (110) and (111) good channeling planes
  Sb precursor thickness
  Pulse Energy
  Number of Pulse repetitions
HRXRD analyses on thick (110) and (111) wafers
Bending analyses on thin (110) test samples
8KeV HRXRD diffractometer
Stylus profilometer

## Slide 17
-0.09 -0.06 -0.03 0 0.03 0.06 0.09
Tilt (°)
-0.09 -0.06 -0.03 0 0.03 0.06 0.09
Tilt (°)
Bragg angle offset (°)
-0.21 -0.14 -0.07 0.00 0.07
Bragg angle offset (°)
-0.15 -0.10 -0.05 0.00 0.05 0.10
2nm Sb on (110) 700mj 8pls
7nm Sb on (110) 500mj 8pls
HRXRD reciprocal space mapping of the film
Tilt
Lattice parameter deformation
Tilt due to defects

## Slide 18
Chart: 2nm 700mJ/cm2 (110)
| 0 | 100 | 200 | 248.3 | 351.9
8pls | 0.224 | 0.217 | 0.11 | 0.064 | 0
2pls | 0.308 | 0.274 | 0.117 | 0.018 | 0.007
Rocking curve simulations
(110) 2nm 700mj/cm2
2pls
(110) 2nm 700mj/cm2
8pls
Chart: 6nm 700mJ/cm2 (111)
| 0 | 70 | 140 | 210 | 301.60000000000002 | 308.82000000000005 | 309
8pls | 0.34 | 0.348 | 0.313 | 0.216 | 0.068 | 0.18 | 0
2pls | 0.394 | 0.363 | 0.205 | 0.01 | 0.0014 | 0
(111) 6nm 700mJ/cm2
8pls
(111) 6nm 700mJ/cm2
2pls

## Slide 19
Chart: 2nm Sb on (110)
| 2 | 8 | 2 | 8 | 2 | 8 | 16 | 2 | 8 | 20
No defects | 400 | 400 | 500 | 500 | 700 | 700 | 700 | 900 | 900 | 1500
Defects | 900
Chart: 2nm Sb on (110)
| 2 | 8 | 2 | 8 | 2 | 8 | 16 | 2 | 8 | 20
No defects | 400 | 400 | 500 | 500 | 700 | 700 | 700 | 900 | 900 | 1500
Defects | 900
Chart: 4nm Sb on (110)
| 8 | 20
No defects | 400 | 1500
Defects | 400 | 500 | 500 | 700 | 700
Chart: 4nm Sb on (110)
| 8 | 20
No defects | 400 | 1500
Defects | 400 | 500 | 500 | 700 | 700
Chart: 7 nm Sb on (110)
| 20
 | 1500
Defects | 400 | 500 | 700 | 700 | 700
Chart: 7 nm Sb on (110)
| 20
 | 1500
Defects | 400 | 500 | 700 | 700 | 700
Chart: 2nm Sb on (111)
| 2 | 8 | 2 | 8 | 2 | 8 | 20
No defects | 400 | 400 | 500 | 500 | 700 | 700 | 1500
Defects
Chart: 2nm Sb on (111)
| 2 | 8 | 2 | 8 | 2 | 8 | 20
No defects | 400 | 400 | 500 | 500 | 700 | 700 | 1500
Defects
Chart: 4 nm Sb on (111)
| 2 | 8 | 2 | 8 | 2 | 8 | 20
 | 400 | 400 | 500 | 500 | 700 | 700 | 1500
Defects
Chart: 4 nm Sb on (111)
| 2 | 8 | 2 | 8 | 2 | 8 | 20
 | 400 | 400 | 500 | 500 | 700 | 700 | 1500
Defects
Chart: 6 nm Sb on (111)
| 2 | 8 | 16 | 2 | 8 | 16 | 2 | 8 | 2 | 8 | 20
 | 400 | 400 | 400 | 500 | 500 | 500 | 700 | 700 | 900 | 900 | 1500
Defects | 700 | 900 | 900
Chart: 6 nm Sb on (111)
| 2 | 8 | 16 | 2 | 8 | 16 | 2 | 8 | 2 | 8 | 20
 | 400 | 400 | 400 | 500 | 500 | 500 | 700 | 700 | 900 | 900 | 1500
Defects | 700 | 900 | 900
, no defects
defects

## Slide 20: Curvature measurement on thin (110) samples
2nm Sb , (110) 500mJ 8pls
2nm Sb , (110) 700mJ 8pls
Parabolic fit

## Slide 21: Curvature measurement on thin (110) samples
Chart: Process
| 2nm 500mj 8pls | 2nm 700mj 8pls | 7-6 nm 700mj 2pls | 7-6 nm 700mj 8pls
Stylus (110) to [1-10] | 19.2174 | 16.9565 | 19.4427 | 23.024
Stylus (110) to [001] | 20.4348 | 14.1739 | 15.8465 | 13.1142
HRXRD/Stoney (110) | 19.895 | 14.605
Defects

## Slide 22: Curvature measurement on thin (110) samples
Chart: Process
| 2nm 500mj 8pls | 2nm 700mj 8pls | 7-6 nm 700mj 2pls | 7-6 nm 700mj 8pls
Stylus (110) to [1-10] | 19.2174 | 16.9565 | 19.4427 | 23.024
Stylus (110) to [001] | 20.4348 | 14.1739 | 15.8465 | 13.1142
HRXRD/Stoney (110) | 19.895 | 14.605
HRXRD/Stoney (111) | 15.587 | 13.1419 | 13.4048 | 8.626
Defects

## Slide 23
Lithography strategies with PLM for periodically bent crystals
Homogenizing optics
X4 image plane
30 mm resolution is expected with actual optics
Laser pattern lithography
Sample lithography
Heidelberg mMLA,
Direct laser riter
1 mm resolution

## Slide 24
Lithography strategies with PLM for periodically bent crystals
Homogenizing optics
X4 image plane
30 mm resolution is expected with actual optics
Laser pattern lithography
Sample lithography
Suorce layer can be patterned by photolitography
Heidelberg mMLA,
Direct laser riter
1 mm resolution

## Slide 25: Patterning FEM simulations
uz
(nm)
ON/OFF patterning
COS patterning

## Slide 26: Conclusions
High quality homogenous straining layers can be created by PLM on (110) Ge. Even higher strain can be obtained in (111) Ge.
Lateral tailoring of layer patterning can be exploited by lithography techniques
Perspectives
Patterning fabrication
Curvature tests on thin (111) Ge
More detailed curvature test by synchrotron techniques.
Simulation of radiation emission starting by FEM deformation calculation of by PBC.

## Slide 28
mm