## Slide 1
New design for Boron-doped diamond undulator
Modelling, Growth, characterization
Thu Nhi Tran CALISTE @ ESRF

## Slide 2
Old model
@ Mainz
New model
@ MBN
Diamond
Diamond
[B]
[B]
1 period
1 period
Initiating with a two-layer sample for testing purposes, due to the increased thickness of each layer in the new model.
Fabrication: Done
Characterization : Done
MAMI measurement
Key parameters:
Layers thickness
Doping profile
Doping extremums
For more information about the new model design@ Andrey V.Solov’yov
Period thickness: (100): 3.75 µm  (110): 5 µm
Period thickness: (100): 14.14 µm  (110): 15 µm
5 µm
15 µm
No channeling signal, do we continue???
2020
2023

## Slide 3: Characterization steps for the new model
Substrate
Growth
Surface characterization
SIMS
Synchrotron characterization
Measurement at MAMI

## Slide 4: Growth: MPCVD PROCESS
Simplified schematic of the MPCVD principle
Ultra high Vacuum of 10-6 Torr inside the MPCVD reactor chamber
Diamond substrate temperature: 850°C
Microwave power: 300W
Microwave pressure: 33 Torr
Hydrogen flow: 100sccm
Methane flow: 4sccm (3.5% methane in the mixture)
Diborane flow is set by a GBF that follows the doping profile determined previously
Growth rate: 25nm/min

## Slide 5: Substrate
Subtract: HPHT Ib standard quality diamond, (100) surface, dislocations density ~102/cm2
The sample's color darkened as a result of the Boron doping process, given that Boron itself possesses a dark hue.
The sample surface after doping.
The starting diamond substrate.
Thickness:
Dislocation density: 103/cm2

## Slide 6
The substrate’s surface characterization of the samples before the growth process .
Backside of the sample
The surface is dominated by the polishing lines and waves induced by the mechanical polishing

## Slide 7
Front side of the sample
By doping the diamond with Boron, Hillocks are formed at the sample’s surface
The surface characterization of the sample after the growth process .

## Slide 8: Surface characterization
Hillocks density | 
Hillocks size (diameter): | 
Hillocks density | 
Hillocks size (diameter): | 
Non uniform surface
More uniformity at the center
Hillocks aligning with the polishing lines on the substrate surface
center
borders
near center

## Slide 9
Old sample
New sample
Growing thicker layers introduces fewer hillocks on the surface with a larger size
Growth process is improving
2020
2023

## Slide 10: Characterization of the new sample
Non-flat surface with very tiny circular figures in the nanometer range on the top surface of the sample.

## Slide 11: Hillocks
Heavily boron-doped diamond grown on scalable heteroepitaxial quasi-substrates: A promising single crystal material for electrochemical sensing applications.
The introduction of Boron atoms disrupts the crystal lattice, creating localized stress points.
The stress points lead to the migration of atoms and the accumulation of material at certain locations on the diamond surface, resulting in the formation of hillocks.

## Slide 12
Synchrotron characterization:
Rocking Curve Imaging techniques at BM05 - ESRF

## Slide 13
Diamond
[B]
Only two-layers sample for testing purposes
From the X-ray Bragg diffraction point of view:
In this case the variation of the effective misorientation d over the extinction length L is of the order of the intrinsic diffraction width wD.
The layer is therefore, not anymore expected to diffract “kinematically” and the “distorted regions” could exhibit a higher integrated intensity than the “perfect crystal matrix”
14.14 µm

## Slide 14: Characterization: Bragg diffraction imaging
Lattice parameter of the layer > lattice parameter of the substrate
substrate
layer
Rocking curves of the layer and substrate separated
The layers display, around an « average lattice parameter » dlayer , a range of lattice parameters (Dd/d) associated to the variation of the doping
FWHM of the peak of the layer ~ (Dd/d) tgq
    Bragg’s law 2dhklsin = 
    dhkl distance between reflecting planes
     angle beam - reflecting planes
     Wavelength of X-rays
layer < substrate
Reflection mode
Transmision mode

## Slide 15: Relaxed or strained layer
è the rocking curves for the layer and the substrate are closer, and can even merge
If the layer is not completely relaxed (usual case) the « average lattice parameter » daverage is strained by the interface with the undoped diamond, and is consequently smaller than the one corresponding to a free doped crystal
layer
substrate
Each of the layers is grown on the previous one, which displays an « average lattice parameter » daverage that is bigger than the one of the substrate è the successive layers can therefore exhibit increasing daverage , and peaks that are increasingly displaced with respect to the one of the substrate
1
2
3
1
2
3
è the successive layers can be associated to peaks on the rocking curve that are increasingly displaced towards small q
substrate

## Slide 16
Global Rocking Curve / Reflection case
FWHM 0.02°, as before, but « more uniform » peak
substrate
layer
layer
degree

## Slide 17
1.2mm
1.6 mm
RC in reflection
Beam width ~0.5 mm
Substrate only
Substrate + layer
Layer only
Integrated intensity map
1.2 mm
Tentative Preliminary conclusions:
- Observation of dislocations in the substrate ( ~2 x 103 cm-2 )
- Small curvature (upper to the lower part) of the substrate (R ~ 40 m)
- Vertical lines on the layer image : dislocations?

## Slide 18
RCI maps in transmission mode
1.2mm
1.2mm
Integrated Intensity
Peak Position
We mainly see a large scale waviness of the layer planes (pseudo period ~0.5 mm; ~75 µm for the « old design »)
This waviness implies a variation of the angular position of the reflecting planes that is ~ 6 arcseconds

## Slide 19
The “old design” :
1) 2 layers exhibit an average lattice parameter that increases when the layer departs from the substrate. These layers are only partially relaxed and display an “egg foam crate” like curvature that could help accommodating the variation of lattice parameter.
2) Similar features for the “old design” 4 layers The “new design”:
for the Boron-doped diamond appears to be associated with changes in the observed features (preliminary):
dislocations are observed on the “substrate only” image, and maybe also (as vertical lines) on the “layer only” image.
2) the waviness is a large scale one with a “period” one order of magnitude bigger than for the “old design”
Present Conclusions

## Slide 20: Characterization steps for the new model
Substrate
Growth
Surface characterization
Synchrotron characterization
SIMS
6. Measurement at MAMI ( for 4 periods)