## Slide 1
Fabbricazione di Q-bit 3d
Francesco Mattioli
Fabio Chiarello

## Slide 2
Francesco Mattioli, Fabio Chiarello
Q-bit 3D
High resistivity 4 inch Wafer
Thickness 650-670 mm
Chip 14mm x 2mm
Notes: 2

## Slide 3
Francesco Mattioli, Fabio Chiarello
Q-bit 3D
High resistivity 4 inch Wafer
Thickness 650-670 mm
Chip 14mm x 2mm
Geometry
Radius 500 mm
Distance 486 mm
Notes: 3

## Slide 4
Francesco Mattioli, Fabio Chiarello
Q-bit 3D
High resistivity 4 inch Wafer
Thickness 650-670 mm
Chip 14mm x 2mm
Geometry
Square 556x144 mm
Distance 20 mm
Notes: 4

## Slide 5
Francesco Mattioli, Fabio Chiarello
Q-bit 3D
Bilayer
COP 33 10% AR-P ≈ 1mm
    3500 giri/min per 60”
Hot Plate 5’ @ 170 °C
PMMA 6% AR-P 669.06 ≈ 1mm
    3000 giri/min per 60”
Hot Plate 5’ @ 170 °C
100 Å Al (anticharging)
O2 5 min. 1.0 mbar
155° 600 Å Al
90° 700 Å Al
Notes: 5

## Slide 6
Francesco Mattioli, Fabio Chiarello
Q-bit 3D
First results
Circular geometry
Giunction
170x420nm
Angle and geometry to be optimized
Notes: 6

## Slide 7
Francesco Mattioli, Fabio Chiarello
Q-bit 3D
First results
Square geometry
Litography, angle and geometry to be optimized
Notes: 7

## Slide 8
Francesco Mattioli, Fabio Chiarello
Risuonatori
High resistivity 4 inch Wafer
Thickness 650-670 mm
Chip 25mm x 50mm
10mm capacitance gap
Notes: 8

## Slide 9
Francesco Mattioli, Fabio Chiarello
Risuonatori
Bilayer for Lift off approach
PMMA 6% AR-P 669.06 ≈ 1mm
3000 giri/min 60”
    Hot Plate 5’ @ 170 °C
HSQ
  1500 giri/min 60” ≈ 0,3mm
    Hot Plate 2’ @ 150 °C
    Hot Plate 2’ @ 220 °C
100 Å Al (anticharging)
Advantages:
Less exposure time
No metal contamination on the surface
Notes: 9

## Slide 10
Francesco Mattioli, Fabio Chiarello
Risuonatori
1500 Å Al and lift off
Advantages:
Less exposure time
No metal contamination on the surface
Notes: 10

## Slide 11
Francesco Mattioli and Fabio Chiarello
“Fabbricazione di Q-bit 3D”
25/10/2023
Thank you for your attention!