## Slide 1
Speaker:
Giovanni Marconato
QubIT JOINT MEETING
Aluminum resonant cavities development for 3D transmon application
Giovanni Marconato

## Slide 2
Outline
Design of a 7.46 GHz cavity
Fabrication using
pure Al vs Al alloy
Characterization of the Cavity + Qubit
Fabrication improvements
Introduction

## Slide 3
Outline
Design of a 7.46 GHz cavity
Fabrication using
pure Al vs Al alloy
Characterization of the Cavity + Qubit
Fabrication improvements
Introduction

## Slide 4
Introduction
Most common application is particle accelerators
Important parameters:
Cavity Quality factor (Q0 )
Accelerating field
2 K or 4.2 K operation temperature
Important parameters:
mK operation regime
Cavity Quality factor (Q0 )
Quantum computing and sensing
Depends on shape and frequency
Depends on material/surface treatments
Superconducting Resonant Cavities
Notes: Definisci qui il quality factor come larghezza del picco di trasmissione alla risonanza

## Slide 5
Quantum Computing
Transmon qubit
P. Krantz, et al., Applied Physics Reviews, vol. 6, fasc. 2, giu. 2019
Josephson junction
Capacitor
Al

## Slide 6
Quantum Computing
Qubit coherence time evolution
M. Kjaergaard et al., Annu. Rev. Condens. Matter Phys., vol. 11, fasc. 1, mar. 2020

## Slide 7
Outline
Design of a 7.46 GHz cavity
Fabrication using
pure Al vs Al alloy
Characterization of the Cavity + Qubit
Fabrication improvements
Introduction

## Slide 8
Cavity Design
22 mm
40 mm
20 mm
a
c
b
Antenna 1
Antenna 2
Shape optimization
detuning from qubit at

## Slide 9
Cavity Design
=
Using experimental value of for the aluminum alloy cavity
Only experimentally measurable
Surface resistance estimation

## Slide 10
Cavity Simulation
Lorentzian fitting function
Cavity
S11
1
2
Cavity
S21
1
2
Scattering parameters simulations @7.46 GHz
Transmitted power
Reflected power

## Slide 11
Cavity Simulation
Source | 
Eigenmode | 
Modal Network | 
Experimental | 
Source | 
Eigenmode | 
Modal Network | 
Experimental | 
Lower bound for next cavity performance
Move to Al 5N (99.999% purity)
Simulation can reproduce experimental values
Al alloy
Alloy cavity and qubit
fabricated at TII
(Arab Emirates)
Error most likely due to fit

## Slide 12
Outline
Design of a 7.46 GHz cavity
Fabrication using
pure Al vs Al alloy
Characterization of the Cavity + Qubit
Fabrication improvements
Introduction

## Slide 13
Cavity Fabrication
Tumbling
Electropolishing
Mechanical Machining
𝐻3𝑃𝑂4 : 𝐵𝑢𝐴𝑐
Qubit chip accommodation
Machining defects

## Slide 14
Outline
Design of a 7.46 GHz cavity
Fabrication using
pure Al vs Al alloy
Characterization of the Cavity + Qubit
Fabrication improvements
Introduction

## Slide 15
Cavity Characterization
Already better
than Al alloy cavity!
S11
S21
Scattering parameters results
All measures at 30 mK
Cavity
1
2
Cavity
1
2
7.46 GHz
7.46 GHz
13.98 GHz
13.98 GHz

## Slide 16
Qubit Characterization
Cavity characteristic time
Rabi spectroscopy
Pump power -28 dB
t [μs]
Ramsey spectroscopy
Pump detuning 600 kHz
t [μs]
(Al alloy cavity)

## Slide 17
Qubit Characterization
Cavity
Qubit
M. Kjaergaard et al., Annu. Rev. Condens. Matter Phys., vol. 11, fasc. 1, mar. 2020

## Slide 18
Outline
Design of a 7.46 GHz cavity
Fabrication using
pure Al vs Al alloy
Characterization of the Cavity + Qubit
Fabrication improvements
Introduction

## Slide 19
Cavity Fabrication
Tumbling
Electropolishing
Mechanical Machining
𝐻3𝑃𝑂4 : 𝐵𝑢𝐴𝑐
Critical step

## Slide 20
Cavity Fabrication
Mechanical Machining
Problem is pure aluminum toughness
Try cold machining
Cooling Al in N2(l)
Toughness measurements show no improvement

## Slide 21
Cavity Fabrication
Mechanical Machining
Problem is pure aluminum hardness
Try cold machining
Cooling Al in N2(l)
Toughness measurements show no improvement
Change machining parameters
Slower process and new tools

## Slide 22
Cavity Fabrication
Tumbling
Mechanical Machining
Ongoing in this moment
…
…

## Slide 23
Cavity Fabrication
Tumbling
Electropolishing
Mechanical Machining
𝐻3𝑃𝑂4 : 𝐵𝑢𝐴𝑐
Ongoing in this moment
…
…
Evaluating alternatives:
Plasma Electrolytic Polishing

## Slide 24
Conclusions
Source | or *
Al alloy cavity | 
Pure Al cavity* | 
Source | 
Al alloy cavity | 
Pure Al cavity* | 
The quality factor of the new Pure Al cavity is higher than the previous Al alloy cavity
The critical step proved to be mechanical machining from the pure Al cylinder
Improvements on the machining process are ongoing at LNL
The next prototype will be ready shortly
Al alloy
Pure Al #1
Pure Al #2

## Slide 25
Future Developments
Source | 
Eigenmode | 
Modal Network | 
Source | 
Eigenmode | 
Modal Network | 
Fabrication and surface treatments improvements on the 7.46 GHz
Scaling to 8.50 GHz for future developments:

## Slide 26
Backup
Rabi spectroscopy
Ramsey spectroscopy

## Slide 27
Backup