## Slide 1
Diamond measurements under irradiation and
measurement of CCE and mu-tau
Institute for Structure of Matter (ISM) of the Italian National Research Council (CNR)
Rome, Italy
DiaTHEMA Lab is inside the CNR Research Area of Roma 1
Via Salaria km. 29,300 - 00015 Monterotondo Scalo (RM), Italy
DiaC2Lab
Diamond and Carbon Compounds Laboratory

## Slide 2
D.M. Trucchi, P. Allegrini, P. Calvani, A. Galbiati, K. Oliver, G. Conte, IEEE Electron Device Letters 33 (2012) 615-617
Electronic-Grade Films do not suffer from priming!
No Deep Traps!
Priming
Trapping mechanisms reduce carriers lifetime in competition with thermionic re-emission favored by bias voltage.
“Flat curve” condition is obtained by applying voltages > 150 V (electric field > 3000 V/cm)
Very fast detectors (ms range or less under integrated measurements)
Frequency Dependence
X-ray Diamond Detectors – Photoconductor Performance
Priming process consists of a prolonged pre-irradiation to make the diamond detector signal stable and reproducible (priming is effective even for months).
Signal increases with irradiation time (i.e. accumulated dose) until it saturates (priming dose of about 2 Gy), reaching stable and reproducible conditions.
Why? CVD Diamond has deep traps in the wide band-gap which have to be electrically filled by photo-generated charge carriers to be neutralized.
It is well known that priming process induces:
  An increase of signal,
  But a concomitant increase of dark current
Electronic-Grade Films

## Slide 3
X-Ray Photoconductive Model
Hecht’s Photoconductive Model
Charge induction
Homogeneous illumination
Trapping & detrapping phenomena
 = constant = (3.0 ± 0.5) x 10-5 cm2 V-1
 ≈ 2.2 x 103 cm2 V-1 s-1
 ≈ 14 ± 3 ns
Electronic-Grade Dosimeters
Collection length = F
CCE = V/d2 =
= 100%, V>80 V

## Slide 4
D.M. Trucchi, P. Allegrini, A. Bellucci, P. Calvani, A. Galbiati, M. Girolami, Nucl. Inst. Meth. A 718 (2013) 373–375
Signal shows, as a function of radiation dose-rate, the expected Fowler’s dosimetric relation:
 = 1.02, slightly overlinear under CW operations
The specific sensitivity is about 50×10-3 C Gy-1 cm-3
Dosimetric Evaluation
Minimum detectable dose-rate
Region of no reliable detection
Applying low voltages, the capability of detection increases
Dose-rates even of tens of nGy/min are detectable!
X-ray Diamond Detectors – Photoconductor Performance

## Slide 5
M. Girolami, A. Bellucci, P. Calvani, R. Flammini, and D.M. Trucchi, Applied Physics Letters 103 (2013) 083502
Device Physics: Study of the DOS of shallow traps
Fi is the electric field separating trapping from detrapping
For F > Fi, an electric field parabolic dependence on energy appears
Frenkel Poole transport
Two Frenkel-Poole regimes:
Fi < F < Fc, a Frenkel-Poole-like with slopes of the curves > FP
F > Fc, a classic Frenkel Poole transport
It means that occupied states influence the electric field seen by an emitting charge carrier by effectively decreasing the energy barrier towards the extended band
Electric Transport under DARK CONDITIONS shows a Frenkel-Poole transport only for F > Fc
The electric field is not able to detrap charge carriers for F<Fc because the traps are empty under dark conditions

## Slide 6
Irradiation with Alpha Particles
The short penetration depth of alpha particles can be used to disentangle the transport of photo-electrons and –holes as a function of bias polarity
Data from Girolami, M. et al. Mosaic diamond detectors for fast neutrons and large ionizing radiation fields. Physica Status Solidi a-Applications and Materials Science 212, 2424-2430 (2015). https://doi.org:10.1002/pssa.201532191
The drift velocity of electron and holes can be estimated from the related transit time in the bulk of the detector.
The mobility for electrons and holes can be consequently fitted

## Slide 7
Irradiation with Alpha Particles
By considering the distance of the alpha-particle source from the detector, it is possible to reconstruct the mean flux of alpha particles impinging on the surface also in air.
By knowing the ionization energy in diamond (13.1 eV) and particle flux, it is immediate to reconstruct the CCE from the pulse statistics.
Data from Hirano, S. et al. Substrate Effects on Charge Carrier Transport Properties of Single-Crystal CVD Diamonds and an 8 mm Square Radiation Energy Spectrometer. physica status solidi (a) (2018). https://doi.org:10.1002/pssa.201800333

## Slide 8
Source-detector distance: 10.0 mm
Active area: 4 mm × 4 mm
Test pulse peak channel: 5850
Source-detector distance: 9.5 mm
Active area: 3 mm circular diameter
Test pulse peak channel: 5850
Front-side irradiation
Back-side irradiation
 | Front | Back
+400 V | 4714 | 4725
-400 V | 4622 | 4783
Average charge collection efficiency > 98 % @ F > 1500 V/cm
FWHM of the pulse (energy resolution) is about 1.5 %
CVD Diamond Spectrometer for Alpha Particle Sources

## Slide 9
CVD Diamond detector is a compact and versatile solution for alpha and beta particles, fast neutron spectroscopy and time-of-flight.
Diamond radiation hardness, high radiation sensitivity, low dark current and high thermal conductivity allow room temperature spectroscopy as well as time of flight accurate measurements.
CVD Diamond Spectrometer
For details:
“Pixelated Single-crystal Diamond Detector for fast neutron measurements”, M. Rebai et al., JoI 10 (2015) C03016.
“A diamond based neutron spectrometer for diagnostics of deuterium-tritium fusion plasmas”, C. Cazzaniga et al. Review of Scientific Instruments, 85 (2014) 11E101.
The development of the diamond technology for neutron detection was performed by the DiaTHEMA Lab of CNR-ISM (Rome)*,
in collaboration with CNR-ISTP (Milan) & Bicocca

## Slide 10
Log scale
The energy resolution achieved by CNR-ISTP is better than 1% at 14 MeV obtained with a system capable to operate at MHz counting rates.
The high energy side features about 1% sensitivity relative to the 14 MeV neutron peak
L Giacomelli et al., Rev. Sci. Instr 87(2016) 11D822
140 keV
CVD Diamond Spectrometer for monitoring Thermofusion Plasmas
DD neutrons → elastic scattering on carbon nuclei
DT neutrons → (n, a) reactions on carbon nuclei
12C(n, a)9Be (Qvalue=5.7 MeV, Ethr=6.17 MeV) good for 14 MeV neutron spectroscopy.
12C(n, n’)12C* only possible for 2.5 MeV neutrons.
12C(n,n’)3a (Qvalue= 7.23 MeV, Ethr=7 MeV)
12C(n, D)11B (Qvalue= 13.7 MeV, Ethr=13.8 MeV)

## Slide 11
Thank you for the Attention!