## Slide 1: Introduction to High Power Lasers
Intense Laser Irradiation Laboratory
Leonida Antonio GIZZI, CNR-INO Pisa, Italy
also at INFN, Pisa, Italy

## Slide 2: The Intense Laser Irradiation Laboratory (ILIL)
2018
LASER CAPABILITIES:
240 TW, Ti:Sa, up to 5 Hz, 27 fs;
1kHz, >20 mJ, Ti:Sa + OPA
100 Hz, >1J, TiSA (procurement in progress)

## Slide 3: Grand challenges of laser-plasma science
HEP TeV COLLIDER
C. Benedetti et al., https://doi.org/10.48550/arXiv.2203.08366
INERTIAL FUSION ENERGY
S. D.Batani et al, HPLSE, 2023
COMPACT PLASMA XRAY FEL
R. Assmann et al., https://doi.org/10.1140/epjst/e2020-000127-8
LASER DRIVEN NEUTRON SOURCES
https://www.ile.osaka-u.ac.jp/eng/research/project/project-lans/index.html
EuPRAXIA PP
Proof of principle
Towards CDR
Towards CDR
Based on HP laser technology
Light sources
SATELLITE DEBRIS REMOVAL
C. Phipps , .Advances in Space Research. 49 (9): 1283–1300. (2011)
LASER LIGHTENING ROD
A. Houard. Nat. Photon. 17, 231–235 (2023).
Cost, durability, energy efficiency, mass production of underlying laser components key to enable these developments.
L.Labate et al. Sci Rep, 2020
VHEE FLASH Radiotherapy
Betatron X-ray source
Based on Laser-Plasma Acceleration
Needing broadband for LPI mitigation
Needing high average power short pulses
Needing compact and efficient high power USP laser technology
HEALTH
MULTI-DISCIPLINARY SCIENCE
SECURITY
FUNDAMENTAL SCIENCE
ENERGY

## Slide 4: Contents
High power lasers
Short Pulse Ultraintense Lasers
Amplifying lasing media
Ultraintense Lasers: overview
From amplification to plasma
  Focal spot quality
  Temporal contrast
  Multipulse generation
Scaling laser drivers to large accelerator systems
  Potential and limits of existing Ti:Sa technology
  New schemes for high rep-rate and WPE
kHz laser driver for LPA
  A case study

## Slide 5: High power lasers

## Slide 6: Main principles of a laser
Gain medium
Pump (Energy)
Cooling (loss)
Cooling (loss)
Solid state laser for high power amplification
Excitation (pump radiation)
population inversion
spontaneous emission
stimulated emission

## Slide 7: The origin of lasers in the lab
High power laser pulses
≈ nanosecond pulse duration Q-switch
Power: ≈ GW
Theodore Maiman, 1960
C.H. Townes, N.G.Basov and A.M.Prokhorov, Phisics Nobel rize, 1964
Orazio Svelto, La storia del Laser, in Il Laser, Cinquant’anni di idee luminose, CNR, ISBN 987-88-8080-120-7

## Slide 8: MATERIAL DAMAGE LIMITS AMPLIFICATION
To avoid damage of optics and gain materials due to the growing electric field, laser intensity must be distributed over progressively larger diameters
Oscillator
Telescope
1° Amplifier
Telescope
Telescope
2° Amplifier
3° Amplifier
Consequence? “Gigantism” of high power, high energy lasers …

## Slide 9: Conventional high power (high energy) lasers have huge size
Lawerence Livermore National Lab. California, USA
Alternative approach to laser-matter interaction? High power at low energy per pulse and ultrashort pulse duration.
Pulse duration:
4 ns
Pulse energy:
2 MJ
Peak power:
≈500 TW
Fusion ignition scale laser
Ignition of inertial fusion achieved, Dec. 2022

## Slide 10: Short pulse, ultraintense lasers

## Slide 11: ORIGINAL PAPER
D. Strickland and G. Mourou, “Compression of amplified chirped optical pulses”, Opt. Commun. 56, 219 (1985)

## Slide 12: INSPIRATION from other field
Feb 1985

## Slide 13: Chirped Pulse Amplification
D. Strickland and G. Mourou, “Compression of amplified chirped optical pulses”, Opt. Commun. 56, 219 (1985)
A change of paradigm in high power lasers
Higher peak-power to date: 10 PW
Achievedn at the ELI-NP laser installation in Magurele (Romania)
C. Radier et al., HPLSE, 10, 21 (2022).

## Slide 14: Chirped Pulse Amplification ANIMATION

## Slide 15: The original CPA EXPERIMENT
Dispersion in fibers

## Slide 16: PULSE DURATION AND Bandwidth
We need a spectrum with a large bandwidth to achieve a short pulse

## Slide 17: VIA UNCERTAINTY PRINCIPLE

## Slide 18: WAVELENGTH-WISE
We need a broadband seed pulse and a laser medium capable of amplifying wavelengths from 740 nm to 840 nm: very challenging

## Slide 19: Amplifying lasing media

## Slide 20: Key parameters of lasing media
Main parameters governing high power laser amplifiers:
  Spectral gain bandwidth: short pulse duration
  Thermal conductivity: limits repetition rate
  Abs. and emis. cross sections: gain, pump absorption and saturation
  Fluorescence lifetime: sets conditions on pumping
  dn/dT: limits beam quality

## Slide 21: Key GAIN MATERIAL: Titanium doped Sapphire
Ti:Sa with BW active control
Ti:Sa native spectrum
Large gain bandwidth (680 nm – 1080 nm)
• High quantum efficiency
Thermal conductivity: 35 WK-1m-1
• Relatively long lifetime: 3 μs
• Typically pumped in the green with ns Q-switched pulses
Ti:Al2O3
Currently, most CPA lasers are based on Ti:Sapphire
Active bandwitdth control crucial to
overcome gain narrowing (non linear process) and enable sub-50 fs pulses

## Slide 22: ALTERNATIVE APPROACH
Optical Parametric Chirped Pulse Amplification
Mainly for ultra-broad-band front-end preamplifiers
A. Dubietis et al. “Powerful femtosecond pulse generation by chirped and stretched pulse parametric amplification in BBO crystal,” Opt. Commun. 88, 437 (1992).
I.N. Ross et al. “The prospects for ultrashort pulse duration and ultrahigh intensity using optical parametric chirped pulse amplifiers,” Opt. Commun. 144, 125 (1997).

## Slide 23: Ultraintense lasers: overview

## Slide 24: High intensity lasers: evolution
Major breakthrough following Chirped Pulse Amplification
[1] D. Strickland and G. Mourou, "Compression of amplified chirped optical pulses." Optics communications 55, 447 (1985)
[2] W. Wang, K.Feng et al., Free-electron lasing at 27 nanometres based on a laser wakefield accelerator, Nature 595, 516–520 (2021)
[3] L.A. Gizzi et al., A viable laser driver for a user plasma accelerator, NIM A 909 , 58 (2018); https://doi.org/10.1063/1.4984906
[4] J. W. Yoon et al., “Realization of laser intensity over 1023 W/cm2,” Optica 8, 630-635 (2021), https://doi.org/10.1364/OPTICA.420520
LASER-PLASMA ACCELERATORS
1E23 W/cm2
Current highest intensity in the lab [4]
Current laser technology developmentof CPA lasers [1] mainly driven by extreme intensity applications;
Laser-Plasma acceleration has developed along with progress in laser performance;
Recent LWFA-FEL demonstration [2] highlights the role of laser stability and control;
Need to focus on the technology required to achieve high-repetition rate at multi-joule (≈100 TW) scale [3], with high quality and enhanced control and stability;
Key role of industry to establish turn-key, high average/peak power ultrashort pulse technology;

## Slide 25: ULTRAINTENSE LASERS

## Slide 26
Leonida Antonio Gizzi
CNR-INO, Italy
Topic Editor
- Review article of high power lasers and facilities around the world
2022 Impact Factor
4.8
Review Article
Vol. 7, e54
2019
750 citations as 4/2024
Vol. 11, Issue 3 03000e40 (2023)
- On behalf of all at High Power Laser Science and Engineering we would like to congratulate
the team at LLNL on demonstrating fusion ignition at the National Ignition Facility.
High Power Laser Science and Engineering, (2019), Vol. 7, e54, 54 pages.
doi:10.1017/hpl.2019.36
Notes: The journal (high power laser science and engineering) focuses on the fields of high power lasers, high energy density physics, laser components, advanced laser technology and applications. Its latest JCR impact factor is 4.8. It ranks in JCR Quartile 1.
This journal is the home for facility-related papers. Welcome to submit your latest research to the journal.

## Slide 27: AVAILABLE INDUSTRIAL SYSTEMS
Thales
ALPHA5/XS: 20 J, 25 fs, 5 Hz
Ti:Sapphire
Amplitude Technologies
PULSAR: 5 J, <25 fs, 5-10 Hz
Ti:Sapphire
Current EU industrial systems offer robust solutions, incorporating ultrashort pulse capabilities at the PW level, in a compact footprint
Scientific lasers: still require expert users

## Slide 28: Many PW-CLASS lasers worldwide
LBNL, Berkeley, USA
VEGA Laser Facility
Salamanca, Spain
IBS, Center for Relativistic laser Science
Republic of Korea
And many more … ≈ 20
ELI-NP, Magurele, Romania
Almost unique systems built upon specifications of scientific cases

## Slide 29: EXTREME LIGHT INFRASTRUCTURE(s)
ELI-Beamlines facility, Prague, Czech Republic
ELI Attosecond Light Pulse Source (ELI-ALPS) in Szeged, Hungary
ELI Nuclear Physics (ELI-NP), Magurele, Romania
(Approx 1 Bln € investment)
A joint effort of the whole community
Currently entering full operation phase

## Slide 30: From laser pulse amplification and compression to interaction with plasma

## Slide 31: Relevant blocks of a laser driver
Transport and focusing
Gain medium
Pump (Energy)
Cooling (loss)
Transport
Optical Compressor
(vacuum)
Cooling (loss)
Plasma
loss
Tackle power and coupling efficiencies and losses
Wall plug
May be another DPSSL laser
All blocks from oscillator to focusing are key for stable electron acceleration
Seed pulse

## Slide 32: LWFA: laser power and quality control
Progress in laser specs is key to the development o Laser Wakefield Acceleration
2004: first monoenergetic electron beam 100 MeV
J. Faure et al., C.G.R. Gedders et al., S. Mangles et al., Nature 431 (2004)
2006: Energy gain: 1 GeV
W.P. Leemans et. al, Nature Physics 696 (2006)
1995: First electron beam
A. Modena et al., Nature 377 (606) 1995
2014: Energy gain: 4.3 GeV
W.P. Leemans et. al, PRL 113 (2014)
2019: Energy gain: 8 GeV
A. Gonsalves et. al, PRL 122(2019)
+ staging (proof of principle)
S. Steinke et al., Nature 530 (2016)
LWFA: Theoretical model
T. Tajima, J. M. Dawson PRL 43, 267 (1979)
Peak Power
1 TW
10 TW
100 TW
1 PW
30%
50%
70%
90%
Beam Quality
(Energy in the focal spot)
Phase front correction with adaptive optics (from astronomy)
+ several additional quality parameters
CPA Laser invention,
D. Strickland and G. Mourou" Optics communications 55, 447 (1985)
10 PW

## Slide 33: From laser pulse amplification and compression to plasma irradiation
Focal spot quality

## Slide 34: FOCAL SPOT BEAM QUALITY
Strehl ratio vs. energy
Energy in the focal spot
Energy in the pulse
Sr=
STREHL RATIO
As larger gain media and optics are used, optical aberrations become important and limit the focusability of laser pulses
PHASE FRONT DISTORTIONS
Amplification

## Slide 35: Borrowing Astronomy Adaptive Technology
ESO’s Very Large Telescope (Paranal, Chile)

## Slide 36: ADAPTIVE OPTICS for high power lasers
Active spatial phase control technique can be used to correct severe to moderate phase distortions;
Sensors are used to measure intensity and phase map of the beam;
Deformable mirrors are used to correct the measured wave front distortions in a closed loop;
S.-W. Bahk et al., Optics Letters 29, 2837 (2004)
Key enabling component to reach high intensity
A. PIROZHKOV et al., Optics Express 25, 17 (2017)

## Slide 37: From laser pulse amplification and compression to plasma irradiation
Temporal contrast

## Slide 38: Temporal features: contrast
Autocorrelator
S. Luan et al., “High dynamic range third-order correlation measurement of picosecond laser pulse shapes”, Meas. Sci. Technol. 4, 1426 (1993)
ASE
Prepulse?

## Slide 39: Laser contrast: sub-ps time scale
Ideal
Real
Gizzi, L.A et al., Role of laser contrast and foil thickness in target normal sheath acceleration, Nuclear Instruments and Methods in Physics Research A829, 144–148 (2016)

## Slide 40: TEMPORAL Contrast enhancement
High contrast is crucial to prevent plasma heating and expansion prior to the ultraintense interaction.
IMPORTANT for laser-plasma acceleration schemes based upon gas targets, but standard contrast (≈107 or more) is normally sufficient;
CRITICAL for current schemes of ion acceleration based on laser solid interaction and in particular for nanostractured targets;
Solutions have been developed based on several principles:
Saturable absorber (SA) is the basic solution for a standard pulse cleaning;
Better control of ASE can be obtained using Optical Parametric Amplification (OPCPA);
Plasma mirror (PM) can provide excellent contrast down to the ps range;
  Limits the repetition rate of the laser;
Crossed polarized wave (XPW) generation is another solution1 for suppression of prepulse and amplified spontaneous emission;
Non-linear (frequency doubling) conversion.
1A. Jullien et al.,Opt. Lett., vol. 30, pp.920–922 (2005),
G. I. Petrov et al., Opt. Lett. 26, 355–357 (2001)

## Slide 41: ACCESSIBLE Laser specs on plasma
Pulse duration as short as 15 fs at multi-PW power; band narrowing is managed by using OPCPA and/or bandwidth control/shaping capabilities;
Temporal contrast as high as 1012-1013, at ps timescale to prevent premature disruption of plasma conditions, using contrast enhancement;
Repetition rate ≈10 Hz at PW level;
Focusability close to diffraction limit, using wavefront correction;
Focused Intensity >1022 W/cm2;
Relativistic parameter
>>1
“A Superintense Laser-Plasma Interaction Theory Primer,” Andrea Macchi, Springer, 2013

## Slide 42
Particle acceleration with lasers and plasmas
Acceleration of ions: interaction of tightly focused laser pulses at ultra-high (ultrarelativistic) intensities on high density (solid) targets;
Acceleration of electrons: interaction of ultrashort laser pulses at (moderately) relativistic intensities with underdense (gas) targets;
Very long focal length optics
Larger focal spot diameter (30-50 µm)
Long Rayleigh length – channeling/guiding
Short focal length focusing optics
Small focal spot
Short Rayleigh length
Polarization distortions effects*
* L. Labate, G. Vantaggiato, L.A. Gizzi, Intra-cycle depolarization of ultraintense laser pulses focused by off-axis parabolic mirrors, High Power Laser Science and Engineering, 6, 32 (2018).

## Slide 43: OPEN ISSUES OF Laser Plasma Acceleration
OPEN ISSUES
QUALITY: energy spread, beam divergence, emittance, self-injection dynamics, plasma shaping
=>understanding of the physics of laser-plasma acceleration in real conditions
STABILITY: and control of bunch parameters, pointing
=>improve quality of lasers and laser-target coupling
SCALABILITY: staging (phase space matching) + higher energy, high repetition rate, high average power
=>develop new laser schemes for efficient high average power.
Since 2004, systematic production of electron bunches with energy in the hundreds of MeV range to 10 GeV and moderate energy spread (5-10%)*
Exploration of applications ongoing worldwide – focusing on Xray FEL (EuPRAXIA)

## Slide 44: From laser pulse amplification and compression to plasma irradiation
Multipulse generation

## Slide 45: The Resonant Multi-Pulse Ionization Injection
The Resonant Multi-Pulse Ionization injection is a new bunch injection scheme aiming at generating extremely low-emittance bunches [as low as 0.06 mm mrad]
ReMPI requires ONE short-pulse 100-TW class (e.g Ti:Sa) laser system. Since a unique very large-amplitude Ti:Sa pulse would fully ionize the atoms (N5+ or Ar8+ ), the pulse is shaped as a resonant sequence of sub-threshold amplitude pulses.
A new scheme to generate the train of pulse in a stable, efficient and feasible way « Quasi Lossless Pulse Train generation by Early Amplitude division »
Ionization Threshold
ReMPI
P. Tomassini et al., Phys. Plasmas 24 (2017)

## Slide 46: MULTI-PULSE LASER GENERATION
C. W. Siders et al., “Efficient high-energy pulse-train generation using a 2n- pulse Michelson interferometer,” Applied Optics Vol. 37, Issue 22, 1998.
A. Marasciulli, PhD thesis, 2023
Proof of principle validation using a two-pulse “train”, in progress
Large beams: Delay mask
N-Michelson interferometers
Proof of principle demonstration

## Slide 47: NEXT STEP: STAGING OF ACCELERATING SECTIONS
Advanced staged acceleration with lasers
Multiple stages need multiple laser pulses: scaling of energy and repetition rate

## Slide 48: Scaling lasers drivers to large accelerator systems

## Slide 49
TOWARDS HIGH AVERAGE POWER
Future installations will require PW, fs pulses with kHz rep-rate (multi 10kW) lasers with high efficiency
Aim at laser architectures that can directly exploit diode lasers.
Ti:Sa requires pumping with green laser light with high power and 10ns pulse duration - no existing diode lasers can fulfill these requirements
Choose different gain medium for future multi-kW laser systems

## Slide 50: Average power
Current reqirement for LPA driver: PW-class system, with high repetition rate (≈kHz) Demanding high average power (1-10 kW)
Major effort required to fill the gap between existing and required laser technology
Machine drivers

## Slide 51: Relevant blocks of a laser driver
Transport and focusing
Gain medium
Pump (Energy)
Cooling (loss)
Transport
Optical Compressor
(vacuum)
Cooling (loss)
loss
Tackle power and coupling efficiencies and losses
Wall plug
Plasma
loss
Transmitted laser
Use laser diodes

## Slide 52: CHANGE OF OPTICAL PUMPING TECHNOLOGY
Analysis of available technologies for PW-class, multi kW average power lasers;
Comparison with the requirements of user beamlines;
Current option: TiSa pumped with diode pumped solid state lasers (DPSSL) – robust;
In progress: Direct CPA for higher rep-rate, higher efficiency.
Major developments in laser technology occurring now!
PUMP SOURCE: Flashlamp
PUMP SOURCE: Diode laser

## Slide 53: Roadmap on LPA Laser Driver technology
Laser-driven plasma acceleration needs ultrashort, high power lasers with high average power
Current industrial technology: ≈ Ti:Sa technology, pumped by flash-lamp pumped lasers
  Robust, reliable industrial technology
Mature technology: ≈ Ti:Sa technology, pumped by diode-pumped lasers
  Strong R&D effort in place (e.g HAPLS@ELI)
  ≈ 3-5 years to go to first industrial LWFA demonstrator (e.g. Eupraxia) [1]
Beyond TiSA: targeting higher wall-plug efficiency and rep. rate, kHz and beyond, stability, control (space, time, spectral);
  5-10 yrs for first efficient, multi-kW-scale demonstrator,
  A strategy is needed to steer effort in the LPA laser driver direction: LASPLA
[1] R. Assmann et al., EuPRAXIA Conceptual Design Report, The European Physical Journal Special Topics 229, 3675–4284 (2020)
[2] C. Danson et al., Petawatt and exawatt class lasers worldwide High Power Laser Sci. and Eng. 7, e54 (2019)
The L3-HAPLS at ELI Beamlines Research Center in the Czech Republic. Credit: ELI Beamlines*

## Slide 54: Scaling lasers drivers to large accelerator systems
Scaling existing Ti:Sa technology

## Slide 55: 100 Hz, J-scale laser beamline
OPCPA
front-end
Stretcher
Preamplifier
Ti:SA mutipass
DPSSL pump
Joule scale / 100 Hz / > 100 W
High average power Compressor
Ti:Sa disk amplifiers
High averge power
transport to target
High repetition rate target
HRR Data collection
Laser driver stability
Control
(Eupraxia DN)
Front-end
At the limit of current industrial capability
100 W

## Slide 56: HAPLS: Fully diode-pumped reprated PW system
Beamline (Prague)
Nd:YAG
10 Hz
300 W

## Slide 57: EuPRAXIA LASER (Ti:Sa)
FRONTEND
AMP1
9 (13) J, 0.8 µm
FRONTEND
COMPRESSION
TO FOCUSING
PROPAGATION
AMP1
AMP2
19 (37) J, 0.8 µm
COMPRESSION
PROPAGATION
TO FOCUSING
AMP1
AMP2
AMP3
62 (126) J, 0.8 µm
COMPRESSION
PROPAGATION
TO FOCUSING
20(25)J, 0.5µm
37( 65) J, 0.5µm
105 J / 197 J, 0.5µm
5(7)J, 30(20)fs, 20(100)Hz
15(30)J, 30(20)fs, 20(100)Hz
50(100)J, 60(50)fs, 20(100)Hz
Photocathode and diagnostics
FRONTEND
MASTER Oscillator
LASER1
LASER2
LASER3
150 MeV
1 GeV
5 GeV
2-10 kW

## Slide 58: EuPRAXIA Laser Driver: pump lasers
Developments based on diode pumping technology are in progress, progressively matching requirements
Pump diodes
100Hz Front end
10J amplifier head
Cryostat
VSF
Schematic of DiPOLE 100Hz
Courtesy of P. Mason
Diode pump technology
  100J @ 10Hz
    Summer 2019 demonstrated 60J @ 10Hz, 515nm in LBO with 66% efficiency (91J @ 1030nm)
    Commissioning of DiPOLE100 @ XFEL commenced Q1 2020 – completion end 2021
    Energy scaling 145J @ 10Hz, 1030nm @ HiLASE in January 2021
  10J @ 100Hz
    Build @ CLF near completion – commissioning Q4 2021
Amplitude P60
Flashlamp pumped Nd:YAG
Design: 60 J @ 10 Hz, 532 nm
Conversion to diode pumping fully designed - Premiumlight
Expected specs: 100 Hz – 10 kW (100 J/pulse @ 1µm)
Cost of diode still an issue
currently 5x compared to flash-lamps.
expected to decrease.
Maintenance free operation for 25-30 yrs.
Courtesy of F. Falcoz
More options available and further developing.

## Slide 59: Thermal management
Transmission vs. “active mirror” configuration is currently being evaluated to account for thermal management
Pro: More efficient (double-side) cooling and reduced complexity;
Con: propagation through flowing cooling liquid
Pro: Well established concept with no propagation through cooling fluid
Con: limited cooling (single face), to be modelled
Transmission geometry
“Active mirror” geometry
Gain comparison (AMP3)
*) Water cooled Ti:Sa amplifier (“Active Mirror” configuration) under development at ELI-HU (After V. Cvhykov et al. , Opt. Lett, 41, 3017, 2016)
**) Fluid (D2O ) cooled Nd:YAG laser, 20 kW CW pump power, D2O (After X. Fu et al. , Opt. Express, 22, 18421 (2014)
***) Fluid (Siloxane ) cooled Nd:YLF laser, 5 kW CW pump power (After Z. Ye et al. , Opt. Express, 24, 1758 (2016)

## Slide 60: Underpinning EuPRAXIA-like Laser driver
THERMAL
MANAGEMENT OF
POWER AMPLIFIERS
WATER/GAS COOLING
COMPRESSOR AND TRANSPORT: THERMAL AND MECHANICAL STABILITY
Gold -> MD, MLD, MMLD
reduction of the thermal load
cooling of residual heat
control of thermal effects
Main challenges: large optics, mechanical stability, beam quality control, pointing stability
DiPOLE 100 (STCF)
DPSSL PUMP
SOURCES
TECHNOLOGY
P-60 technology (Amplitude)
Currently no solution for full system specs (P1): development
Multipass transmission
AMPLIFIER GEOMETRY
TRANSMISSION
VS. REFLECTION
Multipass reflection
Prototyping needed
DIODE LASERS EFFICIENCY,
BRIGHTNESS AND
LIFETIME
Needs development
Prototyping needed

## Slide 61: Scaling lasers drivers to large accelerator systems
New schemes for high repetition rate and high WPE

## Slide 62: Efficiency path
TiSa technology is prompt and will demonstrate repetitive operation 24/7 and stability, but not scalable with poor efficiency (% level) due to the indirect pumping architecture:
Direct CPA is a solution for wall-plug (WP) efficiency and high rep-rate.
C. Siders et al., EAAC 2017
From flashlamp to indirect to direct diode pumping
Quantum defect
WP Efficiency > 20% possible:
We need a gain medium that can support amplification on a large bandwidth, has a low quantum defect and can be pumped directly with diode lasers: endless quest for the perfect laser medium!!

## Slide 63: Roadmap on LPA Laser Driver technology
Laser-driven plasma acceleration needs ultrashort, high power lasers with high average power
Current technology: ≈ Ti:Sa technology, pumped by flash-lamp pumped lasers
  Robust, reliable industrial technology
Mature technology: ≈ Ti:Sa technology, pumped by diode-pumped lasers
  Strong R&D effort in place (e.g HAPLS@ELI)
  ≈ 3-5 years to go to first industrial LWFA demonstrator (e.g. Eupraxia) [1]
Beyond TiSA: targeting higher wall-plug efficiency and rep. rate, kHz and beyond, stability, control (space, time, spectral);
  5-10 yrs for first efficient, multi-kW-scale demonstrator,
  A strategy is needed to steer effort in the LPA laser driver direction: LASPLA
[1] R. Assmann et al., EuPRAXIA Conceptual Design Report, The European Physical Journal Special Topics 229, 3675–4284 (2020)
[2] C. Danson et al., Petawatt and exawatt class lasers worldwide High Power Laser Sci. and Eng. 7, e54 (2019)
The L3-HAPLS at ELI Beamlines Research Center in the Czech Republic. Credit: ELI Beamlines*

## Slide 64: Several options under development
L.A Gizzi, F. Mathieu, P. Mason, P P Rajeev, Laser drivers for Plasma Accelerators, in Félicie Albert et al, 2020 roadmap on plasma accelerators, 2021 New J. Phys. 23 031101, https://doi.org/10.1088/1367-2630/abcc62;
O. Jakobsson, S. M. Hooker and R. Walczak, PRL, (2021)
A.L. Viotti et al., Optica 9, 197-216 (2022).
Fiber laser technology targeting the best WPE 30% in CW mode and coherent combination is being developed (FSU Jena-Fraunhofer IOF and Ecole Polytechnique-Thales in France).
  Suited for moderate energy per pulse/high rep-rate (10s of kHz);
  Now 96 fibers delivering 23 mJ and 674 W in a 235 fs pulse
Direct Chirped Pulse Amplification with lasing media pumped directly by diodes is ideal for higher efficiency and higher rep-rate;
  several materials under consideration, Yb:CaF2, Tm:YLF, Tm:Lu2O3 (with cross-relaxation and multi-pulse extraction) …
  PENELOPE (Jena) 150 J, 1 Hz, at 1030 nm
  Available ps kW thin disk lasers using plasma modulation (Oxford2)
OPCPA optical parametric amplification within large-aperture lithium triborate (LBO) crystals;
  ELI-Beamlines facility, L1 ALLEGRA (100 mJ at 1 kHz) and L2 AMOS (100 TW, 2 to 5 J between 10 and 50 Hz), and the Shenguang II Multi-PW beamline(SIOM, China) …
Thin Disk ps Lasers + spectral broadening + post compression3
  Industrial technology with demonstrated >kW operation ar ≈J per pulse energy.

## Slide 65
Diagram: E. Esarey, LBNL
Coherent Combination in Fibers

## Slide 66: Coherent Combination
Coherent combination has been proposed for Ti:Sa beamlets, in a similar approach as fiber combination, but with tiled-aperture.
Z. Li, et al., Laser Photonics Rev.2023,17, 210070
Significant engineering issues to be overcome, but in line with current active control approach
Could relax constraints on heat load management of >kW beamline and need of large optics
Needs CDR

## Slide 67: kHz laser driver development for LPA
A case study: direct DPSSL CPA with Thulium

## Slide 68: Thulium based laser gain materials
Currently under investigation(*): Tm:YLF
  Emission at 1,9 µm, eye safe;
  Ultrashort pulse (<100 fs);
  High peak power ≈ PW;
  High average power(scalable from kW to 300 kW);
  Direct pumping at 808 nm, using diodes operating in CW mode (available and scalable);
  Multi-pulse extraction at high repetition rate
  10 kHz; Ideal for accelerator technology;
  High efficiency;
  Mature material technology (crystal growth);
Ti:Sa
Tm:YLF
C. Haefner et al., EAAC 2017
Absorption peak wavelength 792 nm
Absorption cross-section at peak 0.55×10-20 cm2
Absorption bandwidth at peak wavelength 16 nm
Laser wavelength 1900 nm
Lifetime of 3F4 thulium energy level 16 ms
Emission cross-section @1900 nm 0.4×10-20 cm2
Refractive index @1064 nm no=1.448, ne=1.470
Crystal structure tetragonal
Density 3.95 g/cm3
Mohs’ hardness 5
Thermal conductivity 6 Wm-1K-1
dn/dT -4.6×10-6 (//c) K-1
Thermal expansion coefficient 10.1×10-6 (//c) K-1
Typical doping level 2-4 at.%
Tm: YLF Full specifications
Relatively new approach for short pulse operation: needs R&D, but promising
High Efficiency enabled by multipulse extraction (energy storage)

## Slide 69: Recent advances with Tm:YLF
Issa Tamer, et al., "High energy operation of a diode-pumped Tm:YLF laser," Proc. SPIE 12401, High Power Lasers for Fusion Research VII, 1240109 (14 March 2023); doi:10.1117/12.2649103
Energy density storage and extraction capabilities of Diode pumped Tm:YLF (narrowband)
Amplified pulse energy measurements up to 108.3 J for the 6-pass Tm:YLF power amplifier
Multi-pulse extraction demonstration resulting in 3.6 kW output power
“The multiple proof-of-principle demonstrations [..] reveal the potential for high efficiency, high energy density extraction using Tm:YLF for future high peak and average power laser systems.”
“Additional efforts are currently in progress to conduct chirped pulse amplification of ultrashort pulses using Tm:YLF at the joule-level for the first time.”

## Slide 70: Recent advances with Tm:YLF
**I. Tamer, et al., "High energy operation of a diode-pumped Tm:YLF laser," Proc. SPIE 12401, High Power Lasers for Fusion Research VII, 1240109 (14 March 2023); doi:10.1117/12.2649103
Demonstration of a 1 TW peak power, joule-level ultrashort Tm:YLF laser*
* I. Tamer et al., Optics Letters 49, 1583 (2024)
E=1.59 J
Pulse duration=270 fs
P=1.7 TW
Pump: 35.3 kW p.p. 40 ms

## Slide 71: Laser grade ceramic option
Faster and cheaper vs. single crystal growth process – for cubic crystalline structure.
Large components, -shaping, -graded doping also optimized for thermal management – features not available for single crystals.
Several compositions (e.g. YAG, LuAG , Sc2O3, Lu2O3) and dopants (Nd, Yb, Er, Tm…) already available
Spectroscopic and thermomechanical properties similar to those of the corresponding single crystals
Better uniformity of dopant distribution on large gain elements
Industrial and R&D effort: (Japan); Research in China, Japan, Russia, USA, France and Italy (ISTEC-CNR) (ZENITH Smart Polycrystals)

## Slide 72: Ceramic option: Tm in sesquioxide host
Sesquioxides doped with Tm3+, such as Tm:Lu2O3, Tm:Y2O3, and Tm:Sc2O3, are also emerging materials: their better thermo-optical properties make them promising for power scaling applications.
C. Krankel, IEEE J. Sel. Topics Quantum Electro 21, Art. no. 1602013 (2015)
The growth of sesquioxide single crystals is very complicated, while it is possible to produce them in transparent ceramic form thanks to their cubic crystalline structure and optical isotropy.
Advantages of ceramic medium:
High thermal and mechanical features
Scalable size
Custom doping
Optimize energy efficiency
Tm:Lu2O3
Ceramic
Sample from Konoshima

## Slide 73: Ceramic option: Tm Lu2O3
[Scholle et al., 2010]
Commercial diode lasers
Laser material: Tm:Lu2O3
  Emission at 2 µm;
  Large amplification bandwith
  Direct pumping at 800 nm, using diodes operating in CW mode (available and scalable);
  Cross relaxation partially compensates quantum defect – option of in-band pumping.
  Multi-pulse extraction at high repetition rate > 10 kHz; Ideal for accelerator technology;
  Mature material technology (large ceramic).
[Antipov, 2011]
s
Tm:Lu2O3
Ceramic
Sample from Konoshima

## Slide 74: Test platform
An oscillator cavity has been set up for Tm:Lu2O3 gain material characterization

## Slide 75: Fundamentals for high efficiency?
Accurate characterizaton of absorbed pump energy to measure quantum efficiency
Measures for two different temperatures of 13 and 23°C
Preliminary: quantum efficiency close to 2 : Evidence of full cross relaxation
Slope efficiency ≈ 75%
Quantum efficiency
Slope efficiency
Quantum efficiency ≈ 2

## Slide 76: Higher WPE: In-band pumping for low QD
New path for intra-band pumping and smaller quantum defect: step change in WPE?
Thulium based gain medium can also be pumped with in-band absorption with virtually marginal quantum defect:
High efficiency and lower heat deposition.
M. Lenski et al., Opt. Express 30, 44270-44282 (2022)
>80% slope efficiency demonstrated in fibers
WPE: wall plug efficiency
QD: Quantum Defect

## Slide 77: In-band pumping of Tm:Lu2O3
“1600 nm” Er/Yb pump laser
796 nm pumping
1620 nm pumping
Max QE: 78.4%
Max QE: 38.54%
With cross relaxation up to 77.09%

## Slide 78: In-band pumping of Tm:Lu2O3
1605 nm
1620 nm
Latest: lasing achieved at 2.065 µm @ 1620 nm pumping.
Measured slope efficiency still limited (≈8%)
a=170 m-1
a=243 m-1

## Slide 79: kHz laser development at ILIL
1≈J, 1kHz
A kW-kHz CPA laser development with direct diode pumping
Main development effort in amplifier modules: ELIIT/APOLLO project (CNR)
kHz, mJ, mid-IR, fs front-end
Ti:Sa
s
3 amplification stages, each based on a 2 active
media multipass scheme.
Active mirror config,
with cooling carried out
on both sides
Selected doping: 4% at
Pulse energy (goals/expected):
>1mJ seeding the 1st amp
~8 mJ seeding 2nd amp
>50mJ seeding the 3rd amp
>500mJ from 3rd amp

## Slide 80: kHz front-end: operational
Specs of front end @ 2µm
kHz, mJ, mid-IR, fs front-end:
Ti:Sa (20 mJ, 30 fs) pumped OPA
Pulse duration: <60 fs
Spectrum
Pulse Energy >1.8 mJ
Beam Profile
Center wavelength: 2025 nm
Spectrum FWHM: 182 nm
FTL pulse duration: 33 fs

## Slide 81: Gain medium design and pumping
Side/edge pumped thin disk active mirror configuration [1,2]
Undoped
Doped
Diodes total power: >2kW, Diodes energy (1ms): 1.95 J, Linear bar power: 19.4 W/mm => 1 J output
Geometry
Thermal load
Edge diode pumping
[1] J. Vetrovec, et al., “Wide-Bandwidth Ceramic Tm:Lu2O3 Amplifier”, Proc. SPIE 9834, 983407 (2016); https://doi.org/10.1117/12.2224411
[2] J. Vetrovec, et al., “2-micron lasing in Tm:Lu2O3 ceramic:initial operation”, Proc. SPIE 10511, 1051103 (2018); https://doi.org/10.1117/12.2291380
[3] D. Palla, L. Labate, F. Baffigi, G. Cellamare, L.A. Gizzi, Optics & Laser Technology, 156, 108524 (2022), https://doi.org/10.1016/j.optlastec.2022.108524
Now finalizing technical design and starting construction and tests

## Slide 82: Summary considerations on lasers for LPA
CPA laser technology is mature for LPA studies;
  Scientific lasers are being optimized;
  Suitable for high quality plasma acceleration (FEL);
Limited scaling (thermal, wpe) for HEP accelerator drivers;
New laser technology is needed for high WPE and >kW average power;
Efficient diode pumping is replacing flashlamps;
Suitable schemes and materials are emerging and under investigation.