## Slide 1
Marco Pieruccini CNR-IMM
Substitutional Impurities in Solids
Why substitution with impurities ?
Doping of semiconductors; e.g. Al borrows one electron to build up four sp3 bonds: energy cost. Lattice regularity needed for appropriate level formation
Other issues… e.g. anchoring ions in well defined conditions (again lattice regularity). In this case two electrons are needed to build the four bonds, with a cost of .
Conduction Band
Valence Band
Localized acceptor states
Tetrahedral
Coord.
Si,
SiC,
…
Note the unbalance of electric charge around the impurity

## Slide 2: Ion Implantation in solids
Implanted Si on Si
Si
Main Features
Controlling: Profile Localization Dose
Implantation produces a metastable locally disordered material: an extremely viscous liquid which would tend to approach the thermodynamically more stable crystalline state
Lattice damage
  Beneficial: enhances the probability of substitution (e.g. dangling bonds)
  Drawback: need to recover crystal regularity (possible with low damage);
  this can be done through
    Control of implantation conditions
    Post-implantation annealing
Marco Pieruccini CNR-IMM

## Slide 3: Thermodynamics of a Viscous Liquid
Ideal equilibrium is described by the red line. Viscosity onset is accompanied by a reduction of the mean configurational entropy .
This regime is parametrized by the mean fluctuation :
Entropy
Total Energy
equilibrium
liquid
WORK =
Quenching of SLOW modes: viscosity
Heat Bath
FAST
deg. of freedom
SLOW diffusive d.o.f.
WORK
A system in contact with a Heat Bath consists of two interpenetrating subsystems: one made of FAST d.o.f. (short wavelengths) and the other consisting of the SLOW diffusive d.o.f. (long characteristic lengths).
The subsystems are not physically distinct in the sense that in a given set of units whatsoever the d.o.f. are partitioned between the fast and slow classes.
Marco Pieruccini CNR-IMM

## Slide 4: The mean-field specific pseudo-Potential for a Viscous Liquid (from a general minimization of the overall free energy)
Cooling towards one has , that is
If a unit succeeds crossing a barrier to rearrange, then this energy redistributes among other units in the form of configurational entropy.
Energy
Configurations ( time arrow )
Random probing metastable states
Without a sufficient energy gain the variety of metastable states cannot be explored
Entropy
Energy
Marco Pieruccini CNR-IMM

## Slide 5: Escape from Metastable States in implanted solids…
A defect made of atoms in a semiconductor just implanted is in a metastable state and in regime of strong confinement:
can’t be reached and the disordered spot keeps frozen.
Need of high- post-implantation annealing to reduce the theoretical threshold …
… or wait for an energy supply (fluctuation)
… and Recover Crystal Regularity
Lattice disorder is related to configurational entropy. Evolution towards thermodynamic stability (regular crystal lattice) implies a decrease of in time (relaxation time approximation + cooperativity):
time
Finite number of attempts for damage recovery/substitution
Faster process
Marco Pieruccini CNR-IMM

## Slide 6: Substitutional fraction vs. Implantation/post-impl.-Annealing
1) All attempts for substitution () occurred during implantation or annealing:
for Al in 4H-SiC, consistent with the density saturation value, for which
2) Few attempts for substitution occurred during implantation or annealing:
entropy recovery
0.58 eV
suggests Al-substitutions in damaged sites (in regular ones it would be much higher)
High implantation damage
Compromise is needed; relevance of implantation conditions
For in 4H-SiC (): need of high- implantation due to limits in
Marco Pieruccini CNR-IMM

## Slide 7: END
Marco Pieruccini CNR-IMM

## Slide 8
FAST
SLOW
Fluctuations in the slow d.o.f. subsystem are correlated with fluctuations in the fast d.o.f.
In an ensemble of independent oscillators, for which , the fluctuations able to trigger a structural transition are those of sufficient energy . Alternative picture: cutoff of LONG-wavelength, LOW-energy modes.
increases on cooling… because this way the density of states increases as well, which enhances the probability that the physical group of units attracts energy from the heat bath.
When the amplitude of the oscillations grows enough, then a structural change takes place.
Marco Pieruccini CNR-IMM