## Slide 1: RSD2 performance in the AIDAINNOVA SPS test beam
Luca Menzio (INFN Torino)
on behalf of the AIDAINNOVA testbeam team

## Slide 2: Contents
Introduction
Resistive read-out in silicon detectors
Experimental Set-up
AIDA test beam setup @ SPS
Chubut2 acquisition board
Analysis and Results
Analysis flow
1.3 mm-pitch sensor results
450 µm-pitch sensor characterization
Conclusions

## Slide 3: Contents
Introduction
Resistive read-out in silicon detectors
Experimental Set-up
AIDA test beam setup @ SPS
Chubut2 acquisition board
Analysis and Results
Analysis flow
1.3 mm-pitch sensor results
450 µm-pitch sensor characterization
Conclusions

## Slide 4: Resistive Read-out
e-h pairs are produced by the impinging particle in the sensor volume
Electrons are multiplied (LGAD)
Charge is induced in the n+ layer (resistive layer)
Nearby electrodes see a fast signal
Charges in the n+ flow to ground
AC-coupled electrodes
50 μm
Time resolution typical of thin LGADs
Luca Menzio – INFN Toino
Signal sharing
AC-coupled signals
In normal pixel detectors with
Resistive read-out sensors have

## Slide 5: Resistive Read-out
Charge sharing over silicon surface
Internal gain (LGAD)
Excellent position resolution with large pads
Excellent Timing
Low power consumption
Low material budget
+ 100 % intrinsic fill factor!
Luca Menzio – INFN Toino
Pros
Low channel density
Thin sensors
Promising candidate for 4D tracking

## Slide 6: DUTs – RSD devices
Luca Menzio – INFN Toino
1.3 x 1.3 mm2
450 x 450 µm2
The DUTs come from the second production by FBK of Resistive Silicon Detectors (RSD2)
Two devices tested:
450x450 µm2 from W7
1.3x1.3 µm2 from W13
Same AC-electrodes layout – crosses to help the signal containment
Different n+ layer resistivity

## Slide 7: Contents
Introduction
Resistive read-out in silicon detectors
Experimental Set-up
AIDA test beam setup @ SPS
Chubut2 acquisition board
Analysis and Results
Analysis flow
1.3 mm-pitch sensor results
450 µm-pitch sensor characterization
Conclusions

## Slide 8: AIDA Test Beam
The test beam was performed in the CERN H6 beamline (120 GeV pions/protons)
MIMOSA telescope
CAEN DT5742 digitizer, 16 channels @ 5GS/s
Trigger is a 3x3 mm2 UFSD1 LGAD
DUTs on the Chubut2 read-out board
RSD runs:
  2 DUTs, 1.3 mm and 450 μm pitch biased at 240 V and 200 V, respectively
  No time reference

## Slide 9: AIDA Test Beam

## Slide 10: Chubut2 Acquisition Board
Luca Menzio – INFN Toino
1https://github.com/SengerM/Chubut_2?tab=readme-ov-file
The Chubut2 is a low-noise discrete readout board specifically developed for LGAD testing
It features a
Carrier boards that hosts the DUT
Main board with amplification and power delivery circuitry
The design employed for this test beam has 4 identical channels, each with about 3540 Ω transimpedance on 50 Ω input and output
Good S/N with a budget friendly way of switching between sensors (one main board, multiple carrier boards)
Open source project1

## Slide 11: Contents
Introduction
Resistive read-out in silicon detectors
Experimental Set-up
AIDA test beam setup @ SPS
Chubut2 acquisition board
Analysis and Results
Analysis flow
1.3 mm-pitch sensor results
450 µm-pitch sensor characterization
Conclusions

## Slide 12: Waveforms and Tracks Analysis
Waveforms
Employing the Beta-analysis script
Tracks
Reconstructed with corryvreckan
EUDAQ2 rawfile
SPS RSD Analysis script
Luca Menzio – INFN Toino

## Slide 13: Having a look at the sensors
The sensors overlap in space and have good signals
Luca Menzio – INFN Toino
1.3 x 1.3 mm2
450 x 450 µm2
Sum of the 4 electrodes amplitudes (mV)
Sum of the 4 electrodes amplitudes (mV)
# Entries
# Entries
Trigger
1.3 mm sensor
450 µm sensor
~25 mV MPV
~38 mV MPV

## Slide 14: Having a look at the sensors
The sensors overlap in space and have good signals
Luca Menzio – INFN Toino
1.3 x 1.3 mm2
450 x 450 µm2
Sum of the 4 electrodes amplitudes (mV)
Sum of the 4 electrodes amplitudes (mV)
# Entries
# Entries
All channels of both sensors have low noise ~0.8 mV
~25 mV MPV
~38 mV MPV

## Slide 15: W13 1.3 mm – Position Reconstruction
Firstly, the position was reconstructed with the analytical formula based on the charge (amplitude) imbalance
The distortion of the reconstructed positions map is typical of this reconstruction method
Luca Menzio – INFN Toino

## Slide 16: W13 1.3 mm – Position Resolution
Luca Menzio – INFN Toino
# Entries
# Entries
About 95 µm on each axis – 13 % of the pitch. Better than standard binary pixels (29 %)
As already studied and demonstrated using the data collected with the TCT setup,
the resolution can be improved applying a correction (distortion mostly due to the reconstruction method):
- use of a “migration matrix”
- use of a template to assign the hit position
- use of machine-learning technique

## Slide 17: W13 1.3 mm – Machine Learning studies
82.9 µm
79.6 µm
Luca Menzio – INFN Toino
We tried to implement a Deep Neural Network (presented in the last TREDI)
Although the statistics is very poor for Machine Learning, the results are very promising and present a 15% improvement compared to the non-corrected results

## Slide 18: W7 450 μm – Analytical Method
The results of the 450 μm-pitch sensor benefit from the better signal-to-noise ratio
Luca Menzio – INFN Toino

## Slide 19: W7 450 μm – Analytical Method
The results of the 450 μm-pitch sensor benefit from the better signal-to-noise ratio
Reconstruction with the charge imbalance formula leads to a resolution of about 25 µm on each axis
 5% of the pitch
x_trk – x_rsd [mm]
y_trk – y_rsd [mm]
# Entries
# Entries
Luca Menzio – INFN Toino

## Slide 20: W7 450 um – Template Method
Luca Menzio – INFN Toino
Positions were also reconstructed using the “template method”.
The hit position is extracted starting from the amplitudes read out by the four electrodes, using the template computed with the test beam data @DESY (see Nicolò’s talk)
The template was computed using the same sensor type, but different sensor die, n+ resistivity, and electronics
The template works well!
No position distortion pattern is visible

## Slide 21: W7 450 um – Template Method
Secondly, positions were reconstructed thanks to a template method.
About 20 µm on each axis with the template reconstruction (19.5 µm) – 4% of the pitch
The reconstruction with the template computed in a different experimental setup is viable
x_trk – x_rsd [mm]
y_trk – y_rsd [mm]
# Entries
# Entries
Luca Menzio – INFN Toino

## Slide 22: Comparison with other test beams
Luca Menzio – INFN Toino
Comparing with the best results achieved in other test beams
Suffering from low signals and low statistics.
It would benefit from a dedicated template/Machine Learning training dataset
Performance is very good thanks to the template model created on another test beam facility and on another electronics!
Good results with low signals
Very good results with low signals

## Slide 23: Efficiency
Luca Menzio – INFN Toino
The silicon physically ends here
We defined a hit on a sensor as the combination of three conditions
time: the RSD hit timestamp must be compatible with the tracks in the tracker
amplitude: sum of the four signals amplitudes must be above a certain threshold (~3x sigma noise)
track: there is a reconstructed track pointing inside the sensor area
  But some tracks are reconstructed in the wrong positions!
1.3 x 1.3 mm2
450 x 450 µm2

## Slide 24: Efficiency
Luca Menzio – INFN Toino
1.3 x 1.3 mm2
450 x 450 µm2

## Slide 25: Efficiency
Because of the tracks small mis-reconstruction, one has to use the signals on one of the two sensors to infer the efficiency of the other
→ only the efficiency of the smaller sensor can be computed
Luca Menzio – INFN Toino

## Slide 26: Efficiency
Because of the tracks small mis-reconstruction, one has to use the signals on one of the two sensors to infer the efficiency of the other
→ only the efficiency of the smaller sensor can be computed (completely inside the bigger one)
Luca Menzio – INFN Toino
Values of efficiency typical of silicon are maintained, > 99%
Threshold employed in this work

## Slide 27: Conclusions
The performance of two RSD2 sensors, 1.3mm pitch and 450 μm pitch, were measured during the second AIDAinnova 2023 test beam at SPS.
The devices were bonded to a novel low-noise and open-source electronics: the Chubut2 board
The best spatial resolutions achieved are:
81 m employing a Machine Learning approach (6% of the pitch)
19.5 m with the template method (4.3% of the pitch)
Both designs achieve significantly better results than those of standard pixel detectors (15-30%) with a low number of channels.
The detection efficiency of a 450 μm pitch RSD2 was evaluated to be >99%
Luca Menzio – INFN Toino

## Slide 28: AIDAinnova WP6 Test Beam group
CNM-Barcelona (AIDAinnova): Oscar David Ferrer Naval
IFCA (AIDAinnova + ETL): Ivan Vila Alvarez, Andres Molina
Ribagorda, Jordi Duarte Campderros, Efren Navarrete Ramos,
Marcos Fernandez Garcia, Ruben Lopez Ruiz
IJS (AIDAinnova): Gregor Kramberger, Jernej Debevc
The UFSD group (University of Torino / INFN): Roberta Arcidiacono, Nicolò Cartiglia, Marco Ferrero, Leonardo Lanteri, Luca Menzio, Roberto Mulargia, Federico Siviero, Valentina Sola
INFN Genova: Claudia Gemme
UZH (AIDAinnova): Anna Macchiolo, Matias Senger
Korea: D. Lee, W. Jun, T. Kim
CERN: A. Rummler, V. Gkougkousis
Luca Menzio – INFN Toino

## Slide 29: Acknoledgements
Luca Menzio – INFN Toino
We kindly acknowledge the following funding agencies and collaborations
This project has received funding from the European Union’s Horizon 2020 Research and Innovation programme under Grant Agreement No 101004761
INFN - Gruppo V, UFSD and RSD projects
INFN – FBK agreement on sensor production (convenzione INFN-FBK)
Horizon 2020, grant UFSD66952
Dipartimenti di Eccellenza, Univ. of Torino (ex L. 232/2016, art. 1, cc. 314, 337)
Ministero della Ricerca, Italia , PRIN 2017, progetto 2017L2XKTJ – 4DinSiDe
Ministero della Ricerca, Italia, FARE, R165xr8frt_fare

## Slide 30: Resistive Read-out
In resistive read-out, instead of many p-n diodes, there is a single diode.
The n-doped implant is resistive and acts as a signal divider
Very uniform electric and weighing fields, perfect geometry for timing
Luca Menzio – INFN Toino
TREDI 2024
21st February 2024

## Slide 31: Runs
Two test beam performed: June and August
Practically, only August has good runs (Mimosa problems, not much time for RSDs runs)
41 | Data run, EVERYTHING LOOKS GOOD 🎉 🍻 🥳 | 87470
42 | Data run, EVERYTHING LOOKS GOOD 🎉 🍻 🥳 | 273174
43 | Data run, EVERYTHING LOOKS GOOD 🎉 🍻 🥳 | 27989
44 | Data run, EVERYTHING LOOKS GOOD 🎉 🍻 🥳 CAENGECO2020.log | 127551
50 | Data run, EVERYTHING LOOKS GOOD 🎉 🍻 🥳 | 
51 | 🎉 🍻 🥳 | 409414
52 | 🎉 🍻 🥳 | 39820
4 sensors:
- W13 1.3 mm-pitch
- 2x W7 450 um-pitch
- W3 450 um (low bias due to high current)
2-3 bias points per sensor
Given the nature of the readout board, 4 electrodes were read.
The analysis is restricted to one pixel of the matrix
With trigger signals
But corrupted 6th mimosa plane

## Slide 32: Cuts
1) Tracks within time window
2) Tracks inside the pixel

## Slide 33: First sensor - W13 1.3mm
Very low noise <1 mV
Quite small MPV for the amplitude (as expected) 30 mV
S/N for the single pad is good

## Slide 34: W13 1.3mm
Not very uniform, would benefit from some sort of correction (migration matrix/template/ML)

## Slide 35: Taking a look at the data
W13 1.3 mm has smaller signals
  Although not ideal, it can be used for the reconstruction (rotated by 2.5 degrees)
The data from the first 450 um W7 is good (rotated by 1.7 degrees)
  High-enough signals and
  Another data acquisition was performed in DESY with a similar sensor
The second 450 um W7 has really small signals, even if the bias is almost the same as the first sensor
The fourth sensor (450 um W3) had issues and its signals are very low cannot be used for reconstruction
Taken into consideration in this work
Luca Menzio – INFN Toino

## Slide 36: W13 1.3 mm – Position Reconstruction
Reconstruction with charge imbalance

## Slide 37: W7 450 um
Same as before, slightly better S/N

## Slide 38: W7 450 um
Secondly, positions were reconstructed thanks to the information gathered at another test beam in DESY with a similar sensor. SPS positions are extracted by comparing the pads amplitudes with the ones registered in the DESY data (template)

## Slide 39: W7 450 um – first plane
Resolution is uniform over the whole pixel

## Slide 40: Comparison with TCT – 1.3 mm
TCT data was corrected, but the results are still comparable
This analysis
For sake of completeness, the S/N ratio is different and this point should be further on the right. A correction is needed

## Slide 41: Comparison with TCT – 450 um
TCT data was corrected, but the results are still comparable
This analysis
The difference is more visible in this plot

## Slide 42: RSD2 Gain
UFSD4