## Slide 1
Glass-free SiPMs with Through Silicon Vias for VUV/NUV light detection
J. Dalmasson, L. Parellada-Monreal, F. Acerbi, A. Ficorella, A. Gola, S. Merzi, M. Ruzzarin, N. Zorzi and G. Paternoster
Fondazione Bruno Kessler
Feb 21st 2024
jdalmasson@fbk.eu www.fbk.eu

## Slide 2: Outline
Vacuum Ultra-Violet (VUV)
SiPM Technology
Bulk TSV
First Run of Glassless VUV-sensitive SiPM at FBK
Electrical Characterization
Conclusion

## Slide 3: Vacuum Ultra-Violet (VUV)
Why Vacuum?
This part of the spectrum is strongly absorbed by most gases present in atmosphere labs~0.1-10mm
It propagates only in vacuum (or noble gasses)

## Slide 4: Why is VUV Detection Interesting?
Industrial Gas Analysis
Isomer identification
Interaction with wide variety of gases
Rare Events Physics
Liquid Xenon (LXe) based experiments:
Good Absorber
Chemically Inert
High Yield Scintillator (178nm)
Self-Transparent

## Slide 5: Why is VUV Detection Interesting?
Industrial Gas Analysis
Isomer identification
Interaction with wide variety of gases
Rare Events Physics
Liquid Xenon (LXe) based experiments:
Good Absorber
Chemically Inert
High Yield Scintillator (178nm)
Self-Transparent
Exotic Application for Quantum Technologies

## Slide 6: Single Photon Avalanche Diode (SPAD)
Metal contact
Bulk
epi
Deep
Trench
Isolation
Quenching resistor
Depletion region
=
=
High Field Region
p-n junction biased above the breakdown voltage ()
Photon absorption or thermally generated carriers trigger the avalanche process macroscopic current
Avalanche quenched by an external circuit or a quenching resistor
Properties:
Gain ()
Excellent timing ()
Low operating bias voltage ()
Single photon sensitivity

## Slide 7: Silicon PhotoMultiplier (SiPM)
SPADs connected in parallel and arranged in arrays
Applications:
HEP and AP experiments
Biomedical Imaging (PET, ToF-PET…)
Industrial, automotive, …

## Slide 8: Noise in SiPM
Primary DCR
Primary Dark Count Rate
  Thermally generated carriers or tunneling
Acerbi F., Gundacker S, “Understanding and simulating SiPMs”, Nuclear Instruments and Methods in Physics Research Section A, 926, 2019,16-35,, https://doi.org/10.1016/j.nima.2018.11.118.

## Slide 9: Noise in SiPM
Primary DCR
After Pulse
https://doi.org/10.1016/j.nima.2018.11.118
Primary Dark Count Rate
  Thermally generated carriers or tunneling
After Pulse
  Trapping and release of carriers in the same cell

## Slide 10: Noise in SiPM
Primary Dark Count Rate
  Thermally generated carriers or tunneling
After Pulse
  Trapping and release of carriers in the same cell
Direct Cross Talk
  Secondary photons produced in the avalanche are absorbed in the neighboring cells
Delayed Crosstalk
  Secondary photons produced in the avalanche are absorbed in the neutral region, then the photo-generated carriers diffuse towards the active region and trigger the avalanche in the neighboring cells
Primary DCR
After Pulse
DiCT
DeCT
https://doi.org/10.1016/j.nima.2018.11.118

## Slide 11: Wide SiPM R&D Program at FBK

## Slide 12: Wide SiPM R&D Program at FBK

## Slide 13: VUV-HD Technology
In a nutshell:
  Optimization of the charge collection close to the surface
  Minimization of reflection and absorption in the ARC
  Removal of the Si3N4 layer (strongly absorbs VUV)
https://doi.org/10.1109/TED.2019.2935690
T=165K
p+-on-n junction
35x35mm2 cell size
10x10mm2 SiPM

## Slide 14: Towards High Integration: TSV
Silicon Photo-Multiplier (SiPM)
Single photon sensitive silicon detector
Compact and modular device
High integration capability with Through Silicon Vias (TSV)
What is a TSV?
Vertical electrical connection that passes completely through a silicon wafer, bringing the signal from the top (normally photosensitive side) to the bottom side of the device tier (interface with the front-end electronics)
TSV drawbacks for a SiPM
Device attached to a glass support wafer
Presence of a permanent bonding adhesive
TSV advantages for a SiPM
High density array assembly with reduced non-active area
Wire-bond not required in application where it is potentially critical
Example of SiPM with TSV from Broadcom
Source: onsemi.com

## Slide 15: VUV Related Challenges
200
300
350
400
Wavelength (nm)
0
20
40
60
80
100
Transmission [%]
Borosilicate Glass
SCHOTT
1- 0.70 mm
2- 1.00 mm
3- 2.00 mm
4- 3.00 mm
5- 5.00 mm
250
Borosilicate Glass
SCHOTT
Glass used for support wafer
VUV
Glass can only be present as support structure during manufacturing and removed afterwards

## Slide 16: Solution proposed: Bulk-TSV
SPADs
High resistivity epi-layer
(few µm)
Support Glass
(only for processing)
TSV
Trench isolation
Back contacts
Low resistivity substrate
(> 100 µm)
Bulk-TSV concept
It exploits the low resistivity substrate of SiPM to create TSV without any metallization.
Silicon TSV (no metal filling), delimited by pass-through trenches.
TSV density in the range 1-100 vias/mm2
Low resistivity (estimated ~10 Ohms) per via
TSV width in the range 10 µm – 100 µm. It depends on the Final Silicon Thickness.
For the glass-free version Si thickness ~150 µm. Via diameter = 100 µm
Bulk- TSV
SiPM trench

## Slide 17: Fabrication process flow - TSV Via Last (not to scale)
1- SiPM fabrication
2- Temporary Glass Bonding
3- Grinding down to about 150 µm
4- TSV formation + contacts formation
Front end of line is unchanged
5- Debonding
Thickness at least 150 µm
Metal
Silicon
N-P junction
Oxide
Adhesive
Organic polymer
Glass
Quenching resistor

## Slide 18: SiPM with Via-Last TSV: Device layout
TSV
First produced wafer with TSV at FBK
The fill factor is reduced by less than 1% compared with non-TSV SiPM
150 µm Silicon thickness wafer
10 mm x 10 mm SiPM
10 TSV in parallel per SiPM
Vias diameter: 100 µm

## Slide 19: Electrical characterization: SiPM with TSV
Series Resistance of 2 TSV
Single TSV Rs ~ 6-15 Ohm
(dominated by the resistance of the epitaxial layer)
(2-wires measurements. Parasitic resistances are included)
10 TSV in parallel per SiPM
Total TSV resistance/SiPM ≤ 1.5 Ohm/SiPM
Ongoing approaches to further reduce the TSV resistance:
Removing the epitaxial layer
Doping the epitaxial layer
Increasing the number of TSV

## Slide 20: Electrical characterization: SiPM with TSV at RT
I-V curves of SiPM with and without TSV are comparable at RT
Pre-breakdown current
Breakdown voltage
2nd divergence

## Slide 21: Electrical characterization: SiPM with TSV at RT
I-V curves of SiPM with and without TSV are comparable at RT
Pre-Breakdown current

## Slide 22: Electrical characterization: SiPM with TSV vs Temp.
I-V curves of SiPM with and without TSV are also comparable at -40C

## Slide 23: Electrical characterization: SiPM with TSV at RT
Delayed 2nd divergence: most probably due to a reduction of external optical crosstalk probability due to the absence of the glass carrier
Effect of the glass wafer
2nd divergence related to the correlated noise

## Slide 24: Electrical characterization: SiPM with TSV at RT
Delayed 2nd divergence: most probably due to a reduction of external optical crosstalk probability due to the absence of the glass carrier
Light emitted during avalanche
External crosstalk is generated by secondary photons emitted during an avalanche that escape from the silicon device, are reflected on the different optical interfaces above the SiPM, and return to the device generating a new avalanche in a different cell.
Increase of the correlated noise
↓
Anticipated 2nd divergence
↓
Limited maximum excess bias
↓
Limited PDE
Gola, Alberto, et al. "SiPM optical crosstalk amplification due to scintillator crystal: effects on timing performance." Physics in Medicine & Biology 59.13 (2014): 3615.
Effect of the glass wafer

## Slide 25: Electrical characterization: SiPM with TSV at RT
Delayed 2nd divergence: most probably due to a reduction of external optical crosstalk probability due to the absence of the glass carrier
Light emitted during avalanche
Effect of the glass wafer
2nd divergence related to the correlated noise

## Slide 26: Electrical characterization: SiPM with TSV at RT
Yields
Fraction of OPEN TSV
top metal is not in contact with the back metal
Fraction of SHORT TSV
the bulk is contacted with the TSV
NO OPEN TSV
OBSERVED

## Slide 27: Electrical characterization: SiPM with TSV at RT
Yields
Fraction of OPEN TSV
top metal is not in contact with the back metal
Fraction of SHORT TSV
the bulk is contacted with the TSV
Fraction of Shorted TSV [%]
NO OPEN TSV
OBSERVED

## Slide 28: Conclusions
FBK has successfully fabricated Glass-less SiPM with Through Silicon Vias for VUV light detection preserving the main parameters of the device such as:
                - Pre-breakdown current
      - Breakdown voltage
      - Wafer yield for 10x10mm2 SiPM
Bulk-TSV technology using silicon as a conductive material has been presented
TSV resistance achieved is in the range of 10 Ohm/TSV. Process-related approaches to further reduce it are ongoing
      Debonding the glass carrier wafer has shown a shift on the 2nd divergence most probably due to a reduction of the external optical cross-talk probability
at RT and at -40C
Bulk-TSV technology can be easily applied to different applications apart from physics experiments such us for TOF-PET applications

## Slide 29
lparelladamonreal@fbk.eu www.fbk.eu
Thank you
9th November 2023

## Slide 30: Future and ongoing work with Bulk-TSV technology
Bulk- TSV
SiPM trench
~ 20 µm
~ 50 µm
Record of Timing
Petvision project
JS-03-02 Digilog: A digital-analog SiPM towards 10 ps prompt-photon tagging in TOF-PET
S. Gundacker et al.
Very fine TSV pitch  “miniSiPM”
M-03-043 Next generation PET imager
R. Pestotnik et al.

## Slide 33: Other TSV approach: Via Mid
Via Mid
SiPM fabrication + TSV formation
Edge Trimming + BONDING
THINNING
High thermal budget allowed (high quality and conformal material deposition)
Necessity to adapt the device process flow  Critical lithography needs to be carried out after the TSV fabrication
DEBONDING
NO-DEBONDING
Thickness 10-50 um
Thickness at least 150 um
Contacts formation

## Slide 34: PDE VUVHD4 at 340 nm
VUV-HD4, HD5 and HD6 have the same technology so similar PDE performances are expected among the three runs

## Slide 35: VUVHD4

## Slide 36: Cyclotene transmittance
Few um of BCB are used as the adhesive for permanent bonding

## Slide 37: # of Short TSV/ SiPM
# SiPM per wafer

## Slide 38: 3. SiPM with Via-Last TSV: IV curves
W7
R ~ 16.8Ω
Example of a “good” device
Same I-V curves, regardless of the used TSV channel
150um
100um
BACK
Front
few um width
Organic polymer
Marked as good SiPM
Good TSV
Reverse
Forward

## Slide 39: 3. SiPM with Via-Last TSV: IV curves – Failure analysis
W7
R ~ 13Ω
Marked as 1 bad TSV
R ~ 4Ω
150um
100um
BACK
Front
few um width
Organic polymer
Reverse
Forward

## Slide 40: 3. SiPM with Via-Last TSV: IV curves – Failure analysis
W7
R ~ 16.5Ω
Example of a defective SiPM with good TSVs
Same I-V curves, regardless of the used TSV channel
Reverse
Forward
Marked as good TSV
Bad SiPM
150um
100um
BACK
Front
few um width
Organic polymer

## Slide 41: Forward I-V
Chart: 
| 0 | 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9 | 0.95 | 1 | 1.05 | 1.1000000000000001 | 1.1499999999999999 | 1.2 | 1.25 | 1.3 | 1.35 | 1.4 | 1.45 | 1.5
s10_03_05_01 | 1.5056e-09 | 6.4944e-07 | 1.3095e-06 | 1.9958e-06 | 2.7469e-06 | 3.682e-06 | 5.25e-06 | 9.3804e-06 | 2.4343e-05 | 8.2435e-05 | 0.00028172 | 0.00072342 | 0.0013665 | 0.002146 | 0.0030366 | 0.0040409 | 0.0051647 | 0.0064133 | 0.0077878 | 0.0092871 | 0.010908 | 0.012645 | 0.014496 | 0.016458 | 0.018518 | 0.020674 | 0.022918 | 0.025246 | 0.02765 | 0.030127 | 0.032671
s10_11_02 | 2.01e-11 | 2.5898e-09 | 1.1501e-08 | 4.3666e-08 | 1.5755e-07 | 5.615e-07 | 2.0187e-06 | 7.509e-06 | 2.9828e-05 | 0.00012944 | 0.00057846 | 0.0020502 | 0.0048639 | 0.0085926 | 0.012829 | 0.017364 | 0.022085 | 0.026937 | 0.031891 | 0.036908 | 0.041983 | 0.047104 | 0.052263 | 0.057457 | 0.062681
SiPM with TSV
R ~ 16.8 Ω
SiPM without TSV
R ~ 11.3 Ω
I (A)
V (V)
Forward