## Slide 1
Innovative calorimeters with optical readout
Crystal detectors (Sub-task 8.3.1):
Results from beam tests of fast crystals and nanocomposite scintillators
AIDAinnova WP8 Face-to-Face Meeting
18 January 2024
Matthew Moulson, INFN Frascati
For the Frascati, Torino, Glass To Power groups
with contributions from Ferrara, Napoli, Insubria, and CERN

## Slide 2: Beam tests and measurement program
S1, S2 Trigger scintillators
C1, C2 Si-strip trackers, 10×10 cm2, σ = 50 μm
T0 Timing reference, σt = 25-50 ps
Module Device under test, with goniometer
PbGl Lead-glass calorimeter
SPS H2 e−, mips, 20-150 GeV
PS T9 e−, mips, 1-10 GeV
Frascati BTF e−, 450 MeV
Setup:
Facilities and beams:
Topics to investigate:
Crystals for fast, compact calorimeters (WP8.3.1)
Nanocomposite scintillators for calorimetry (WP8.3.1 + 13.5)

## Slide 3: Fast, compact crystal calorimetry
R&D for future experiments to develop new concepts for crystal calorimeters
    Cerenkov radiators like PbF2 or ultra-fast scintillators such as PWO-UF
  Transverse and longitudinal segmentation for γ/n discrimination
  Exploit coherent interactions in crystals to reduce thickness?
PWO-UF (ultra-fast):
Dominant emission with τ < 0.7 ns
M. Korzhik et al., NIMA 1034 (2022) 166781
CRILIN calorimeter for muon collider
arXiv:2206.05838
5 layers
40x10x10 mm3
HIKE small-angle calorimeter
4 layers
40x20x20 mm3

## Slide 4: Tests with single crystals in 2022
Sept/Oct 2022 run at SPS H2 beamline:
20-120 GeV e− and MIPs (150 GeV π)
Validate CRILIN readout electronics
Study systematics of light transport in small crystals with high n
Measure time resolution achievable for PbF2 and PWO-UF
CRILIN 2-crystal module
Positioning of module on beamline
Beam image from Si-strip tracker with condition on signal from crystal
SiPM readout scheme

## Slide 5: Time resolution for single crystals
σMT = σ(tch0 – tch1)/2
FC Beam incident from front
BC Beam incident from back
(SiPM side)
Conclusions:
Effects of light transport degrade timing resolution for frontal incidence, despite higher light yield
PbF2 provides better time resolution due to pure Cerenkov emission, even with 50% light yield of PWO-UF
Both single crystals give σt < 30 ps for Edep > 3 GeV!
Front. Phys 11 (2023) 1223183
PbF2
PWO-UF

## Slide 6: Tests of CRILIN prototype in 2023
From single crystals to first calorimeter prototype:
New prototype with two 3x3 CRILIN test layers
Load layers with different crystals: PbF2, PWO-UF
  Different surface treatments to damp internal reflections
Test objectives:
Perform complete operational test
Test cluster reconstruction capability
Conceptual test of longitudinal segmentation
Study angular effects: align beam with central crystal
Test beam runs in 2023:
June: Commissioning
1-4 GeV e−, mips in T9
450 MeV e− at BTF
Aug: Data taking
20-120 GeV e− in H2
Oct: Alignment studies
4 GeV e− in T9

## Slide 7: CRILIN results
Total energy
MC 120 GeV e−
Total energy
Data 120 GeV e−
Tracking data with cuts on each crystal
Central crystal layer 1
σt = 9 ps!
H2 beamline, Aug 2023

## Slide 8: Radiation resistance of crystals
60Co γ irradiation at Calliope, ENEA Casaccia, June 2023
Easy to accumulate MGy doses, full dosimetry support
Support with transmission, light yield, fluorescence spectrometry measurements
At 360 kGy ~ 20% transmission loss at λ = 400 nm
Substantial recovery after annealing several days in ambient light
At 2100 kGy ~ 5% transmission loss at λ = 400 nm
Only modest recovery after annealing several days in ambient light
Preliminary results:

## Slide 9: Coherent effects in crystals
Coherent effects increase cross-section for electromagnetic shower processes (bremsstrahlung, pair production)
Decrease effective value of X0
Exploit coherent effects for calorimetry?
Coherent superposition of Coulomb fields
Electric field ε approx. const. ~ 1010-1012 V/cm
Effective field ε′ = γeff (γeff = E/mec)
For ε′ ~ ε0 = 2πm2c3/eh virtual pairs disassociate
Pair production enhanced by coherent effects at small θγ and high Eγ
Early initiation of EM showers
Minimize fluctuations of deposited energy vs depth
Amorphous
Aligned
Geant4 simulation: e− on PWO
Bandiera et al., NIMA 936 (2019)

## Slide 10: Calorimetry with aligned crystals
Exploit effects of coherent interactions in crystals to develop a highly compact calorimeter
OREO project for aligned PWO-UF crystal calorimeter
Developed techniques for crystal characterization, shaping, alignment and assembly
  Front. Phys, 11 (2023) 1254020
Obtained alignment of 1-dim and 2-dim matrices to ~ 0.2 mrad
Aligned layer
OREO prototype
Excellent response to photons
  Enhanced probability for γ conversion
High transparency to hadrons
γ/n discrimination
E deposited vs absorbed
120 GeV e− on 4.6X0 PWO
STORM collab
In preparation

## Slide 11: OREO results
Crystal imaged with beam
3x1 crystals with SiPM on goniometer
Energy loss
PWO-UF
Axial vs. random
Crystal planes in PWO-UF revealed by scintillation light read out from crystals
rotation [rad]
Forward energy [MeV]
x [cm]
y [cm]
Lead glass energy [GeV]
OREO ADC [cts]
Lead glass energy [GeV]
Mixed beam: Anticorrelation for e− between forward energy and light from crystals
40 GeV mips + e−

## Slide 12: Nanocomposite scintillators for calorimetry
Semiconductor nanostructures can be used as sensitizers/emitters for ultrafast, robust scintillators:
Perovskite (typically CsPbX3, X = Br, Cl…) nanocrystals cast into polymer matrix
  Cast with polymer matrix
  Emission components with τ << 1 ns
  Radiation hard to O(1 MGy)
NanoCal project: Construct a calorimeter prototype with NC scintillator and test with high-energy beams
Shashlyk design naturally ideal as a test platform:
Easy to construct with very fine sampling
Primary scintillator and WLS materials required: both can be optimized using NC technology
Additionally exploring:
New dyes for optimized conventional scintillators
Fast, bright green scintillators for additional radiation hardness
KOPIO/PANDA design
Fine-sampling shashlyk

## Slide 13: NanoCal project goals and status
Oct 2022: First shashlyk component test at CERN: fibers/tiles/SiPMs
2023: Further iterations to improve performance of NC scintillator prototype
2024: Construction of full-scale shashlyk modules; performance comparison
Possible application for construction of HIKE (future NA62) calorimeter
Prototypes tested in summer 2023:
Conventional scintillator (Protvino), Y-11 fibers
Conventional scintillator (PVT + DDB), Y-11 fibers
PMMA + CsPbBr3 0.2%, O-2 fibers
PMMA + CsPbBr3 0.2%, Custom NCA-1 fibers
PMMA + CsPb(Br,Cl)3 + coumarin-6, NCA-1 fibers

## Slide 14: Example of nanocomposite optimization
Previously used CsPbBr3 in PMMA (green emission) → too much self absorption
A promising solution:
Use CsPb(Br,Cl)3: Substitution of some Br with Cl shifts emission to blue
Add coumarin-6 as a high-Stokes-shift WLS → shifts emission back to green
Synthesis of CsPbBr3
Substitution of 50% of Br with Cl
Addition of coumarin-6
However, surface passivation of nanocrystals destroyed during substitution reaction, leading to aggregation (milky appearance, poor transparency)
First prototype tested anyway with custom (NCA-1) fibers at June test beam

## Slide 15: Results from shashlyk prototypes
June test beam: Efficiency maps with 10 GeV μ, threshold = 5σnoise
Disappointing result from new nanocomposite: only light is from readout fibers
Protvino
CsPb(Br,Cl)3 + WLS
However: Lots of good ideas for next steps
Direct synthesis of CsPb(Br,Cl)3 to preserve surface passivation
Use of an aromatic matrix material, e.g., PVT as in conventional scintillator
  Current formulations use PMMA: gives no primary scintillation contribution
  Now have new protocol to use perovskites with thermally polymerized matrix, with or without additional WLS
New samples synthesized and tested in fall 2023:
  Develop scintillator to test in beam at BTF in spring 2024

## Slide 16: Light yield tests with new samples
Protvino
Bic 4
Bic 5
Bic 1
Bic 2
Bic 3
Tests with mip and e− beams at PS and BTF:
Reference sample:
  1.5% PTP + 0.04% POPOP in PVT (“Protvino”)
Bicocca 4, 5: CsPbBr3:Yb perovskites in PVT
  ~50% light yield of ref. sample
  Our first nanocomposites with good mip response!
Bicocca 3: Coumarin-6 in PVT with PTP + BTP
  ~160% light yield of ref. sample!
Frascati BTF, Nov 2023
Normalized counts
Normalized charge spectra
Single 450 MeV e− events
Frascati BTF, Nov 2023
Charge [pC]

## Slide 17: New scintillators and future directions
New samples with 1-2.5% CsPbBr3:F in PVT with/without additional dyes to be tested at BTF in Feb 2024!
Surface passivation with fluorine allows use of thermally polymerized matrix (PVT) and higher nanocrystal concentration
Additional BTF beam time reserved for Apr 2024 if needed (new ideas?)
Ready to build new prototypes as soon as optimized candidates are ready