## Slide 1
Study on Surface Asperities
in Bakelite-RPC
N. Majumdar1, S. Mukhopadhyay1, P. Bhattacharya1, S. Biswas3, S. Bhattacharya1, S. Saha1,
S. Chattopadhyay2
1Saha Institute of Nuclear Physics, Kolkata, India
2Variable Energy Cyclotron Centre, Kolkata, India
3GSI, Dermstadt, Germany
RPC2012 Workshop, 5-10 February, 2012
INFN Frascati

## Slide 2: Introduction
Main goal of the study
To develop large bakelite RPC without linseed oil coating for the experiment in India-based Neutrino Observatory
&
For operation in streamer mode
The active detector in India-based Neutrino Observatory (INO) RPC
S. Biswas et al., RPC2010

## Slide 3
Arrangement of the scintillators and the RPC
Cosmic ray test bench
Power supply, front-end electronics and DAQ
Flow rate: 0.4 ml/min
(3 detector volume/day)
4 gas mixing unit
S. Bose et al., Nucl. Instr. and Meth. A 602 (2009) 839.
S. Biswas et al., RPC2010
Notes: 3
3

## Slide 4: Initial results
With silicone coating
Efficiency plateau >90% obtained.
Counting rate decreased.
Current decreased,
A few small prototypes have been tested.
Without silicone coating
Current increases rapidly.
After a certain voltage efficiency decreases in all cases.
S.Biswas, et al., Nucl. Instr. and Meth. A 602 (2009) 749
S. Biswas et al., RPC2010

## Slide 5
Gas Mixtures:
TFE + Isobutane (95:5))
TFE + Isobutane +SF6 (95:4.5:0.5, 95:2.5:2.5, 92:3:5)
Ph. D. Thesis, S. Biswas
Induced Charge Measurements
Measured charge in avalanche mode of operation of silicone coated RPC

## Slide 6
AFM Images and Analysis of Bakelite Surfaces
2 mm thick
1.6 mm thick (Smoother surface)
This material was selected for most of the RPC fabrication
S. Biswas et al., RPC2010

## Slide 7
Least square fitting of profilometer data and plot of residuals
Estimation of Surface Roughness
7
S. Biswas et al., RPC2010
Notes: 7

## Slide 8
Electric field configuration inside the gas gap and in close proximity to a square pillar of height 4 micron and base 100x100 micron2
Modeling of Surface Asperities
Voltage: 9kV
Analytic field: 29.67 kV/cm

## Slide 9
Electric field configuration inside the gas gap and in close proximity to a cone-shaped asperity of height 4 micron and base 100x100 micron2
Modeling of Surface Asperities
Voltage: 9kV
Analytic field: 29.67 kV/cm

## Slide 10
TFE + Isobutane mixture (95:5)
Operating voltage: 8.9 kV – 10.39 kV
Analytic Field: ~ 29.34 – 34.26 kV/cm
Transport Properties
Amplification by a few tens of electrons accompanied by negligible attachment !!
Operating region

## Slide 11
TFE + Isobutane + SF6 (95:4.5:0.5)
Operating voltage: 8.91 – 10.39 kV
Analytic field: 29.37 – 34.56 kV/cm
Transport Properties
Amplification by a few tens of electrons accompanied by a few hundreds of attachment !!
Operating region

## Slide 12
Avalanche of an electron released at the centre
Operating voltage 9.86 kV
Gas: TFE + Isobutane (95:5)
Electron Avalanche

## Slide 13
Avalanche of an electron released at the centre
Operating voltage: 12 kV
Gas: TFE + Isobutane (95:5)
Electron Avalanche

## Slide 14
With silicone-treated
Bakelite
Effect of Surface Asperity
Simulated electric field with 12 kV potential applied to the RPC
With a cone shaped asperity on Bakelite
A sharp rise in the field near asperity which can alter the induced charge or signal. Surface treatment removes the spike and the field is larger throughout!!

## Slide 15
With silicone-treated
Bakelite
Effect of Surface Asperity
Simulated induced current with 12 kV potential applied to the RPC
With a cone shaped asperity on Bakelite
Larger signal is induced in surface treated Bakelite which follows the field configuration.

## Slide 16
The present simulation in general seems to under-predict the induced signal in Bakelite RPC in comparison to the measurements.
Possible reasons for the disagreement of the simulation with experiment may be: i) improper field simulation ii) underestimated transport properties, iii) experimental uncertainties.
Field has been simulated by neBEM V1.8.7 which produced field values in agreement with analytical ones. However, more accurate configuration can be achieved by introducing more precise geometrical and physical parameters.
The transport properties of TFE based mixtures may require some attention since Magboltz 8.9.3 indicates very low amplification in the relevant parameter space.
Experimentally, there can be uncertainties arising in the geometrical parameters, as well as electrical permittivity of various dielectric media.
The presence of surface asperities has been found to significantly distort the otherwise uniform field configuration depending on their shape and amplitude.
The distorted field can be responsible for localized large currents following larger amplification.
Present calculation shows slightly larger induced current in surface-treated RPC in comparison to that without surface treatment
Further detailed investigation is underway.
Concluding Remarks