## Slide 1: Nb3Sn Magnet status & plan for FCC-hh
Stefania Farinon e Massimo Sorbi

## Slide 2: Understanding Nb3Sn
Nb3Sn in an intermetallic compound of Nb and Tin which is superconductor below 18 K and 30 T.
State of the art Nb3Sn strands can carry up to JC(16 T, 4.2 K)=1200 A/mm2.
14 T are within reach, 16 T could potentially be unachievable even at 1.9 K.
Courtesy D.Novelli
14
16

## Slide 3: Technology Readiness Level
Can we forego the use of Nb3Sn in developing the dipoles for future accelerators?
  NO: HTS are still in R&D phase (TRL 2−3)
Is Nb3Sn ready?
  12 T dipoles are close to demonstration (TRL 6−7)
  14-16 T dipoles still need ~5 years of R&D (TRL 4−5)
If the HEP community settles for 12 T, FCC-hh could be ready by 2045─2050

## Slide 4: R&D on Nb3Sn conductor
R&D is not only required for magnets but also for conductors
  for transport properties:
    JC(16 T, 4.2 K)=1200 A/mm2 state of the art of Nb3Sn strands (HiLumi)
    JC(16 T, 4.2 K)=1500 A/mm2 target performance for FCC-hh @ 16 T
  for field quality:
    SC filament diameter is currently 45-50 mm (HiLumi), which leads to field quality errors of the order of 50-60 units due to persistent currents (these errors are of the order of 7 units in the LHC)
    corrective actions may include: - reducing the filament diameter to 25-30 mm - implementing passive correction systems and enhancing active correction capability

## Slide 5: M.Benedikt, HFM Meeting, Oct. 2023

## Slide 6: M.Lamont, CERN HFM program
Limits of Nb3Sn are in the 14─16 T range
Why confirming the 12 T (FalconD) step?

## Slide 7: Nb3Sn dipoles: 12 T vs 14─16 T
There is a significant technological leap between achieving a magnetic field strength of 12 T and that of 14-16 T
12 T
16 T

## Slide 8: Why confirming the 12 T step?
Feasibility Assessment: By mastering the FalconD project, we validate our capability to construct Nb3Sn coils and manage associated mechanical challenges. Also, we demonstrate our readiness to advance to higher field strengths.
Technical Validation: The FalconD project serves as a validation of our technical expertise and infrastructure in handling Nb3Sn technology. It provides an opportunity to identify any potential issues or limitations early in the process.
Progressive Approach: Opting for a 12 T step allows for a measured and progressive approach towards higher field strengths. It provides a solid foundation upon which to build future developments and advancements in magnet technology.
Timely Deployment: Focusing on the FalconD project ensures timely deployment of a 12 T magnet, which can have significant implications for ongoing research and future accelerator projects.
Overall, confirming the 12 T step with FalconD is essential for ensuring the successful development and deployment of Nb3Sn coils while laying the groundwork for future advancements in magnet technology.

## Slide 9: FalconD in the HFM program
FalconD plays a crucial role in the CERN HFM program's structure.
CERN has confirmed its commitment to the 12 T dipole program.

## Slide 10: The FalconD program
The FalconD program, signed in 2018, is being developed in accordance with the CERN/INFN KE 4102 agreement.
An amendment was issued on March 2023 to update the project's scope and schedule.
The project involves the development and construction of a short model Nb3Sn dipole with the following specifications:
  Single aperture with an inner bore of 50 mm.
  2-layer cos-theta coil, providing a bore field of 12 T at 1.9 K.
  Mechanical assembly using bladder & key technology.
  The total coil length is 1.5 m.

## Slide 11: The FalconD project
The FalconD project includes the following activities:
  At ASG-Superconductors, the manufacturing of:
    1 dummy pole wound with copper cable
    2 practice poles wound with Nb3Sn cable
    5 poles wound with Nb3Sn cable for the single aperture dipole
  At INFN-LASA Lab
    the mechanical assembly and testing @ 4.2 K of the FalconD magnet
ASG Superconductors is responsible for manufacturing the coils, which include 7 Nb3Sn coils and 1 dummy copper coil.
CERN supports all activities and supplies the magnet components, including the cable, spacers, and other necessary items.
INFN is responsible of the magnet design, B&K assembly, and preliminary test @ 4.2 K
at LASA laboratory in Milan.

## Slide 12: Coil production status
The coil drawings are close to be ready
  The longitudinal have been procured from Luvata
  We are finalizing the end spacers; the order has been placed with Tosti
ASG ordered all the tooling from Fantini, with the first batch to be delivered by the end of May
The dummy coil is expected to be ready by the end of this year
2─3 coils could be manufactured in 2025  first magnet assembly in 2026
winding mandrel
pressing bars
curing mould

## Slide 13: Industry in the HFM program
FalconD is the only HFM program that involves industry. This precise strategy adopted since the beginning of the project presents several advantages:
  Expertise and Resources: Industry brings specialized knowledge, experience, and resources which could enhance the program's capabilities and efficiency.
  Scale-up and Production: Industrial partners can easily scale up production processes, enabling larger-scale manufacturing of Nb3Sn coils and magnets.
  Cost Efficiency: Leveraging industry expertise can lead to cost-effective solutions, optimizing the use of resources and potentially reducing overall program costs.
  Quality Control: Industry is adept at implementing robust quality control measures, ensuring the reliability and performance of Nb3Sn coils and magnets.
Overall, partnering with industry in the Nb3Sn program can accelerate progress, improve efficiency, and enhance the quality, ultimately advancing the field of Nb3Sn magnet technology.

## Slide 14: The future of Nb3Sn at INFN
While involving industry in the Nb3Sn program offers numerous advantages, there are also some potential disadvantages to consider:
  Loss of Control: Entrusting key aspects of the program to industry may result in a loss of direct control over certain processes or decisions, potentially impacting the program's direction and outcomes.
  Cost Considerations: While industry involvement can lead to cost efficiencies, it may also incur additional expenses, which could affect the overall program budget.
  Potential Conflict of Interest: Industrial partners may prioritize commercial interests over scientific or research objectives.
  Limited Flexibility: Collaborating with industry may require adhering to established protocols, procedures, or timelines, limiting the program's flexibility to adapt to evolving research needs or opportunities.
For these reasons, INFN, under the IRIS program, is developing a new facility specifically designed for continuous low-intensity research and development of superconducting magnets.

## Slide 15: IRIS Infrastructure at LASA

## Slide 16: IRIS Infrastructure at LASA

## Slide 17: Heat treatment furnace
The heat treatment furnace temporary installed at ASG for the FalconD project has been procured by INFN.
Following the completion of the FalconD project, the furnace will be relocated to LASA in preparation for the 14+ T program.

## Slide 18: INFN 14+ T program (2025─2030)
We are currently discussing with INFN/CERN a program that is a natural evolution of previous efforts (to be funded 50%−50%).
The main objective of this program is to design and implement a demonstrator of an Nb3Sn 14+ T dipole:
  it is designed to reach 14 T at T4 K (with less margin)
  … and 15.5-16 T at 1.9 K
  additional task if the FalconD program will produce 4 viable coils:
    assembly at LASA a double aperture 12 T magnet
     double aperture 12 T dipole can be proved by 2026-27! Important input of the EU strategy.
Full approval received from E.Todesco (HFM Program Leader)

## Slide 19: Nb3Sn 14+ T program timeline
  Year 1 (Jun-2024):
    Focus on electromagnetic design to optimize temperature margin, enhance windability, and assess conductor and cable feasibility.
    Conduct 2D mechanical design to manage peak stress levels.
    Select materials for components and establish manufacturing processes such as curing and impregnation.
    Conduct tests and studies on critical aspects and design choices, including splicing and quench protection.
  Year 2:
    Refine design based on simulation results and insights from mockup testing.
    Procure necessary materials, components, and tooling.
    Establish the cold test station at the LASA laboratory in Milan.
    Continuously improve and refine the quench protection system for enhanced safety and efficient energy removal.
  Year 3:
    Conduct initial tests on the conductor to evaluate windability under realistic conditions.
    Analyze test results and identify areas for improvement in design and manufacturing processes if necessary.
    Construct the first dummy coil and initiate the mechanical assembly process.
  Year 4:
    Finalize design and manufacturing processes for the four-layer Nb3Sn accelerator magnet.
    Start manufacturing of the final magnet version, including spares.
    Complete the configuration of the test station settings.
  Year 5:
    Conduct comprehensive testing of the magnet and perform measurements under various operating conditions.

## Slide 20: Conclusions
FalconD activities are well progressing:
  First dummy coil will be ready by 2024
  First 23 Nb3Sn coils ready by 2025
  First 12 T dipole assembled and tested in single aperture mode in 2026
If the new Nb3Sn program will be approved:
  First 14+ T dipole ready by 2030
  First 12 T dipole assembled and tested in double aperture mode in 2026/2027

## Slide 21: Thanks for the attention