## Slide 1: HTS magnets challanges for Muon Collider cooling cells Marco Statera, INFN-MI LASA

## Slide 2: Outline
intro
Motivation
magnets
MuCol
The HTS magnets for International Muon Collider Collaboration and MuCol
Schedule
HTS magnets specific requirements
Selected examples of HTS magnets
Timeline highlights
Conclusions

## Slide 3: Motivation
Why
Increase performance and/or sustaibability of research institutes
How
High Temperature Superconductors
High current densities at higher temperatures
https://nationalmaglab.org/magnet-development/applied-superconductivity-center/plots

## Slide 4: Motivation
Grateful thanks to fusion
L. Bottura et al, HFM annual meeting
https://indico.cern.ch/event/1302031
C. Senatore et al., Field and temperature scaling of the critical current density in commercial REBCO coated conductors - https://arxiv.org/abs/1512.01930
0.5 T – 19 T
Lines are not a forecast

## Slide 5: Motivation
Sustainability is a driver for next generation Research Institutes and projects
HTS may be one important option for the future colliders
The 60…80 K range would be a dream…
LHC
(FCC)
ESS
This could be the best range of operating temperature of a future HEP collider
RHIC
Tevatron
HERA
LHC
Nb-Ti
8T
5T
Nb3Sn
16T
12…14T
HTS
40…60T
20…40T
a few T
1.9
4.2
77
Credits to P. De Sousa and R. Van Weelderen and L. Bottura, CERN
W/W

## Slide 6: IRIS and Muon Collider are the actual driver for next generation Magnets in HTS
INFRATECH proposal
EUMAHTS: ADVANCING HTS MAGNET TECHNOLOGY FOR EUROPEAN RESEARCH INFRASTRUCTURES
PI L. Bottura, CERN
Split Coil - RFMTF
Magnet Test Facility for RF (and other use)
ESMA
Energy Saving MAgnet
10 T gradient
20 K operation
Conduction cooled
300 mm warm bore
10 T dipole
20 K operation
Conduction cooled
70 mm bore
2025
SCIENCE FOR SUSTAINABILITY
Common R&D to increase TRL of HTS magnet technology

## Slide 7: Present R&D Targets of HFM
A ~14 T operational field LTS dipole magnets for FCC-hh
  Establish the operational margins
  Select the magnet design among multiple variants
  Scale to 14-m-long magnets
A ~20 T operational field HTS or hybrid dipole magnet for FCC-hh
  Close Technology-Readiness-Level Gap with LTS
    Establish HTS technology-stack variants
    Demonstrate accelerator quality
  Establish the operational margins
  Select the magnet design among multiple variants
  Scale to 14-m-long magnets
E. Todesco and B. Auchman
1.9 K
10 K – 20 K
ESMA 10T
https://hfm.web.cern.ch/

## Slide 8: HTS magnets in Muon Collider
Field up 20 T, ≥ 1.2 m, L  18 m
Radiation heat load ≈ 5…10 kW Radiation dose: 80 MGy
IEEE TAS 34,5 C. Accentura et al.
40 T on axis
4 K
Bore size 50 mm
Non Insulated
NC +/- 1.8 T up to 4 kT/s
30 x 100 mm aperture
HTS 10 T steady state
30x100 mm aperture
1+1 km of solenoids
Field Up to 20 T – 25 T
Controlled Insulation
16 T
Bore size 150 mm
Insulated - CI

## Slide 9: 6D cooling
12 unique stages:
  4 cooling stages before bunch recombination (A1-A4)
  8 cooling stages after bunch recombination (B1-B8)
Each stage has a repeating series of a cell type
High field, very compact solenoids
Each cell has symmetric solenoids of opposite polarity
superconducting coil
RF
adsorber

## Slide 10: 6D cooling solenoids design
Some stats:
Fields on axis: 2 to 15 T
Cell Lengths: 0.8 to 2.7 m
Total length of all Stages: ~ 2 km
Total number of solenoids: 5000
based on US MAP original design (field on axis)
Coils size
Stored energy
Quench protection
Current density
Modeling
Conductor and coil behavior
Mechanics
Stress/Force
Magnetic field
TECHNOLOGY OPTIONS
NbTi
Nb3Sn @4K
HTS
HTS @20K
Design challenges
J. Pavan, UMIL and S. Fabbri, CERN
R&D ongoing
CERN, INFN , CEA….

## Slide 11: Accelerator Superconducting Magnets
Parameters
10 T at the center
Rectangular aperture 30 mm x 100 mm
Field quality bn < 10 units (TBC) in beam diameter (20 mm)
Same technology used for ESMA and 6D Cooling solenoids
HTS windings (for robustness)
High current density (for cost reasons)
Operation at high temperature (for energy efficiency)
ESMA
good field region
400 x 30 x 50 mm3
1.5% field homogeneity
 20 mm – b3 20 units
CEA - CERN HFM collaboration
Demonstrator of metal-insulated ReBCO high field coils

## Slide 12: Collider Magnets Requirements
V.V. Kashikhin et al.
3 TeV collider (5 km ring):
Close to state of the art
11T / 140 mm (Nb3Sn)
600 magnets, 5 m length
Operating temperature: 4.5 K
10+ TeV collider (10 km ring):
HTS magnets, R&D is required
15T / 140 mm (ReBCO, hybrid)
1200 magnets, 5 m length
Operating temperature: 4.5…20 K
Challenges
High field dipoles to minimize collider ring size and maximize luminosity
Combined function (B1, B2 and B3)
Large aperture shielding (muon decay)
Proposed solution
Nb3Sn for the 3 TeV machine and HTS (ReBCO) for the 10 TeV collider.
Constraints
Stress limit, mechanical challenges (conductor, force management)
Margin limit, critical current density and stored magnetic energy (quench protection)
Cost, maximum cost per meter of magnet fixed 400 k€/m (about 2 x Eurocircle)

## Slide 13: Dipole design charts
Design target 10 TeV
HTS falls short of required performance with classical insulated coils. Assuming MI or NI magnets, the protection limit becomes comparable with the other limits.
Nb3Sn falls short of required performance because of operating margin and peak stress (at affordable cost !)
Design target 3 TeV
Nb3Sn
HTS
Design target 10 TeV
Design target 3 TeV

## Slide 14: HTS options
What might improve the HTS design?
Fixed the cost per meter of magnet
A reduction of HTS cost
(actually driven by fusion market)
A reduction of operating temperature to 10 K
reduction
Cost
reduction

## Slide 15: R&D and production schedule
Split Solenoids for RFMFTF
Fast pulsed NC dipole for RCS
0
20
5
10
15
RCS string test
20T/20K solenoid model coil for the target
6D cooling cell magnets
NI UHF solenoid
10 TeV HTS short models
3 TeV full-length prototypes
HCS SC dipole prototypes
10 TeV full-length prototypes
1
26
2050
2024
2044
Series production

## Slide 16: Conclusion
HTS magnets are feasibile and sustainable for MC (steady state, high field, high operating temperature)
  Magnetization effects for (slow) ramping and field quality over time are a challenge
  Further modeling, testing and technology development
The 2050 goal may be reasonable considering a strong effort (manpower, R&D and funds)
  The effort involves heavily industry for series production (5k+ magnets)
A promising path for increasing sustainability is 10 K to 20 K operation of HTS magnets
  Intensive R&D and modeling is required to increase the TRL
  Steady state operation is less demanding
Contribution by
CERN: C. Accentura, B. Auchman, B. Bordini, L. Bottura, S. Fabbri, E. Todesco
UMIL: S. Mariotto, J. Pavan, L. Rossi, S. Sorti - INFN: B. Caiffi, D. Novelli, C. Santini - Fusion for Energy: A. Portone
Funded by the European Union (EU). Views and opinions expressed are however those of
the author only and do not necessarily reflect those of the EU or European Research
Executive Agency (REA). Neither the EU nor the REA can be held responsible for them.

## Slide 17: spares

## Slide 18: Existing plants
Temperature | COP-1 in Wpower/Wcool | Source
250 K | 1 | CO 2 plant ATLAS IT
100 K | 12 | LN 2 plant ATLAS
80 K | 16 | LN 2 plant ATLAS
20 K | 50 | 20 K/50 kW Frey’s plot *
10 K | 150 | LHC cryoplant data
4.5 K | 240 | LHC cryoplant data
2.0 K | 960 | LHC cryoplant data
Data from:
Cryogenic options for future accelerators: Muon Collider P. Borges de Sousa, M. Rhandi, T. Koettig, R. van Weelderen Muon Collider Magnets WG Meeting 30th March 2023, online
* Tieftemperatur–Technologie, von H. Frey und R. A. Haefer. Herausgegeben von F. X. Eder. VIII-Verlag, Düsseldorf 1981

## Slide 19: Few considerations on costs
By L. Bottura
6D cooling solenoids are built once
Acceleration for 10 TeV is the highest relative cost
More challenging single magnets are few % of the total cost (also for cooling)

## Slide 20: Comments
HTS magnets may increase the performance and the sustainability HEP facilities, research institutes and society falicilities
The cost of HTS tapes is decreasing thanks to higher request (fusion)
TRL of the magnets have to be increased and the performance have to be demonstrated
R&D, modeling and test devices are ongoing and in construction
Dedicated test bed are requested due to the peculiarities of HTS
A dedicated test station at INFN LASA commissioning starting in 2024 and fully operational mid 2025
The HTS R&D is common to different scientific projects (HFM, FCC, MuCol) and paves the road for societal applications
Industry is deeply involved in the construction of new test beds