## Slide 1
Implantation substrates for the efficient recovery of radionuclides
F. Nicente
March 15th, 2024
Laboratori Nazionali di Legnaro – INFN

## Slide 2
Outline
Implantation substrates
Innovative targets
Characterization and metal recovery
Notes: 2

## Slide 3
Implantation substrates
Mechanical properties
Vacuum resistance
Handling and falling resistance
Appropriate size for IRIS fitting
Low porosity to ensure superficial deposition of radionuclides
Technological properties
Contaminants-free materials
Highly flowing and compacting pow-ders, forming resistant disks
High radionuclides release
Compatibility with a wide panel of radionuclides
Size
Morphology
Porosity
Breaking load
Flowability of the powders
Disaggregation time/behavior
Metals uptake and release
Notes: 3

## Slide 4
State of the art
Soluble targets (e.g. salts, sugars) prepared by powder compaction
 Good metal recovery, but contaminants potentially interfering with separation processes
Notes: 4

## Slide 5
Innovative targets
Targets produced with innovative methods
SPS: sorbitol, PVP 1%(w/w), stearic acid 1%(w/w)
S100: sorbitol 100%
Targets produced with traditional methods
Direct compression:
Polyols
Cellulose and PVA 25:75 w/w crosslinked
Freeze-thaw:
Cellulose
HP: PVP 50%, HPMC 1%
HPS: PVP 50%, HPMC 1%, sorbitol 0,4%
Solution casting:
Polyvinylpyrrolydone (PVP)
Notes: 5

## Slide 6
Characterization and metal recovery
Dimensioni appropriate per l’utilizzo in IRIS
Massa >100mg
Spessore tra 1,15 e 1,56mm
Superficie liscia e omogenea
Forma regolare
Rigidità
SPS
1,55 ± 0,05
1,32 ± 0,02
S100
HP
HPS
13,01 ± 0,01
12,78 ± 0,15
13,86 ± 0,15
1,32 ± 0,02
12,99 ± 0,01
1,51 ± 0,07
Diameter (mm)
Thickness (mm)
20,03±0,14
7,86±0,23
≈0
9,78±0,09
7,02±0,17
≈0
≈0
9,78±0,09
Dimensional analysis
Weight loss in vacuum
After 24 h (%)
After 7 days (%)
Notes: 6

## Slide 7
Characterization and metal recovery
S100
SPS
HP
HPS
Higher degree of fissures
SPS: 2,16%
S100:2,85%
HP:26%
HPS:25%
Notes: 7

## Slide 8
Characterization and metal recovery
High recovery of both metal ions
S100
Bulk solution
≈100
100
SPS
HPS
91,06±1,30
95,09±6,55
≈100
100
91,53±17,36
Recovery (%)
Cu²⁺
Ag⁺
92,68 ± 5,11
Notes: 8

## Slide 9
Conclusions
Notes: 9