## Slide 1
© Klaus Barth
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
Domenico Colella
University and INFN Bari
ALICE ITS3 how to integrate a large dimension MAPS sensor in a bent configuration detector + ALICE3
Torino, 22-23 April 2024
RD_FCC WP-Silicon Mini-workshop

## Slide 2
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3

## Slide 3
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 detector concept
Required improvements
Removal of water cooling → low flow air cooling
Removal of circuit board from the sensitive region
Removal of mechanical support from the sensitive region, profiting from increased stiffness of bent Si wafers
ITS2-IB
Inner-most layer (ITS2)
ITS3
Inner-most layer (ITS2)
Mean X/X0 = 0.05%
Mean X/X0 = 0.364%

## Slide 4
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 detector concept
Key ingredients
Wafer-scale chips (up to ~28x10 cm), fabricated using stitching
Si MAPS sensor based on 65 nm technology
Sensor thickness ≤ 50 μm
Chips bent in cylindrical shape at target radii
Ultra light carbon foam structures
Air cooling

## Slide 5
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 detector concept
Key ingredients
Wafer-scale chips (up to ~28x10 cm), fabricated using stitching
Si MAPS sensor based on 65 nm technology
Sensor thickness ≤ 50 μm
Chips bent in cylindrical shape at target radii
Ultra light carbon foam structures
Air cooling

## Slide 6
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 detector concept
Key ingredients
Wafer-scale chips (up to ~28x10 cm), fabricated using stitching
Si MAPS sensor based on 65 nm technology
Sensor thickness ≤ 50 μm
Chips bent in cylindrical shape at target radii
Ultra light carbon foam structures
Air cooling

## Slide 7
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 detector concept
Key ingredients
Wafer-scale chips (up to ~28x10 cm), fabricated using stitching
Si MAPS sensor based on 65 nm technology
Sensor thickness ≤ 50 μm
Chips bent in cylindrical shape at target radii
Ultra light carbon foam structures
Air cooling

## Slide 8
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 detector concept
Key ingredients
Wafer-scale chips (up to ~28x10 cm), fabricated using stitching
Si MAPS sensor based on 65 nm technology
Sensor thickness ≤ 50 μm
Chips bent in cylindrical shape at target radii
Ultra light carbon foam structures
Air cooling

## Slide 9
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 detector concept
Key ingredients
Wafer-scale chips (up to ~28x10 cm), fabricated using stitching
Si MAPS sensor based on 65 nm technology
Sensor thickness ≤ 50 μm
Chips bent in cylindrical shape at target radii
Ultra light carbon foam structures
Air cooling

## Slide 10
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 detector concept
Key ingredients
Wafer-scale chips (up to ~28x10 cm), fabricated using stitching
Si MAPS sensor based on 65 nm technology
Sensor thickness ≤ 50 μm
Chips bent in cylindrical shape at target radii
Ultra light carbon foam structures
Air cooling

## Slide 11
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 detector concept
The whole detector will comprise six chips and barely anything else!
Key ingredients
Wafer-scale chips (up to ~28x10 cm), fabricated using stitching
Si MAPS sensor based on 65 nm technology
Sensor thickness ≤ 50 μm
Chips bent in cylindrical shape at target radii
Ultra light carbon foam structures
Air cooling
Beam pipe inner/outer radius (mm) | 16.0/16.5 |  | 
IB Layer Parameters | Layer 0 | Layer 1 | Layer 2
Radial position (mm) | 18.0 | 24.0 | 30.0
Length of sensitive area (mm) | 280.0 |  | 
Pseudo-rapidity coverage | ±2.5 | ±2.3 | ±2.0
Active-area (cm2) | 610 | 816 | 1016
Pixel sensor dimension (mm2) | 280 × 56.5 | 280 x 75.5 | 280 x 94
Number of sensors per layer | 2 |  | 
Pixel size (μm2) | O (10 x 10) |  | 

## Slide 12
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 detector concept
This talk content:
Silicon bending
Carbon foam properties
Sensor cooling
Mechanical characterization
Interconnection
The whole detector will comprise six chips and barely anything else!
Key ingredients
Wafer-scale chips (up to ~28x10 cm), fabricated using stitching
Si MAPS sensor based on 65 nm technology
Sensor thickness ≤ 50 μm
Chips bent in cylindrical shape at target radii
Ultra light carbon foam structures
Air cooling

## Slide 13
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 R&D - Silicon bending
Three points bending force measurements:
  MAPS ~50 μm thick are quite flexible
  Large benefit from going thinner
  Project goal thicknesses and desired bending radii achievable
50
30
Layer 0 radius
65 nm
180 nm

## Slide 14
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 R&D - Silicon bending
https://doi.org/10.1016/j.nima.2021.166280
Nominal operating point
https://doi.org/10.1016/j.nima.2021.166280
ALPIDE 180 nm
Laboratory and test beam measurements (Jun 2020) allow to conclude that chip (180 nm CMOS) performance doesn’t change after bending
  Pixel matrix threshold distribution does not change when sensor is bent
  Efficiency above 99.9% at a threshold of 100 e-

## Slide 15
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 R&D - Silicon bending
Nominal operating point
μITS3
180 nm
Laboratory and test beam measurements (Jun 2020) allow to conclude that chip (180 nm CMOS) performance doesn’t change after bending
  Pixel matrix threshold distribution does not change when sensor is bent
  Efficiency above 99.9% at a threshold of 100 e-

## Slide 16
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 R&D - Silicon bending
Board
Sensor
Comparison between flat and bent MLR1 (65 nm CMOS) sensors ongoing
  Bending procedure developed and proximity board adapted to bent configuration
  Few samples prepared and under measurements in laboratory with 55Fe source
MLR1 reticle
Ongoing at INFN Trieste

## Slide 17
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 R&D - Silicon bending
Large dimension silicon bending procedure
  Bending tool: tensioned mylar foil wrapping around cylindrical mandrel
Ongoing at INFN Bari

## Slide 18
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 R&D - Silicon bending
Large dimension silicon bending procedure
  Bending tool: tensioned mylar foil wrapping around cylindrical mandrel
Ongoing at INFN Bari

## Slide 19
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 R&D - Silicon bending
Large dimension silicon bending procedure
  Bending tool: tensioned mylar foil wrapping around cylindrical mandrel
@CERN
40 μm thick MRL1 super-matrix
Ongoing at INFN Bari

## Slide 20
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 R&D - Carbon foam properties
ALLCOMP HD
0.45-0.68 kg/dm3 85-170 W/m∙K
ALLCOMP LD (K9)
0.2-0.26 kg/dm3 >17 W/m∙K
ERG DUOCEL (RVC)
0.06 kg/dm3 0.033 W/m∙K
Silicon sensor kept in position by:
Half-rings Support structures and cooling radiator
Longerons Support structures
Carbon foams characterised for machinability and thermal properties
  ERG Duocel (RVC)
  ALLCOMP LD (K9)

## Slide 21
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 R&D - Carbon foam properties
Cylindricity granted within 0.05 mm using the half-ring
Carbon fleece veil (120 μm thick) between silicon and carbon foam used to:
  Control the glue thickness
  Reduce thermal contact resistance
  Reduce carbon foam footprints on the silicon
X-ray scan of Engineering Model 2 (EM2)

## Slide 22
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 R&D - Sensor cooling
Flow distributors
Dummy beam pipe
CYSS
Cover
C-side
A-side
Thermal characterization setup
dummy silicon equipped with copper serpentine simulating heat dissipation in matrix (25 mW/cm2) and end-cap (1000 mW/cm2) regions
8 PT100 temperature sensors distributed over the surface of each half-layer
airflow from A-side to C-side

## Slide 23
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 R&D - Sensor cooling
Flow distributors
Dummy beam pipe
CYSS
Cover
C-side
A-side
Thermal characterization setup
dummy silicon equipped with copper serpentine simulating heat dissipation in matrix (25 mW/cm2) and end-cap (1000 mW/cm2) regions
8 PT100 temperature sensors distributed over the surface of each half-layer
airflow from A-side to C-side
Layer 0 - Matrix
Layer 0 - End-cap
Comparison between CFD simulations and experiments
Conclusion
with an average airflow free-stream velocity between the layers of about 8 m/s, the detector can be operated at a temperature of 5 degrees above the inlet air temperature
temperature uniformity along the sensor can be also kept within 5 degrees
Temperature sensor position and nomenclature
C-side
A-side

## Slide 24
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 R&D - Mechanical characterization
Short-term position stability of the sensor over time affected by
thermoelastic expansion caused by short-term temperature fluctuation
airflow

## Slide 25
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 R&D - Mechanical characterization
Thermoelastic expansion setup
differential thermoplastic expansion among different components could introduce failures
final grade material half-layer assembly in climate chamber (up to 36ºC by steps of 2 ºC)
Conclusion
several thermal cycles for a total of 9h → assembly unaffected
further tests will be performed to investigate: rapid increase of the temperature and maximum failure temperature
Short-term position stability of the sensor over time affected by
thermoelastic expansion caused by short-term temperature fluctuation
airflow

## Slide 26
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 R&D - Mechanical characterization
No flow - Center
Vibration characterization setup
measurement of the out-of-plane vibrations of the half-layers
confocal chromatic displacement sensors → avoids perturbation to the airflow
Conclusion
RMSairflow < 0.4 μm for L2 (largest sensor), smaller for L0 and L1
8 m/s - Center
8 m/s - C-side
Short-term position stability of the sensor over time affected by
thermoelastic expansion caused by short-term temperature fluctuation
airflow

## Slide 27
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ITS3 R&D - Interconnection
Flexible printed circuits for communication and powering
placed outside the sensible area
three double copper layers flex, multi-strip shaped (15-30 cm long), connected in a merging area
interconnected via wire-bonding at the edge of the sensor verified
  wire-bonds loops optimisation based on pull-force measurements
  present setup (not final grade material): 6.6±0.3 g at ~900 μm pad-to-pad distance
Merging area

## Slide 28
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ALICE3
ALICE3: a silicon sensor based experiment

## Slide 29
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ALICE3 - IRIS
IRIS tracker - Open
IRIS tracker - Closed
Based on wafer-scale, ultra-thin, curved MAPS
Basic requirements
  radial distance from interaction point: 5 mm (inside beam pipe, retractible configuration)
  unprecedented spatial resolution: ≈ 2.5 μm
  unprecedented low material budget X/X0 (per layer): ≲ 0.1%
  radiation tolerance: ≈ 1016 1 MeV neq/cm2 + 200 Mrad
  hit rates up to: 94 MHz/cm2
R&D will largely leverage on the ITS3 developments and push improvements on a number of fronts

## Slide 30
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ALICE3 - IRIS
4 x Petals
Single petal
Sensors (Layers and disks)
Carbon foam and cold plate
Secondary vacuum case

## Slide 31
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ALICE3 - IRIS
0.33 mm wall
Al 5083
3D printed Aluminium
AlSi10Mg
Petal case
bread board model
800 mm long

## Slide 32
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ALICE3 - IRIS
Outgassing studies at INFN Bari
Carbon (LAYPUS) Substrate of the cold plate
Carbon Fleece of the cold plate
Carbon foam All comp high density
Carbon foam All comp low density
Carbon foam ERG duocel
Optical Fiber with connector
NASA Epoxy
Si wafer
Wire bonded Si wafer
FPC
3D printed aluminium nitride (AIN) samples disks
Al2O3 samples disk: 3D printed alumina (Al2O3) samples disks
3D printed AlSi samples disks

## Slide 33
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ALICE3 - MIDDLE LAYER
Prototype by INFN Padova

## Slide 34
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ALICE3 - MIDDLE LAYER
Prototype by INFN Padova

## Slide 35
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ALICE3 - MIDDLE LAYER
Prototype by INFN Padova

## Slide 36
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
ALICE3 - MIDDLE LAYER
Prototype by INFN Padova

## Slide 37
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
Backup

## Slide 38
Oct 2018
Sep 2019
Sep 2019
Dec 2019
Spring 2020
Jun 2020
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
Expression of Interest
[ALICE-PUBLIC-2018-013]
https://cds.cern.ch/record/2644611
Letter of Intent
[CERN-LHCC-2019-018 ; LHCC-I-034]
https://cds.cern.ch/record/2703140/
R&D kick-off (Dec 2019)
LHCC 139 (Sep 2019)
“The LHCC is impressed by the new concept for the ITS3…”
LHCC 142 (Jun 2020)
“The LHCC congratulates the ITS3 groups for the successful start of the project.”
ALICE 2.1
Project setup (spring 2020)
Project leaders
Work packages conveners
Institutes joining
Backup

## Slide 39
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
Backup - Interconnection

## Slide 40
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
Backup - Super-ALPIDE project
Super-ALPIDE
  18 not diced ALPIDE chips
  dimensions close to the ones for L0 sensor
Goals
  verify bending tools for large-size working chips
  verify mechanical support alignment tools
  develop wire-bonding over bent surface tools
  develop first bent flex prototype (for powering and data streaming)
  assemble first working large dimension bent sensor → by October 2023

## Slide 41
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
Backup - Carbon foam properties
200M events @ 5.4 GeV (~300Hz rate)
Preliminary
Kink angle distributions at the scattering position
Carbon foam material budget study though particle deviation angle measurement
Air
Material
ALPIDE

## Slide 42
RD_FCC WP-Silicon Mini-workshop | 22-23 April 2024 | Domenico Colella
Backup - Carbon foam properties