## Slide 1: HISOL
High performance ISOL systems for the production of radioactive ion beams
CSNV Experiment
Work package 3
Material Characterization and Multiphysics Simulation – Status update
Michele Ballan – INFN-LNL

## Slide 2: HISOL Objectives
Such aim foresees three fundamental objectives:
Study and development of innovative recipes and methods to produce ISOL targets
Study and development of innovative methods to produce and operate ion sources
Characterization and multiphysics simulation of the obtained components by means of advanced techniques
Main goal:
Development of a new generation of High Performance ISOL Targets and Ion Sources with cutting edge technologies available within INFN and its collaboration network.

## Slide 3: Work package 3 organization
Work package 3: Materials Characterization and Multiphysics Simulation
emissivity and thermal conductivity measurements
electrical resistivity measurements
microstructural characterization
multiphysics simulations
thermionic emission measurements
Reliable Material Property Data at High Temperature are required for Robust Multiphysics Simulation of ISOL Targets and Ion Sources

## Slide 4: Work package 3 timetable and milestones
 |  | Year 1 |  |  |  | Year 2 |  |  | 
 |  | M3 | M6 | M9 | M12 | M15 | M18 | M21 | M24
WP3 | Materials Characterization and Multiphysics Simulation |  |  |  |  |  |  |  | 
T3.1 | Microstructural Characterization |  |  |  | MS3.1 |  |  |  | 
T3.2 | Thermal and Electrical Characterization |  |  |  |  |  |  |  | 
T3.3 | Mechanical Characterization |  |  |  |  |  | MS3.2 |  | 
T3.4 | Multiphysics Simulation of High Performance ISOL Targets |  |  |  |  |  |  |  | MS3.3
T3.5 | Multiphysics Simulation of High Performance ISOL Ion Sources |  |  |  | MS3.4 |  |  |  | MS3.5
WP3 milestones |  | Date
MS3.1 | Microstructural Characterization | M12
MS3.2 | Thermal, Electrical and Mechanical Characterization | M18
MS3.3 | Multiphysics Simulation of High Performance ISOL Targets | M24
MS3.4 | Definition of the Multiphysics Simulation strategy for High Performance ISOL Ion Sources | M12
MS3.5 | Multiphysics Simulation of High Performance ISOL Ion Sources | M24

## Slide 5: T3.1: Material development and microstructural characterization
Giacomo Voltan, Master thesis in Materials Engineering, UNIPD, Supervisor M. Manzolaro - to be defended end of 2024
Emmanuel Tochukwu Ezeaba, Master thesis in Materials Engineering, UNIPD, Supervisor M. Manzolaro - to be defended end of 2024

## Slide 6: T3.2: Thermal and Electrical Characterization
Chart: ρ vs T
| 1052 | 1166 | 1268 | 1356 | 1439 | 1511 | 1581 | 1643 | 1697 | 1751 | 1799 | 1846 | 1891 | 1934 | 1970
TAAM2_1 | 66.2117 | 70.949 | 75.5906 | 79.1901 | 82.6342 | 85.6145 | 88.6089 | 91.263 | 93.4222 | 95.6547 | 97.6378 | 99.4841 | 101.2073 | 103.2258 | 105.1181
TAAM2_2 | 70.7612 | 74.9938 | 78.9291 | 82.5497 | 85.7266 | 88.4081 | 91.3386 | 93.8835 | 95.9419 | 98.4544 | 100.3375 | 102.5251 | 104.5669 | 106.477 | 108.2677
TAAM2_3 | 68.6244 | 73.3508 | 77.4472 | 81.1339 | 84.6494 | 87.6736 | 90.5991 | 93.1234 | 95.748 | 97.8801 | 99.8542 | 102.1372 | 104.2628 | 105.8268 | 107.2898 | 109.0551
TAAM4_1 | 47.8393 | 53.0886 | 57.7935 | 62.1818 | 65.9707 | 69.3993 | 72.5752 | 75.3612 | 78.015 | 80.3079 | 82.5626 | 84.4564 | 86.4891 | 88.1168 | 89.8972
TAAM4_2 | 47.1859 | 52.4652 | 57.1406 | 61.4172 | 65.2785 | 68.806 | 72.0126 | 74.832 | 77.5209 | 79.8631 | 82.1399 | 84.0678 | 86.1172 | 87.868 | 89.5899
TAAM4_3 | 46.5501 | 51.8543 | 56.6373 | 61.0677 | 64.9509 | 68.4219 | 71.6178 | 74.4407 | 77.1535 | 79.5083 | 81.8289 | 83.8222 | 85.9166 | 87.6008 | 89.4364
Literature Desai | 36.04 | 38.14 | 40.26 | 42.28 | 44.24 | 48.15 | 51.93 | 55.61 | 59.23 | 62.75 | 66.25 | 69.78 | 73.22 | 76.6 | 79.94 | 83.32 | 86.68 | 89.99 | 93.22 | 96.52 | 99.77 | 103.1 | 106.3 | 109.7 | 112.7 | 115.9 | 119.1
Literature Cezariliyan | 75.56 | 78.8 | 82 | 85.14 | 88.23 | 91.26 | 94.24 | 97.17 | 100.04 | 102.86 | 105.63 | 108.34 | 111 | 113.6
Giacomo Voltan, Master thesis in Materials Engineering, UNIPD, Supervisor M. Manzolaro - to be defended end of 2024
Emmanuel Tochukwu Ezeaba, Master thesis in Materials Engineering, UNIPD, Supervisor M. Manzolaro - to be defended end of 2024

## Slide 7: T3.4: Multiphysics Simulation of High Performance ISOL Targets
Proton Beam Properties
(energy, intensity, profile)
Monte Carlo simulations:
Particle transport and interaction with matter
Target characteristics
(composition, geometry, density)
Power deposition
Isotope production
Multiphysics FEM simulations:
Thermal and structural analyses
A complex multistep simulation process
Target temperature field
Thermal analysis
required material properties:
k (thermal conductivity)
ε (emissivity)
Strucutral analysis
required material properties:
E (Young’s modulus)
ν (Poisson’s ratio)
α (coeff. of th. expansion)
Target stress field

## Slide 8: SiC target geometry
1
2
3
4
5
6
7
Disk | Thickness | Diameter | Material
\ | [mm] | [mm] | \
1 | 1 | 13 | SiC
2 | 0,9 | 13 | SiC
3 | 0,9 | 13 | SiC
4 | 0,8 | 13 | SiC
5 | 0,7 | 13 | SiC
6 | 0,6 | 13 | SiC
7 | 0,5 | 13 | SiC
SiC disk thickess and spacing were carefully checked and implemented in the MC model geometry

## Slide 9: SiC target material – operation limits: Tlim and σlim
Manzolaro, M. et al.; Materials 2021, https://doi.org/10.3390/ma14102689
Effect of target overheating: target degradation
Effect of excessive thermal stresses: target failure
Safe temperature range
Target degradation
T<Tlim
T>Tlim
Typical target temperature distribution {T} during irradiation:
Radial temperature gradients
{T} causes the occurrence of thermal stresses {σ}
If σmax > σlim
High risk of target instantaneous failure
σlim for SiC SA: 190 MPa

## Slide 10: Isotope production: SiC target
In-target yields – 40 MeV 2 μA p+ on SiC
[particles/s]
Al beams: reference M. Barbui (2008)
https://doi.org/10.1016/j.nimb.2008.05.04
Na beams: reference J. Jeong (2023)
https://doi.org/10.1016/j.nimb.2023.05.060

## Slide 11: Target possible operation conditions
Chart: Heater current [A]
| 0 | 100 | 200 | 300 | 400 | 500 | 600 | 700 | 800 | 845.12885232108283
1800°C | 11.5276 | 10.4326 | 10.0684 | 9.4943 | 8.7023 | 7.572 | 6.0338 | 3.8258 | 1.1856 | 0
1700°C | 9.2982 | 8.5547 | 8.1414 | 7.5625 | 6.6852 | 5.4022 | 3.5853 | 1.3651 | 0
1600°C | 7.5751 | 6.8302 | 6.3469 | 5.7009 | 4.7036 | 3.2737 | 1.4677 | 0
0% mass loss every 24 hours
slower release rate
Acceptable operation conditions
0.2% mass loss every 24 hours
acceptable release rate
0.5% mass loss every 24 hours
faster release rate
T<Tlim

## Slide 12: Optimisation of TiC target performance: Monte Carlo simulation
40 MeV proton beam
Target disk
One-disk target equivalent simulated to define thicknesses of TiC target disks so as to distribute energy loss equally
Chart: 
| 2.6 | 2.2999999999999998 | 2.1 | 1.9 | 1.6 | 1.3 | 0.9
 | 2.69 | 2.59 | 2.59 | 2.64 | 2.6 | 2.63 | 2.76
disk thickness (mm)
Energy loss (MeV)
Best solution: 7 disks, dicrepancy in energy loss by about 6%!
Thickness (mm) | Energy loss (MeV/prot) | Discrepancy %
2,6 | 2,69 | 2,5
2,3 | 2,59 | 6,2
2,1 | 2,59 | 6,2
1,9 | 2,64 | 4,3
1,6 | 2,60 | 5,8
1,3 | 2,63 | 4,7
0,9 | 2,76 | 0
0,9 | 1,92 | 30,43
13,6 | 20,4 | 
The 8th disk absorbs less than 2 MeV: shall we remove it?
The FEM thermal and structural analyses has to be completed
A. Donzella & D. Pagano - UNIBS

## Slide 13: T3.5: Multiphysics Simulation of High Performance ISOL Ion Sources
Step 0:
Standard FEBIAD source
(cathode)
A path towards a FEBIAD ion source with enhanced performances benefitting of the flexibility of the LPBF technology
Step 1:
First AM FEBIAD source component
(cathode)
Step 2:
Enhanced AM FEBIAD source
Step 3:
Innovative anode-cathode interfaces

## Slide 14: Conclusions - planned activities
T3.2 & T3.3: Thermal, electric and mechanical Characterization
Completion of the characterization of LPBF Ta
Characterization of LPBF Nb Characterization of LPBF W and Ta based alloys
T3.1: Material development and microstructural characterization
Development of Innovative LPBF W and Ta based alloys
T3.4: Multiphysics Simulation of High Performance ISOL Targets
New set of simulations on the optimised TiC standard targets
T3.5: Multiphysics Simulation of High Performance ISOL Ion Sources
Completion of thermal-electric simulations on conical anode-cathode interfaces

## Slide 15: Thank you
Notes: This is the question that your experiment answers