## Slide 1: HISOL
High performance ISOL systems for the production of radioactive ion beams
CSNV Experiment
Work package 3
Thermal and electrical characterization of LPBF metals
Giacomo Voltan – INFN-LNL

## Slide 2: Characterization of LPBF Ta and W
Ta STD
Ta AM90
Ta AM45
Completion of the characterization regarding Additively Manufactured refractory metals
Electrical characterization of new AM Ta samples
Thermal characterization of standard and AM Ta samples
Mechanical characterization of AM W samples

## Slide 3: Electrical characterization of AM Ta
Voltmeter
Tantalum wires
Electrodes
Vacuum chamber
Pyrometer
Sample
Setup for electrical resistivity measurements

## Slide 4
Electrical characterization of AM Ta
Chart: ΔV vs I
| 0 | 25 | 50 | 75 | 100 | 125 | 150 | 175 | 200 | 225 | 250 | 275 | 300 | 325 | 350 | 375 | 400 | 425 | 450 | 475 | 500 | 525 | 550 | 575 | 600 | 625 | 650 | 675 | 700 | 725 | 750 | 775 | 800
TAAM2_1 | 0 | 1.2 | 2.6 | 4 | 5.5 | 7.1 | 8.9 | 11 | 13.5 | 16.5 | 20 | 24.6 | 30.3 | 37 | 46.7 | 58.2 | 70 | 83 | 94.6 | 107 | 120 | 132 | 144.3 | 156.3 | 168.8 | 181.1 | 192.8 | 205 | 217 | 229 | 241 | 254 | 267
TAAM2_2 | 0 | 1.6 | 3.2 | 4.8 | 6.5 | 8.5 | 10.8 | 13.3 | 16.3 | 19.9 | 24.1 | 29.6 | 36 | 44.3 | 54 | 65 | 76.4 | 89 | 101.1 | 113.1 | 125.3 | 137.6 | 149.7 | 161.4 | 174 | 186.3 | 198 | 211 | 223 | 236 | 249 | 262 | 275
TAAM2_3 | 0 | 1.8 | 3.5 | 5.3 | 7.3 | 9.3 | 11.7 | 14.5 | 17.8 | 21.7 | 26.6 | 32.4 | 39.4 | 48.2 | 58.1 | 69.2 | 80.8 | 92.6 | 104.8 | 116.8 | 128.8 | 141.1 | 153.1 | 165.4 | 177.4 | 190 | 202 | 214 | 227 | 240 | 252 | 264 | 277
TAAM4_1 | 0 | 1.314 | 2.56 | 3.898 | 5.332 | 6.945 | 8.774 | 10.892 | 13.408 | 16.191 | 19.913 | 24.348 | 29.956 | 37.002 | 45.089 | 54.178 | 64.131 | 74.178 | 84.505 | 94.635 | 104.793 | 115.068 | 125.175 | 135.473 | 145.518 | 155.837 | 165.788 | 176.308 | 186.279 | 196.83
TAAM4_2 | 0 | 1.314 | 2.557 | 3.887 | 5.31 | 6.902 | 8.704 | 10.787 | 13.247 | 16.166 | 19.602 | 23.815 | 29.187 | 36.235 | 44.24 | 53.438 | 63.378 | 73.34 | 83.466 | 93.642 | 103.897 | 114.176 | 124.296 | 134.615 | 144.712 | 155.039 | 165.025 | 175.55 | 185.753 | 196.157
TAAM4_3 | 0 | 1.314 | 2.556 | 3.891 | 5.308 | 6.884 | 8.59 | 10.62 | 13.084 | 15.982 | 19.558 | 23.838 | 29.113 | 35.605 | 43.535 | 52.718 | 62.64 | 72.694 | 82.991 | 93.172 | 103.317 | 113.55 | 123.646 | 133.977 | 144.069 | 154.452 | 164.543 | 175.141 | 185.188 | 195.821
Potential drop measured
Ohm’s laws
Electrical resistivity
Chart: ρ vs T
| 1052 | 1166 | 1268 | 1356 | 1439 | 1511 | 1581 | 1643 | 1697 | 1751 | 1799 | 1846 | 1891 | 1934 | 1970
TAAM2_1 | 66.2117 | 70.949 | 75.5906 | 79.1901 | 82.6342 | 85.6145 | 88.6089 | 91.263 | 93.4222 | 95.6547 | 97.6378 | 99.4841 | 101.2073 | 103.2258 | 105.1181
TAAM2_2 | 70.7612 | 74.9938 | 78.9291 | 82.5497 | 85.7266 | 88.4081 | 91.3386 | 93.8835 | 95.9419 | 98.4544 | 100.3375 | 102.5251 | 104.5669 | 106.477 | 108.2677
TAAM2_3 | 68.6244 | 73.3508 | 77.4472 | 81.1339 | 84.6494 | 87.6736 | 90.5991 | 93.1234 | 95.748 | 97.8801 | 99.8542 | 102.1372 | 104.2628 | 105.8268 | 107.2898 | 109.0551
TAAM4_1 | 47.8393 | 53.0886 | 57.7935 | 62.1818 | 65.9707 | 69.3993 | 72.5752 | 75.3612 | 78.015 | 80.3079 | 82.5626 | 84.4564 | 86.4891 | 88.1168 | 89.8972
TAAM4_2 | 47.1859 | 52.4652 | 57.1406 | 61.4172 | 65.2785 | 68.806 | 72.0126 | 74.832 | 77.5209 | 79.8631 | 82.1399 | 84.0678 | 86.1172 | 87.868 | 89.5899
TAAM4_3 | 46.5501 | 51.8543 | 56.6373 | 61.0677 | 64.9509 | 68.4219 | 71.6178 | 74.4407 | 77.1535 | 79.5083 | 81.8289 | 83.8222 | 85.9166 | 87.6008 | 89.4364
Literature Desai | 36.04 | 38.14 | 40.26 | 42.28 | 44.24 | 48.15 | 51.93 | 55.61 | 59.23 | 62.75 | 66.25 | 69.78 | 73.22 | 76.6 | 79.94 | 83.32 | 86.68 | 89.99 | 93.22 | 96.52 | 99.77 | 103.1 | 106.3 | 109.7 | 112.7 | 115.9 | 119.1
Literature Cezariliyan | 75.56 | 78.8 | 82 | 85.14 | 88.23 | 91.26 | 94.24 | 97.17 | 100.04 | 102.86 | 105.63 | 108.34 | 111 | 113.6

## Slide 5: Electrical characterization of AM Ta
Sample 2
Sample 4
Recrystallization phenomena
Influence on the material behaviour

## Slide 6
Chart: ε vs T
| 25 | 679 | 781 | 881 | 991 | 1030 | 1118 | 1199 | 1277 | 1352 | 1413 | 1474 | 1528 | 1576 | 1621 | 1664 | 1706
 | 0.438 | 0.41 | 0.39 | 0.364 | 0.676 | 0.625 | 0.602 | 0.596 | 0.591 | 0.594 | 0.595 | 0.596 | 0.603 | 0.605 | 0.609 | 0.613
Thermal characterization of AM Ta
Chart: ε vs T
| 1052 | 1166 | 1268 | 1356 | 1439 | 1511 | 1581 | 1643 | 1697 | 1751 | 1799 | 1846 | 1891 | 1934 | 1970
TAAM2_1 | 0.341 | 0.347 | 0.358 | 0.373 | 0.385 | 0.397 | 0.408 | 0.419 | 0.429 | 0.439 | 0.449 | 0.457 | 0.467 | 0.476 | 0.489
TAAM2_2 | 0.368 | 0.377 | 0.386 | 0.397 | 0.408 | 0.418 | 0.428 | 0.44 | 0.449 | 0.46 | 0.468 | 0.476 | 0.484 | 0.495 | 0.508
TAAM2_3 | 0.383 | 0.386 | 0.396 | 0.407 | 0.419 | 0.429 | 0.442 | 0.451 | 0.462 | 0.471 | 0.48 | 0.489 | 0.499 | 0.509 | 0.519 | 0.531
TAAM4_1 | 0.348 | 0.356 | 0.369 | 0.382 | 0.398 | 0.413 | 0.429 | 0.443 | 0.458 | 0.471 | 0.483 | 0.496 | 0.507 | 0.518 | 0.532
TAAM4_2 | 0.346 | 0.351 | 0.363 | 0.375 | 0.391 | 0.406 | 0.422 | 0.436 | 0.451 | 0.464 | 0.477 | 0.488 | 0.5 | 0.511 | 0.526
TAAM4_3 | 0.348 | 0.35 | 0.361 | 0.374 | 0.39 | 0.406 | 0.42 | 0.435 | 0.45 | 0.464 | 0.477 | 0.488 | 0.5 | 0.511 | 0.524
HT emissivity measurements during electrical resistivity tests
Matching of 2-color mode and 1-color mode temperatures

## Slide 7
Thermal characterization of AM Ta
LT emissivity measurements
Ta STD
Ta AM90
Ta AM45
Experimental apparatus

## Slide 8
Thermal characterization of AM Ta
LT emissivity measurements
Tantalum oxide is stable up to 1500°C
Heat treatment for removing the superficial oxide layer
Tantalum tube containing a graphite box
Graphite support covered with a tantalum foil
Thermal treatment at 1100A for 2 hours

## Slide 9
Thermal characterization of AM Ta
Chart: I vs t
Chart: T vs t
| 3 | 7 | 11 | 15 | 19 | 23 | 27 | 31 | 35 | 39 | 43 | 47 | 51 | 55 | 59 | 63 | 67 | 71 | 75 | 79 | 83 | 87 | 91 | 95 | 99 | 103 | 107 | 111 | 115 | 119 | 123 | 127 | 131 | 135 | 139 | 143 | 147 | 151 | 155 | 159 | 163 | 167 | 171 | 175 | 179 | 183 | 187 | 191 | 195 | 199 | 203 | 207 | 211 | 215 | 219 | 223 | 227 | 231 | 235 | 239 | 243 | 247 | 251 | 255 | 259 | 263 | 267 | 271 | 275 | 279 | 283 | 287 | 291 | 295 | 299 | 303 | 307 | 311 | 315 | 319 | 323 | 327 | 331 | 335 | 339 | 343 | 347 | 351 | 355 | 359 | 363 | 367 | 371 | 375 | 379 | 383 | 387 | 391 | 395 | 399 | 403 | 407 | 411 | 415 | 419 | 423 | 427 | 431 | 435 | 439 | 443 | 447 | 451 | 455 | 459 | 463 | 467 | 471 | 475 | 479 | 483 | 487 | 491 | 495 | 499 | 503 | 507 | 511 | 515 | 519 | 523 | 527 | 531 | 535 | 539 | 543 | 547 | 551 | 555 | 559 | 563 | 567 | 571 | 575 | 579 | 583 | 587 | 591 | 595 | 599 | 603 | 607 | 611 | 615 | 619 | 623 | 627 | 631 | 635 | 639 | 643 | 647 | 651 | 655 | 659 | 663 | 667 | 671 | 675 | 679 | 683 | 687 | 691 | 695 | 699 | 703 | 707 | 711 | 715 | 719 | 723 | 727 | 731 | 735 | 739 | 743 | 747 | 751 | 755 | 760
 | 642 | 681 | 726 | 751 | 784 | 820 | 855 | 889 | 922 | 954 | 988 | 1019 | 1047 | 1079 | 1107 | 1136 | 1164 | 1193 | 1220 | 1247 | 1271 | 1294 | 1316 | 1337 | 1358 | 1380 | 1402 | 1377 | 1350 | 1324 | 1297 | 1272 | 1245 | 1220 | 1193 | 1166 | 1137 | 1110 | 1080 | 1052
Increase the roughness of the samples with mechanical operations
Perform the test manually making use of FLUKE® pyrometers
Chart: ε vs T
| 3 | 7 | 11 | 15 | 19 | 23 | 27 | 31 | 35 | 39 | 43 | 47 | 51 | 55 | 59 | 63 | 67 | 71 | 75 | 79 | 83 | 87 | 91 | 95 | 99 | 103 | 107 | 111 | 115 | 119 | 123 | 127 | 131 | 135 | 139 | 143 | 147 | 151 | 155 | 159 | 163 | 167 | 171 | 175 | 179 | 183 | 187 | 191 | 195 | 199 | 203 | 207 | 211 | 215 | 219 | 223 | 227 | 231 | 235 | 239 | 243 | 247 | 251 | 255 | 259 | 263 | 267 | 271 | 275 | 279 | 283 | 287 | 291 | 295 | 299 | 303 | 307 | 311 | 315 | 319 | 323 | 327 | 331 | 335 | 339 | 343 | 347 | 351 | 355 | 359 | 363 | 367 | 371 | 375 | 379 | 383 | 387 | 391 | 395 | 399 | 403 | 407 | 411 | 415 | 419 | 423 | 427 | 431 | 435 | 439 | 443 | 447 | 451 | 455 | 459 | 463 | 467 | 471 | 475 | 479 | 483 | 487 | 491 | 495 | 499 | 503 | 507 | 511 | 515 | 519 | 523 | 527 | 531 | 535 | 539 | 543 | 547 | 551 | 555 | 559 | 563 | 567 | 571 | 575 | 579 | 583 | 587 | 591 | 595 | 599 | 603 | 607 | 611 | 615 | 619 | 623 | 627 | 631 | 635 | 639 | 643 | 647 | 651 | 655 | 659 | 663 | 667 | 671 | 675 | 679 | 683 | 687 | 691 | 695 | 699 | 703 | 707 | 711 | 715 | 719 | 723 | 727 | 731 | 735 | 739 | 743 | 747 | 751 | 755 | 760
 | 0.332 | 0.332 | 0.408 | 0.482 | 0.494 | 0.496 | 0.494 | 0.498 | 0.494 | 0.496 | 0.482 | 0.476 | 0.474 | 0.464 | 0.46 | 0.458 | 0.458 | 0.454 | 0.449 | 0.446 | 0.443 | 0.444 | 0.444 | 0.447 | 0.449 | 0.449 | 0.259 | 0.257 | 0.255 | 0.253 | 0.251 | 0.248 | 0.245 | 0.241 | 0.238 | 0.237 | 0.233 | 0.23 | 0.225
 | 0.25 | 0.25
LT emissivity measurements

## Slide 10: W AM mechanical characterization
6 samples of AM tungsten ready for performing compression tests
Mechanical operation required for the removal of the growth substrate

## Slide 11: Conclusions - planned activities
Tantalum AM
Thermal characterization of 4 specimens
Comparison between STD and AM results
Electrical characterization of further specimens
Tantalum STD
Thermal characterization of 4 specimens
Tungsten AM
Mechanical characterization of 6 specimens

## Slide 12: Thank you
Notes: This is the question that your experiment answers