## Slide 1: Muon beams manipulation with crystals
A. Mazzolari

## Slide 2: Coherent effects in crystals
Planar channeling
Particles reaching the crystal within the «critical angle» for channeling feels interatomic potential and are deflected
Observed for the first time in the late ‘70 @ Dubna, then spread worlwide (FNAL, CERN, etc…)
Steering efficiency as high as 85%, limited by «dechanneling»
Optimal for high‐energy (GeV–TeV) beams
Key applications: beam extraction, precision steering, crystalline‐undulator radiation sources

## Slide 3: Coherent effects in crystals
Volume Reflection in Bent Crystals
Coherent deflection by the averaged potential of curved lattice planes
Deflection angle ≈ 2 critical angle for channeling with ≈ 100 % beam acceptance
Efficiency 95–99% across GeV–TeV energies (limited by “volume capture”)
Simplified crystal alignment requirements
Key applications: beam steering, collimation, halo extraction

## Slide 4: Coherent effects in crystals
400 GeV proton beam
Deflection at channeling ~ 160 mrad
Channeling efficiency ~ 60%
Volume reflection deflection at about 13.5 mrad
Fraction of diverted particles larger that 97%
Large acceptance
1  Primary beam
2  Channeling
3  Dechanneling
4  Volume reflection
5  Volume capture
6  Primary beam
1
6
2
3
4
5

## Slide 5: Coherent effects in crystals
Positively charged particle beams
(400 GeV protons)
Negatively charged particle beams
(180 GeV pions)

## Slide 6: Coherent effects in crystals
Crystal axis mechanically aligned to the beam direction
Particles feels so called «axial potential», about 6 times. stronger than «planar potential»axial channeling

## Slide 7: Coherent effects in crystals
400 GeV proton beam@SPS
150 GeV negative
pions beam@SPS

## Slide 8: Primary beam manipulation
Collimation of beam (like LHC)
Beam extraction
Beam shadowing (i.e. in assistance of electrostatic beam scraping)
Beam focusing
arXiv:1809.06164
10.1063/1.56430

## Slide 9: Coherent effects in crystals
E.m. processes: occuring for charged particles or high-energy photons
PROS
High steering power up to hundreds of Tesla dipole
Low material budget (<0.1X0)
Zero power consumption
Selective interaction with discrete section of beam/ halo
CONS
Require precise alignment between particles and crystal
Parameters scale typically with E or E1/2
For some effects lower efficiency in negative charged particles

## Slide 10: Application in accelerators
Beam halo collimation (tested with protons and ions at LHC)
Beam halo extraction (U70, FNAL, CERN)
Beam focusing: both long (meters) and short (cm) focusing length
Beam shadowing: currently developing crystal to assist Mu2e proton beam extraction

## Slide 11: Crystal-assisted beam collimation
Unavoidably particles diverge from desired trajectory and form a halo around beam
Traditional approach stops the halo with a series of amorphous absorber
Cons: development of showers in collimators
Channeled particles in bent crystal while being steered avoid strong scattering: shower development strongly suppressed
High efficiency in removing halo from beam in controlled manner
BEAM
Coll >1m
Abs
BEAM
Abs
shower
Crystal
few mm

## Slide 12: Anticlastic deformation
Rp
Beam
Ra
55 mm
4 mm

## Slide 13: Crystals for LHC beam collimation
Thickness along the beam: 4.0±0.1 mm
Height < 55 mm.
Weight < 150 g
Channeling plane: (110)
Channeling axis: <111> or <110>
Miscut for planar channeling: < 10 μrad.
Torsion: < 1 μrad/mm
Bending angle: 50-55 μrad
Dislocation density < 1 cm2
Specifications defined in collaboration with CERN
Beam

## Slide 14: Crystals for LHC beam collimation
Silicon micromachining
Nuclear reaction analysis
Analytical sciences
Ultra-high precision optics
Laser interferometry
Crystal
Deterministic polishing
Lower the angle between crystal’s surface and its atomic planes
SEM, TEM, µ-Raman, AFM, HR-XRD
Analytical techniques asses the “quality” of crystal’s surfaces
Chemo-mechanical
Borrowed from silicon micromachining
Rutherford back-scattering
Investigate the first atomic layers of the crystal
Fizeau interferometry
Records the topography of the crystal’s surfaces

## Slide 15: Crystals for LHC beam collimation
Essential to have surfaces free from sub-surface lattice damage: a dedicated manufacturing process have been established
A large set of characterization techniques is exploited to validate the manufacturing process.
  HR-XRD probe up to few tens of microns
  µ-raman (probe up to few microns)
  RBS-Channeling (probe up to few hundred nm)
  TEM (probe the first atomic layers)
Beam

## Slide 16: Double crystal setup EDM/MDM measurement
P. Hermes (CERN)

## Slide 17: Manufacturing of «long» crystals
Manufacturing and characterization approach similar to the one used for «short» crystals. Bending angle several mrad
Special care must be paid to uniformity of bending radius.

## Slide 18: Ultra-thin crystals
QUASI-MOSAIC DEFORMATION
855MeV e-
530MeV e+

## Slide 19: Applications at LINAC
5GeV (or 10 GeV) protons are well suited for planar channneling
Bent crystal can assist collimation of beam
Beam shadowing of delicate portion of insertion devices to reduce beam losses

## Slide 20: End of cooling
Particle energy 339MeV
Thin crystals (15-30μm thickness) to redirect halo particles into accelerator stage
  Planar channeling
  Axial channeling
  Volume reflection
530MeV e+
855MeV e-

## Slide 21: Crystal application with BIB
Low energy and large energy spread are detrimental to crystals applications (also low efficiency for diffraction of photons and neutrons)
2 MeV mirroring with very thin crystals (100 nm) was already performed experimentally, but strict energy spread condition
For incoherent e+/e- pairs, (higher energy) channeling in bent crystal might be of assistance (see slide 7)
D. Calzolari, ICHEP 2024

## Slide 22: μ- planar channeling efficiency 1.5TeV
1mm<Optimal crystal length <2mm, possible increase with multi-turn efficiency

## Slide 23: μ- planar channeling efficiency 5TeV
2mm<Optimal crystal length <5mm, possible increase with multi-turn efficiency

## Slide 24: Conclusions
Different kind of coherent effect in crystals can be optimized
Each application strongly depends on beam parameters and requirements in each portion of the muon collider machine
Strong inputs are well accepted to design suitable crystal-assisted schemes

## Slide 26: Backup slides

## Slide 27: Crystal-assisted beam manipulation
Past uses:
U70 proton beam extraction
Spin precession measure of Σ+ baryons at FERMILab
Present and Past Proposal
UA9: SPS collimation, septum shadowing, extraction
CRYSBEAM: LHC beam extraction
SELDOM: charmed baryons spin precession
SHERPA: positron slow extraction at LNF
DESY electron baem extraction
Current R&D
LHC ion beam collimation
“INFN KE4350/EN/HL-LHC” between INFN and CERN was signed: 4 crystals collimators have been already provided to CERN by INFN Ferrara

## Slide 28: Negative particle steering
May 29, 2024 Laura Bandiera, INFN Ferrara
9
Planar channeling is significantly less efficient for negative particles, as incoherent scattering with atomic nuclei is enhanced instead of being suppressed.
Axial Stochastic Deflection was first proposed by А.А. Greenenko and N.F. Shul’ga in 1991
Experimentally observed by H8-RD22/UA9 collaboration at CERN in 2008 for protons and in 2009 for π– mesons
The mechanism involve over-barrier motion: particles scattering converge stochastically along the axis direction. Efficient for both positive and negative particles

## Slide 29: Axial Stochastic Deflection and Planar channeling
Negative particles in planar channeling exploit weaker potential and more incoherent nuclear scattering wrt positive case
Stochastic axial deflection has the potential to steer efficiently both negative and positive particles
Maximum deflection angle scale with different power law: E-0.075 (planar) vs E-0.25 (axial)

## Slide 30: Comparison of planar and axial stochastic deflection at 1 TeV
A large simulation campaign has been carried out with both muon and anti-muon of 1 TeV/c momentum
Optimal radius of curvature has been obtained for deflection angles from 2 μrad up to 200 μrad
Cases for 200μrad, 50μrad are presented as example in this work

## Slide 31: Large angle deflection μ- (200μrad)
Optimal radius of curvature for R ~6-7m
Better single pass efficiency with planar channeling
(111) plane
<110> axis
Courtesy of I. Kyryllin

## Slide 32: Large angle deflection μ+ (200μrad)
Optimal R between 15-20m
Better single pass efficiency with planar channeling
(111) plane
<110> axis
Courtesy of I. Kyryllin

## Slide 33: Small angle deflection μ- (50μrad)
Optimal R between 20-25m
Better single pass efficiency with planar channeling
(111) plane
<110> axis
Courtesy of I. Kyryllin

## Slide 34: Small angle deflection μ+ (50μrad)
Optimal R between 15-20m
Better single pass efficiency with planar channeling
(111) plane
<110> axis
Courtesy of I. Kyryllin

## Slide 35: μ- planar channeling efficiency 1.5TeV
1mm<Optimal crystal length <2mm, possible increase with multi-turn efficiency

## Slide 36: μ- planar channeling efficiency 5TeV
2mm<Optimal crystal length <5mm, possible increase with multi-turn efficiency

## Slide 37: Conclusion
Comparison of axial stochastic deflection and planar channeling as steering mechanism for TeV muon was carried out. Planar channeling was more efficient option as we reach multi-TeV scale
Optimal single pass efficiency condition was obtained for 1.5 TeV and 5 TeV negative muon case.
Future study of volume reflection phenomena such as Multiple Volume Reflection in One Crystal and Multiple Volume reflection in a series of aligned bent crystals.

## Slide 38: Multiple Volume Reflection
Volume reflection deflects small angle, but a series of crystals can add up steering with high efficiency
This can provide deflection comparable with channeling, with good efficiency for both negative and positive particles
Or near axial alignemtn, multiple volume reflections can occur in a single crystal (MVROC)
10.1016/j.physletb.2009.11.026
10.1088/1748-0221/7/04/P04002