## Slide 1: CUPRUM-TTD (2023-25) Planned activities and Budget Requests 2025 67/64CU PRoduction and Use in Medicine – Target Technology Development

## Slide 2: CUPRUM-TTD (2023-2025) main project goals
to acquire a robust and reliable target manufacturing technology to produce 70ZnO target
to manufacture targets able to sustain beam power levels from medical cyclotrons (i.e. 18-20 MeV, 2/3 kW max);
to develop/optimize the radiochemistry separation/purification methods: ZnCu to achieve a clinical-grade 67Cu radionuclide;
in-vitro cells studies with 67Cu-labelleded RPs using NOTA derivate as chelating agent;
phantom imaging studies of produced 67Cu with pre-clinical and clinical SPECT;
to develop/optimize technology for the costly 70Zn-enriched target material recovery.
To develop a reliable technology aimed at producing clinical-grade batches of 67Cu- 64Cu by small medical cyclotrons on a routine basis.
CT-SPECT-PET

## Slide 3: CUPRUM-TTD project organization
CUPRUM-TTD project is organized in Work Packages (WP),interacting each-other in a synergic way
WP2 | 
Petra Martini | INFN-FE UNIFE
Alessandra Boschi | 
Francesca Porto | 
Teresa Ghirardi | UNIFE INFN-Fe
Licia Uccelli | 
Lorenza Marvelli | 
Emiliano Cazzola | HSCDC
Giancoarlo Gorgoni | 
WP3 | 
Liliana Mou | LNL
Gaia Pupillo | 
Juan Esposito | UNIFE INFN-Fe
Emiliano Cazzola | HSCDC
Giancarlo Gorgoni | 
Luciano Canton | UNIPD INFN-PD
Francesca Barbaro | 
Lucia De Dominicis | 
Flavia Groppi | UNIMI INFN-MI
Simone Manenti | 
Fiorella M. Cagnetta | 
Michele Colucci | 
WP4 | 
Laura De Nardo/ Laura Melendez-A. | INFN-PD IOV
Alessandra Zorz | IOV
Marta Paiusco | 
Michele Bello | UNIPD INFN-PD
Diego Cecchin | 
Cristina Bolzati | ICMATE CNR
Giov. Di Domenico | UNIFE INFN-Fe
Angelo Taibi | 
WP1 | 
Sara Cisternino | LNL
Juan Esposito | UNIFE INFN-Fe
Alisa Kotliarenko | 
Giorgio Keppel | Osp. SCDC
Umberto A. Tamburini | UNIPV

## Slide 4: CUPRUM-TTD Timetable and milestones planned
First 18 months activities

## Slide 5
Resume on R&D activities performed (as of June 2024)

## Slide 6: CUPRUM-TTD WP1 (LNL+FE): Target manufacturing, characterization, and material recovery
D1: no. 2-3 ZnO targets for surface analyses investigations (WP2); D2: no. 5 ZnO targets for cold test chemical processing optimization (WP2); D3: 3 70ZnO targets for production test; D4: recovered natZnO powders.
Final Target material
2.0 g [70Zn]ZnO-enriched material already purchased (~ 20$/mg) – 1 target 500 mg  ~ 4 targets manufacturing
Magnetron Sputtering technique
- Investigation of thick ZnO deposition onto different substrates (Au/Nb – DLC)
Target recovery and recycling in collaboration with WP2
Activities shared with WP2
A. Kotliarenko et al., First Results on Zinc Oxide Thick Film Deposition by Inverted Magnetron Sputtering for Cyclotron Solid Targets Production. Materials, 16, 10, 3810, 2023. DOI: 10.3390/ma16103810
Suspended activities because SPS technique is more promising at this stage of the project
WP1 | 
Sara Cisternino | LNL
Juan Esposito | 
Alisa Kotliarenko | 
Gaja Piteo | UNIPD/LNL
U. Anselmi-Tamburini | UNIPV
Petra Martini | UNIFE
Alessandra Boschi | 
Francesca Porto | 
Giorgia Speltri | 
Lorenza Marvelli | 
Main activities
Target manufacturing:
SPS technique
Sintering of ZnO powder  pellet in a holder for irradiation
Sintering of ZnO powder and target system investigation (ZnO/Au/Nb)
@ Pavia (S. Cisternino and G. Piteo)
Optimization of ZnO pellet sintering
ZnO powder and pellets to Ferrara University for chemistry and recovery studies (WP2)
ZnO pellets for irradiation with the capsule & composite target (WP3)
ZnO – baking adhesion trials
@ LNL/UNIPD (S. Cisternino, A. Kotliarenko, G. Piteo)
SEM, XRD analysis and heat treatments for residual carbon removal

## Slide 7
N of EXP | Mass [mg] | SPS parameters |  |  |  |  |  | Results |  |  |  | 
N of EXP | Mass [mg] | step | Temp. [°C] | Force [kN] | Pressure on sample [MPa] | Time [min] | Heating rate [°C/min] | mass after [mg] | mass lost [mg] | thickness [µm] | density [g/cm3] | %bulk density
(n=41) | 263.9 ± 5.9 | 1 | 600 | 4 | 51 | 0,1 | 200 | 255.9 ± 10.4 | 8.0 ± 7.8 | 612.4 ± 23.1 | 5.3 ± 0.1 | 95.0 ± 2.1
 |  | 2 | 1000/850 | 5 | 64 | 10 | 10 |  |  |  |  | 
 |  | 3 | 300 | 5 | 64 | 0,1 | 20 |  |  |  |  | 
(n=3) | 267.5± 1.2 | 1 | 600 | 4 | 51 | 0,1 | 200 | 261.7± 0.6 | 5.7± 1.0 | 626.8± 2.0 | 5.3± 0.0 | 94.8± 0.2
 |  | 2 | 850 | 5 | 64 | 10 | 10 |  |  |  |  | 
 |  | 3 | 300 | 5 | 64 | 0,1 | 20 |  |  |  |  | 
Reproducible Exp
Sintering of 3 pellets at once (in series)
CUPRUM-TTD WP1 (LNL): natZnO pellets SPS R&D program underway
TOP
CENTRAL
BOTTOM
1 cm
1 cm
1 cm
Cross-section view
Density [g/cm3] / % bulk (n=5) | 5.31±0.09 / 94.7±1.6% | 5.35±0.08 / 95.3±1.4% | 5.29±0.09 / 94.4±1.6%
Mass densities and the microstructure are compared to the one-pellet-sintered

## Slide 8: CUPRUM-TTD WP1 (LNL): New target configuration - ZnO pellet bonding to backing (Au/Nb) by SPS
3.
Adhesion of ZnO-Au to backing (Au-Nb)
1.
ZnO pellet preparation
2.
Au-foil-layered ZnO pellet
1+2 in one sintering process (3 sample simultaneously)
#9 targets from ZnO commercial powder were already realized and tested under irradiation and used for radiochemical processes
SEM cross section of pellet
SEM cross section of target
ZnO

## Slide 9: CUPRUM-TTD WP1 (LNL+FE): Irradiations for thermomechanical test
After irradiation
Prior irradiation
Pellet in Al holder configuration:
@ ACSI TR19/300 Sacro Cuore Don Calabria Hospital cyclotron
Main considerations
- Not easy to open the capsule
- The pellet is attached to the capsule;
- Energy on pellet 14 MeV, not optimal for 67Cu production
Max beam power areal density achieved = 1.2 kW/cm2
ZnO-Au/Au-Nb configuration
#2 irradiations 15-30 µA; 19 MeV; 5 min
#4 irradiations 15-25-35-50 µA; 19 MeV; 5 min
Prior irradiation
After irradiation
Targets manufactured by SPS LARAMED technology withstand the maximum proton beam current intensity available at SCDCH cyclotron (solid target station available)
Several irradiation and radiochemistry dissolution/separation/purification tests were performed based upon this target configuration
System suitable when low radioactivity batches are needed for research purposes
Prior irradiation

## Slide 10: CUPRUM-TTD WP2 (FE): Target radiochemistry processing
D5: Zn/Cu separation and purification procedure D6: semi-automatic module for the separation and purification of 67Cu from ZnO target D7: 67Cu radiochemistry product quality assessment
Cold tests for protocol optimization
ICP-MS analysis revealed that in the final product Ga, Co and Zn content is below the instrumental detection limit.
Recovery yield >98% (reproducibility tests are ongoing)
γ-spectrometry analysis revealed that in the final product no Ga, Co and Zn radioisotopes are present
Difficulties in the automation and reproducibility of the results due to old and incomplete module (valves not working properly, no gas/air flow control, no pressure control, syringe pumps not calibrated etc….)
  NOT SUITABLE FOR ENRICHED TARGET PROCESSING TEST
Recovery yield ongoing determination
Hot test for validation and SEMI-automation
PRODUCT
WASTE
WP2 | 
Petra Martini | INFN-FE UNIFE
Alessandra Boschi | 
Francesca Porto | UNIFE INFN-Fe
Licia Uccelli | 
Lorenza Marvelli | 
Giorgia Speltri | 
Emiliano Cazzola | HSCDC
First  spectra obtained @SCDCH

## Slide 11: CUPRUM-TTD WP2 (FE): Target radiochemistry processing
WP2 | 
Petra Martini | INFN-FE UNIFE
Alessandra Boschi | 
Francesca Porto | UNIFE INFN-Fe
Licia Uccelli | 
Lorenza Marvelli | 
Giorgia Speltri | 
Emiliano Cazzola | HSCDC
D5: Zn/Cu separation and purification procedure D6: semi-automatic module for the separation and purification of 67Cu from ZnO target D7: 67Cu radiochemistry product quality assessment
strategy

## Slide 12: CUPRUM-TTD WP2 support to WP1 (LNL+FE): ZnO recovery processes – closing the Zn target material cycle
Recovery yield 84.8%±3.6%
at 25°C
(from pellet)
Cold dissolution planned for SEM analysis
at 18°C
(from pellet)
at 0°C
(from powder)
Flakes evaporation condition to be optimized
irradiation and radiochemical purification planned
at 0°C (from pellet)
Modified evaporation protocol
Sample 247
ZnO pellet density ~ 84%
Sample 212
ZnO pellet density ~ 95%
ZnO pellet density ~ 95%
irradiation and radiochemical purification planned
Sample 268
ZnO pellet density ~ 65%
ZnO recovery process steps performed in different conditions:
- Dissolution of pellet or powder in HCl or use of eluate from radiochemistry process
- Precipitation with NaOH at different temperatures
- Evaporation and final calcination
Starting material: Zn-rich eluate from radiochemical separation protocol (from pellet) simulation of real exp
From Zn-rich eluate from radiochemical separation protocol (from powder)
ZnO pellet density ~ 55%
at 0°C
at 0°C
Recovery yield 99%
Recovery yield  to be optimized
Optimization experiments and analysis of powders and targets still ongoing…
First results:
WP1 and WP2
SEM analyses ongoing

## Slide 13: CUPRUM-TTD WP3 (LNL-MI-PD): Irradiation, γ-spectr. and QC test
WP3 | 
Liliana Mou | LNL
Gaia Pupillo | 
Lucia De Dominicis | UNIFE INFN-Fe
Juan Esposito | 
Emiliano Cazzola | HSCDC
Giancarlo Gorgoni | 
Luciano Canton | UNIPD INFN-PD
Yuliia Lashko | 
Francesca Barbaro | 
Flavia Groppi | UNIMI INFN-MI
Simone Manenti | 
Fiorella M. Cagnetta | 
Michele Colucci | 
Milestones and deliveries planned
M9: natZnO targets irradiation for thermomechanical stability tests M10: natZnO targets irradiations for radiochemical separation optimization procedure M11: γ-spectrometry meas. to determine radiochemical procedure efficiency (natZn/natNi targets) M12: 3 irradiations on 70ZnO targets for 67Cu batches production (2 irradiations on 64Ni targets for 64Cu). M13: γ-spectrometry meas. to determine the activity and RNP of 67Cu produced by irradiation of 70Zn targets M14 xs measurements for alternative nuclear reaction route with alpha beams 64Ni(α,p)67Cu (energy range 30 – 15 MeV) as well as 59Co(α,2n)61Cu
D8: RNP determination of the produced 67Cu radionuclides from 70ZnO/64Ni D9: xs measurements determination with alpha beams for alternative 6xCu productions
Irradiation runs on natZnO/natNi for targets and related spectrometry measurements
selection of beam parameters suitable to yield small batches of 67Cu/ 64Cu based on theoretical calculations;
nat-ZnO target irradiations for thermomechanical stability tests
3 irradiation runs on 70ZnO for first batches of 67Cu;
2-3 irradiations runs on natNi and 59Co with alpha beams for 61,64,67Cu optimization production (xs meas. @ARRONAX) UNIMI+INFN-Mi
2 irradiations runs on thick target of 64Ni for TTY, RNP, SA det.
γ-spectrometry analysis for yield and RNP determination

## Slide 14: CUPRUM-TTD WP3 (MI): Investigations on alternative nuclear reaction routes with alpha beams 59Co(α,2n)61Cu
To do in 2024/2025
Copper isotopes
Other contaminants
Four irradiation performed with α particles in the 14-59 MeV energy range at GIP ARRONAX.
Gamma spectrometry continued at LASA labs for 4/8 months after irradiations for long lived RN.
TTY and RNP
determnation
Optimized parameters for 61Cu
Irradiation time: 7 h
α energy: 59 MeV
Energy losses: 44 MeV
TTY 61Cu = 1800 MBq/µA
RNP > 99% 4h after EOB

## Slide 15: CUPRUM-TTD WP3 (PD): theoretical activities on alternative nuclear reaction routes to yield 67Cu  68Zn(t,α)67Cu
UniPD/INFN-PD
F. Barbaro
L. Canton
Y. Lashko
Started investigation of the triton production route: 68Zn(t,α)67Cu
Comparison with the “standard” production routes: 68Zn(p,2p)67Cu, 70Zn(p,α)67Cu
Bibliography study and data search
Started simulation analysis with Nuclear Reaction Codes Talys
Supervision of a master thesis on this topic

## Slide 16: CUPRUM-TTD WP4 (PD-IOV-CNR-UNIFE): RP activities (Synthesis of new Cu conjugates)
D10: NOTA-PSMA conjugates D11 A reproducible method to obtain Cu-PSMA RPs with high radiochemical yield D12: Minimum activity and dimension of the tumour to obtain good imaging
WP4 | 
Laura De Nardo/ Laura Melendez-A. | INFN-PD IOV
Alessandra Zorz | IOV
Marta Paiusco | 
Michele Bello | UNIPD INFN-PD
Diego Cecchin | 
Cristina Bolzati | ICMATE CNR
Giov. Di Domenico | UNIFE INFN-Fe
Angelo Taibi | 
As the LARIM laboratory, built in the 1993, did not comply with current safety regulations on the use of experimental animals (2014) and on the use of radioactive material (2020), it was necessary to close it for ~ 1 year to be able to completely renovate it.
Both civil/electric renovation works are about to be completed.
The planned activity of synthesis of new conjugates (M15) will be started in the 4th quarter of 2024.

## Slide 17: CUPRUM-TTD WP4 (PD-IOV-CNR-UNIFE): RP activities (Synthesis of new Cu conjugates)
Feasibility of Radiopharmaceutical research studies within LNL LARIM (Padua Univ.)
LARIM is located close to SPES building. Now under renewal of HVAC/Electric/safety plants (Dec. ’23 –July ’24) Expected to re-start first operations (new instr. included) on Sept/Oct ‘24
HPLC instrumentation in the radiochemistry lab
Radiochemical and Biological hoods
Last-generation small animal scanner: MILABS Vector 5 CT
Set of phantoms with different geometries

## Slide 18: CUPRUM-TTD WP4: Cellular dosimetry calculations
D10: NOTA-PSMA conjugates D11 A reproducible method to obtain Cu-PSMA RPs with high radiochemical yield D12: Minimum activity and dimension of the tumour to obtain good imaging
WP4 | 
Laura De Nardo/ Laura Melendez-A. | INFN-PD IOV
Alessandra Zorz | IOV
Marta Paiusco | 
Diego Cecchin | UNIPD INFN-PD
Cristina Bolzati | ICMATE CNR
Giov. Di Domenico | UNIFE INFN-Fe
Angelo Taibi | 
Input data required: specific uptake and internalization in PSMA-positive and -negative PCa cells.
MIRDCell calculations for 67Cu and 64Cu in spherical clusters of cells by assuming 100% subcellular distribution of radionuclides in Cytoplasm, Nucleus or Cell Surface provide preliminary information about dosimetric results to be obtained with a realistic distribution of RPs.
%N, %Cy, %CS→N

## Slide 19: CUPRUM-TTD project 2025 FTE (subject to further refinement) Personnel and FTE distribution expected among units taking part
LNL | FTE | INFN-Fe | FTE | INFN-Mi | FTE
Esposito J. (R.Naz.-Loc.) | 0.50 | Martini P. (R. Loc) | 1.00 | Groppi F. (Res. Loc) | 0.40
Pupillo G. | 0.25 | Taibi A. | 0.10 | Manenti S. | 0.25
Mou L. | 0.20 | Di Domenico G. | 0.20 | Cagnetta F.M. | 0.45
Cisternino S. | 0.70 | Boschi A. | 1.00 | Colucci M.**** | 0.60
De Dominicis L. | 0.40 | Uccelli L. | 1.00 |  | 1.70
Melendez-Alafort L.** | 1.00 | Marvelli L. | 1.00 |  | 
Bello M. | 0.80 | Porto F.* | 1.00 |  | 
Piteo G. | 1.00 | Speltri G.* | 1.00 |  | 
Anselmi-Tamburini U. | 0.20 |  | 6.30 |  | 
Cazzola E. # | 1.00 |  |  | TOTALE FTE | 17.55
Gorgoni G.# | 1.00 | INFN-Pd | FTE |  | 
Cecchin D. § | 0.20 | De Nardo L. (R. Loc) | 0.80 |  | 
 | 7.25 | Canton L. | 0.20 |  | 
 |  | Barbaro F. | 0.60 |  | 
 |  | Paiusco M. ** | 0.20 |  | 
 |  | Zorz A. § | 0.20 |  | 
 |  | Bolzati C.*** | 0.20 |  | 
 |  | Lashko Y. | 0.10 |  | 
 |  |  | 2.30 |  | 
* studenti PhD associate INFN-Fe (da nov 2023)
** personale IOV associato LNL
*** personale CNR associato INFN-Pd
**** studente PhD associato INFN-MI
§ personale UNIPD associato INFN-LNL
# personale SCDCH associato INFN-LNL

## Slide 20
Summary overall budget request CUPRUM-TTD FY2025
Sezioni / Lab | Missioni | Consumo/ Altri consumo | Trasporti | Manutenzione | Inventario | apparati | Sp- servizi | Tot. per sez/lab | FTE previsto
LNL | 7,0 | 10,0 | 0,0 | 0,0 | 0,0??? | 0,0 | 0,0??? | 17,0 | 7.25
FE | 4,0 | 15,0 | 2,0 | 0,0 | 17,0 | 0,0 | 0,0 | 38,0 | 6.30
PD | 1,0 | 7,0 | 0,0 | 0,0 | 0,0 | 0,0 | 0,0 | 8.0 | 2.30
MI | 8,5 | 8,0 | 8,5 | 4,0 | 0,0 | 0,0 | 0,0 | 29,0 | 1.70
TOTALE | 20.5 | 40.0 | 10.5 | 4.0 | 17.0 | 0.0 | 0.0 | 92.0 | 17.55
*Consumables: Solvents for HPLC analysis, reagents for stability test, buffers and cell culture media, Sep-Pack cartridges for radiopharmaceutical purification, plastic and glassware (4Keuro).
64Cu to radiolabel the developed Radiopharmaceuticals (2x10mCi) (3keuro)

## Slide 21
  SPES-MED (Gr III, 2024-26)
  Nuclear cross section measurements
  68Zn,70Zn(p,x)67Cu,64Cu for proton beams with energy higher than 70 MeV, in collaboration with the i-Themba facility (LNL team, 1 and 2 year);
  70Zn(p,x)67Cu,64Cu in the energy range 25-50 MeV at SPES (LNL team, 3 year)
  DECURTA DEvelopment of 67Cu-Radiopharmaceuticals for Theranostic of prostate cAncer (Bando IOV Ricercatori Sanitari 2023) PI Laura Alafort Melendez
[Pupillo, G. et al. Radiochim. Acta 108, 593–602 (2020)]
Further developments or applications