## Slide 1
Associate Professor. Dr. Daniele Dondi
Director in Laboratory of Radiation Chemistry and EPR Spectroscopy
Department of Chemistry, University of Pavia, 27100, Italy.
Thursday, July 4th, 2024
CH4rLiE

## Slide 2
Experiment-1
100mg of Z-5 sample is dried under high vacuum at 200°C(immediately removed)
Experiment-2
100mg of Z-5 sample is dried under high vacuum at 200°C(removed after 3 hours)
Experiment-3
100mg of Z-5 sample is dried under high vacuum at 200°C(removed after 5 hours)
Experiments for drying Z-5 zeolite under vacuum
Experiment for drying Z-5 in Muffle furnace
Experiment-1
100mg of Z-5 sample is dried in muffle furnace at 400°C(3 hours)
Experiment-2
100mg of Z-5 sample is dried in muffle furnace at 600°C(after 3 hours)
Experiment-3
100mg of Z-5 sample is dried in muffle furnace at 550°C(after 4 hours)
Experiments

## Slide 3
TGA of Z-5 200°C 25-1000°C @ 20 °C/MIN

## Slide 4
DSC of Z-5 200°C : at 40-400°C @ Ramp 5°C/min to 400°C

## Slide 5
TGA of Z-5 200°C 5Hr 25-1000°C @ 20 °C/MIN

## Slide 6
DSC of Z-5 200°C 5Hr : at 40-400°C @ Ramp 5°C/min to 400°C

## Slide 7
DSC of Z-5 400°C : at 40-400°C @ Ramp 5°C/min to 400°C

## Slide 8
TGA of Z-5 600 °C 25-1000°C @ 20 °C/MIN

## Slide 9
DSC of Z-5 600°C : at 40-400°C @ Ramp 5°C/min to 400°C

## Slide 10
TGA of Z-5 550 °C 25-1000°C @ 20 °C/MIN

## Slide 11
Conclusion and further Experiments
Drying of zeolites proved to be difficult.
The experiments under high vacuum and heating in Muffle Furnace even at 600C failed to remove moisture from the sample.
We doubt that after heating of the sample, The time taken for introducing the sample to atmosphere is when the Zeolite recaptures moisture from the atmosphere.
We are planning an experiment to heat the zeolite in an oven flushing nitrogen before and after heating the sample and removing sample for Measurement under nitrogen. We hope that avoiding the contact of the sample with atmosphere will show removal of moisture from Zeolites.

## Slide 12
Gas chromatography-Mass spectrometry for Barn samples 25/03/24
Samples obtained from the Barn are Measured in the order 4A, 6A, 5A, 2A, 3A, 1A
Samples were observed for CH4(16), NH3(17), H2O(18), N2(28), O2(32), CO2(44)
Samples 5A, 2A, and 3A shift in signals were observed

## Slide 13
CH4
4A
5A
6A
2A
3A
1A

## Slide 14
NH3
4A
5A
6A
3A
2A
1A

## Slide 15
H2O
4A
5A
6A
3A
2A
1A

## Slide 16
N2
4A
5A
2A
3A
1A
6A

## Slide 17
O2
4A
5A
6A
3A
1A
2A

## Slide 18
CO2
4A
6A
5A
1A
2A
3A

## Slide 19
Thank you
Acknowledgement