## Slide 1
Associate Professor. Dr. Daniele Dondi
Director in Laboratory of Radiation Chemistry and EPR Spectroscopy
Department of Chemistry, University of Pavia, 27100, Italy.
Thursaday, August 29th, 2024
CH4rLiE

## Slide 2
Experiments performed
1. Pyrolysis of 50%Melamine-Z5 sample at 200 °C under N2.
2. Pyrolysis of 50% Melamine-Z5 sample at 400 °C under N2.
3. Pyrolysis of 50% Melamine-Z5 sample at 400 °C under vacuum.
4. Pyrolysis of 50% Melamine-Z5 sample at 400 °C under vacuum and removing quartz tube at high temperature.
5. Pyrolysis of 20% kraft lignin-Z5 sample at 550 °C under vacuum.
6. Drying of Z5 zeolite under vacuum and introducing CH4.
7. Drying of Z5 zeolite under vacuum and introducing CH4 repeated.
8. Pyrolysis of 20% kraft lignin-Zeosil 1165MPunder vacuum.
9. Pyrolysis of 20% wood lignin-Zeosil 1165MPunder vacuum.
10. Pyrolysis of 20% kraft lignin-Zeosil 1165MPunder vacuum- Changed procedure of preparation.

## Slide 3
Z5-Melamine pyrolysis under N2 at 200 °C

## Slide 4
Z5-Melamine pyrolysis under N2 at 400 °C

## Slide 5
Z5-Melamine 50% After pyrolysis under vacuum

## Slide 6
Z5-Melamine 50% After pyrolysis under vacuum 1 minute

## Slide 7
Z5-Kraft lignin 20%

## Slide 8
Z5-Kraft lignin 20% After pyrolysis TGA N2

## Slide 9
Z5-Kraft lignin 20% After pyrolysis TGA Air
Carbon content-16.6%

## Slide 10
Z5 dried under vacuum CH4 introduced

## Slide 11
Z5 dried under vacuum CH4 introduced repeated

## Slide 12
Zeosil 1165MP-Kraft lignin 20%

## Slide 13
Zeosil 1165MP-Kraft lignin 20% After pyrolysis TGA N2

## Slide 14
Zeosil 1165MP-Kraft lignin 20% After pyrolysis CH4 introduced

## Slide 15
Zeosil 1165MP-Kraft lignin 20% After pyrolysis TGA Air
Carbon content-0.1%

## Slide 16
Zeosil 1165MP-Wood lignin 20%

## Slide 17
Zeosil 1165MP-Wood lignin 20% After pyrolysis TGA N2

## Slide 18
Zeosil 1165MP-Wood lignin 20% After pyrolysis TGA Air
Carbon content-8.1%

## Slide 19
Zeosil 1165MP-Kraft lignin 20% Washed procedure

## Slide 20
Zeosil 1165MP-Kraft lignin 20% Washed procedure After pyrolysis TGA N2

## Slide 21
Zeosil 1165MP -Kraft lignin 20% Washed procedure After pyrolysis TGA Air
Carbon content-0.1%

## Slide 22
Conclusions from Completed experiments
Z5-incorporated Melamine sample failed to produce carbon even after 50% Melamine.
Z5- incorporated Kraft Lignin Sample successfully produced carbon.
Removing the sample out of the pyrolysis oven as soon as drying completion proved successful as earlier drying, the 6% weight loss in TGA was reduced to 4%.
Insertion of methane in the dried Z5 was inconclusive.
Kraft and wood type lignin was successfully incorporated inside Zeosil 1165MP.
Pre-treatment of Hydrothermal is completed and ready for use.
Further Planning
Investigation of Z-10 such as drying, carbon incorporation.
Synthesis of Material using Hydrothermal reactor.

## Slide 23
Thank you
Acknowledgement