## Slide 1: SPS: Mitigation Strategy at CERN
José Miguel JIMENEZ
On behalf of the LIU-SPS WG special thanks to M. Taborelli & P. Costa-Pinto

## Slide 2
Introduction
Status Report
Pending Issues
Review of objectives
Conclusions
Main Topics

## Slide 3: LIU-SPS Electron Cloud issues
SPS has to be prepared to digest:
  High bunch intensity: up to 2.5 1011 ppb @ 25 ns ; 3.5 1011 ppb @ 50 ns
  and
  Small emittances (LHC requirements)
cannot be guaranteed since electron cloud limitations have been identified:
  Beam instabilities: transverse emittance blow-up and single bunch vertical instability
  Pressure rise: beam gas scattering, dose rates to tunnel and components
Improvements considered against Electron Cloud:
  Suppression of the build-up: Clearing electrodes and very low SEY (<1.1) coatings
  Mitigation of the build-up: Scrubbing Runs
  Cure of the induced effects (single bunch vertical instability): High bandwidth feedback systems
Introduction

## Slide 4: Criteria for decision
Safety
  The solution shall be safe for the operation of ALL SPS beams
  The implementation shall not induce major personnel safety issues e.g. radiation, handling...
Performance
  The solution shall allow a routine operation with the bunch populations required by HL-LHC
Reliability
  The solution shall not degrade with time and behaviour shall be predictable and reproducible
Operation margin
  The solution shall provide contingency in case real situation is worst than our expectations
Other important criteria
  “Best value for money”
  Implementation duration compatible with a long shutdown
  Infrastructures required must be compatible with CERN existing options
Introduction

## Slide 5: Feasibility study is completed…
Effective suppression at all tested B fields with low (<100 V) bias voltage
Clearing electrodes can ONLY be applied on few places of the machine: aperture restriction
No solution found to apply clearing electrodes inside existing main magnet chambers
Feasibility studies are now stopped
  KEK clearing electrode tested successfully with beams in the SPS in field free and dipole field conditions
  Without dipole field, Ecloud dominated by alumina surface, rough sprayed tungsten had a SEY=1.3
Status Report EC Suppression – Clearing Electrodes

## Slide 6: Validation being completed…
Status Report EC Suppression – Very low SEY a-C Coatings
Very low SEY achieved by purifying the discharge during the coating process
  SEY below 1 obtained systematically
Lifetime
  Very small effect (drift up to 1.1) visible after 3 years in the SPS
Effect of venting
  Small increase up to 1.1, still bellow the EC threshold
Industrialisation of coating solutions
  Coating ex-situ (new beampipes)
    Magnetron sputtering has been validated for both MBB and MBA beampipes
  Coating in-situ (existing beampipes)
    Hollow cathode as baseline
      Successfully industrialised for MBB profiles
      Delays with MBA due to inhomogeneity other the 7 m length will need about a year to validate the coating since the tooling is being optimised
Hollow cathode

## Slide 7: Reliability and Performances…
Status Report EC Suppression – Very low SEY a-C Coatings
Static outgassing of a-C coating
  As expected, static outgassing is higher but no difference can be seen after 2nd pump down
  Dynamic vacuum is expected to be lower because of the intrinsic good properties of a-C coating

## Slide 8: Is it required to coat the entire beampipe?
Status Report EC Suppression – Very low SEY a-C Coatings
In dipole magnets, coating the top and bottom surfaces is required
In field free regions, coating the entire inner surface is required

## Slide 9: What’s required?
Status Report EC Mitigation – Scrubbing Runs
Beam scrubbing is successfully used since 1999 to reduce the EC activity, BUT:
  No scaling rule exists: EC builds-up can be non-monotonic and depends on:
    Parameters which totally change the picture: Chamber’s shape and size, Bunch spacing, Presence of an externally applied magnetic field
    Minor changes are also observed passing from the 26GeV to the 450GeV scenario due to change in: Bunch length, Geometrical emittance
  SPS is more demanding than LHC
  Full suppression was never achieved except in field free regions
  Corresponds to a mitigation solution and NOT to a suppressing method
Beampipe profile | SEY threshold @ 1.1 1011 p/bunch | SEY threshold @ 2.5 1011 p/bunch
ID 156 (LSS) | 1.4 | 1.1
ID 130 (LSS) | 1.45 | 1.05
MBA (Dipole) | 1.4 | 1.45
MBB (Dipole) | 1.15 | 1.25

## Slide 10: Some issues to be followed…
Status Report EC Mitigation – Scrubbing Runs
Beam scrubbing has intrinsic limitations:
  Reaching smaller SEY (d) need larger electron bombardment doses: log behaviour
    Lower bombardment dose when going closer to threshold for a given bunch population: ~3 orders of magnitude decrease!
      Some materials like Stainless Steel show saturation of the dose effect in the Lab
  Induces collateral effects: heating of kickers, internal dump heavily loaded
SPS = StSt / LHC = Copper
10 times less dose rate!
10 times more integrated dose!
Saturation...
x 100 more beam time!

## Slide 11: Scrubbing and limitations linked to material
Aluminium MUST be avoided!! Except if coated...
REMINDER !

## Slide 12: How to enhance the EC close to threshold?
Status Report EC Mitigation – Scrubbing Runs
Strategies of e-cloud enhancement (input for SPS scrubbing run tests):
  5ns bunch spacing
  Slip stacking
  5-10% uncaptured beam
    (alternative to) Filling SPS with 8 x 72 b @ 25 ns and 26 GeV
  PS bunch splitting deregulation (Bunch intensity modulation)
Beam configuration | Scrub. dose enhancement factor | Entirely scrubs the required region | Additional remarks
5 ns beam | 4 | NO | At least two batches required
Slip stacking | 5 | YES | (10+15)ns much better than (5+20)ns
5-10% uncaptured beam | 1.3 Much more if sat. not reached in 4 batches | YES | In worst case, it can be employed to scrub with 3 batches (factor 2000) instead of 4 (less heating, less outgassing)
PS splitting deregulation | <1 | YES | 
At SPSU-BD meeting (12 October) it was pointed out that the first two options are not feasible with the installed RF system.

## Slide 13: R&D for SPS high bandwidth transverse feedback system
Status reviewed in November 2011 by the LIU project:
  https://indico.cern.ch/conferenceDisplay.py?confId=162989
Aimed at:
  Demonstrating transverse damping of intra bunch headtail motion caused by impedance and e-cloud, GHz bandwidth
  Full system implementation could be ready for 2018 if proof of principle shown before LS1, i.e. 2012
  Test-set-up operational in SPS
Status Report EC Cure - High bandwidth feedback systems
*supported by US-LARP and LIU project, joint effort of CERN, SLAC, LBNL

## Slide 14: Scrubbing or Coating?
Secondary electron yields
  SEY measurements and dose effects, venting to atmosphere
Multipactor test bench
  Testing the multipacting performances of the coatings
  combined with:
  Pressure gauges which provide also indication of multipacting in the beampipe
Coating features
  Dynamic behavior (electron stimulated desorptions), static outgassing
  Ageing, peel-off
Pending Issues Measurements in the Lab
MBA not tested yet

## Slide 15: Scrubbing or Coating?
Strip detectors, pick-ups, sample extractor, Pressure rise...
  Nothing yet inside real long magnet: MBB or MBA
  Installing an electron probe at the centre of a dipole magnet was abandoned
    Simulations and observations made with the strip detectors with dipole fields confirmed that the EC build-up will not take place or will be strongly perturbed
    Magnetic field combined with collector will “kill” locally the multipacting
Pending Issues Measurements with Beams
Symmetric holes on top and bottom half yokes to avoid longitudinal effects

## Slide 16: SPS HC514: a-C coated beampipes instead of magnets…
Pending Issues Measurements with Beams

## Slide 17: SPS HC513: a-C coating magnets as from June’12…
Pending Issues Measurements with Beams

## Slide 18
Pending Issues Measurements with Beams
External solenoid
on StSt bellow
(L=128 mm)
External solenoid on
StSt chamber
(L=850 mm)
Central solenoid
on carbon coated chamber
(L=12324 mm)
Solenoids in drift space in sextant 5 (51420-51460)

## Slide 19
Pending Issues Measurements with Beams
W13, Dynamic pressure with solenoids on/off, 3 batches 25 ns
The dynamic pressure rise is influenced only by the external solenoids:
in the coated drift section there is
no p rise due to
e-cloud
Q
MBA
MBA
MBB
MBB
GIX
Q

## Slide 20
An amazing work done…  presented at the Electron Cloud LIU-SPS meeting (Jan’12)
Simulations are required to assess the EC induced instability threshold in dipoles
  Electrons in dipole field are, after some scrubbing, far away from beams
    Faster scrubbing at the centre where high energetic electrons are concentrated
    Lateral strips move away from beam while increasing bunch population
2004 data
Pending Issues Simulations

## Slide 21
Review of objectives As re-evaluated for Chamonix’12
Slide N°11 / Electron Clouds in the SPS: progress in the analysis of cures/mitigations… Session 09, J.M. Jimenez – Chamonix’11
2012
2012
2012
2012
 4 coated half-cells coated installed
 4 new coated half-cells to be installed if 2012 measurements are not conclusive
(4 coated half-cells)

## Slide 22: The guaranty of suppression…
a-C coating technology is at the same level of validation than NEG when approved for LHC…
  Very low SEY is compatible with ultimate bunch populations for all beampipe shapes
  Solution of coating in-situ magnets is the only solution considered for the future
  Industrialization process is getting validated, only MBA is pending
  Long straight section beampipes will be coated as well (easy)
  Reversibility is not an issue since coating can be remove using and oxygen glow discharge
  Large scale quality is not a showstopper since already done for LHC NEG coated beampipes
  Static vacuum behavior, slightly higher outgassing of the coating, will be worked out
Remaining concerns essentially logistical:
  Cost, Resources, Infrastructures, Duration, Radiation dose to personnel
aC coating is project baseline and presently working towards assumption that this will be needed
Conclusions Amorphous Carbon Coatings

## Slide 23: The low-cost alternative…
The ongoing simulations and Scrubbing MDs are prerequisite to decision…
  Solutions exists on paper to enhance the multipacting close to EC threshold and thus speed up the Dose effect on SEY
  Only MBB dipoles (1/3 of SPS) shows a very low EC multipacting threshold
  Benefit expected on the instability threshold resulting from the non-homogeneous distribution of electrons in dipoles required to compensate for the saturation of the SEY dose effect on StSt
  Simulations ongoing to determine required scrubbing time/feasibility - profiting from excellent LHC data and simulations
Remaining concerns:
  Saturation of the Dose effect on SEY of Stainless Steel beampipes is a major issue
  Beam type required to enhance EC close to threshold
  Unexpected limitation on beam equipments like RF, kickers due to heating
Conclusions Scrubbing Runs

## Slide 24
Acknowledgements
Many thanks to all contributors: Jeremie Bauche; Mauro Taborelli; Giovanni Iadarola; Gianluigi Arduini; Elias Metral; Pedro Costa Pinto; Paolo Chiggiato; Fritz Caspers; Yannis Papaphilippou; Holger Neupert; Brennan Goddard; Roland Garoby; Elena Chapochnikova; Malika Meddahi; Hannes Bartosik; Karel Cornelis; Wolfgang Hofle; Giovanni Rumolo. (My excuses if the list is not complete)
It was a great pleasure to lead the LIU-SPS Electron Cloud Study team and I am very happy to pass this role (as from Feb’12) to:
  Mauro TABORELLI [TE-VSC-SCC Surface, Chemistry and Coating Section Leader]