## Slide 1: Radiation resistance properties of electronic devices interacting with different radiation sources
Beatrice D'Orsi Final seminar – PhD in Accelerator Physics XXXVI cycle
Advisors:
Prof. Patrizio Antici
Prof. Mauro Migliorati
Rome, September 30th, 2024
Co-advisor:
Dr. Alessia Cemmi

## Slide 2: Summary of the presentation
Part 1 Introduction Experimental results
Part 2 Results elaboration
Results comparison
Part 3 Other activities

## Slide 3
Part 1

## Slide 4: Aim of the work
Commercial
Radiation tolerant
Radiation hardened
Photons
Protons
Electron
Neutrons
Heavy ions
Etc.
Study of radiation effects
Electronic measurements
Data analysis (stress testing optimization)
Electronic devices
Irradiation

## Slide 5: PhD research
Gamma rays
Neutrons
Protons (innovative and conventional sources – stress testing method validation)
2 $
Study of
radiation effects
Electronic devices
Irradiation
Radiation resistance testing of specific electronic devices
Investigate different irradiation methods for optimization of stress testing
Radiation tolerant
Commercial Off-the-Shelf (COTS)
80 $

## Slide 6: Electronic components characterization before and after irradiation
COTS NPN and PNP Bipolar Junction Transistors (BJTs)
Radiation tolerant opto-isolator
Tested components
6
https://www.imtsrl.it/
Many parameters (currents, voltages and gain) were evaluated before and after the irradiation tests.
2 cm
2 cm
Microsemi. TECHNICAL DATASHEET – 2N2222A NPN silicon switching transistor.
Microsemi. TECHNICAL DATASHEET – 2N2907A PNP small signal silicon transistor.
Skyworks. TECHNICAL DATASHEET - OLS249: Radiation-Tolerant Phototransistor Hermetic Surface-Mount Optocoupler.
Not reported here

## Slide 7: Irradiation facilities: Italy and Canada
Gamma irradiation Calliope facility at ENEA Casaccia R.C. (Rome, Italy)
Neutron irradiation Frascati Neutron Generator at ENEA Frascati R.C. (Frascati, Italy)
Proton irradiation TOP IMPLART at ENEA Frascati R.C. (Frascati, Italy)
Conventional radiation sources for stress testing
Proton irradiation Advanced Laser Light Source (ALLS) ion beamline at INRS-EMT (Varennes, Québec, Canada)
Innovative radiation source for stress testing
14 MeV neutrons
60Co gamma photons (mean energy 1.25 MeV)
Dosimetric laboratory available
2.8 MeV conventional protons
Ultra-intense ultra-short laser pulse is focused on a thin target
Proton acceleration
Target Normal Sheath Acceleration
(TNSA) mechanism
Laser-driven protons (from few keV up to 5MeV)

## Slide 8: Possible radiation effects on electronics
Energy loss by ionization: interactions of atomic particle which result in the excitation or emission of atomic electrons
Non Ionizing Energy Loss (NIEL) processes: interactions in which the energy imparted by the incoming particle result in atomic displacement.
Total Ionizing Dose (TID) damage
Displacement Damage (DD) dose
The active material of electronic devices is often made of silicon.
Single event effect (SEE): related to single individual interactions:
single event upset (SEU): bit flips in memory circuits;
single event latchup (SEL): locally deposited charge.
Surface damage
Cumulative effects
Bulk damage
Single interaction
Incident particle
V
I
V: vacancy
I: interstitial
e-h pair generation
Holes transport through localized state in SiO2 bulk
Hole trapping near Si/SiO2 interface
Interface traps within Si bandgap
Radiation Handbook for electronics, Texas Instruments (2018) www.ti.com/radbook
Leroy C, Rancoita PG. Particle interaction and displacement damage in silicon devices operated in radiation environments. Reports Prog Phys. 2007;70(4):493–625
Notes: The active material of electronic devices is often made of silicon and according to the occurring radiation matter interaction, the radiation effects can be divided into:
TID, SEE, DD
SEE can occur at any moment of the operation
TID and DD cumulative effects
Gamma radiation is used to simulate TID damage since the displacement damage is negligible with respect to TID until large value of absorbed doses (dipende dalla fluenza di elettroni che a loro volta dip da config campione, non c’è un valore di dose)
Protons and neutrons are useful to evaluate displacement damage and heavy ion beams to evaluate SEE.
---------------------------------------------------------------------------------
Electronic components used for the fabrication of electronic systems are fundamental in many fields of application. Many of them are characterized by adverse radiation environment, for example high luminosity machines, nuclear facilities, Space environment and thus can be a threat for the devices operation since they can cause radiation induced damage.
The interaction of incoming particles with matter results in two major effects: the collision energy loss and the atomic displacement. The interactions which result in the excitation or emission of atomic electrons are referred to as energy loss by ionization (or by collision) and cause the so called ionization damage. The Non Ionizing Energy Loss (NIEL) processes are interactions in which the energy imparted by the incoming particle result in atomic displacement or in collisions where the knock on atom does not move from its lattice location end the energy is dissipated through lattice vibrations and cause displacement damage.
The energy deposition by non-ionization processes is much lower (except for neutrons) than that by ionization.
The employed electronics must be able to withstand high radiation environments and must be tested before operation.
---------------------------------------------------------------------------------------------------------------------------------------------------------------------------------
→ single event latchup (SEL): locally deposited charge which can generate a kind of short circuit between the power supply and the ground (causing power dissipation);
---------------------------------------------------------------------------------
The incoming radiation may also inflict temporary or permanent damage to the detectors
material and readout electronics. In most cases - for moderate exposure to
irradiation fields -, detectors are not prevented from operating normally, but - in
presence of large irradiation fields and/or as a result of exposure to large accumulated
fluences - induced radiation effects may degrade devices performance.
This edition presents a comprehensive treatment of the Coulomb scattering on
screened nuclear potentials resulting from electrons, positrons, protons, light- and
heavy-ions - ranging from (very) low up to ultra-relativistic kinetic energies - and
allowing the derivation of the corresponding NIEL (non-ionizing energy-loss) doses
deposited in any material, because of atomic displacements caused by the interaction.
Silicon is the active material of radiation detectors and in electronic devices used
in the fabrication and development of electronic circuits of large to very large scale
integration (VLSI) applications. As discussed in the previous section, these devices
are commonly used for a large variety of applications in many fields including particle
physics experiments, reactor physics, nuclear medicine, and space. These fields
generally present adverse (or, even, very adverse) radiation environments that may
affect the operation of the devices and are described in the chapters on Radiation
Effects and Displacement Damage in Semiconductors, Radiation Environments and
Damage in Semiconductors and Displacement Damages and Interactions in Semiconductor
Devices. These environments are generated by i) the operation of the
high-luminosity machines [e.g., the Large Hadron Collider¶ (LHC)] for particles
physics experiments , ii) the cosmic rays and trapped particles of various origins in
interplanetary space and/or Earth magnetosphere and iii) the operation of nuclear
reactors. Their potential threats to the devices operation, in terms of radiationinduced
damage by displacement are also described in that chapter. Furthermore
to understand the way it may affect the devices operation, the particles energy
deposition mechanisms are discussed with i) the radiation-induced damage and ii)
resulting effect on bulk and device parameters evolution. These latter modifications
depend on the type of irradiation particles, their energy and irradiation fluence. A
treatment is done of damage inflicted by total ionizing dose and non-ionizing energyloss
(NIEL) effects for which the accumulated fluence causes permanent degradation
because of the induced displacement damage.
The experimental data obtained with silicon
radiation detectors demonstrate that the non-ionizing energy-loss (NIEL) must account for i) the relativistic Coulomb cross section and ii) hadronic interactions -
which are not included in the SRIM code [Ziegler, Biersack and Littmark (1985a)]
- also for low energy protons ( 10MeV).

## Slide 9: Typical radiation effects on BJTs
Spreading of BE depletion region and increased recombination increased base current
e--h creation and separation
e- drift outside the oxide
h migration and trapping in
the Si-SiO2 interface
Interstitials-vacancies creation
These effects translate in BJTs current gain degradation
AFTER IRRADIATION
J Assaf 2018 Chinese Phys. B 27 016103
Radiation Handbook for electronics, Texas Instruments (2018) www.ti.com/radbook
Reduction of minority carriers lifetime (increased recombination)
BEFORE IRRADIATION
SiO2
Si
Metal contact
depletion zone
base
emitter
SiO2
Base Emitter (BE) junction of NPN BJTs

## Slide 10: COTS BJTs: Radiation effects evaluation
To evaluate the radiation effect, the parameter, corresponding to the transistor current gain, the leakage currents and saturation voltages were measured.
: collector current
: base current
: emitter current
Leakage currents
() ()
()
Current that flows when the device is in off state
Saturation voltages
collector to emitter saturation voltage
base to emitter saturation voltage
Voltage beyond which the remains constant as the increases.
measured for
measured for
measured for
measured for
measured for
: collector to emitter voltage
: base to emitter voltage
: base to collector voltage
NPN
PNP
IC-VCE characteristic curves
Collector current versus the collector to emitter voltage at a fixed (50 µa)
Other measured parameters
Gain

## Slide 11: COTS BJTs: Summary of performed irradiation tests
 | COTS NPN bipolar transistor (2N2222A) | COTS PNP bipolar transistor (2N2907A)
Gamma irradiation (Calliope) |  | 
Neutrons (FNG) |  | 
Conventional protons (TOP IMPLART) |  | 
Laser-driven protons (ALLS) |  | Next step
 | COTS NPN bipolar transistor (2N2222A) | COTS PNP bipolar transistor (2N2907A)
Gamma irradiation (Calliope) |  | 
Neutrons (FNG) |  | 
Conventional protons (TOP IMPLART) |  | 
Laser-driven protons (ALLS) |  | Next step
The components were characterized before and after irradiation.

## Slide 12: COTS BJTs: gamma irradiation tests and measurements - 1
Irradiation tests:
Irradiation at room temperature and parametric tests after irradiation
Annealing followed by parametric tests:
-24 hours at room temperature
-168 hours at 100 °C
36 samples (18 NPN and 18 PNP BJTs) two for each irradiation condition
Irradiation at different absorbed doses
Dose rate = 1 kGy(Si)/h
Irradiation setup
All samples were biased
during irradiation (+30 V).
Irradiation test | Total absorbed dose (kGy)
1 | 1
2 | 2.3
3 | 26
4 | 72
5 | 120
6 | 240
7 | 320
8 | 420
9 | 515
60Co gamma radiation
1 kGy(Si): 1 kGy absorbed dose in silicon. All reported doses are referred to silicon.
COTS

## Slide 13: COTS BJTs: gamma irradiation tests and measurements - 2
Parameter | Test condition | Datasheet
 |  | <
 |  | <
 |  | <
 |  | <
Parameter | Test condition | Datasheet
60Co gamma radiation
Parameter | Test conditions | Datasheet
 |  | <
 |  | <
 |  | <
Parameter | Test conditions | Datasheet
PNP
IC-VCE characteristics
IC decreases with increasing dose
Saturation voltages
No modification except for VCE(sat)2
fluctuations
Leakage currents

## Slide 14: COTS BJTs: gamma irradiation tests and measurements - 3
60Co gamma radiation
NPN
 | >50
 | >75
 | >100
 | >100
 | >30
 | >50
 | >75
 | >100
 | >100
 | >30
Datasheet allowed values
PNP
 | >75
 | >100
 | >100
 | >100
 | >50
 | >75
 | >100
 | >100
 | >100
 | >50
Datasheet allowed values
8 kGy
7 kGy
3 kGy
0.6 kGy
100 kGy
15 kGy
20 kGy
35 kGy
20 kGy
70 kGy
Out of range
Out of range
HEAVILY damaged after:
HEAVILY damaged after:

## Slide 15: COTS BJTs: annealing tests and measurements - 4
Slight recovery of the samples irradiated up to 2.3 kGy(Si) after the annealing tests
No recovery of the heavily damaged samples after the annealing tests
60Co gamma radiation
After irradiation, two annealing tests were performed in order to evaluate the recovery of the parameters.
NPN
End of irradiation
Annealing step:
25 °C for 24 hours.
Parametric test
Annealing step: 100 °C for 168 hours.
Parametric test
End of test
PNP
Recovery
Recovery

## Slide 16: COTS BJTs: neutron irradiation tests and measurements - 1
COTS
20 samples (10 NPN and 10 PNP BJTs) two for each irradiation condition
Irradiation up to different neutron fluences (14 MeV neutrons)
Irradiation test | Neutron fluence
1 | 2 ּ 109 n/cm2
2 | 2 ּ 1011 n/cm2
3 | 2 ּ 1012 n/cm2
4 | 1 ּ 1013 n/cm2
5 | 2 ּ 1013 n/cm2
All samples were unbiased
during irradiation.
Irradiation setup
Irradiation tests:
Irradiation at room temperature and parametric test after irradiation
Annealing followed by parametric tests:
-24 hours at room temperature
-168 hours at 100 °C
https://www.sr-niel.org/index.php/sr-niel-web-calculators/niel-calculator-for-neutrons-using-astm-standards/neutrons-niel-calculator
ASTM E722-19: Standard Practice for Characterizing Neutron Fluence Spectra in Terms of an Equivalent Monoenergetic Neutron Fluence for Radiation-Hardness Testing of Electronics
14 MeV neutrons

## Slide 17: COTS BJTs: neutron irradiation tests and measurements - 2
14 MeV neutrons
 | >50
 | >75
 | >100
 | >100
 | >30
 | >50
 | >75
 | >100
 | >100
 | >30
Datasheet
NPN
PNP
 | >75
 | >100
 | >100
 | >100
 | >50
 | >75
 | >100
 | >100
 | >100
 | >50
Datasheet
No recovery after annealing tests
HEAVILY damaged after:
5.0 1012 n/cm2
3.5 1012 n/cm2
2.5 1012 n/cm2
2.0 ּ 1012 n/cm2
No out of range
No out of range
HEAVILY damaged after:
7.0ּ 1012 n/cm2
8.0 1012 n/cm2
1.5 1013 n/cm2
No out of range
No out of range
No out of range
No out of range

## Slide 18: COTS BJTs: samples preparation for proton irradiation (TOP IMPLART and ALLS)
For proton irradiation tests the BJTs were decapped.
The lid thickness was about 300 µm.
Projected range of 5 MeV protons in Nickel 73 µm
Gamma rays and neutrons: not attenuated
6 mm
The lid was removed
Magnitude 66X
Magnitude 400X
SEM analysis

## Slide 19: COTS BJTs: proton irradiation (TOP IMPLART) and measurements - 1
12 decapped samples (6 NPN and 6 PNP BJTs) two for each irradiation condition
Irradiation up to different proton fluences (2.8 MeV protons)
Irradiation test | Proton fluence
1 | 3.38 ּ 109 p/cm2
2 | 3.38 ּ 1010 p/cm2
3 | 2.5 ּ 1011 p/cm2
Irradiation tests:
Irradiation at room temperature and parametric test after irradiation
Annealing followed by parametric tests:
-24 hours at room temperature
-168 hours at 100 °C
https://www.sr-niel.org/index.php/sr-niel-web-calculators/niel-calculator-for-neutrons-using-astm-standards/neutrons-niel-calculator
ASTM E722-19: Standard Practice for Characterizing Neutron Fluence Spectra in Terms of an Equivalent Monoenergetic Neutron Fluence for Radiation-Hardness Testing of Electronics
All samples were unbiased
during irradiation.
Irradiation setup
Conventional protons
COTS

## Slide 20: COTS BJTs: proton irradiation (TOP IMPLART) and measurements - 2
Conventional protons
 | >50
 | >75
 | >100
 | >100
 | >30
 | >50
 | >75
 | >100
 | >100
 | >30
Datasheet
NPN
HEAVILY damaged after:
1.2 1011 p/cm2
0.8 1011 p/cm2
0.5 1011 p/cm2
0.4 ּ 1011 p/cm2
1.8 ּ 1011 p/cm2
 | >75
 | >100
 | >100
 | >100
 | >50
 | >75
 | >100
 | >100
 | >100
 | >50
Datasheet
PNP
HEAVILY damaged after:
No recovery after annealing tests
2.1 1011 p/cm2
2.5 1011 p/cm2
No out of range
No out of range
No out of range
No out of range
No out of range
No out of range

## Slide 21
Irradiation tests:
Irradiation at room temperature and parametric test after irradiation
Annealing followed by parametric tests:
-24 hours at room temperature
-168 hours at 100 °C
6 decapped samples (NPN BJTs)
Irradiation at different number of shots
COTS BJTs: proton irradiation tests (ALLS) and measurements - 1
Irradiation test | Number of shots
1 | 1
2 | 5
3 | 50
4 | 100
5 | 250
6 | 400
Laser-driven protons
Irradiation setup
All samples were unbiased
during irradiation.
COTS

## Slide 22
COTS BJTs: proton irradiation tests (ALLS) and measurements - 2
No recovery after the annealing tests
Laser-driven protons
 | >50
 | >75
 | >100
 | >100
 | >30
 | >50
 | >75
 | >100
 | >100
 | >30
Datasheet
NPN
HEAVILY damaged after:
4 shots
3 shots
2 shots
2 shots
No out of range
Zoom in:
1-5 shots

## Slide 23
Part 2

## Slide 24: Dose deposition study – 1
Leroy C, Rancoita PG. Principles of Radiation Interaction in Matter and Detection. WORLD SCIENTIFIC (2016).
TID: Surface damage
TID depends on radiation type and irradiation conditions
NIEL:
Bulk damage
NIEL dose proportional to the number of created bulk defects independently of the radiation type
For each radiation source DoseNIEL contribution to
DoseTOTAL was evaluated
To compare different stress testing methods the DoseTOTAL due to each radiation source was investigated.
Fluences and number of shots were transformed into DoseTOTAL values

## Slide 25: Dose deposition study – 2 60Co gamma photons
MCNP simulation
60Co source
γ
Sample
Sample geometry
Sample position inside the irradiation cell
Irradiation conditions (dose and dose rate)
The electron spectrum after one second of gamma irradiation at 1 kGy/h
https://www.sr-niel.org/index.php/sr-niel-web-calculators
ASI sr-niel calculator
After one hour of irradiation:
DoseTOTAL = 1 kGy
DoseNIEL = 8ּ 10-3 Gy
60Co gamma radiation
DTOTAL deposited by gamma radiation is provided by the facility (dosimetric systems)
60Co photons directly induce only TID damage but can create Compton electrons responsible of DD. DNIEL evaluation:

## Slide 26
Dose deposition study – 3 Neutrons
14 MeV neutrons
https://www.sr-niel.org/index.php/sr-niel-web-calculators
Neutrons DTOTAL evaluation:
Neutrons DNIEL evaluation:
The International Commission on Radiation Units and measurements (ICRU). Fundamental quantities and units for ionizing radiation (Report No. 85), volume 11. Oxford University Press, 2011.
The kerma K can be obtained using the kerma coefficient k:
For a fluence = 2 1012 n/cm2:
DoseTOTAL = 25 Gy
DoseNIEL = 1.2 Gy
R.S. Caswell, J.J. Coyne, and M.L. Randolph. Kerma factors of elements and compounds for neutron energies below 30 MeV. The International Journal of Applied Radiation and Isotopes, 33(11):1227–1262, 1982.
ASI sr-niel calculator

## Slide 27
Dose deposition study –4
Conventional protons
Conventional protons
2.8 MeV protons are completely absorbed by the silicon depth.
Conventional protons DTOTAL evaluation:
Proton stopping power
Proton fluence
Conversion factor
Conventional protons DNIEL evaluation:
For a fluence = 3.38 109 p/cm2:
DoseTOTAL = 48 Gy
DoseNIEL = 1.33 10-2 Gy
ASI sr-niel calculator
J.F. Ziegler. SRIM - The Stopping and Range of Ions in Matter. http://www.srim.org/.

## Slide 28
Simon Carrier-Vallieres. PhD Thesis - Towards reliable, intense and high repetition-rate laser-driven ion beamlines. Université de Bordeaux; INRS (2020)
Laser-driven protons
Dose deposition study – 5 Laser-driven protons
Laser accelerated protons DNIEL evaluation
For each shot:
DoseTOTAL = 3.5 Gy
DoseNIEL = 2.5 10-3 Gy
y
Without the lid
Laser accelerated protons DTOTAL evaluation (MATLAB simulation)
ASI sr-niel calculator
DoseTOTAL
[°C]
Notes: The code takes as input the proton spectrum ((𝑑^2 𝑁_𝑝)/𝑑𝐸𝑑Ω(𝐸_𝐾)), the cone half-angle divergence (𝜎_𝜃 (𝐸_𝐾)) and the virtual point source position (𝑑_𝑣𝑖𝑟𝑡𝑢𝑎𝑙 (𝐸_𝐾)).

## Slide 29: Results summary
The results obtained after irradiation of BJTs and the results of the dose deposition study were merged.
 | Gamma | Neutrons | Conventional protons | Laser-driven protons
 | 8 kGy | 5.0 1012 n/cm2 | 1.2ּ 1011 p/cm2 | 4 shots
 | 7 kGy | 3.5 1012 n/cm2 | 0.8 1011 p/cm2 | 3 shots
 | 3 kGy | 2.5 1012 n/cm2 | 0.5 1011 p/cm2 | 2 shots
 | 600 Gy | 2.0 ּ 1012 n/cm2 | 0.4 ּ 1011 p/cm2 | 2 shots
 | 100 kGy | / | 1.8 ּ 1011 p/cm2 | /
 | Gamma | Neutrons | Conventional protons | Laser-driven protons
 | 8 kGy |  |  | 4 shots
 | 7 kGy |  |  | 3 shots
 | 3 kGy |  |  | 2 shots
 | 600 Gy |  |  | 2 shots
 | 100 kGy | / |  | /
 | Gamma | Neutrons | Conventional protons
 | 15 kGy | 7.0ּ 1012 n/cm2 | 2.1ּ 1011 p/cm2
 | 20 kGy | 8.0 1012 n/cm2 | 2.5 1011 p/cm2
 | 35 kGy | 1.5 1013 n/cm2 | /
 | 20 kGy | / | /
 | 70 kGy | / | /
 | Gamma | Neutrons | Conventional protons
 | 15 kGy |  | 
 | 20 kGy |  | 
 | 35 kGy |  | /
 | 20 kGy | / | /
 | 70 kGy | / | /
NPN
PNP
Doses/fluences causing gain to exit allowed ranges
 |  | Gamma | Neutrons | Conventional protons | Laser-driven protons
 | DoseTOTAL | 8 kGy | 62.5 Gy | 2.05 kGy | 13.6 Gy
 | DoseNIEL | 0.06 Gy | 3.0 Gy | 0.46 Gy | 0.01 Gy
 | DoseTOTAL | 7 kGy | 43.8 Gy | 1.37 kGy | 10.2 Gy
 | DoseNIEL | 0.06 Gy | 2.1 Gy | 0.31 Gy | 0.01 Gy
 | DoseTOTAL | 3 kGy | 31.3 Gy | 856 Gy | 6.8 Gy
 | DoseNIEL | 0.02 Gy | 1.5 Gy | 0.24 Gy | 5.0 10-3 Gy
 | DoseTOTAL | 600 Gy | 25 Gy | 685 Gy | 6.8 Gy
 | DoseNIEL | 5.0 10-3 Gy | 1.2 Gy | 0.14 Gy | 5.0 10-3 Gy
 |  | Gamma | Neutrons | Conventional protons | Laser-driven protons
 | DoseTOTAL | 8 kGy | 62.5 Gy | 2.05 kGy | 13.6 Gy
 | DoseNIEL | 0.06 Gy | 3.0 Gy | 0.46 Gy | 0.01 Gy
 | DoseTOTAL | 7 kGy | 43.8 Gy | 1.37 kGy | 10.2 Gy
 | DoseNIEL | 0.06 Gy | 2.1 Gy | 0.31 Gy | 0.01 Gy
 | DoseTOTAL | 3 kGy | 31.3 Gy | 856 Gy | 6.8 Gy
 | DoseNIEL | 0.02 Gy | 1.5 Gy | 0.24 Gy | 
 | DoseTOTAL | 600 Gy | 25 Gy | 685 Gy | 6.8 Gy
 | DoseNIEL |  | 1.2 Gy | 0.14 Gy | 
 |  | Gamma | Neutrons | Conventional protons
 | DoseTOTAL | 15 kGy | 87.5 Gy | 3.02 kGy
 | DoseNIEL | 1.2 10-1 Gy | 4.3 Gy | 0.83 Gy
 | DoseTOTAL | 20 kGy | 100 Gy | 3.6 kGy
 | DoseNIEL | 1.6 10-1 Gy | 5 Gy | 1 Gy
 |  | Gamma | Neutrons | Conventional protons
 | DoseTOTAL | 15 kGy | 87.5 Gy | 3.02 kGy
 | DoseNIEL |  | 4.3 Gy | 0.83 Gy
 | DoseTOTAL | 20 kGy | 100 Gy | 3.6 kGy
 | DoseNIEL |  | 5 Gy | 1 Gy
NPN
PNP
All the values were transformed into absorbed doses

## Slide 30: Results comparison
Two orders of magnitude difference in total absorbed dose for conventional protons and laser-driven protons
Similar energy ranges
Approximately the same amount of protons
A significant distinction lies in the total irradiation time: Conventional: pulse length 400 s to deliver 1011 protons
Laser-driven: pulse length 6 s to deliver 1011 protons
Therefore laser-driven protons require two order of magnitude less time to deliver the same amount of protons.
Gamma radiation highest required absorbed dose
Neutrons DoseNIEL contribution to DoseTOTAL is the largest in percentage -> lower DoseTOTAL required
Conventional protons require two orders of magnitude higher than neutrons for similar effects
Laser-driven protons lowest required dose
 |  | Gamma | Neutrons | Conventional protons | Laser-driven protons
 | DoseTOTAL | 8 kGy | 62.5 Gy | 2.05 kGy | 13.6 Gy
 | DoseNIEL | 0.06 Gy | 3.0 Gy | 0.46 Gy | 0.01 Gy
 | DoseTOTAL | 7 kGy | 43.8 Gy | 1.37 kGy | 10.2 Gy
 | DoseNIEL | 0.06 Gy | 2.1 Gy | 0.31 Gy | 0.01 Gy
 | DoseTOTAL | 3 kGy | 31.3 Gy | 856 Gy | 6.8 Gy
 | DoseNIEL | 0.02 Gy | 1.5 Gy | 0.24 Gy | 5.0 10-3 Gy
 | DoseTOTAL | 600 Gy | 25 Gy | 685 Gy | 6.8 Gy
 | DoseNIEL | 5.0 10-3 Gy | 1.2 Gy | 0.14 Gy | 5.0 10-3 Gy
 |  | Gamma | Neutrons | Conventional protons | Laser-driven protons
 | DoseTOTAL | 8 kGy | 62.5 Gy | 2.05 kGy | 13.6 Gy
 | DoseNIEL | 0.06 Gy | 3.0 Gy | 0.46 Gy | 0.01 Gy
 | DoseTOTAL | 7 kGy | 43.8 Gy | 1.37 kGy | 10.2 Gy
 | DoseNIEL | 0.06 Gy | 2.1 Gy | 0.31 Gy | 0.01 Gy
 | DoseTOTAL | 3 kGy | 31.3 Gy | 856 Gy | 6.8 Gy
 | DoseNIEL | 0.02 Gy | 1.5 Gy | 0.24 Gy | 
 | DoseTOTAL | 600 Gy | 25 Gy | 685 Gy | 6.8 Gy
 | DoseNIEL |  | 1.2 Gy | 0.14 Gy | 
NPN
Different kind of damage induced by ionizing and non-ionizing dose.

## Slide 31: Conclusion
In this work, the effects of conventional and innovative radiation sources on electronics were compared to validate innovative sources for stress testing and to propose alternative, advantageous methodologies.
Gamma radiation, neutrons, conventional protons and laser-driven protons require different dose levels (ionizing and NIEL dose) to cause the same damage:
  Gamma radiation requires the highest total absorbed dose (DoseTOTAL 106 DoseNIEL);
  Neutrons have the largest NIEL dose contribution to the total dose leading to a lower required dose (DoseTOTAL 10 DoseNIEL);
  Conventional protons require a dose two orders of magnitude higher than neutrons to achieve similar effects (DoseTOTAL 103 DoseNIEL);
  Laser driven protons require the lowest dose (DoseTOTAL 103 DoseNIEL).
Conventional protons require a dose two orders of magnitude higher than laser-driven protons to induce similar damage. This effect lies in the time needed to deliver the same amount of protons:
  Laser-driven protons can induce intense damage within an extremely short timeframe making them a promising tool for stress testing.

## Slide 32
Part 3

## Slide 33: Calliope and REX dosimetric intercalibration
ESR alanine spectrum
Dosimetric systems
Fricke solution (primary dosimeter)
Alanine (secondary)
Alanine Electron Spin Resonance (ESR) dosimeters
REX
To identify suitable electron irradiation conditions for electronics, experimental dosimetric measurements were performed at the REX facility (ENEA Frascati R.C.)
The REX facility is based on a S band 5 MeV electron linac equipped with a removable beta-gamma conversion unit for secondary X-Ray emission.
Removable Electron to X-ray target
Alanine dosimeters were irradiated at different positions within the REX chamber.
40cm x 40cm x 80cm irradiation chamber
e-
Equation: y = A + Bx A: 0,021
B: 0,0037
Equation: y = A + Bx + Cx2 + Dx3
A: -12.36
B: 0,0092
C: -6.73· 10-7
D: 3.43 · 10-11
Low dose range calibration
High dose range calibration
Calliope

## Slide 34: Other activities
Optical spectroscopic analysis
Radiation resistance tests
Optical spectroscopic analysis
Reflectance measurements
Fluorescence measurements
Neutron and gamma radiation resistance tests
EPR analysis
FTIR/ATR analysis
UV-Vis measurements
Raman
Colorimetric
Viscosimetric
Scintillators studies (PbF2, LYSO)
Components for ITER detector
Cultural Heritage characterization

## Slide 35: Scientific production: papers and conferences
F. Addesa, M. Campana, A. Cemmi, I. Dafinei, I. Di Sarcina, B. D’Orsi et al, Optical spectroscopic characterization of LYSO crystals at the Calliope facility (ENEA Casaccia R.C.), RT/2020/15/ENEA. ISSN/2499-5347
A. Cemmi, I. Di Sarcina, B. D’Orsi et al, Radiation study of Lead Fluoride crystals, JINST 17 (2022) T05015. doi: 10.1088/1748-0221/17/05/t05015
F.M. Addesa, M. Campana, A. Cemmi, I. Dafinei, I. Di Sarcina, B. D’Orsi et al, Comparative characterization study of LYSO:Ce crystals for timing applications, JINST 17 (2022) 08028. doi: 10.1088/1748-0221/17/08/p08028
A. Cemmi, B. D’Orsi et al, Le radiazioni ionizzanti in ‘soccorso’ dei beni culturali, ENEA magazine 1/2022. doi: 10.12910/EAI2022-032
A. Cemmi, I. Di Sarcina, B. D’Orsi, Gamma radiation-induced effects on paper irradiated at absorbed doses common for cultural heritage preservation, Radiation Physics and Chemistry 202 (2023) 110452.
A. Cemmi, A. Cirigliano, I. Di Sarcina, B. D’Orsi et al, Calliope gamma irradiation facility for Cultural Heritage: the PERGAMO project challenges, ENEA - Ricerca, sviluppo e applicazioni per i Beni Culturali Dai risultati del progetto VADUS alle future collaborazioni, C.R. ENEA Frascati 9 - 10 May 2023
A. Cemmi, A. Cirigliano, I. Di Sarcina, B. D'Orsi et al, Gamma radiation effects on Cultural Heritage artifacts at Calliope facility (Enea Casaccia R.C. - Rome, Italy), Proceeding of AIES XIV International Conference, 2023
B. D’Orsi, R. Carcione, I. Di Sarcina, G. Ferrara, J. Scifo, A. Verna, A. Cemmi, Optimization of paper characterization procedures for cultural heritage, RT/2024/2/ENEA (2024).
B. D’Orsi et al, Gamma irradiation for Cultural Heritage conservation: comparison of the secondary effects on new and old paper, under review at Journal of Cultural Heritage (2024).
A. Cemmi, B. D’Orsi, E. Di Meco, I. Di Sarcina et al, The CRILIN calorimeter: gamma radiation resistance of crystals and SiPMs, Accepted for publication in JINST (2024).

## Slide 36
Thank you for your attention!
beatrice.dorsi@inrs.ca
beatrice.dorsi@uniroma1.it
CALLIOPE

## Slide 37
Backup slides

## Slide 38: Calliope gamma irradiation facility at the ENEA Casaccia R.C. (Rome, Italy)
Pool-type irradiation facility equipped with a 60Co gamma source in a large volume (763.9 m3) shielded cell. Dosimetric and characterization laboratories are available.
Cherenkov effect around the 25 source rods in the plane rack (activity of around 70 kCi)
Maximum available dose rate (April 2024): 6.2 kGy/h
Irradiation tests at different dose rates, atmospheric and temperature conditions and under bias.
Simulation of the gamma field by Fluka/MCNP code (irradiation cell and irradiated samples).
Online tests and remote acquisition.
ISO 9001 – ISO 17025 (by 2024)
Activities (research & qualification):
Space, Nuclear, High Energy Physics, environment, radiobiology, Cultural Heritage, agrifood, medicine…
https://www.enea.it/it/seguici/pubblicazioni/pdf-opuscoli/calliope.pdf
Maximum allowed activity: 3.7x1015 Bq (100 kCi)
Mean energy: 1.25 MeV

## Slide 39: Frascati Neutron Generator at the ENEA Frascati R.C. (Frascati, Italy)
The Frascati Neutron Generator (FNG) is a medium intensity neutron source housed in a large shielded cell (11.5129 m3).
It consists of a linear electrostatic accelerator of D+ ions up to 270 keV and 1 mA.
Research activities:
Benchmark experiments, detector calibration, detector development, Space, Nuclear, Biology, High Energy Physics, environment…
Target | Neutron energy | Maximum neutron flux
Tritiated | 14 MeV (T(d,n)4He) | 5 ּּ 109 n/cm2/s
Deuterated | 2.45 MeV (D(d,n)3He) | 5 ּּ 107 n/cm2/s
Simulation of the neutronic field by MCNP code
Test with high flux, on bias and online data acquisition from the Control Room
M. Martone, M. Angelone, M. Pillon, The 14 MeV Frascati Neutron Generator (FNG), Journal of nuclear materials, Volume 212-215 Part II, pp. 1661-1664 (1994)

## Slide 40: TOP IMPLART at the ENEA Frascati R.C. (Frascati, Italy)
Intensity Modulated Proton Linear Accelerator for Radiotherapy TOP IMPLART Technology demonstrator of a pulsed, fully linear machine for proton therapy developed at ENEA Frascati Research Centre in collaboration with the Italian Institute of Health (ISS) and the Oncological Hospital Regina Elena-IFO.
C. Ronsivalle, M. Carpanese, C. Marino, G. Messina, L. Picardi, et al. The TOP-IMPLART project. The European Physical Journal Plus, Volume 126, pp. 1–15 (2011)
Beam Energy | 1-6 MeV
Energy spread | 0.2 MeV
Pulse duration | 15-60 µs
Repetition rate | 25 Hz
Typical beam spot | 16 mm
protons
Research activities:
Radiobiology, Space, Dosimetric characterization of proton pulsed beams, High Energy Physics…
Beam Energy | 71 MeV
Energy spread | 0.6 MeV
Pulse duration | 2.5 µs
Repetition rate | 25 Hz
Beam size at SCDTL exit | <3 mm
Horizontal line (high energy)
Vertical line (low energy)
Notes: It comprises a commercial injector, by ACCSYS-Hitachi, and 8 Side Coupled DTL structures (SCDTL), patented by ENEA, accelerating the proton beam to a maximum energy of 71 MeV and maximum intensities of 4.5 108 protons per pulse.
The TOP-IMPLART (Oncological Therapy with Protons - Intensity Modulated
Proton Linear Accelerator for Therapy) facility at the ENEA Frascati Research Center
is equipped with a multipurpose Radio Frequency (RF) proton linear accelerator,
developed by ENEA in collaboration with the Italian National Institute of Health
(ISS) and the Regina Elena National Cancer Institute (IFO) of Rome [127, 128]. It
was designed for proton therapy applications, it boasts features that enable precise
control of the intensity and energy released from pulse to pulse.
Situated within a bunker measuring 27 meters in length and 3 meters in width, the
TOP-IMPLART facility is depicted in Figure 3.16.
The TOP-IMPLART linac consists of a 7 MeV commercial injector (Duoplasmatron
Source, Radio Frequency Quadrupole (RFQ), and Drift Tube Linac (DTL)) produced
by ACCSYS-Hitachi (PL7 model) operating at 425 MHz, and a high-frequency linear segment is composed of Side Coupled Drift Tube Linac (SCDTL) structures up to
71 MeV.
Exiting the injector, there is a low-energy vertical extraction line with an energy
range of 1 to 6 MeV. The minimum energy is obtained by powering only the RFQ
and transporting the beam through the DTL. Intermediate energies (1 to 6 MeV) are
achieved by varying the relative phase and/or the input RF power level of the DTL.
These energies are selected using a 90° dipole magnet that acts as a spectrometer.
The effective energy on a target placed outside the 50 μm Kapton window is in the
1 to 6 MeV range. The beam spot size is 16 mm in diameter with a homogeneity of
The resultant beam, characterized by an energy spread (FWHM of the Gaussian
energy distribution) of 600 keV, is bunched into pulses lasting 2.5 μs, each containing
approximately 3 ・ 108 protons, operating at a repetition frequency of 25 Hz. The
number of pulses can be selected based on the desired proton fluence. The beam spot
diameter is less than 3 mm at the exit of the last SCDTL structure, but it increases
to 17 mm FWHM at the end of the beam high energy transport line. Utilizing a
pair of X-Y scanning magnets, it becomes feasible to irradiate samples over an area
of up to 10 x 10 cm2 at a nominal target distance of 2.60 m from the linac exit. The
homogeneity on the target is a function of the spot mesh resolution: the higher the
number of spots, the higher the homogeneity. The main parameters of the horizontal
and vertical extraction lines of the TOP-IMPLART accelerator are summarized in
Table 3.2 and Table 3.3, respectively.

## Slide 41: ALLS facility at INRS-EMT (Varennes, Québec, Canada)
At the Institut National de la Recherche Scientifique in Québec (Canada), laser-accelerated protons with a broad energy spectrum are available at the ALLS (Advanced Laser Light Source) laboratory.
https://alls.inrs.ca/beamlines-endstations
Laser beam peak power | 750 TW
Central wavelength | 800 nm
Pulse repetition rate | 2.5 Hz (5 shots each 2 seconds)
Energy per pulse | Up to 13 J
Pulse duration | 17 fs
Beam diameter | 170 mm
Picosecond contrast | 
Laser beam peak power | 750 TW
Central wavelength | 800 nm
Pulse repetition rate | 2.5 Hz (5 shots each 2 seconds)
Energy per pulse | Up to 13 J
Pulse duration | 17 fs
Beam diameter | 170 mm
Picosecond contrast | 
Titanium-Sapphire laser
The most powerful available in Canada
Boule rouge: multiple target holder (800 targets that can be shot automatically), proton source, optics, samples
Thomson Parabola with a MicroChannel Plate (allows high repetition-rate shots) as ion detector.
Mini-chamber e.g. for laser-PIXE experiments.
Proton axis
Notes: The beam has a peak power of 750 TW and can be focused on targets with an extremely high-field intensity. In such conditions, the laser-matter interactions lead to the generation of secondary sources. The ion acceleration beamline (laser-irradiation of solid targets via the Target Normal Sheath Acceleration mechanism) features a multiple target holder with 800 targets that can be shot automatically. The 100 mm-wide laser beam is focused down to an intensity of 1.3 x 1020 W/cm2. The main ion detector is a Thomson Parabola with a MicroChannel Plate that enables high repetition-rate shots. On the proton axis, a mini-chamber allows experiments interacting with the protons, e.g. for laser-PIXE experiments.

## Slide 42: ALLS facility at INRS-EMT : TNSA mechanism and proton spectrum
Laser beam is focused down to an intensity of 1.3x1020 W/cm2
Ion acceleration
Target Normal Sheath Acceleration
(TNSA) mechanism
Preplasma creation at the front side of the target
Main high-intensity laser pulse interaction with the plasma
Hot electrons acceleration and propagation through the target
Dense sheath generation at the rear side of the target
Electric field creation
Ionization of target rear surface and ions acceleration
Thin target irradiation by an intense laser pulse:
Routinely available proton spectrum at ALLS
M. Roth and M. Schollmeier. IonAcceleration – Target Normal Sheath Acceleration. In CAS - CERN Accelerator School: Plasma Wake Acceleration, pages 231–271, Geneva, 2016.CERN.
Notes: When a Thin target irradiated by an intense laser pulse, a preplasma is created at the front side of the target by the laser prepulse. Thus, the main high-intensity laser pulse interacts with the plasma and accelerates hot electrons, mainly in the forward direction. The electrons propagate through the target.
When the electrons leave the target, generate a dense sheath at its rear side and, as a results of the charge separation, an electric field is created.

## Slide 43: REX facility Electron linac and X-ray
The REX test facility is based on a S band 5 MeV electron linac equipped with a removable beta-gamma conversion unit for secondary X-Ray emission.
Vadrucci, M., Borgognoni, F., Campani, L., Ferrari, P. (2019) doi: 10.1016/j.nima.2019.02.066.
Activities (research & qualification):
Space components, life science, structural defects of crystals and minerals, polymers treatment, controlled damage of materials for nuclear fusion, microbiology of biodeteriogens, cultural heritage…
Removable Electron to X-ray target
Electron linac and X-ray production
40cm x 40cm x 80cm irradiation chamber

## Slide 44: REX facility Main parameters and dosimetric systems
Alanine-EPR
dosimeters
Pulse length | 3 µs
Pulse current (max) | 150 mA
Electrons per pulse (max) | 2.95 ·1012
Pulse Repetition Frequency (max) | 20 Hz
Average current (max) | 9 µA
Electrons per second (max) | 5.6·1013
Dosimetric systems
Radiochromic
films
HD-V2 gafchromic for electrons spectrum measurements
REX
main
parameters
Linac extraction point
Markus
ionization
chamber
Energy (MeV)
Spectrum (MeV-1)

## Slide 45: Alanine dosimeter
Alanine powder substrate pressed into pellet shape.
The irradiation of alanine amino acid () induces the formation of free radicals.
Practice for use of the alanine-EPR dosimetry system ISO/ASTM 51607:2012(E)
4 mm
EPR Bruker e-scan spectrometer: X-band frequency of 9.4 GHz microwave power of 0.14 mW magnetic field in the range 3350–3650 G
Magnetic Field (G)
Intensity (a.u.)
Alanine EPR spectrum

## Slide 46: CALLIOPE facility - alanine dosimeters calibration
By using the absolute Fricke dosimeter, calibration curves for the alanine dosimetry system were obtained:
Equation: y = A + Bx A: 0.021 ± 0.023
B: (3.72 ± 0.04) · 10-3
Equation: y = A + Bx + Cx2 + Dx3
A: -12.4 ± 7.0
B: (9.3 ± 3.1) · 10-3
C: (-6.7 ± 3.8) · 10-7
D: (3.4 ± 1.3) · 10-11
Magnetic Field (G)
Intensity (a.u.)
Gamma radiation
High dose range calibration
Low dose range calibration

## Slide 47: REX - alanine irradiation
Distance (cm)
20
30
40
Irradiation setup
Alanine holder
20 cm
1 cm
Alanine dosimeters were irradiated under different conditions.
Pulse Repetition Frequency (PRF):
15 Hz
5 MeV electrons
e-

## Slide 48: REX beam characterization
EPR spectrum acquisition after irradiation
The value /m (mg-1) is reported in the calibration curve made at Calliope to get an equivalent dose (kGy)
Distance (cm) | hpp/m (mg-1) | Absorbed dose (Gy) | Irradiation time (s) | Dose rate (Gy/s)
20 | 4235 | 17436 | 45 | 387.5
30 | 2545 | 9488.1 | 60 | 158.1
40 | 2402 | 8958.6 | 90 | 99.54
Distance (cm) | hpp/m (mg-1) | Absorbed dose (Gy) | Irradiation time (s) | Dose rate (Gy/s)
20 | 4235 | 17436 |  | 387.5
30 | 2545 | 9488.1 |  | 158.1
40 | 2402 | 8958.6 |  | 99.54
Dose per pulse at centre (Gy/pulse)
25.8
10.5
6.6
17.4 kGy
4235 mg-1
2545 mg-1
9.49 kGy
8.96 kGy
2402 mg-1
Low dose range calibration curve
High dose range calibration curve

## Slide 49: REX – gafchromic film vs alanine
A comparison between gafchromic film HD-V2 (measured data in the plots) and alanine measurements was performed.
d = 30 cm
d = 40 cm

## Slide 50
Typical radiation effects on opto-isolators
Opto-isolator component | Main degradation mechanism
LED | DD
Phototransistor | TID, DD
Coupling medium | TID
An opto-isolator consists in a LED optically coupled to a phototransistor.
Radiation effects on opto-isolator are mainly due to:
Light Output (HIGH)
Light Output (LOW)
Non radiative recombination
Non radiative recombination
centres
Radiative recombination (LOW)
Space charge zone
Radiative recombination
Space charge zone
Mukherjee, Bhaskar & Simrock, Stefan, Application of low cost GaAs LED as neutron kerma dosimeter and fluence monitor at FLASH (2007)
Reed, Robert., Guideline for Ground Radiation Testing and Using Optocouplers in the Space Radiation Environment (2007)
A. Cemmi et al, Optical characterization and irradiation tests at ENEA Calliope lab, 17th B2GM ECL meeting (2014)
Notes: LEDs produce light by means of radiative recombination of injected minority charge carriers with majority carriers in the depletion region. As such, any damage that decreases the efficiency of radiative recombination or introduces competing processes will degrade device performance. Irradiation by heavy particles such as protons and neutrons can displace nuclei from the crystalline lattice, causing DDD. These defects can serve as sites for nonradiative recombination, decreasing the efficiency of the light source

## Slide 51: Radiation tolerant opto-isolators: gamma irradiation tests and measurements - 1
Irradiation tests according to ESCC Basic Specification No. 22900 (Issue 5):
Irradiation at room temperature and parametric tests after each step of irradiation
Annealing followed by parametric tests:
-24 hours at room temperature
-168 hours at 100 °C
Three samples (optoisolators OLS249)
Different steps of irradiation up to 300 Gy(Si) absorbed dose
Dose rate = 3.3 Gy(Si)/h
Radiation-tolerant
1
6
5
3
4
LED
PHOTOTRANSISTOR
2 cm
Irradiation step | Absorbed dose per step (Gy) | Total absorbed dose (Gy)
1 | 56.7 | 56.7
2 | 74.3 | 131.0
3 | 19.1 | 150.1
4 | 68.6 | 218.7
5 | 74.6 | 293.3
All samples were biased
during irradiation.
Skyworks. TECHNICAL DATASHEET - OLS249: Radiation-Tolerant Phototransistor Hermetic Surface-Mount Optocoupler.
Notes: Chiedi foto irraggiamento
Anche nelle missioni unbiased e biased perché se un componente è spento è unbiased
Controlla carattere titolo e aggiungi box con radiation tolerant
Optoelectronic components are the most sensitive devices of systems exposed to radiation environments

## Slide 52: Radiation tolerant opto-isolators: gamma irradiation tests and measurements - 2
C
E
B
To evaluate the radiation effect, the voltage, defined as the when the transistor is in saturation mode, i.e. is maximum and does not depend on , was measured.
(V)
Opto-isolators
The value of increased after each step of irradiation.
LED
PHOTOTRANSISTOR
Datasheet
SLIGHTLY damaged
Leakage currents (Current that flows when the device is in off state)
() ()
Breakdown voltages (Threshold voltage at which breakdown occurs)
(collector to emitter breakdown voltage)
(collector to base breakdown voltage)
Other measured parameters:
No modifications
Notes: Prima di iniziare l’irraggiamento sono state effettuate le misure di alcuni parametri caratteristici del componente elettronico. Tali misure sono state ripetute dopo ogni step di irraggiamento per valutare l’andamento dei parametri.
Quando il transistor è in saturazione la Vcesat è definite come la differenza tra la tensione di collettore e quella di emettitore per una specifica corrente di collettore (massima)
, it is defined as the collector to emitter voltage when the transistor is in saturation mode, i.e. is maximum and does not depend on .
Prima di iniziare l’irraggiamento sono state effettuate le misure di alcuni parametri caratteristici del componente elettronico. Tali misure sono state ripetute dopo ogni step di irraggiamento per valutare l’andamento dei parametri.
Quando il transistor è in saturazione la Vcesat è definite come la differenza tra la tensione di collettore e quella di emettitore per una specifica corrente di collettore (massima)
, it is defined as the collector to emitter voltage 𝑉_𝐶𝐸 when the transistor is in saturation mode, i.e. 𝐼_𝐶 is maximum and does not depend on 𝐼_𝐵.

## Slide 53: Radiation tolerant opto-isolators: gamma irradiation tests and measurements - 3
End of irradiation
Annealing step at room temperature
Parametric test
Annealing step at 100 °C (biased)
Parametric test
End of test
All samples recovered the original value of after the second step of annealing.
(V)
End of irradiation
Annealing tests
24 h at room temperature + 168 h at 100 °C
After the last irradiation step
24 h at room temperature
Notes: VCEsat viene impostata una corrente I_F vengono polarizzati diodo con 30mA e Ic 1mA in uscita VCE
tensiona di polarizz della giunzione CE e questa tensione si abbassa fino ad un certo punto e questo deve stare sotto un certo valore
Il valore della dose dipende dall’orbita della missione, a seconda dell’altezza il campione è più sensibile ad una certa radiazione e ad una determinate energia (dipende dall’orbita del satellite)