## Slide 1
Radboud University Nijmegen, the Netherlands
Inge van Rens
21 November 2024
Quantum Hall effect in hydrogenated graphene

## Slide 2: Why?
Understanding graphene and the effect of hydrogen on the system
  If we know the band structure, we can predict behaviour
Low resistivity to limit potential differences
  Influenced by temperature, magnetic field and doping
  Fully hydrogenated graphene is an insulator

## Slide 3: Why & how?
Understanding graphene and the effect of hydrogen on the system
  If we know the band structure, we can predict behaviour
Low resistivity to limit potential differences
  Influenced by temperature, magnetic field and doping
  Fully hydrogenated graphene is an insulator
Temperature dependence
Magnetic field effects
Band structure simulations

## Slide 4: Graphene Field Effect Transistor
SiO2
gate insulator
Si backgate
Au contacts
graphene
Graphenea, GFET-S10 data sheet
Geim, A. K. & Novoselov, K. S. The rise of graphene. In Nanoscience and technology: a collection of reviews from nature journals, 11–19 (World Scientific, 2010)

## Slide 5: Hydrogenation process
Start with annealed sample
Exposed 1 mbar hydrogen plasma for 5 minutes
Exposed to air for 10 minutes
Repeat until we reach the wanted state
Notes: Hydrogenated both samples, meanwhile cooling them with liquid nitrogen to check when the band gap starts to open -> 80s for first sample, 25 min for second

## Slide 6: Temperature dependence
Peak resistance increased as temperature decreased
Pristine state: no temperature dependence
From vrh fit: band gap 2.1±0.4K

## Slide 7: Temperature dependence
Neutrality point shifted
Temperature dependence similar
From vrh fit: band gap 2.6±1.1K

## Slide 8: Temperature dependence
Compare samples g12 and g3
Similar band gap opening
Band gap is far smaller than for a fully hydrogenated graphene sample (Elias et al., Science 323, 610-613 (2009))

## Slide 9: Magnetic field effects
A. J. M. Giesbers, U. Zeitler, M. I. Katsnelson, L. A. Ponomarenko, T. M. Mohiuddin, and J. C. Maan, Quantum-Hall Activation Gaps in Graphene. In PRL 99, 206803 (2007)
Notes: At nu -2: only localised states -> no charge carriers -> no potential difference? Check with Uli

## Slide 10: Quantum Hall Effect
𝜈=-2
𝜈=+2

## Slide 11: Quantum Hall Effect
𝜈=-2
𝜈=-6

## Slide 12: Activation energy
Notes: Pristine graphene: activation sqrt in B
Hydrogenated becomes linear due to curved band structure

## Slide 13: Activation energy
Activation gap depends on Landau level broadening and peak-to-peak distance
Effective electron mass can be extracted from the slope of the activation gap
25 minutes of plasma exposure, filling factor -2:
30 minutes of plasma exposure, filling factor -2:
For pristine graphene, Δ∝

## Slide 14: Simulations
Pristine graphene
12.5% H coverage

## Slide 15: Simulations
Pristine graphene
25% H coverage

## Slide 16: Simulations
Pristine graphene
50% H coverage

## Slide 17: Implications for PTOLEMY
H-graphene resistance depends on temperature, magnetic field, electric field, doping and coverage
A small electric field at the target might help reduce the resistance, and the risk of potential differences on the surface, significantly
We might be able to reduce the resistance by doping the sample or applying a electric field

## Slide 18: Implications for PTOLEMY
H-graphene resistance depends on temperature, magnetic field, electric field, doping and coverage
A small electric field at the target might help reduce the resistance, and the risk of potential differences on the surface, significantly
We might be able to reduce the resistance by doping the sample or applying a electric field
Contact with KIT for tritium measurements

## Slide 19
Backup slides

## Slide 21: Quantum hall resistance
Only localised states:
  finite

## Slide 22: The Nijmegen Group
Uli Zeitler
(RU HFML-FELIX)
Nicolo de Groot
(RU IMAPP)
Oleksandr Zheliuk
(RU HFML-FELIX)
Nicoleta Cucu-Laurenciu
(RU IMAPP)
Inge van Rens
(RU IMAPP)
Martijn Velders
(RU IMAPP)
Bram Breugelmans
(RU HFML-FELIX)
Thomas Derks
(RU HFML-FELIX)
And our students:

## Slide 23: Temperature dependence

## Slide 24: Temperature dependence

## Slide 25: Quantum Hall effect

## Slide 26: Quantum Hall effect

## Slide 27: Transfer curves after hydrogenation

## Slide 28: Compare simulations to hydrogenation results

## Slide 29: H exposure

## Slide 30: H exposure

## Slide 31: H exposure
Hydrogen exposure may increase or decrease resistance