## Slide 1: Results of 100 mm thin BULLKID detectors
15/01/2025
Giovanni Luca Pesce

## Slide 2: Scale-Up
5 mm Si Thickness
72,6 mm Diameter
60 Pixels
20 g of active mass
5 mm Si Thickness
100 mm Diameter
145 Pixels
50 g of active mass

## Slide 3: 100 mm thin detectors
Features:
  100 mm diameter
  300 thick
Why use them?
  For electrical tests to evaluate the performance of newly lithographed KID designs
Industrial Production
  Easy to obtain and test

## Slide 4: MKID Components
CoPlanar Waveguide (CPW)
Inductive Meander
Guard Ring
Interdigitated Capacitors
Feedline
Ground Plane

## Slide 5: Single Pixel Design Edits

## Slide 6
1) Larger Feedline (: lower risk of interruptions
2) No narrowing of the CPW: avoid impedance mismatch
3) Thinner guard ring (reduction of passive metal
More sensitive area ( : improve phonon collection
Current Design
New Design

## Slide 7
5) Centering in the voxel: remove position effects
Current Design
New Design

## Slide 8: Matrix-level Edits

## Slide 9
EM Cross-Talk
Definition
  Crosstalk refers to the unintended electromagnetic interaction between nearby KIDs, where the excitation of one resonator affects the response of another.
Causes
  Physical and frequency proximity among resonators
Consequences
  Signal interference in the readout
KID 1
KID 2
KID 3
KID 4

## Slide 10
Pixel Randomization Algorithm
Trying to mitigate this phenomenon an algorithm has been developed
Goal:
  Maximize the pysical distance between frequency adjacent pixels within the array
With a base frequency step of 1,5 MHz between consecutive resonances, this configuration ensures a minimum spacing of 27 MHz between adjacent KIDs
10

## Slide 11: Experimental Results on Fabricated Devices

## Slide 12: BULLKID RM-00 07 24
Features:
All detectors implement the new design
Pixel distribution follows the randomization scheme
Goals:
To evaluate Quality Factors distributions
To perform temperature and power scans
12

## Slide 13
  133 out of 145 resonances detected
  Issue: Quality Factors higher than expected
Median | 7.2e+05 | 2.5e+06 | 1.3e+06
Median | 7.2e+05 | 2.5e+06 | 1.3e+06
Simulation
Internal losses
Coupling losses
Notes: Aggiungere nota sul Qc

## Slide 14
Simulation granularity not precise enough to properly simulate a distance of just
Evaluate the signal-to-noise ratio (SNR) across KIDs with different quality factors
New Goal
Data collected from 11 pixels:
All at their Optimum Power (to minimize noise from amplifiers)
ranging from 300k to 1M

## Slide 15: SNR Vs Q
SNR remains constant : no significant improvements but also no noticeable degradation
Quality Factor’s target can be slightly shifted above the current 150k benchmark value
Higher Q Less Drive Power

## Slide 16: BULLKID RM-01 07 24
Features:
Three variants of the new design implemented within the same array
Goals:
Temperature scan to evaluate across the 3 variants
Temperature scan to evaluate 𝛼=𝐿_𝑘/(𝐿_𝑘+𝐿_𝑔 ) across the 3 variants
Analyze noise features across the 3 variants
Goals:

## Slide 17: Differences on the 3 variants
8
4
20/12
20/8
20/4

## Slide 18: Expectations
20/12
20/8
20/4
more compact meanders reduce -> increase of
Noise: ?

## Slide 19
20/12
45 out of 50
20/8
49 out of 50
20/4
29 out of 45

## Slide 20: Evaluation
20/12
20/8
20/4
  Increment T step by step, perform VNA acquisition and calculate
  Fit the scatter plot with the equation shown in the plot to extract
 | 20/12 | 20/8 | 20/4
Median | 0,0461 | 0,0473 | 0,0523
 | 20/12 | 20/8 | 20/4
Median | 0,0461 | 0,0473 | 0,0523
(Mattis-Bardeen)

## Slide 21: Noise Features Analysis
The Noise Power Spectrum (NPS) was analyzed across pixels from the 3 subsets at their Optimum Power
NPS in terms of frequency shift variable:
  Remove Q dependency
The more compact is the meander, the higher is the noise level exhibited
Main source: TLS
Notes: The advantage of using the frequency shift is that it uniforms the responsivity of the KIDs, meaning that comparing the NPSDs is the same as comparing the noise to signal ratio.
Cambia legenda levando da run a pow e cambia la k con px e metti in grassett 4/8/12 (ovunque).

## Slide 22: Next KID’s generation
Wider meanders in future KIDs could reduce noise
20/12 configuration seems to be promising with respect to the current 20/8 (minimal impact on reduction; less noise)
Further works could validate these results and exploring new design optimization
 | 20/12 | 20/8 | 20/4
Median | 0,0461 | 0,0473 | 0,0523
 | 20/12 | 20/8 | 20/4
Median | 0,0461 | 0,0473 | 0,0523
Current configuration
Notes: Segna configurazione attuale

## Slide 23: Thanks for your attention
Giovanni Luca Pesce, MSc
Università di Roma la Sapienza
INFN-Roma1

## Slide 24: Backup

## Slide 25: Quality Factors
: Combination between losses due to quasi-particles and other internal mechanism losses ( metal film quality, substrate losses, radiation ecc. )
: energy loss due to coupling mechanisms. It measures the efficiency of energy transfer to or from the resonator
Higher values indicating a weaker coupling and lower energy loss through external connections

## Slide 26: Noise Sources in MKIDs
3 main noise sources:
Generation-Recombination Noise
Two Level System Noise
Readout Noise

## Slide 27: TLS Noise
Electrical fluctuations between the ground and an excited state at the surface of the substrate.
These fluctuations cause instabilities in the dielectric constant of the substrate material

## Slide 28: Alpha
In the simulation context is possible to estimate extracting the resonant frequency in the condition of

## Slide 29: Phase Response Vs Frequency Response
A direct measurable quantity from deposited energy
Non-linear behavior with respect to energy
Q dependent
energy conversion efficiency
: Kinetic/Total inductance
: Complex response (releated to )
: Quality factor
: Density of states at Fermi level
: Inductor volume
: Superconductive gap
Reconstructed indirectly from variations in the magnitude and phase of the resonator’s complex response
Q independent

## Slide 30: SNR Evaluation
Data collected from 11 pixels at their Optimum Power with a ranging from 300k to 1M, covering the main dispersion band
From the fit of each resonance onto IQ plane it’s possible to estimate the proportianal constant between and (WP)
WP represents the point of maximum responsivity of the KID
Constant term
Dependent on detector’s parameters

## Slide 31: Cross-Talk Simulation Analysis
A repetead simulation analysis has been performed with 2 KIDs spaced 6 mm apart (BULLKID config.)
At each simulation step the capacitance of one KID was varied by varying the lenght of one of the finger capacitors; instead the other one was left always unchanged

## Slide 32: SNR of BULLKID RM-01 07 24
Worst cases:
Average Pulse Fitted:

## Slide 33
RMS of original noise: 3.02 mrad
RMS of filtered noise: 1,30 mrad
RMS of original noise: 3.02 mrad
RMS of filtered noise: 1,38 mrad
Original Average Pulse
Fitted Average Pulse
6 %

## Slide 34
RMS of original noise: 5.22 mrad
RMS of filtered noise: 2.87 mrad
RMS of original noise: 5.22 mrad
RMS of filtered noise: 3,20 mrad
Original Average Pulse
Fitted Average Pulse
11 %

## Slide 35: SNR of BULLKID RM-01 07 24
Data normalized wrt of each variant of KIDs

## Slide 36: NPS similar Q