## Slide 1: Design of next-generation LGADs with TCAD tools
A. Fondacci, A. R. Altamura, R. Arcidiacono, A. Bisht, M. Boscardin, N. Cartiglia, M. Centis Vignali, T. Croci, M. Ferrero, L. Lanteri, L. Menzio, A. Morozzi, F. Moscatelli, D. Passeri, G. Paternoster, F. Siviero, V. Sola, R. S. White
Fourth INFN Workshop on Future Detectors, Sestri Levante, Italy

## Slide 2: Technology Computer Aided Design (TCAD)
DEVICE
SIMULATION
&
1
Geometry definition
Microscopic information (carrier density, electric field,…)
Macroscopic information (current, capacitance,…)
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025

## Slide 3: Technology Computer Aided Design (TCAD)
1
Acceptor Removal
Acceptor Creation
If
else
NEW UNIVERSITY OF PERUGIA RADIATION DAMAGE MODEL
DEVICE
SIMULATION
&
Geometry definition
Microscopic information (carrier density, electric field,…)
Macroscopic information (current, capacitance,…)
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025
A. Morozzi et al., PoS Vertex2019 (2020) 050
M. Ferrero et al., CRC Press (2021)

## Slide 4: Technology Computer Aided Design (TCAD)
1
Acceptor Removal
Acceptor Creation
If
else
NEW UNIVERSITY OF PERUGIA RADIATION DAMAGE MODEL
DEVICE
SIMULATION
&
Geometry definition
Microscopic information (carrier density, electric field,…)
Macroscopic information (current, capacitance,…)
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025
A. Morozzi et al., PoS Vertex2019 (2020) 050
M. Ferrero et al., CRC Press (2021)

## Slide 5: Technology Computer Aided Design (TCAD)
1
Acceptor Removal
Acceptor Creation
If
else
NEW UNIVERSITY OF PERUGIA RADIATION DAMAGE MODEL
DEVICE
SIMULATION
&
Geometry definition
Microscopic information (carrier density, electric field,…)
Macroscopic information (current, capacitance,…)
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025
A. Morozzi et al., PoS Vertex2019 (2020) 050
M. Ferrero et al., CRC Press (2021)

## Slide 6: Technology Computer Aided Design (TCAD)
1
Acceptor Removal
Acceptor Creation
If
else
NEW UNIVERSITY OF PERUGIA RADIATION DAMAGE MODEL
DEVICE
SIMULATION
&
Geometry definition
Microscopic information (carrier density, electric field,…)
Macroscopic information (current, capacitance,…)
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025
A. Morozzi et al., PoS Vertex2019 (2020) 050
M. Ferrero et al., CRC Press (2021)

## Slide 7: DC-coupled Resistive Silicon Detectors (DC-RSD)
2
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025

## Slide 8: DC-coupled Resistive Silicon Detectors (DC-RSD)
2
IMPORTANCE OF THE CONTACT RESISTANCE
MIP
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025

## Slide 9: DC-coupled Resistive Silicon Detectors (DC-RSD)
2
IMPORTANCE OF THE CONTACT RESISTANCE
CONFINEMENT WITH SiO2 TRENCHES
MIP
MIP
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025

## Slide 10: DC-coupled Resistive Silicon Detectors (DC-RSD)
2
IMPORTANCE OF THE CONTACT RESISTANCE
CONFINEMENT WITH SiO2 TRENCHES
CONFINEMENT WITH RESISTIVE STRIPS
MIP
MIP
MIP
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025

## Slide 11: DC-coupled Resistive Silicon Detectors (DC-RSD)
2
IMPORTANCE OF THE CONTACT RESISTANCE
CONFINEMENT WITH SiO2 TRENCHES
CONFINEMENT WITH RESISTIVE STRIPS
MIP
MIP
MIP
Simulations guided the design of FBK's first DC-RSD batch, released in late 2024
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025

## Slide 12: DC-coupled Resistive Silicon Detectors (DC-RSD)
2
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025

## Slide 13: DC-coupled Resistive Silicon Detectors (DC-RSD)
2
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025

## Slide 14: DC-coupled Resistive Silicon Detectors (DC-RSD)
2
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025

## Slide 15: Compensated LGADs
3
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025

## Slide 16: Compensated LGADs
3
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025

## Slide 17: Compensated LGADs
3
C-V CHARACTERISTICS
Compensated gain implant doping profiles calibrated on a SIMS;
and is known;
and is changed until measurements agree.
Assuming the same dependence on the initial doping density and considering the different initial concentrations of implanted boron and phosphorus,
Carbon reduces acceptor removal to a level comparable to that seen in standard LGADs, even with the presence of phosphorus in the gain layer region.
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025

## Slide 18: Compensated LGADs
3
C-V CHARACTERISTICS
SHEET RESISTANCE (van der Pauw)
Compensated gain implant doping profiles calibrated on a SIMS;
and is known;
and is changed until measurements agree.
Assuming the same dependence on the initial doping density and considering the different initial concentrations of implanted boron and phosphorus,
Carbon reduces acceptor removal to a level comparable to that seen in standard LGADs, even with the presence of phosphorus in the gain layer region.
NPLUS
PGAIN W5
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025

## Slide 19: Compensated LGADs
3
C-V CHARACTERISTICS
SHEET RESISTANCE (van der Pauw)
Compensated gain implant doping profiles calibrated on a SIMS;
and is known;
and is changed until measurements agree.
Assuming the same dependence on the initial doping density and considering the different initial concentrations of implanted boron and phosphorus,
Carbon reduces acceptor removal to a level comparable to that seen in standard LGADs, even with the presence of phosphorus in the gain layer region.
NPLUS
PGAIN W5
Valuable information for designing the next Compensated LGAD batch
A. Fondacci et al.
Design of next-generation LGADs with TCAD tools
IFD 2025

## Slide 20: Thank you for your attention
A. Fondacci, A. R. Altamura, R. Arcidiacono, A. Bisht, M. Boscardin, N. Cartiglia, M. Centis Vignali, T. Croci, M. Ferrero, L. Lanteri, L. Menzio, A. Morozzi, F. Moscatelli, D. Passeri, G. Paternoster, F. Siviero, V. Sola, R. S. White
Fourth INFN Workshop on Future Detectors, Sestri Levante, Italy