## Slide 1: Metallic ion beam production and diagnostic with the CAPRICE ECRIS at GSI
Aleksandr Andreev
GSI Helmholtzzentrum für Schwerionenforschung GmbH
Aleksandr Andreev
PIBHI Workshop, Aci Trezza, Italy, 7-9.04.25

## Slide 2: Evaporation technique for metal ion beam production @ HLI
Standard Temperature Oven (STO)
Layout
Resistively heated by current running around the heater body, central current entry
Aperture ring if the material is liquid at the required vapor pressure (e.g. Fe, Ni)
Crucible (Ta or W) to avoid chemical reactions with the heater ceramic (for e.g. Mg, Ca, Li)
Operating parameters
Power: 2-120W
Temperature: 400 -1550°C
Consumption: 0,2 – 5 mg/h
Lifetimes days: 48Ca  30, 64Ni  6
* Ti with High Temperature Oven (HTO)
*
yellow = Al2O3; green = Ta; orange = Mo;
violet = CuBe2; black = WRe(26%Re)
Aleksandr Andreev

## Slide 3: Tungsten mesh shielding: preventing passive MW heating
Mesh clogged after
one day of 55Mn operation
Tungsten mesh shielding used to prevent passive microwave heating of the oven during low sublimation temperature element operation (e.g. 48Ca)
  Specifications: Type 100 holes/inch, 25.4 µm wire, 81% transparency
Improves beam stability and reduces material consumption by protecting the oven from uncontrolled material evaporation
Observed Limitations:
Mesh performance depends on the element:
  Successful for Ca (no clogging, stable beam)
  Clogging for Cr and Mn, limiting long-term beam production
Clogged mesh limits material flow and reduces beam intensity
Microwave shielding
Aleksandr Andreev
Mesh clogged after
few hours of 54Cr operation
Mesh after 1 month of
48Ca operation

## Slide 4: Optical diagnostic devices @ HLI
Optical spectroscopy as a diagnostic tool for metal ion beam production with an ECRIS
F.Maimone, J.Mäder, R.Lang, P.T.Patchakui, K.Tinschert R.Hollinger , Rev. Sci. Instrum. 90, 123108, 2019
A CCD camera looks through the straight beam line and the extraction aperture into the plasma chamber
810 nm
Mn II
827 nm
CCD Camera
Telephoto Lens
Optical Beam Splitter and Glass Fiber
..to the Optical Emission Spectrometer
Plasma Image
CAPRICE ECRIS
Aleksandr Andreev

## Slide 5: OES for metal ion beams
Aleksandr Andreev
Provides early indicators of changes in plasma composition and oven temperature
Detects passive microwave heating of the oven
Allows for more stable ion source operation and higher average intensity
Enables proactive rather than reactive adjustments
Reduces on call interventions
55Mn9+ beam establishment test in 2024
48Ca10+ beam run in 2022
OCEAN OPTICS QE Pro
Entrance slits: 25 µm
Wavelenght Range 449-833 nm
Resolution 0.95 nm
oven ↓
auxiliary gas ↑
oven ↓
microwave power ↑
auxiliary gas ↑
Ca burst

## Slide 6: Ta liner: reducing material condensation
Aleksandr Andreev
Discharges appear
55Mn9+ intensity at the Faraday Cup w/o hot screen
Without hot screen:
Discharges started on Day 1
Occurred once every few minutes
Strong impact on beam stability
With hot screen:
Discharges delayed until Day 2
Lower discharge frequency
Improved beam stability
Discharges appear
55Mn9+ intensity at the Faraday Cup with hot screen
Ta Liner
Injection
cap
Extraction cap

## Slide 7: Ta liner: reducing material condensation
Aleksandr Andreev
Discharges appear
55Mn9+ intensity at the Faraday Cup w/o hot screen
Without hot screen:
Discharges started on Day 1
Occurred once every few minutes
Strong impact on beam stability
With hot screen:
Discharges delayed until Day 2
Lower discharge frequency
Improved beam stability
Discharges appear
55Mn9+ intensity at the Faraday Cup with hot screen
Ta Liner
Injection
cap
Extraction cap
Operational Experience:
Successfully used for Ca, Sr, Mg and Mn
Currently under testing for Cr
Improves long-term performance
Reduces material condensation and consumption

## Slide 8: Thank you for your attention!
THE ECRIS TEAM
Ralph Hollinger (dpt. Leader)
Fabio Maimone
Michael Galonska
Ralf Lang
Jan Mäder
Michael Händler
Me

## Slide 9: Ta liner: reducing material condensation
Aleksandr Andreev
55Mn9+ intensity at the Faraday Cup w/o hot screen
Without hot screen:
Discharges started on Day 1
Occurred once every few minutes
Strong impact on beam stability
With hot screen:
Discharges delayed until Day 2
Lower discharge frequency
Improved beam stability
Discharges appear
55Mn9+ intensity at the Faraday Cup with hot screen
Discharges appear
Operational Experience:
Successfully used for Ca, Sr, Mg and Mn
Currently under testing for Cr
Improves long-term performance
Reduces material condensation and consumption

## Slide 10: Backup slides

## Slide 11: Evaporation technique for metal ion beam production @ HLI
Standard Temperature Oven (STO)
Enables stable and reproducible metal ion beam production with low material consumption
Modular assembly with the 3 main components:
  Push Rod: Supplies heating current and cooling water
  Sluice: Allows oven refilling or exchange without breaking the source vacuum
  Oven head: Contains material for evaporation

## Slide 12
GSI Resistive Oven Concept
  The oven head: Two types for different temperature ranges (STO and HTO)
  The sluice (exactly the same for both oven types): Stainless steel part flanged with DN 16 ISO KF for oven exchange without breaking the vacuum (a gate valve is mated)
  The push rod (nearly the same for both oven types): System of three concentric stainless steel tubes for cooling water flow. Inside the inner tube an Al2O3 insulated rod inserted for the current connection.

## Slide 13
Resistive evaporation oven heads
STANDARD TEMPERATURE OVEN (STO)
yellow = Al2O3; green = Ta; orange = Mo; violet = CuBe2; black = WRe(26%Re)
HIGH TEMPERATURE OVEN (HTO)
yellow = Al2O3; green = Ta; orange = Mo; violet = WL20; dark red = WVM
Outer dimensions: length 70 mm, diameter 14.5 mm

## Slide 14
Resistive evaporation oven heads
STANDARD TEMPERATURE OVEN (STO)
yellow = Al2O3; green = Ta; orange = Mo; violet = CuBe2; black = WRe(26%Re)
Outer dimensions: length 70 mm, diameter 14.5 mm
Tungsten wire wound around a ceramic body (heater)
Aperture ring necessary if the material is liquid at the required vapour pressure (i.e. Fe, Ni)
Ta or W crucible used inside the ceramic to avoid chemical reactions (i.e. Mg, Ca, Li)
Ta and Mo parts dismounted, cleaned and re-used

## Slide 15
Resistive evaporation oven heads
HIGH TEMPERATURE OVEN (HTO)
yellow = Al2O3; green = Ta; orange = Mo; violet = WL20 dark red: WVM
Outer dimensions: length 70 mm, diameter 14.5 mm
Removed ceramic body (heater) and ceramic parts where high temperature is expected
Free standing heating wire made of an Aluminum Potassium Silicate doped Tungsten (WVM) (Plasnee GmbH company)
Crucible retainer made of a Tungsten alloy with 2% La2O3 (WL20 provided by Witstar company)
Interpolated curve
based on
Thermocouple
Measurement
Extrapolated
data
Test with TiO2 at Testbench
2230 °C achieved at 560 W

## Slide 16
Fabio Maimone
MICROWAVE SHIELDING
Material: Tungsten
Mesh 18 (1 mm) - 50 µm wire
OES measurements for different oven powers without and with mesh at the oven head
Measurements carried out with the shielded empty oven inserted inside the ECRIS.
Helium plasma generated by coupling up to 650 W microwave power.
Oven power settings: 8.4, 12.5, 17.4 W.
Up to 69% shielding due to the mesh.
Succesfull test at EIS testbench with 40Ca
Optical spectroscopy as a diagnostic tool for metal ion beam production with an ECRIS
F.Maimone, J.Mäder, R.Lang, P.T.Patchakui, K.Tinschert R.Hollinger , Rev. Sci. Instrum. 90, 123108, 2019
Workshop Targets - Ion Sources, GANIL, 06-08 September 2023
Mesh 100 (149 µm) – 25.4 µm wire
Microwave shielding of the
oven orifice
24

## Slide 17: Oven preparation stand @ HLI
Purpose:
Essential tool for conditioning ovens before beam operation
Minimizes downtime during operation
Improves beam stability and reproducibility
Key features:
Controlled environment for oven outgassing and material preheating (e.g. Ni)
Simultaneous oven insertion with 6 airlocks (previously 4)
Water cooling system for ovens and the stand
Online monitoring (planned: 2-3 cameras) for material conditioning
Residual gas analyzer (planned) for better analysis and process control

## Slide 18: 48Ca charge states distributions and CCD plasma images
48Ca
100 μA
Dipole Current [a.U.]
Ion Current [μA]
Spectrum of 48Ca + He optimized on 48Ca10+
48Ca10+
Plasma image recorded with the CCD camera
Changes in brightness and color → changes in plasma density and charge state distribution
Plasma image recorded with the CCD camera
Changes in brightness and color → changes in plasma density and charge state distribution
Plasma image recorded with the CCD camera
A CCD camera positioned to look through the straight beam line and the extraction aperture into the plasma chamber for plasma behavior monitoring

## Slide 19: 48Ca charge states distributions and CCD plasma images
48Ca
100 μA
Dipole Current [a.U.]
Ion Current [μA]
Spectrum of 48Ca + He optimized on 48Ca10+
48Ca10+
Plasma image recorded with the CCD camera
Changes in brightness and color → changes in plasma density and charge state distribution

## Slide 20: 48Ca charge states distributions and CCD plasma images
48Ca
100 μA
Dipole Current [a.U.]
Ion Current [μA]
Spectrum of 48Ca + He optimized on 48Ca10+ after an excessive oven power increased
48Ca10+
Brighter image compared to the optimized operation – higher amount of the evaporated material in the plasma
Plasma image recorded with the CCD camera

## Slide 21: 48Ca charge states distributions and CCD plasma images
48Ca
100 μA
Dipole Current [a.U.]
Ion Current [μA]
Spectrum of 48Ca + He optimized on 48Ca10+ during an overheating of the oven
Extremely bright image compared to the optimized operation – clear excess of the evaporated material in the plasma
48Ca3+
Plasma image recorded with the CCD camera

## Slide 22: 48Ca charge states distributions and CCD plasma images
Spectrum of 48Ca + He optimized on 48Ca10+ after a power reduction of the oven
48Ca
100 μA
Dipole Current [a.U.]
Ion Current [μA]
48Ca10+
Darker image compared to the optimized operation – lower amount of the evaporated material in the plasma
Plasma image recorded with the CCD camera

## Slide 23: 48Ca charge states distributions and CCD plasma images
48Ca
100 μA
Dipole Current [a.U.]
Ion Current [μA]
Spectrum of 48Ca + He re-optimized on 48Ca10+
Time consuming process – several hours of optimization
Increased consumption of a rare and expensive material
Reduced beam intensity for experiments
48Ca10+
Similar image compared to the initial optimized state
Plasma image recorded with the CCD camera