## Slide 1: High Temperature Oven Development at IMP
L. Sun
IMP
Institute of Modern Physics, CAS, 730000, Lanzhou, China
PIBHI’25, April. 7~9, 2025, Acitrezza, Italy

## Slide 2
Typical Methods for Metallic Ion Beams
Plasma Heating
MIVOC
Sputtering
RIKEN, MSU, IMP
Metallic oven (Resistance oven, Inductive oven, etc)
LBNL, MSU, RIKEN, GSI, IMP, JYFL…
Laser Ablation
Notes: Needs: SHE, CEE, HIAF
HCI production: metallic beams with CAFe-2 (LECR5 & SECRAL 3), Uranium beam with HIRFL@SECRAL-I & SECRAL-II
New Techniques towards intense beams: HTO, Vlasov launcher, 2-frequency AG, Biased probe + AG effect
HIAF requirements in long range, FECR

## Slide 3
Ovens at IMP
Notes: Needs: SHE, CEE, HIAF
HCI production: metallic beams with CAFe-2 (LECR5 & SECRAL 3), Uranium beam with HIRFL@SECRAL-I & SECRAL-II
New Techniques towards intense beams: HTO, Vlasov launcher, 2-frequency AG, Biased probe + AG effect
HIAF requirements in long range, FECR

## Slide 4
High Temp. Oven: Trial 1
Feedthrough
Copper Rod
304 SS Rod
Ta
W
Ta
Notes: Needs: SHE, CEE, HIAF
HCI production: metallic beams with CAFe-2 (LECR5 & SECRAL 3), Uranium beam with HIRFL@SECRAL-I & SECRAL-II
New Techniques towards intense beams: HTO, Vlasov launcher, 2-frequency AG, Biased probe + AG effect
HIAF requirements in long range, FECR

## Slide 5
High Temp. Oven : Trial 1
Ioven
Br
Br
Bz
Fz
Fr
Fr
Forces caused by Br
Forces caused by Bz
Notes: Needs: SHE, CEE, HIAF
HCI production: metallic beams with CAFe-2 (LECR5 & SECRAL 3), Uranium beam with HIRFL@SECRAL-I & SECRAL-II
New Techniques towards intense beams: HTO, Vlasov launcher, 2-frequency AG, Biased probe + AG effect
HIAF requirements in long range, FECR

## Slide 6
Upper W lead
Lower W lead
Ta crucible lower connector melted
Ta crucible bent
Ta crucible bent
Crucible connect point bent and melt caused by resistor heating caused by detaching
High Temp. Oven : Trial 1
Notes: Needs: SHE, CEE, HIAF
HCI production: metallic beams with CAFe-2 (LECR5 & SECRAL 3), Uranium beam with HIRFL@SECRAL-I & SECRAL-II
New Techniques towards intense beams: HTO, Vlasov launcher, 2-frequency AG, Biased probe + AG effect
HIAF requirements in long range, FECR

## Slide 7
Cu
Ta
Ta purity
Thermal expansion forces
High Temp. Oven : Trial 2
Notes: Needs: SHE, CEE, HIAF
HCI production: metallic beams with CAFe-2 (LECR5 & SECRAL 3), Uranium beam with HIRFL@SECRAL-I & SECRAL-II
New Techniques towards intense beams: HTO, Vlasov launcher, 2-frequency AG, Biased probe + AG effect
HIAF requirements in long range, FECR

## Slide 8
Principle of inductive heating and its features
Lorenz force free when work in high magnetic field environment (B>3-6 T);
Fast temperature respond to the heating power;
Material compatibility under high temperature;
Thermal radiation and thermal conduction shielding;
: skin depth, cm
ρ: resistivity of heated metal,
μr: Relative permeability
: AC current frequency, Hz
Challenges:
Pros:
With inductive heating oven, MSU got ~200 euA of U33+ in 2012. But the performance of oven degrades quickly!
High Temp. Oven : Trial 3
Notes: Needs: SHE, CEE, HIAF
HCI production: metallic beams with CAFe-2 (LECR5 & SECRAL 3), Uranium beam with HIRFL@SECRAL-I & SECRAL-II
New Techniques towards intense beams: HTO, Vlasov launcher, 2-frequency AG, Biased probe + AG effect
HIAF requirements in long range, FECR

## Slide 9
Sketch of inductive oven at IMP
Design temperature: 1800 -2100 0C
Design working life: >200 hours
Control mode: Close loop (open loop at the first step)
Capacity: Ø8 mm×50 mm crucible
Main features: Add gap between crucible and ZrO2
Original Design at MSU
W. Lu in 2019
High Temp. Oven : Trial 3
Notes: Needs: SHE, CEE, HIAF
HCI production: metallic beams with CAFe-2 (LECR5 & SECRAL 3), Uranium beam with HIRFL@SECRAL-I & SECRAL-II
New Techniques towards intense beams: HTO, Vlasov launcher, 2-frequency AG, Biased probe + AG effect
HIAF requirements in long range, FECR

## Slide 10
Inductive oven assembling
1 mm of Susceptor (Ta)
2 mm of ZrO2
Al2O3 End plate
Inductive oven-2019
Inductive oven after assembling
RF power generator (0-2 kW, 200 kHz)
Ta support
For pumping
End cape and rod
High Temp. Oven : Trial 3
Notes: Needs: SHE, CEE, HIAF
HCI production: metallic beams with CAFe-2 (LECR5 & SECRAL 3), Uranium beam with HIRFL@SECRAL-I & SECRAL-II
New Techniques towards intense beams: HTO, Vlasov launcher, 2-frequency AG, Biased probe + AG effect
HIAF requirements in long range, FECR

## Slide 11
Off-line Test
ZrO2 and Ta crucible survived
Similar performance in thermal-cycle test
Coil
ZrO2
Ta crucible
Heat station
5 days continuous running
High Temp. Oven : Trial 3
Notes: Needs: SHE, CEE, HIAF
HCI production: metallic beams with CAFe-2 (LECR5 & SECRAL 3), Uranium beam with HIRFL@SECRAL-I & SECRAL-II
New Techniques towards intense beams: HTO, Vlasov launcher, 2-frequency AG, Biased probe + AG effect
HIAF requirements in long range, FECR

## Slide 12: 238U35+ stability test
High Temp. Oven : Trial 3
Notes: Needs: SHE, CEE, HIAF
HCI production: metallic beams with CAFe-2 (LECR5 & SECRAL 3), Uranium beam with HIRFL@SECRAL-I & SECRAL-II
New Techniques towards intense beams: HTO, Vlasov launcher, 2-frequency AG, Biased probe + AG effect
HIAF requirements in long range, FECR

## Slide 13
Summary
High temperature oven is one key technology for ECRIS
Inductive heating oven is so far the most reliable HTO
Key issues for IHO:
  Proper selection of materials
  Thermal expansion control in mechanical design
  Sufficient offline test
IHO is still facing challenges:
  Very high current metallic ion beam long-term operation
  Very refractory metallic ion beam production