## Slide 2: Contents
Introduction
Prototypes with industry
Preparing series production: the cavity example
Series production better than prototypes

## Slide 3: Contents
Introduction
Prototypes with industry
Preparing series production: the cavity example
Series production better than prototypes

## Slide 4: Eu-XFEL by-product of TESLA
The European XFEL has been the by-product of TESLA, the Superconducting Linear Collider developped since 1990 by a large International Collaboration
as in 1992

## Slide 5: The goals of the TESA Mission
Basic goals on SRF Technology
  Increase gradient by a factor of 5: from 5 to 25 MV/m
    Push cavity performances close to the physical limit, understanding practical limits
    Set all the required quality control for reproducibility and industrial production
  Make possible pulsed operation: Lorentz force detuning
    Combine SRF and mechanical engineering in cavity design
    Develop efficient Modulators and Klystrons
    Develop new ancillaries: slow and fast tuners, couplers
  Reduce cost per MV by a factor 20: to make the LC feasible
    New cryomodule concept for cryolosses, cost and filling factor (for real estate gradient)
    All subsystems designed for large scale production
    Reliability and quality control as a general guideline
Basic goals on Machine Design
  Design a Linear Collider based on the Cold Linac peculiarities
  Maximize Luminosity and optimize cost for a given plug power
  Design and quote major subsystems: DR, Positron Source, BDS, etc.
  Put all together in a consistent TDR, including cost estimation

## Slide 6: First Steps of the TESLA Game
R/Q | 1036 | W
Epeak/Eacc | 2.0 | 
Bpeak/Eacc | 4.26 | mT/(MV/m)
Df/Dl | 315 | kHz/mm
KLorentz |  -1 | Hz/(MV/m)2
TESLA cavity parameters
9-cell, 1.3 GHz
Major contributions from: CERN, Cornell, DESY, CEA-Saclay, INFN-LASA

## Slide 7: TESLA cavity design and rules

## Slide 8: TTF: a new infrastructure at DESY
TTF as operated for SASE FEL

## Slide 9: Preparation of TESLA Cavities

## Slide 10: Contents
Introduction
Prototypes with industry
Preparing series production: the cavity example
Series production better than prototypes

## Slide 11: The way to improve SRF Performances
In parallel with the machine design, all major TESLA sub-components have been conceived, designed and protopyped for TTF.
Most of the process has been performed in strict collabotration with industry.
Concerning SRF cavities, all the technology already mastered by industry have been further improved with the help of Labs experience. All the mechanical fabrication done in industry.
The acquisition of an EB Welding machine at DESY had the strong opposition by the Director Biorn Wiik
The matured experience on the Niobium welding has been transferred directly from Labs to industry
Clean room operation and special surface treatments were developped at the DESY infrastructure and promptly tranferred to Industry

## Slide 12: Eddy Current Scanner for Nb Sheets
Scanning results
Rolling marks and defects are visible on a niobium disk to be used to print a cavity half-cell.
Surface analysis is then required to identify the inclusions

## Slide 13: Learning curve with BCP
3 cavity productions from 4 European industries: Accel, Cerca, Dornier, Zanon
BCP = Buffered Chemical Polishing
Cornell
1995
5-cell
Module performance in the TTF LINAC
Improved welding
Niobium quality control
<Eacc> @ Q0  1010
<Eacc> @ Q0  1010
at Q = few 109
<1997>
<1999>
<2001>

## Slide 14: 3rd cavity production with BCP
Still some field emission at high field
Q-drop above 20 MV/m not cured yet
AC67 discarded (cold He leak)
TESLA original goal
Vertical CW tests of naked cavitis

## Slide 15: Further Improvement with EP
EP (Electro-Polishing) developed at KEK by Kenji Saito (originally by Siemens)
Coordinated R&D effort: DESY, KEK, CERN, CEA-Saclay & INFN LASA
TESLA 800 specs:
35 MV/m @ Q0 = 5  109
Vertical CW tests of naked cavitis
1400 °C heat treatment
AC76: just 800 °C annealing
9-cell EP cavities from 3rd production
EP at Nomura Plating (Japan) by KEK

## Slide 16: EP at DESY from the KEK Experience

## Slide 17: EP system at RI

## Slide 18: EP system at Zanon
Courtesy EZ

## Slide 19: Not Just Cavities: From Prototype to Cry 3
Extensive FEA modeling (ANSYS™) of the entire cryomodule
Transient thermal analysis during cooldown/warmup cycles,
Coupled structural/thermal simulations
Full nonlinear material properties
Detailed sub-modeling of new components and Laboratory tests
Finger-welding tests at ZANON
Cryogenic tests of the sliding supports at INFN-LASA

## Slide 20: Cryomodule Evolution in TTF-II
RF gun
400 MeV
120 MeV
800 MeV
ACC 1
ACC 2
ACC 3
ACC 4
ACC 5
4 MeV
ACC 4 & ACC 5
ACC 2 & ACC 3
ILC Acc. Workshop
16 August 2005

## Slide 21: 10 MW Klystrons Developped by Industry

## Slide 22: RF Waveguide Components @ 1.3 GHz
3 Stub Tuner (IHEP, Bejing, China)
Hybrid Coupler (RFT, Spinner)
E and H Bends (Spinner)
Circulator (Ferrite)
RF Load (Ferrite)
Peak Power = 5 MW
RF Load (Ferrite)
Peak Power = 1 MW
Peak Power = 0.4 MW
Peak Power = 2 MW

## Slide 23: Ancillaries: Coupler R&D at LAL-Orsay
TTF III Design
Clean room assembly
High Power Coupler Test Stand
Alternative Designs

## Slide 24: Ancillaries: Cavity Tuners
The Saclay Tuner in TTF
The INFN Blade-Tuner
Successfully operated with superstructures

## Slide 25: RF Distribution: the TESLA RF Unit
Mechanical tuner
(frequency adj.)
and piezo-electric tuner
(Lorentz force compensation)
DAC
DAC
ADC
ADC
Low
Level
RF System
vector sum
vector demodulator
pickup signal
MBK Klystron
vector modulator
cavity #1
cavity #12
coaxial coupler
circulator
stub tuner (phase & Qext)
accelerator module 1 of 3
1 klystron for 3 accelerating modules, 12 nine-cell cavities each

## Slide 26: Pulse Transformer Modulator Layout

## Slide 27: New QC tools in 4th Production
© V. Singer

## Slide 28: TESLA Technical Design Report: March 2001
As in the TDR
Updated tunnel cross section

## Slide 29: Industrial Studies for TESLA TDR & E-XFEL

## Slide 30: Cavity Fabrication Industrial Studies
Production Plan for 20,000 cavities

## Slide 31: TTF2 as XFEL Injector Prototype
RF-GUN
ACC5 ACC4 ACC3 ACC2 ACC1
BC3 BC2
e- beam
500 MeV

## Slide 32: Outstanding Results with module # 5
6 cavities exceed 30 MV/m
1 cavity shows field emission at high field
1 cavity is quenching at 25 MV/m
5 Hz Test limited to demonstrate 25 MV/m module

## Slide 33: TESLA/XFEL Milestones
TTF II
TESLA Collider
TESLA X-Ray FEL
Infrastructure
@ DESY in Hall 3
TTF I
July 1990 – 1° International TESLA Workshop @ Cornell University
February 1992 – 1° TESLA Collaboration Board Meeting @ DESY
March 1993 - “A Proposal to Construct and Test Prototype Superconducting RF Structures for Linear Colliders”
March 1995 -TESLA Test Facility Linac Design Report
SASE FEL included in TESLA → TTF 2
May 1996 – first beam at TTF1
March 2001 – TESLA Technical Design Report with XFEL. First SASE-FEL Saturation at TTF
July 2002 – from the German Science Council: Two independent projects: TESLA X-FEL and TESLA LC
February 2003 –TESLA X-FEL proposed as an European Facility, 50% funding from Germany
June 2004 – TTF II: First beam accelerated
August 2004 – TESLA Technology chosen for ILC
June 2007 – European XFEL Project Starts

## Slide 34: TTF: 10 years of experience
Taking into account all data from 1995
Eacc = ½ Esurf

## Slide 35: Contents
Introduction
Prototypes with industry
Preparing series production: the cavity example
Series production better than prototypes

## Slide 36: European XFEL Cavity Production - 1
At the end of the long prequalification process (TTF, FLASH, ILC,…)
Ettore Zanon, EZ & Research Instruments, RI
were contracted at the end 2010 to produce each
8 Cavities for infrastructure rump/up and qualification
  4 Dummy CVs (DCV), 4 Reference CVs (RCV)
280 XFEL type series cavities (first 8 are PCV)
12 ILC HiGrade cavities
Additional 120 cavities allocated end 2012 to each companiy
Nb & NbTi supplied by DESY
Production precisely following detailed specifications which also include the exact definition of infrastructure to be used (build to print)
Final treatment after main EP: final EP for RI / flash BCP for EZ

## Slide 37: European XFEL Cavity Production - 2
No performance guaranty by the vendors, i.e. the risk of unexpected low gradient or field emission is taken over by XFEL/DESY (responsibility for re-treatment).
Goal: average usable XFEL gradient 23.6 MV/m at Q0=1x1010, X-Rays <1x10-2mGy/min
First series cavities (PCV) to be delivered end 2012 – begin 2013
All cavities to be delivered till end 2014 – begin 2015
Delivery rate: about 8 CVs/week (4/each vendor)
Supervision of the CV production: DESY & INFN/LASA

## Slide 38: Treatments as from Experience on Prototype

## Slide 39: e-Documentation in EDMS - Data Bank
All XFEL SC cavity documents (specifications, inspection sheets, meeting minutes, PED data etc.) recorded in EDMS
EZ and RI have access to documents and data (to relevant only)
Data
Fabrication
Cavity-DB
Inspection sheets for QM documentation
Fabrication structure. Subassembly parts related. Procedure related
Statistical analysis
Phys. Part
Files
Inspection sheet
Document
EDMS

## Slide 40: PED Activities and TUEV Control
Test piece (TP) is composed by 2 cell with helium vessel, without end groups, representing all pressure bearing parts and welds. It is built using exactly the same manufacturing methods and welding parameters that will be later used for production. Two EBW machines/company. Then two test pieces had been built.

## Slide 41: Good performance of reference cavities
D.Reschke, A.Sulimov, D.Kostin
8 RCVs: acceptance test successful

## Slide 42: Major Infrastructures at EZ & RI
2 EBW (Electron Beam Welding) plants, equipped with cryo-pumps
ISO 7 and ISO 4 Clean Rooms with cleaning and rinsing facility
UPW (Ultra Pure Water - 18 MW·cm) production system (>3000 l/h)
HPR (High Pressure Rinsing – 100 bar) apparatus
800 °C and 120 °C ovens operating with High Vacuum.
Cavity Tuning Machine, CTM, provided by DESY
RF tests set up (for HalfCell, DumbBells and EndGroups), provided by DESY
US (Ultra Sonic) cleaning baths
Complete chemical processing plants (EP, BCP or both)
Cavity internal visual inspection systems

## Slide 43: Special Equipments installed in Industry

## Slide 44: CTM cavity tuning machine and HAZEMEMA
CTM and HAZEMEMA installed at RI
DESY developed, build and delivered to both companies a cavity tuning machine CTM and equipment for RF measurement on half cells, dumb-bells and end groups HAZEMEMA
CTM in installation at EZ

## Slide 45: Cavity Infrastructure Layout at EZ
Building layout: clean rooms ISO10, ISO7, ISO4, US and BCP treatment, 120oC baking, 800oC oven, EBW, tuning machine etc.

## Slide 46: Examples of EZ Infrastructure (courtesy of EZ)
New EBW machine
New oven for 800oC treatment
Borescope for optical inspection

## Slide 47: Examples of EZ Infrastructure (courtesy of EZ)
US cleaning and BCP in ISO 10 clean room
ISO 4 installed in the new building
The UPW (Ultra Pure Water) production system

## Slide 48: Deep Defect Analysis Capability @ Labs - 1
Topographical defects at the welding seams

## Slide 49: Deep Defect Analysis Capability @ Labs - 2
Etching pits: EBSD with strain maps via grain reference orientation deviation (GROD)

## Slide 50: Deep Defect Analysis Capability @ Labs - 3
Dangerous surface defects generated by bad HPR (Hihg Pressure Water rinsing)

## Slide 51: Contents
Introduction
Prototypes with industry
Preparing series production: the cavity example
Series production better than prototypes

## Slide 52: 1.3 GHz E-XFEL cavities «as received»
EZ
RI
EZ
RI
EP
BCP

## Slide 53: As Received Maximum Gradient
200 W Pfor limit

## Slide 54: As Received Usable Gradien
Include operations spec
  Q0 ≥ 1×1010
  FE threshold (X-ray)
 Usable Gradient
23.6 MV/m

## Slide 55: As Received Usable Gradient
Include operations spec
  Q0 ≥ 1×1010
  FE threshold (X-ray)

## Slide 56: Final performance: Eacc Total after 313 retreatments performed on 237 of the 831 cavities
Before:
E usable 27.7 ± 7.2 [MV/m]
(RI): E usable 29.0 ± 7.3 [MV/m])
(EZ): E usable 26.4 ± 6.6 [MV/m])
After:
E usable 29.8 ± 5.1 [MV/m]
(RI): E usable 31.2 ± 5.2 [MV/m])
(EZ): E usable 28.6 ± 4.8 [MV/m])
Before:
E max 31.4 ± 6.8 [MV/m]
(RI): E max 33.0 ± 6.5 [MV/m])
(EZ): E max 29.8 ± 6.6 [MV/m])
After:
E max 33.0 ± 4.8 [MV/m]
(RI): E max 34.7 ± 4.4 [MV/m])
(EZ): E max 31.5 ± 4.9 [MV/m])

## Slide 57: Final performance: Q0 Total after 313 retreatments performed on 237 of the 831 cavities
Before:
Q0 @ 23.6 MV/m 1.31 ± 0.26 [1.1010]
(RI): Q0 @ 23.6 MV/m 1.29 ± 0.24 [1.1010])
(EZ): Q0 @ 23.6 MV/m 1.34 ± 0.28 [1.1010])
After:
Q0 @ 23.6 MV/m 1.37 ± 0.25 [1.1010]
(RI): Q0 @ 23.6 MV/m 1.34 ± 0.22 [1.1010])
(EZ): Q0 @ 23.6 MV/m 1.41 ± 0.26 [1.1010])
Before :
Q0 @ 4 MV/m 2.15 ± 0.32 [1.1010]
(RI): Q0 @ 4 MV/m 2.11 ± 0.32 [1.1010])
(EZ): Q0 @ 4 MV/m 2.18 ± 0.32 [1.1010])
After:
Q0 @ 4 MV/m 2.23 ± 0.34 [1.1010]
(RI): Q0 @ 4 MV/m 2.21 ± 0.34 [1.1010])
(EZ): Q0 @ 4 MV/m 2.26 ± 0.33 [1.1010])

## Slide 58: E-XFEL experience on cavity production rate
2013
2014
2015
EZ cavity production udated on May 6th, 2015

## Slide 59: Vertical TEST Infrastructure at DESY
Multiple vertical tests started in Feb 2013 (IFJ-Pan & DESY)
2 independent cryostats and RF stations for six 4-cavity inserts
Parallel commissioning of inserts + vertical tests on series cavities
New software for vertical tests
  no Second Sound, no T-Mapping at AMTF

## Slide 60: XFEL cavities: verticat test rate

## Slide 61: Effect of HPR after transportation: Eacc

## Slide 62: Effect of HPR after transportation: Q0

## Slide 63: EP vs BCP: average Eacc and Q0 /mounth
Final BCP
Final EP
31 April 2015

## Slide 64: E-XFEL: Usable Installed Voltage

## Slide 65: XFEL definition of usable gradient

## Slide 66: Some consideration on the series production
Industry, once trained, is doing as well as the lab behind
Results obtained are very close to those available more than 13 years ago, the time of the ITRP
  Results depend on the technology applied
  The complete cycle in Industry improves the yield, but not dramatically
The possibility of a second treatment is still mandatory to improve the yield
  HPR is usually sufficient, flash BCP can be required, EP is excluded (HT installed)
  Second treatment is improving the yield, both for high field and field emission

## Slide 67: Reference for CW after LCLS II
After XFEL, EZ & RI produced all the 1.3 GHz cavities for LCLS II, including final treatment and Nitrogen doping
All the cryomodules, modified for CW, are now produced in China by Wuxi, originally with IHEP supervision
DOE sbuscribed the high nominal value for the cavity Qo (as promissed by the succesfull application of the nitrogen doping) but doubled the cryoplant: just in case
Costing of XFEL was succesfully based on industrial studies performed by experienced companies
New large Projects should consider a very similar approach
Cavity packadge, criomodule and ancillaries are going together

## Slide 68
Thank you for your attention