## Slide 1: UK Programme
Outline:
  Mechanics
  Sensor Bench tests
  2012 Test beam plans

## Slide 2: Mechanics
Filippo visited before the summer break to discuss plans to make a prototype of the interaction region by the end of 2013.
  Discussion mainly focussed on the support cones and space frame assembly.
  Detailed problem:
    Space frame
      CFRP Rings, tubes, assembly jigs
      alignment jigs
    Cones
      CFRP
      Faraday cage
      cooling rings (with mounting buttons)
Fred, John, Jag & Filippo
N.B. for now we plan to use up our old stock of epoxy resin based CFRP, would want to use a more rad hard cyanite-ester resin for the real thing.

## Slide 3: Can we increase cooling for L1/L2?
Same profile from the detector point of view, larger x-sectional area for coolant.
Fred

## Slide 4: Splitting the support structure
Aim to use the logical split (vertically) through the SVT)
Started to think about assembly of the cones and support frame relative to parts. Can either
  Fix the cooling rings and build around them (using buttons as datums).
  Build up structure from the inside out (starting with cones).
Fred

## Slide 5
Working on mould design for cones: aim to co-cure copper mesh into the cone surface to provide the faraday cage in a natural way.
  Have mould resin ready to machine. Aim is to finish producing mould by the end of the year.
Cooling rings shown are basic model from Filippo.
Co-curing copper mesh to main part of the mould shown to work well on test sample.
Aim to push forward to finalise basic cone design before making mould.
Fred

## Slide 6: Prototyping space-frame
Looking at various materials: Foam Core or Solid?
Foam Core
Advantages: Light weight, less material (possibly!)
Disadvantages: Is core material rad hard? Would need to run tests.
Requires extra material (pads) at fixed points due to thin walls.
Requires inserts where rings fit together (as above).
Edges will need to be sealed.
Solid Profile
Advantages: Very strong – could be lightened by machining.
Good mechanical contact at fixed points.
Rad hard.
Disadvantages: Time consuming to build (approx 40 layers).
More material (possibly!)
Initial aim to try making a solid ring of CFRP to machine as required.
John & Jag

## Slide 7: Foam Core (showing additional support pads)
CF Tube Support
Support
Pad
John

## Slide 8: Solid Ring CF Lay-up Strategy (alternating layers)
Layer 1
Layer 2 etc
Final machined
profile
John

## Slide 9: CF Lay-up Jig
John

## Slide 10: Solid CF Ring
John

## Slide 11
In the process of making jigs for the first solid ring prototypes
Will need to finish off a few parts, and coat with Teflon before we can try making some samples.
May require a bit of trial and error given we need to produce relatively thick CFRP parts & want uniform curing of the material.
Using Amber Composites E722 twill (200g/m2)
  (our stock of prepreg is past its shelf life, so it is usable for prototypes, but not for a production part)
Jag

## Slide 12: Support alignment frame
Initial rough concept for discussion:
  Base the support around a long silver steel bar to form central axis of the detector for assembly purposes.
  Will need to mount cones accurately onto this, and build the space-frame with a combination of alignment and assembly jigs.
  Ideally would like to be able to put this all under our new CMM (will be a tight fit).
Fred, John, Jag

## Slide 13: Sensor bench tests
Concentrating on reference pixel tests initially
  Basic functionality tests:
    pedestals, noise, Fe55 and LED response
    Gain determined from Photon Transfer Curve (PTC)
    Prepared laser stage scan using RAL setup.
  In progress: Debugging on chip ADC "Strixel" firmware at the moment.
  The following slides are based on results from the collaboration shown by James Mylroie-Smith at Pixel 2012.
with James, Gianluca, Fergus + our Arachnid collaborators at Bristol, RAL and Daresbury

## Slide 14: PTC Results
PTC performed using IR illumination
Results show good uniformity across the pixels
Gain ≈ 0.17 ADC/e
Noise ≈ 12e rms
Linear full well ≈ 11500e
Maximum full well ≈ 14700e
Log(Signal)
Log(Noise2)
Signal
Noise2
with James, Gianluca, Fergus + our Arachnid collaborators at Bristol, RAL and Daresbury
From James' talk at Pixel 2012

## Slide 15: Pedestals
Readout is performed on a column by column basis
Shows common noise in columns
Pedestal Value (ADC counts)
with James, Gianluca, Fergus + our Arachnid collaborators at Bristol, RAL and Daresbury
From James' talk at Pixel 2012

## Slide 16: Noise and Gain
Noise and gain are uniform across the sensor
Average noise value ~12 e RMS
Average gain value 0.17 => 51𝜇V/e
Noise from each pixel
RMS Noise(e)
Gain from each pixel
Gain(ADCs)
with James, Gianluca, Fergus + our Arachnid collaborators at Bristol, RAL and Daresbury
From James' talk at Pixel 2012

## Slide 17: Noise vs Temperature
Chart: 
| 26.662 | 30.817 | 35.857 | 40.69 | 45.435 | 50.366 | 48.061 | 43.314 | 38.752 | 33.688 | 21.647
Peak | 6442 | 6433 | 6426 | 6493 | 6699 | 7039 | 6841 | 6582 | 6525 | 6511 | 6597
Chart: 
| 26.662 | 30.817 | 35.857 | 40.69 | 45.435 | 50.366 | 48.061 | 43.314 | 38.752 | 33.688 | 21.647
Noise | 97.51 | 96.84 | 96.31 | 96.06 | 97.72 | 114.91 | 98.4 | 96.83 | 96.85 | 97.51 | 99.92
Chart: 
| 26.662 | 30.817 | 35.857 | 40.69 | 45.435 | 50.366 | 48.061 | 43.314 | 38.752 | 33.688 | 21.647
Noise | 97.51 | 96.84 | 96.31 | 96.06 | 97.72 | 114.91 | 98.4 | 96.83 | 96.85 | 97.51 | 99.92
At 50C the noise becomes large.
Increase in noise at 20C
Temperature (C)
Noise (ADCs)
Noise (ADCs)
ZOOM
Temperature (C)
Pedestal
Noise
with James, Gianluca, Fergus + our Arachnid collaborators at Bristol, RAL and Daresbury
From James' talk at Pixel 2012

## Slide 18: 55Fe
Fe55 spectrum shows a sharp cut-off at
Good S/N up to 150
Consistent with noise and gain from PTC
with James, Gianluca, Fergus + our Arachnid collaborators at Bristol, RAL and Daresbury
Reference pixel results
From James' talk at Pixel 2012

## Slide 19: Test beam
CERN test beam at T4-H6 mid-November
  Clarifying dates with regard to latest schedule.
  Preparing for this: will have a stack of sensors with trigger in a stand alone system to simplify the setup.
  Will perform pion beam irradiation of these sensors.
  RAL group leading preparations for this.
    Aim to have a lab based test of the setup in the coming month.

## Slide 20: Summary
Clear plan forward on the mechanical side:
  Some issues are well understood, and we can start prototyping.
  Others: we're starting to try out ideas to determine the best way forward.
Sensor testing:
  First results are now available from Cherwell.
  Reference pixels are behaving as expected, and we hope to be in a position to study the other pixel types soon.
  Test beam plans progressing well.