## Slide 1: Preliminary Design and Challenges of High Field Magnets for the Collider Ring

## Slide 2: Outline
Overview of current work carried out by INFN – Genova/Milano
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses in conductors due only to Lorentz Forces
Summary

## Slide 3: Magnets studied at INFN – Genova/Milano
Dipole Magnets for the Accelerator
Combined Function Magnets for the Collider Ring
Dipole Magnets for the Collider Ring
10 T
(30x100) mm
Top = 20 K
(4 – 8) T + (100 – 330) T/m
Φ = (100-200) mm
Top = 20 K
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary
Detector Magnet
16 T
Φ = 140 mm
Top = 20 K
Only SC magnets non-ramped
See A. Bersani’s presentation

## Slide 4: Dipole Magnet for Collider Ring
Dipole Magnets for the Collider Ring
16 T
Φ = 140 mm
Top = 20 K
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary
Dipole Magnets for the Accelerator
Combined Function Magnets for the Collider Ring
10 T
(30x100) mm
Top = 20 K
(4 – 8) T + (100 – 330) T/m
Φ = (100-200) mm
Top = 20 K
Detector Magnet
See Bersani’s presentation

## Slide 5: Dipole Requirements
Courtesy of Patricia Borges de Sousa
https://indico.cern.ch/event/1250075/contributions/5357594/
Assuming 10 TeV machine and coil at 4.5 K
Main challenges
High magnetic field for compactness
Large aperture to host radiation shielding for the muon decay product
Parameter | Value | U.M.
φ | 140 | mm
Bore field | ≥16 | T
Top | 20 | K
Tmargin | 2.5 | K
Max. Budget | 400 | k€/m
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary
HTS cable

## Slide 6: Objectives of the Study
Produce a preliminary conceptual design
Defining a cable geometry
Electromagnetic design optimization through a sensitivity study of geometrical parameters via F.E.M. software
Estimation of hysteretic losses
Mechanical stresses evaluation in the conductors due only to Lorentz Forces via F.E.M. software
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary

## Slide 7: Cable Assumption
Fujikura FESC-SCH 12
0.11 mm
12 mm
Non-twisted stacked tapes cable co-wounded with a SS layer.
Easy to scale to high current densities
Flexible
Easy to model
x
y
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary
CORC cable
ROEBEL cable
Stacked cable
For the same current, the engineering current density is lower due to the voids
Manufacturing complexity and sensitivity to mechanical stress

## Slide 8: Electromagnetic Desing
Parameter | Value | U.M.
N° tape | 3640 | -
Iop | 1403 | 
Jeng | 433 | 
Bbore | 17.5 | 
Bpeak_max | 19.4 | 
Margin | 2.5 | 
Estored | 6968 | 
L | 2.26 | 
Fx | 15.56 | MN/m
Fy | -10.84 | MN/m
Parameter | Value | U.M.
N° tape | 3640 | -
Iop | 1403 | 
Jeng | 433 | 
Bbore | 17.5 | 
Bpeak_max | 19.4 | 
Margin | 2.5 | 
Estored | 6968 | 
L | 2.26 | 
Fx | 15.56 | MN/m
Fy | -10.84 | MN/m
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary
Main results
Field map
Optimization of blocks width and position
3D conceptual design

## Slide 9: New Ends Winding Proposal
Easy-way
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary
Hard-way

## Slide 10: New Ends Winding Proposal
Easy-way
Hard-way
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary

## Slide 11: New Electromagnetic Design
1
2
3
x
Parameter | Value | U.M.
N° tape | 3176 | -
 | 2481 | 
 | 386 | 
 | 766 | 
 | 17.5 | 
 | 19.7 | 
 | 2.5 | 
E | 7575 | 
L | 2461 | 
Fx | 16.03 | MN/m
Fy | -12.13 | MN/m
Parameter | Value | U.M.
N° tape | 3176 | -
 | 2481 | 
 | 386 | 
 | 766 | 
 | 17.5 | 
 | 19.7 | 
 | 2.5 | 
E | 7575 | 
L | 2461 | 
Fx | 16.03 | MN/m
Fy | -12.13 | MN/m
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary
Main results
Field map
Optimization of blocks width and position
3D conceptual design

## Slide 12: Innovative Approach of Grading
1
2
3
x
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary
Joined together and powered as single unit

## Slide 13: Hysteretic Losses
Bean’s critical state model
Hard-way
Easy-way
x
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary
Intrinsic losses of SC materials independent of cycle time
2a

## Slide 14: Evaluation of Stresses in Conductors
Gap of 0.3 mm between all coils and case
Infinitely rigid structure (Nodal Displacement = 0)
Standard type contact without friction
Ecoil = 174 GPa 1
Νcoil = 0.3
Assumption
1 C. Barth et al., Electro-mechanical properties of ReBCO coated conductors from various industrial manufactures at 77 K, self-field and 4.2 K, 19 T, 2015, Supercond. Sci. Technol. 28 045011
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary

## Slide 15: Evaluation of Stresses in Conductors
 | Value | U.M.
 | -238 | MPa
 | -218 | MPa
 | Value | U.M.
 | -238 | MPa
 | -218 | MPa
Easy-way
Hard-way
 | Value | U.M.
 | -300 | MPa
 | -50 | MPa
 | Value | U.M.
 | -300 | MPa
 | -50 | MPa
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary

## Slide 16: Evaluation of Stresses in Conductors
 | Value | U.M.
 | 2.96 | MPa
 | -4.48 | MPa
 | Value | U.M.
 | 2.96 | MPa
 | -4.48 | MPa
Easy-way
Hard-way
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary
 | Value | U.M.
 | 4.25 | MPa
 | -3.8 | MPa
 | Value | U.M.
 | 4.25 | MPa
 | -3.8 | MPa

## Slide 17: Maximum Allowable Stresses of Tape
 | Value | U.M.
 | -1001,2 | MPa
 | -4001,2 | MPa
 | Value | U.M.
 | -1001,2 | MPa
 | -4001,2 | MPa
x
y
1 Value related to RT
 | Value | U.M.
 | - | MPa
 | - | MPa
 | 6002 | MPa
 | 11.273 | MPa
 | Value | U.M.
 | - | MPa
 | - | MPa
 | 6002 | MPa
 | 11.273 | MPa
All the stresses seen before are below the max. allowable stress
2 Superconductor Business Development Division Fujikura Ltd., “Introduction of Fujikura re-based high temperature superconductor,” Fujikura Global, Tech. Rep., 2024
Max. compressive stresses
Max. tensile stresses
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary
3 P. Gao, X. Geng, G. Man and X. Wang, "Measurement of Shear Delamination Strength of REBCO Coated Conductors," in IEEE Transactions on Applied Superconductivity, vol. 32, no. 4, pp. 1-5, June 2022, Art no. 6600305, doi: 10.1109/TASC.2021.3136831

## Slide 18: Summary
INFN Genova – Milano: study of accelerator and collider dipoles
Non-twisted stacked tapes cable co-wounded with a SS layer
New ends winding always in easy way direction
Innovative approach of grading powering two cables joined together as a single unit
Hysteretic losses 18 % higher than in the first configuration
All mechanical stresses below the max. allowable stress of tape
Mucol Italia
Torino, 05/12/2024
luca.alfonso@ge.infn.it
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary

## Slide 19: A(aperture)-B(bore field) plots
Innovative approach to instantly understand which magnets are feasible
Analytical evaluation of the bore field for a cos-theta magnets in sector coil approximation
The limit curve takes into account:
  Maximum stress on conductors
  Temperature margin on the loadline
  Maximum Tquench
Forbidden region
Allowed region
See Novelli’s presentation
Overview of work
Dipole Magnet for Collider Ring
Cable Assumption
Electromagnetic Design
Hysteretic Losses
Evaluation of stresses
Summary