## Slide 1
1Sapienza University of Rome, 2INFN – Genoa , 3INFN and University of Milan
4Tampere University, 5CERN
Performance Limits of Dipole and Quadrupole for the Collider Ring
D. Novelli1,2, L. Alfonso2, A. Bersani2, L. Bottura5, B. Caiffi2,
S. Farinon2, F. Mariani1, S. Mariotto3 , A. Pampaloni2, T. Salmi4
Funded by the European Union (EU). Views and opinions expressed are however those of the author only and do not necessarily reflect those of the EU or European Research Executive Agency (REA). Neither the EU nor the REA can be held responsible for them.
December 2024
MuCol Italia – Torino

## Slide 2: The Muon Collider Complex
Main stages of a muon collider complex
Purpose:
Evaluate realistic performance targets for the collider magnets, in close collaboration with studies of beam physics, cryogenics, and energy storage.
Produce a credible and affordable design study (contain costs, energy efficiency, sustainable operation).
Task 7.4
Magnets:
Dipoles
Quadrupoles
Sextupoles

## Slide 3: Introduction on SC magnets
[ref]
[ref]
[ref]
NbTi is used for the LHC’s magnets.
It is a ductile alloy with mechanical properties which make it easy to fabricate and use.
Typically works at 1.9 K with superfluid helium and produces B up to 8 T.
Nb3Sn is a brittle intermetallic compound characterized by a strong propensity to fracture.
It was recently used for quadrupoles of Hi-Lumi project.
Can reach operating temperatures of 4.5 K with good em performance.
ReBCO can work at high operating temperatures, such as 20 K, preserving good em. performance.
It is difficult to protect from quench and it is complicated to produce large-sized tapes (so it is expensive).
It still requires a lot of R&D.

## Slide 4: Collider Magnets Requirements
3 TeV collider (5 km ring):
Close to state of the art
11T/150mm (Nb3Sn)
600 magnets, 5 m length
Operating temperature: 4.5 K
10+ TeV collider (10 km ring):
HTS magnets, R&D is required
15T/150mm (ReBCO, hybrid)
1200 magnets, 5 m length
Operating temperature: 4.5…20 K
High field dipoles to minimize collider ring size and maximize luminosity.
Beam loss protection
High-energy electrons and positrons arising from muon decay and striking the collider ring magnets can cause radiation damage and unwanted heat load.
Courtesy of Patricia Borges de Sousa
https://indico.cern.ch/event/1250075/contributions/5357594/
Assuming 10 TeV machine and coil at 4.5 K
with HTS @20K the absorber can be thinner (138 mm)
Courtesy of Anton Lechner
Shielding
Large aperture
P < 5 W/m working at 4.5 K
P < 10 W/m working at 20 K with HTS

## Slide 5: Collider Magnets Requirements
3 TeV collider (5 km ring):
Close to state of the art
11T/150mm (Nb3Sn)
600 magnets, 5 m length
Operating temperature: 4.5 K
10+ TeV collider (10 km ring):
HTS magnets, R&D is required
15T/150mm (ReBCO, hybrid)
1200 magnets, 5 m length
Operating temperature: 4.5…20 K
High field dipoles to minimize collider ring size and maximize luminosity.
Difficult to define
a single magnet
specification
Final Focusing Magnets
Courtesy of Daniele Calzolari
Beam loss protection
High-energy electrons and positrons arising from muon decay and striking the collider ring magnets can cause radiation damage and unwanted heat load.
Shielding
Large aperture

## Slide 6: Introduction to A-B plots
Forbidden area
Need for high fields in large apertures
We perform plots that can show the allowed area between aperture diameter (A) and bore field (B).
We consider Nb3Sn for the 3 TeV machine and HTS (ReBCO) for the 10 TeV collider.
Innovative approach, useful for interfacing the needs of beam dynamics with the technological limits (of today and the near future) related to superconducting magnets.
Immediate feedback capable of analyzing many possible configurations in a single plot
Allowed area
Forbidden area
Allowed area

## Slide 7: Introduction to A-B plots
Need for high fields in large apertures
We perform plots that can show the allowed area between aperture diameter (A) and bore field (B).
We consider Nb3Sn for the 3 TeV machine and HTS (ReBCO) for the 10 TeV collider.
Limit curves are introduced by mechanical challenges (stress limit), critical current density (margin limit) and stored magnetic energy (quench protection), depending on the superconducting material.
Allowed area
Forbidden area
Allowed area
Forbidden area

## Slide 8: Method and Assumptions
A Python code is used to implement the analytic formulas for the cos-theta magnets in sector coil approximation.
Dipole
Quadrupole
(
( is 60° for the dipole and 30° for the quadrupole)

## Slide 9: Method and Assumptions
A Python code is used to implement the analytic formulas for the cos-theta magnets in sector coil approximation.
Cost model: by setting an upper limit to the cost of the magnet, the maximum coil width can be calculated for each aperture, taking into account the other components.
Total cost of the magnet = 400 kEUR/m (FCC-hh [ref])
Cost of the labour = 20 kEUR/m (LHC)
Aperture
150 mm
Bore
Coil
Structures
Iron
Example diagram with bore aperture set at 150 mm.
Aperture
150 mm
Aperture
150 mm
Coil width:
Structures:
SS cost: 10 EUR/kg (HL-LHC)
Iron yoke:
Fe cost: 8 EUR/kg (HL-LHC)
Materials | SC cost [EUR/kg] | Aspirational SC cost [EUR/kg]
Nb3Sn | 2000 | 700 (FCC target)*
ReBCO | 8000 | 2500 (realistic projection)**
The maximum total cost of the magnet is the same for both materials.
  ** 50 €/kAm: 1/3 of today prize (150€/kAm)
  Also based on projection of ref
  A. Molodyk and C. Larbalestier, Science, 2023
* 7€/kAm, FCC target 5€/kAm

## Slide 10: Method and Assumptions
A Python code is used to implement the analytic formulas for the cos-theta magnets in sector coil approximation.
Cost model: by setting an upper limit to the cost of the magnet, the maximum coil width can be calculated for each aperture, taking into account the other components.
The protection scheme consists in QH (or CLIQ) for classical insulated coils, limiting the hotspot temperature and the stored energy in the coils.
Materials | Hotspot T [K]
Nb3Sn | 350
ReBCO | 200
Courtesy of Tiina Salmi https://indico.cern.ch/event/1240045/
For the ReBCO, high cost requires small coil and very high current density  Protection will be a limiting factor
  Need to devise alternative protection schemes!
     Non-Insulated and Metal-Insulated coils
40 ms protection delay

## Slide 11: Method and Assumptions
A Python code is used to implement the analytic formulas for the cos-theta magnets in sector coil approximation.
Cost model: by setting an upper limit to the cost of the magnet, the maximum coil width can be calculated for each aperture, taking into account the other components.
The protection scheme consists in QH (or CLIQ) for classical insulated coils, limiting the hotspot temperature and the stored energy in the coils.
The margin limit is the limit due to the SC material itself, starting from the Bottura’s fit for the critical current density.
Materials | Operating T [K] | T margin [K]
Nb3Sn | 4.5 | 2.5 (HL-LHC)
ReBCO | 20 | 2.5
Jc refers to:
Nb3Sn: FCC cable target performance
ReBCO: Fujikura FESC-AP tape

## Slide 12: Method and Assumptions
A Python code is used to implement the analytic formulas for the cos-theta magnets in sector coil approximation.
Cost model: by setting an upper limit to the cost of the magnet, the maximum coil width can be calculated for each aperture, taking into account the other components.
The protection scheme consists in QH (or CLIQ) for classical insulated coils, limiting the hotspot temperature and the stored energy in the coils.
The margin limit is the limit due to the SC material itself, starting from the Bottura’s fit for the critical current density.
The stress limit considers the maximum mechanical stress we can have on the coils, starting from the analytical formula for the midplane pressure of cos-theta magnet in sector coil approx. (Reference: https://doi.org/10.15161/oar.it/143359 )
Materials | Peak Stress [MPa]
Nb3Sn | 150
ReBCO | 400
Currently, only stresses generated by Lorentz forces are considered.
LARP TQ
(P. Ferracin)
Tevatron dipole
(P. Ferracin)

## Slide 13: Dipoles A-B Plots
Allowed area
Forbidden area
Allowed area
Forbidden area
ReBCO is considered the baseline for 10 TeV.
Nb₃Sn is not considered for the 10 TeV as it falls short of the required performance.
It may be an option for the 3 TeV.
Allowed area
Forbidden area
NbTi is a good reference for the study. It can be also an option for the 3 TeV with the same tunnel of the 10 TeV.

## Slide 14: HTS ARC dipoles A-B plots
Budget: 400 kEUR/m for each magnet.
SC cost: 2500 EUR/kg (aspirational value).
These plots apply to ARC dipoles.
Operating temperature: 20 K
→ tungsten shield with a radius of 3 cm
Operating temperature: 10 K
→ tungsten shield with a radius of 4 cm
Operating temperature: 4.5 K
→ tungsten shield with a radius of 4 cm
ReBCO is considered the baseline for 10 TeV.
Allowed area
Forbidden area
Allowed area
Forbidden area
Allowed area
Forbidden area
The Limit curve includes:
Cost model: including coils, iron, structures and labour
Protection: Non-insulated or Metal-insulated cable
Margin: Fujikura FESC AP Tape for the Jc fit
Maximum midplane stress: 400 MPa

## Slide 15: Quadrupoles A-G Plots
Allowed area
Forbidden area
Allowed area
Forbidden area
Allowed area
Forbidden area
ReBCO is considered the baseline for 10 TeV.
Nb₃Sn is not considered for the 10 TeV as it falls short of the required performance.
It may be an option for the 3 TeV.
NbTi is a good reference for the study. It can be also an option for the 3 TeV with the same tunnel of the 10 TeV.

## Slide 16: HTS ARC quadrupoles A-G Plots
Allowed area
Forbidden area
Allowed area
Forbidden area
Allowed area
Forbidden area
Budget: 400 kEUR/m for each magnet.
SC cost: 2500 EUR/kg (aspirational value).
These plots apply to ARC quadrupoles.
Operating temperature: 20 K
→ tungsten shield with a radius of 3 cm
Operating temperature: 10 K
→ tungsten shield with a radius of 4 cm
Operating temperature: 4.5 K
→ tungsten shield with a radius of 4 cm
ReBCO is considered the baseline for 10 TeV.
The Limit curve includes:
Cost model: including coils, iron, structures and labour
Protection: Non-insulated or Metal-insulated cable
Margin: Fujikura FESC AP Tape for the Jc fit
Maximum midplane stress: 400 MPa

## Slide 17: HTS FF quadrupoles A-G Plots
Allowed area
Forbidden area
Allowed area
Forbidden area
Allowed area
Forbidden area
Budget: 800 kEUR/m for each magnet.
SC cost: 2500 EUR/kg (aspirational value).
These plots apply to FF quadrupoles.
Operating temperature: 20 K
→ tungsten shield with a radius of 3 cm
Operating temperature: 10 K
→ tungsten shield with a radius of 4 cm
Operating temperature: 4.5 K
→ tungsten shield with a radius of 4 cm
ReBCO is considered the baseline for 10 TeV.
The Limit curve includes:
Cost model: including coils, iron, structures and labour
Protection: Non-insulated or Metal-insulated cable
Margin: Fujikura FESC AP Tape for the Jc fit
Maximum midplane stress: 400 MPa

## Slide 18: FEM Crosscheck for Stress Curves
FEM models for a sector dipole and quadrupole in ANSYS were implemented.
A Python code able to work with Ansys software was developed to run FEM simulations with the same inputs as the analytical study.
In the comparison, the FEM curves are always more restricting than the analytical ones since they take the maximum pressure on the midplane instead of an average over the coil width.

## Slide 19: Combined Function Magnet
Arc:
Combined function magnets: B1, B1+B2 and B1+B3
B ≈ 8…16 T; G ≈ 320 T/m; G’ ≈ 7100 T/m2
Aperture ≈ 160 mm
Final focus:
Combined function magnets: B1, B2, B1+B2 , B1+B3
B ≈ 4…16 T; G ≈ 100…300 T/m; G’ ≈ 12000 T/m2
Aperture ≈ 120…300 mm
Quad into dipole:
(ReBCO @20 K)
Dipole into quad:
(ReBCO @20 K)
Preliminary results obtained with ANSYS in a sector coil approximation
Quadrupole inside dipole is more efficient, in agreement with US-MAP [ref]

## Slide 20: Combined Function Magnet
a1_quad
w_quad
w_dip
30 mm
30 mm
We would like to produce B-G plots in order to provide the allowed area for the combined function magnets.
Difficult to study analytically → Python-Ansys interface
Chart: B-G plot at 20 K
| 72.123255999999998 | 126.90125 | 176.34506999999999 | 204.92930000000001 | 245.65516 | 287.96249 | 334.69869 | 348.94319000000002
a1=25mm, T=20K | 15.5614 | 14.6228 | 13.6394 | 11.5894 | 10.3515 | 8.8415 | 7.0798 | 3.5074
a1=50mm, T=20K | 13.4546 | 12.3428 | 11.0556 | 9.726 | 6.9337 | 4.5102
a1=75mm, T=20K | 11.7349 | 10.3561 | 8.8823 | 6.8017 | 3.3089
a1=100mm, T=20K | 10.941 | 9.1017 | 6.6109 | 3.5206

## Slide 21: Conclusions
The allowed magnet aperture (A) - magnetic field (B) phase spaces are provided and discussed, representing the starting point to define possible beam optics which are also acceptable from a technological point of view.
To address the issue of neutrino flux in the straight sections, combined function magnets must be used in the Muon Collider. In this regard, we are working to identify realistic target designs from a technological point of view.
Thanks to the A-B plots, we were able to identify a target design, allowing us to begin studying specific designs.
  In particular, we are exploring a cos-theta design and a block coil design.
Courtesy of F. Mariani
Courtesy of L. Alfonso

## Slide 22
Thank you
for your attention
December 2024
1Sapienza University of Rome, 2INFN – Genoa , 3INFN and University of Milan
4Tampere University, 5CERN
D. Novelli1,2, L. Alfonso2, A. Bersani2, L. Bottura5, B. Caiffi2,
S. Farinon2, F. Mariani1, S. Mariotto3 , A. Pampaloni2, T. Salmi4
MuCol Italia – Torino

## Slide 23
Backup
slides
December 2024
1Sapienza University of Rome, 2INFN – Genoa , 3INFN and University of Milan
4Tampere University, 5CERN
D. Novelli1,2, L. Alfonso2, A. Bersani2, L. Bottura5, B. Caiffi2,
S. Farinon2, F. Mariani1, S. Mariotto3 , A. Pampaloni2, T. Salmi4
MuCol Italia – Torino

## Slide 24: HTS dipole A-B Plots
The curves shown in the plots are the limit curves,
i.e., for each aperture value the strictest limit is taken, excluding the limit for insulated magnets.
reduction
Cost
reduction
A reduction of HTS cost will result in wider design A-B range
A reduction of operating temperature will result in wider design A-B range
ARC [16T, 140 mm]
IR [10T, 300 mm]
ARC [16T, 140 mm]
IR [10T, 300 mm]

## Slide 25: HTS quadrupole A-B Plots
A reduction of HTS cost will result in wider design A-B range
A reduction of operating temperature will result in wider design A-B range
reduction
Cost
reduction
The curves shown in the plots are the limit curves,
i.e., for each aperture value the strictest limit is taken, excluding the limit for insulated magnets.
IR [115T/m, 290 mm]
ARC [240T/m, 170 mm]
ARC [330T/m, 130 mm]
IR [115T/m, 290 mm]
ARC [240T/m, 170 mm]
ARC [330T/m, 130 mm]