## Slide 1: SABRE North crystals meeting
Aldo Ianni
Lecce, Nov 27th, 2024

## Slide 2: NaI-40
Grown without Thallium from 10 kg of Astro Grade.
Broken into chunks to make NaI-41
(test growth from chunks).
Opportunity to take samples from tip, tail and middle part for ICP-MS assay.
keq = 0.67±0.1 from the fit
<5.8±0.7> ppb

## Slide 3: NaI-33 and NaI-35 tip/tail
keq = 0.59 ± 0.06
keq = 0.52 ± 0.04

## Slide 4: NaI-41
210Pb
cosmogenics
210Pb
preliminary
underground since December 15th, 2023
LY = 10.02 +/- 0.03 phe/keV
FWHM energy resolution: 15.7% @59.6 keV
39K: 5.7±0.9 ppb
keq = 0.63±0.1
Satisfactory results: important test toward
the production of NaI-42 from zone refined
powder
 | 39K [ppb] | 65Cu [ppb] | 85Rb [ppb] | 138Ba [ppb] | 133Cs [ppb] | 208Tl [ppm]
Tip | <4 | <5 | <0.8 | <0.2 | <0.3 | 520±4
Tail | 13.4±0.3 | <5 | <0.8 | 1.1±0.2 | 1.7±0.1 | 1343±10
Far Tail | 20.2±0.4 | 10.8±0.8 | <0.8 | 2.8±0.3 | 4.2±0.3 | 1607±12
Results of ICP-MS measurements

## Slide 5: Production of NaI-42
Zone refining of 12 kg of powder
Minimum 4 runs of ZR required
Production of crystal could start in Jan-Feb
Decision on encapsulation and transportation

## Slide 6: Production of NaI-Korea
15 kg of purified powder from COSINE to RMD
RMD will grow a crystal with 8 kg
RMD send samples of powder to LNGS and LSC for screening
After growth RMD send sample of tip and tail to LSC
Crystal enclosure at RMD
Transportation by boat
Crystal ready early January
GOALS:
  Test radiopurity from Korean powder with different growth method
  Could ask COSINE collaboration to make use of distilled water for powder purification
  An alternative to Merck

## Slide 7: ZR for crystal production
It takes place at MELLEN
Procedure:
  Dry powder for 1 week at RMD
  Increase temperature at 400 C
  Add SiCl4 for 20 min
  Remove gas from ampoule
  Seal ampoule
  Move ampoule to MELLEN
  Leak test
  Consolidation run
  ZR run 25 passes at 2 inch/h
keq = CS / CL segragation coefficient, the lower k the greater impurities are moved away from crystal matrix

## Slide 8: ZR accident
During first run for NaI-42 production: ampoule burst
Caused by leak in ampoule
Risk mitigation:
  Consolidation run done at MELLEN
  Leak test before starting ZR at MELLEN

## Slide 9
H2O + C –> H2 + CO water consumes C coating at high temperature
NaI + H2O --> NaOH + HI water produces NaOH which dissolve fused quartz
SiCl4 + 2H2O --> SiO2 + 4HCl
NaOH + HCl --> NaCl + H2O SiCl4 consumes NaOH
Side effect of HCl
NaI + HCl --> NaCl + HI
2HI --> I2 + H2

## Slide 10: ZR efficiency
keq can be measured from phase diagram, crystal growth (tip/tail), zone refining data
  K ~ 0.45 – 0.67 expected significant reduction
  Rb ~ 0.18 – 0.37 expected very significant reduction
  Pb ~ 1.1 (PbI2) no reduction expected, slight worsening
    If Pb in the powder it can be removed by purging during ZR (PbI2 volatile at 661 C) or, if coming from water, improve water quality in powder production

## Slide 11: ZR Run4
Sample Run4 | 39K [ppb] | 65Cu [ppb] | 85Rb [ppb] | 133Cs [ppb] | 138Ba [ppb] | 208Pb [ppb]
 | LSC/ Seast. | LSC/ Seast. | LSC/ Seast. | LSC/ Seast. | LSC/ Seast. | LSC/ Seast.
powder | 7 | 5 | <0.2 | 1 | 3.6 | 1.1
Zone 1 | <4 | <4 | <0.8(<0.6) | <0.3 | <0.3 | 2.0±0.3(2)
Zone 2 | <4 | <4 | <0.8(<0.6) | <0.3 | 1.2±0.3 | 2.0±0.2(1.3)
Zone 3 | 10±0.4 | <4 | <0.8(<0.6) | <0.3 | 2.7±0.2 | 1.6±0.3(1.2)
Zone 4 | 22±0.5 | <4 | <0.8(<0.6) | 1.1±0.1 | 8.1±0.5 | 1.9±0.3(1.2)
Zone 5 | 65±2 | 12±2 | <0.8(<0.6) | 9±0.2 | 17±0.9 | 1.4±0.3(1.1)
All beta-like contribution in ROI for NaI-33 spectral fit (~30% of rate) corresponds to ~0.4 ppb of 85Rb

## Slide 12: Qualitative comparison with the model: K
RUN1
RUN4
Within 80% length ~92% reduction
Within 75% length ~95% reduction

## Slide 13: Qualitative comparison with the model: Ba
RUN4
Within 80% length ~77% reduction
Within 75% length ~84% reduction
RUN4
Ba is a proxy of Ra

## Slide 14: Expected background in SABRE crystals
Use spectral fit from NaI-33
Apply reduction as from zone refining purification
Produce spectrum with MC code