## Slide 1
Millisecond flash lamp treatment for SRF accelerating cavities
Cristian Pira, INFN
Status of the activity at March 2024
cristian.pira@lnl.infn.it
Slawomir Prucnal, HZDR

## Slide 2: Goal
The goal of Msec Flash annealing project is to develop a novel thermal process to improve performances of SC coating by suppressing (reducing) Cu substrate heating
I.FAST WP9 demonstrate that Tc and performances of Nb3Sn coating are strongly affected by substrate
Tc of Nb3Sn coatings depends on the thickness of Nb barrier layer

## Slide 3: First results on planar samples
NbN on Cu
Nb on Cu
Nb3Sn on Cu
Material crystallinity improved in all thin film superconductor tested
On Nb and NbN coatings FLA produce a narrower hysteresis curve
On Nb3Sn coatings FLA improve lattice parameter (closer to bulk values)

## Slide 4: FLA system for 6 GHz cavities
Holding system ready
Vacuum system designed and commissioned
First test planned in June 2024
Holding system for the flash lamp and cavity
3D design of the complete system

## Slide 5: Schedule
MS1 - Demonstrated FLA improvement (Nb on Cu)
MS2 – FLA system for 6 GHz ready
MS3 – Nb3Sn Tc improved by FLA
MS4 - Demonstrated FLA uniformity (Nb on Cu 6GHz)
MS5 – High Q cavity at 4.2 K
today
Sample test on track (MS1)
Delay of 3 months on MS2

## Slide 6: Collaboration with industrial partners
Piccoli Srl produced 2023 more than 30 seamless 6 GHz Cu cavities for WP9 and FLA project with an optimized process

## Slide 7: Sustainability
Our technology will significantly reduce the environmental impact and energy-costs of SRF accelerator technology:
The goal is to realize SC resonant cavities operating at higher T than bulk Nb reducing cryogenic power costs by 60%
The thermal load and hence the temperature throughout the entire substrate is much lower compared to conventional annealing: FLA consume less energy (20-30% power reduction (1), resulting in a reduction of CO2 emissions
(1) Rovak GmbH experience on Semiconductors