## Slide 1: TARGET DEVELOPMENTS AT LUNA
Denise Piatti1 and Matteo Campostrini2
1 = University and INFN of Padua, via Marzolo 8 35136 Italy
2 = INFN - Laboratori Nazionali di Legnaro, viale dell’Università 2 35020 Italy

## Slide 2: Where and how are they produce?
Perspective at the Bellotti IBF workshop, LNGS (Italy), October 8th - 10th 2025
Speaking of LUNA
JUNA
2400 m underground
400 kV: H+, He+, He++
Imax = 1200 e𝜇A
Since 2021
Felsenkeller
45 m underground (shallow)
5 MV: H+, He+, C+, C++
Imax = 30e𝜇A
Since 2019
LUNA
1400 m underground
50 kV: H+, He+
400 kV: H+, He+
Imax = 100 -1000 e𝜇A
Since 1991/2003
CASPAR
1290 m underground
1 MV: H+, He+
Imax = 250 𝜇A
Since 2017
Bellotti IBF
1400 m underground
3.5 MV: H+, He+, C+, C++
Imax = 1000 e𝜇A
Since 2023

## Slide 3: A successful 35 years long story…
Reaction | Accelerator | Astrophysical Motivation/Scenario
D(α,γ)6Li; 3He(α,γ)7Be; D(p,γ)3He | LUNA400kV | Big Bang Nucleosynthesis (BBN), Lithium problem(s)
3He+3He; D(p,γ)3He | LUNA50kV | pp-chain and Solar neutrinos
6Li(p,γ)7Be | LUNA400kV | Stars, cosmic-ray spallation and BBN; Resonance NOT confirmed
12,13C(p,γ)13,14N | LUNA400kV | CNO cycle kick off reactions; only few, poorly constrained data
14,15N(p,γ)15,16O | LUNA400kV | CNO cycle bottleneck;
17,18O(p,α)14,15N | LUNA400kV | CNO cycle; crucial for oxygen isotopic abundance in AGB stars
16,17,18O(p,γ)17,18,19F | LUNA400kV | CNO cycle and CNO leak
20,21,22Ne(p,γ)21,22,23Na | LUNA400kV | NeNa cycle; affecting abundances up to P
23Na(p,γ)24Mg | LUNA400kV | NeNa-MgAl cycle link
25Mg(p,γ)26Al | LUNA400kV | MgAl cycle; poorly constrained resonances dominate the rate
13C(α,n)16O, 22Ne(α,γ)26Mg | LUNA400kV | s-process crucial for production of isotopes heavier than iron
Perspective at the Bellotti IBF workshop, LNGS (Italy), October 8th - 10th 2025

## Slide 4: Where and how are they produce?
… but also painful…
Perspective at the Bellotti IBF workshop, LNGS (Italy), October 8th - 10th 2025
LUNA performs direct measurement for which some ingredients are required:
High stability and intensity beam
Low beam spread
High efficiency and resolution
Low intrinsic background
Versatile geometry
…
High density
Favorable stoichiometry
High stability under irradiation
Wide thickness range
High purity
Not fragile, easy to handle
Enriched on demand
Cheap
…

## Slide 5: Where and how are they produce?
… indeed
Perspective at the Bellotti IBF workshop, LNGS (Italy), October 8th - 10th 2025
The perfect target is a unicorn!
PERFECT
TARGET

## Slide 6: Where and how are they produce?
LUNA Solid Targets - Oxygen Targets
The (recent) aim: the first direct determination of the 64.5 keV resonance of the 17O(p,𝛾)18F reaction
Technique: anodic oxidation of Ta in enriched (at 90% level in 17O) water solution which acts as the electrolyte
Perspective at the Bellotti IBF workshop, LNGS (Italy), October 8th - 10th 2025
pot for
enriched water

## Slide 7: Where and how are they produce?
LUNA Solid Targets - Oxygen Targets
The (recent) aim: the first direct determination of the 64.5 keV resonance of the 17O(p,𝛾)18F reaction
Technique: anodic oxidation of Ta in enriched (at 90% level in 17O) water solution which acts as a electrolyte
Target features [Gesué, R.M. et al., PRL 133 (2024), Caciolli, A. et al, EPJ A 48 (2012) and references therein]:
easy and fast to produce (1h per target on average)
uniform
well known target stoichiometry, Ta2O5
well known target stability (10-20% degradation with Qtot = 25-30 C)
well known voltage-thickness relation in the range 50 - 400 nm
target areal density of 1017-1018 atoms/cm2
online characterization via NRRA doping the solution with 18O
if handled with care no contaminants introduced in the production
SO FAR IT SEEMS VERY CLOSE TO THE UNICORN!!!!
BUT….
Perspective at the Bellotti IBF workshop, LNGS (Italy), October 8th - 10th 2025

## Slide 8: Where and how are they produce?
LUNA Solid Targets - Oxygen Targets
Perspective at the Bellotti IBF workshop, LNGS (Italy), October 8th - 10th 2025
SO FAR IT SEEMS VERY CLOSE TO THE UNICORN!!!!
BUT
Ta backing is a sponge for contaminants (bulk and surface) [Campostrini, M. et al., EPJ ST 233 (2024)]:
Superficial Fluorine can be reduced by 3 orders of magnitude via acid bath
Boron contamination is reduced by 2 orders of magnitude via acid bath
Deuterium, however, could be reduced by a factor of 4 applying a Mo coating to the Ta but this was not useful for the 17O(p,𝛾)18F investigation
    AND GUESS WHAT…
Good electrical
and thermal conductivity
high Z
and of course suitable for anodic oxidation
Low H permeability [Katsuka H., J. Phys. Chem. Solids 43 (1982)]

## Slide 9: Where and how are they produce?
LUNA Solid Targets - Oxygen Targets
SO FAR IT SEEMS VERY CLOSE TO THE UNICORN!!!!
BUT
Ta backing is a sponge for contaminants (bulk and surface) [Campostrini, M. et al., EPJ ST 233 (2024)]:
Superficial Fluorine can be reduced by 3 orders of magnitude via acid bath
Boron contamination is reduced by 2 orders of magnitude via acid bath
Deuterium, however, could be reduced by a factor of 4 applying a Mo coating to the Ta but this was not useful for the 17O(p,𝛾)18F investigation
AND GUESS WHAT…
Perspective at the Bellotti IBF workshop, LNGS (Italy), October 8th - 10th 2025
ROI
At this point you can only be smart [Gesué, R.M. et al., PRL 133 (2024)]

## Slide 10: Where and how are they produce?
LUNA Solid Targets - Carbon Targets
The aim: the measurement of the 13C(𝛼,n)16O reaction cross section.
Technique: Evaporation (PROUDLY) performed at ATOMKI, using a Leybold UNIVEX 350 vacuum evaporator, 99% enriched 13C powder and Ta as backing
Perspective at the Bellotti IBF workshop, LNGS (Italy), October 8th - 10th 2025
Cu melting pot
Adjustable arm
Ta holder

## Slide 11: Where and how are they produce?
LUNA Solid Targets - Carbon Targets
The aim: the measurement of the 13C(𝛼,n)16O and 12,13C(p,𝛾)13,14N reaction cross sections.
Technique: Evaporation (PROUDLY) performed at ATOMK, using a Leybold UNIVEX 350 vacuum evaporator, 99% enriched 13C powder and Ta as backing
Target Features [Ciani, G.F. et al, PRL 127 (2021) and Ciani, G.F. et al., EPJ A 56 (2020)]:
powder stable with time
uniform
high stability under proton irradiation
target stability under 𝛼 irradiation was poor -> setup designed to change target often
Online monitoring such as NRRA not available -> Peak shape analysis
Perspective at the Bellotti IBF workshop, LNGS (Italy), October 8th - 10th 2025
Made in ATOMKI offline

## Slide 12: Where and how are they produce?
LUNA Solid Targets - Fluorine Targets
The aim: the measurement of the 19F(p,𝛾)20Ne reaction cross section
Technique:
Evaporation starting from CaF2 powder, performed in ATOMKI (favorable stoichiometry but bad stability)
Implantation on Ta and Fe, performed at University NOVA in Lisbon, with 1015-1017 atoms/cm2
Fluorination, performed by external company, Ta was dipped in gaseous F2 at 500 mbar for 2’ and at 100°
Perspective at the Bellotti IBF workshop, LNGS (Italy), October 8th - 10th 2025
3
2
2

## Slide 13: Where and how are they produce?
LUNA Solid Targets - Fluorine Targets
The aim: the measurement of the 19F(p,𝛾)20Ne reaction cross section
Technique:
Evaporation starting from CaF2 powder, performed in ATOMKI (favorable stoichiometry but bad stability)
Implantation on Ta and Fe, performed at University Nova in Lisbon, with 1015-1017 atoms/cm2 and HZDR in Dresden
Fluorination, performed by external company, Ta was dipped in gaseous F2 at 500 mbar for 2’ and at 100°
Target features:
both target types thin as desired
and stable up to high accumulated charge
stoichiometry under investigation
Boron content similar in both Fe and Ta
Perspective at the Bellotti IBF workshop, LNGS (Italy), October 8th - 10th 2025
3
A paper is in preparation!

## Slide 14: Where and how are they produce?
LUNA Targets - Gas target
Perspective at the Bellotti IBF workshop, LNGS (Italy), October 8th - 10th 2025
Three differential pumping stages windowless gas target
Pressure in the chamber 0.3 - 2 mbar and kept constant within 0.5%
Target density of 1015 atom/cm2
High stability under irradiation
Recirculation mode for expensive gas
Calorimeter for current reading
High precision obtained for the p+D measurement
High purity BUT contaminants along beamline and at the beam stop must be annoying (B, C, N and F)
[Ferraro F., et al., EPJ A 54 (2018); Mossa V., et al., EPJ A 56 (2020) and reference therein]
Ultrasonic bath to reduce contaminants level and runs w. noble gas to subtract it

## Slide 15
Speaking of Perspectives

## Slide 16
CN facility
AN2000 facility
Laboratory of Materials Physics for Nuclear Physics
NATIONAL LABORATORIES OF LEGNARO (LNL)
Other Laboratories involved in targets production:
LNL (Padua-Italy)
LNGS (L’Aquila-Italy)
ATOMKI (Debrecen-Hungary)
University NOVA (Lisbon-Portugal)
HZDR (Dresden-Germany)
Edinburgh University (UK)
Notre Dame (USA)
……

## Slide 17
Legnaro WG activities
LNL Group:
Valentino Rigato (DT)
Carlo Roncolato (PT)
Matteo Campostrini (IIIT-TD)
INFN CSN3 nuclear physics
Solid targets development and characterization
INFN CSN5 interdisciplinary physics
Functional coatings with nanostructured multilayers
Sigle ion irradiation for quantum technologies
Ion-matter interaction and beam induced damage
INFN Technological Transfer
Large area irradiations, accelerated tests for satellite components
Nanostructured coatings Mechanical reinforcement coatings
Legnaro laboratory activities and user's support
LNL Target service (technical support and IBA characterization)
SPES (target analysis, beam diagnostics, coatings…) Accelerator Division (Beam characterization, coating for RF accelerator windows)
……..
Research Fields:
Surface engineering and materials synthesis
Characterizations (IBA, morphological Compositional and structural analysis)
High Vacuum deposition systems design and development
Ion beam irradiation
Detector testing

## Slide 18
LNL ion beam facilities
Available beams:
1H+ 0.8÷5.5 MeV
2H+ 0.8÷5.5 MeV
3He+ 0.8÷5.5 MeV
4He+ 0.8÷5.5 MeV
Pulsed beam
Available beams:
1H+ 0.2÷2.0 MeV
3He+ 0.2÷2.0 MeV
4He+ 0.2÷2.0 MeV
1H+ and 4He+ µ-probe 2-5 µm spot size
AN2000
CN
Main activities:
IBA (EBS,NRA and PIXE)
ASIF (large area irradiation HE-facility)
Main activities:
IBA (EBS, NRA)
ASIDI (Single ion irradiation)
ASIF (large area irradiation LE-facility)
Detector testing
Quantum technology

## Slide 19
LNL ion beam facilities
AN2000
CN
µ-probe scattering chamber
(2-5 µm spot size)
IBA scattering chamber
(1-25 mm2
spot size)
Total IBA scattering chamber
(1-25 mm2
spot size)

## Slide 20
Large area ion beam irradiations
Large area ASIF irradiation facility (ASI Supported Irradiation Facilities )
  Monochromatic Beams: 1H+, 4He+
  Energy: 0.2÷5.5 MeV
Spatial uniformity: target ≤ ±1%
XY beam scanning (up to 20cmx20cm)
Beam dynamics design
https://doi.org/10.1063/1.2982370
High temperature Superconductive materials (REBCO), compact fusion reactor
Single Photon Emitters production for Quantum Technology
Photo luminescence emission
Ion-matter interaction
satellite optical components
Irradiation Activities…

## Slide 21
Laboratory of Materials Physics for Nuclear Physics
Alkali materials (Na, Mg,…)
Materials:
NaNbO3, Mg2Si
Characteristics:
Heated sample holder (up to 600 °C)
Characteristics:
3 sputtering source (50mmx140mm)
2 sputtering source (150mmx230mm)
Active gettering system
Optical emission plasma diagnostics for reactive processes
Different power supply technologies (HiPIMS, DC, pulsed-DC, RF)
2 different sample holder
Materials: Pure materials (Ta, Ti, Zr, Cr, Cu, Nb…)
Compounds:
Oxides (natural O, 16O and 17O)
Nitrides (natural N, 14N, 15N)
Hydrides (natural H, Deuterium)
Pure metal and compounds materials synthesis
Characterization techniques:
Optical microscope
SEM (Scanning electron microscope)
EDS (Energy-dispersive X-ray spectroscopy)
AFM (Atomic force microscope)
Avaible in other collaborators laboratory:
XRD (X-ray Diffraction)
Raman
TEM (transmission electron microscope)
STEM (scanning TEM)
FIB (focused ion beam)
…
Sputtering systems

## Slide 22
Laboratory of Materials Physics for Nuclear Physics
Magnetron sputtering PVD deposition process
DOI: 10.13140/RG.2.1.3855.5605
Magnesium Silicide (Mg2Si) deposition (Argon plasma process gas)

## Slide 23
Magnetron sputtering PVD deposition process
DOI: 10.13140/RG.2.1.3855.5605
High quality coatings
Ion bombardment assisted film growth
Low Oxygen contamination
Active gettering system
Synthesis of compound targets using REACTIVE magnetron sputtering technology
Nitrides, Oxides and Hydrides with natural and isotopically enriched gas
Plasma study and monitoring
Optical emission spectroscopy (UV-VIS) and Time resolved OES
Process control and system improvements
Laboratory of Materials Physics for Nuclear Physics
Magnesium Silicide (Mg2Si) deposition (Argon plasma process gas)

## Slide 24
Laboratory of Materials Physics for Nuclear Physics
NRA
D(3He, p)4He
1MeV 3He AN2000
EBS (p,p) 2MeV, AN2000
Hydrides targets
ZrD2
EBS (α,α) 1.6MeV, AN2000
Nitrides targets
Ta15N
Oxides targets
Ta2natO5
EBS (α,α) 2MeV, AN2000

## Slide 25
23Na(p,a)20Ne
ELDAR
Elements in the Lives
and Deaths of stARs
14N(p,g)15O
SoCIAL
SOlar Composition Investigated At Luna
24Mg(p,g)25Al
experiments at LUNA400
experiments at BELLOTTI ion beam facility
12C+12C
CaBS
Carbon Burning in Stars
14N(p,g)15O
First experiment at Bellotti facility
Targets production, characterization and experimental supports
LNL is involved in LUNA experiments

## Slide 26
14N(p, g)15O target production and characterization (first IBF experiment)
Fluorine contaminant reduction
Oxygen contaminant reduction
RBS characterization
High endurance target
19F(p,αγ)16O @ LNGS facility
Acid cleaning procedure
14N(p, g)15O experiments

## Slide 27
14N(p, g)15O target production and characterization (first IBF experiment)
Fluorine contaminant reduction
Oxygen contaminant reduction
RBS characterization
High endurance target
19F(p,αγ)16O @ LNGS facility
Acid cleaning procedure
14N(p, g)15O experiments

## Slide 28
14N(p, g)15O target production and characterization (first IBF experiment)
Fluorine contaminant reduction
Oxygen contaminant reduction
RBS characterization
High endurance target
TiN
Ta14N
19F(p,αγ)16O @ LNGS facility
Acid cleaning procedure
14N(p, g)15O experiments
14N isotopically enriched (99.99% )

## Slide 29
14N(p, g)15O target production and characterization (first IBF experiment)
Fluorine contaminant reduction
Oxygen contaminant reduction
RBS characterization
High endurance target
TiN
Ta14N
NRA Oxygen No detectable
16O(d,p0)17O
EBS (α,α) stoichiometry measurement TaN compound
DOI: 10.1140/epja/s10050-025-01658-7
DOI: 10.1140/epja/s10050-025-01561-1
DOI: 10.1140/epjs/s11734-024-01349-2
19F(p,αγ)16O @ LNGS facility
EBS (α,α) measurement stoichiometry TiN compound
Acid cleaning procedure
14N(p, g)15O experiments
14N isotopically enriched (99.99% )

## Slide 30
High lifetime:
Max 12C implantation power: 400 W
Expected lifetime: 50-100 C
Characterization pre/post irradiation with IBA (AN2000, CN), SEM – EDS, AFM, RAMAN
Target design and production
12C + 12C experiment
Purity : semiconductor grade
Structure: selected fine grain size

## Slide 31
High lifetime:
Max 12C implantation power: 400 W
Expected lifetime: 50-100 C
Characterization pre/post irradiation with IBA (AN2000, CN), SEM – EDS, AFM, RAMAN
Purity : semiconductor grade
Structure: selected fine grain size
Thich Ta-PVD coating:
prevent BIB for eventual target failure
Graphite 1-3mm
Tantalum coating
>3µm
Cu backing
~1-3mm
Target design and production
3.9 µm
12C + 12C experiment

## Slide 32
Preliminary irradiation test performed at Felsenkeller HZDR (2024) E. Masha (HZDR) unpublished data LUNA test performed at IBF 2025 F. Ferraro (LNGS) unpublished data
NOT IRRADIATED
12C IRRADIATED
Sintered Graphite
No evidence of damage after 7.5C of 2.9MeV of 12C+ beam
Other Carbon
Strong damage after 0.6C of 2.9MeV of 12C+ beam
Target testing and analysis
12C + 12C experiment
Graphite irradiated target

## Slide 33
RAMAN spectroscopy proves amorphization of graphite surface IBA analysis shows no contamination on irradiated regions
Preliminary irradiation test performed at Felsenkeller HZDR (2024) E. Masha (HZDR) unpublished data LUNA test performed at IBF 2025 F. Ferraro (LNGS) unpublished data
NOT IRRADIATED
12C IRRADIATED
Other Carbon
Strong damage after 0.6C of 2.9MeV of 12C+ beam
(RAMAN analysis F. Pezzoli (Bicocca University)
Target testing and analysis
12C + 12C experiment
Graphite irradiated target
Sintered Graphite
No evidence of damage after 7.5C of 2.9MeV of 12C+ beam

## Slide 34
The target was:
stable in air
good adhesion
good uniformity
RBS confirm a good stoichiometry
SEM and EDS shows nanometrically crystal enriched in Na
RBS spectrum NaNbO3 /SI Eα=1.6MeV
ΘEBS=160°
NO degradation up to 35C
23Na(p,γ)24Mg, BGO detector
L. Barbieri and C. Bruno (PI)
First test of NaNbO3 Sputtered Target endurance tests 23Na(p,γ)24Mg, BGO detector
23Na(p,α)20Ne experiment

## Slide 35
ELDAR experiment setup for 23Na(p,α)20Ne analysis (PI C. Bruno)
23Na(p,α)20Ne experiment

## Slide 36
ELDAR experiment setup for 23Na(p,α)20Ne analysis (PI C. Bruno)
L. Barbieri and C. Bruno
The measurement cannot be performed due to the BIB caused by 11B and 6Li contamination
23Na ROI
6Li(p, 3He)a
6Li(p, a)3He
23Na(p,α)20Ne experiment
23Na(p,a)20Ne ROI

## Slide 37
thickness > 2.5mm (Epmax=400keV)
SETUP for NRA @ AN2000
J.Liu et al. NIMB190(2002)107
B reduction using PVD Ta thick coating
Li reduction in Vapour phase
23Na(p,α)20Ne experiment

## Slide 38
Boron and Lithium contamination reduction: results
Lithium content reduction ~ 80% ~2 ppm of 6Li
Ta(PVD-LNL)
Ta(acid etched LNL)
Ta(after laser cut)
NRA 11B(p,α)8Be[2α]
Ep=680keV, ~13µm Mylar
ΘNRA=150° ; sample tilt=70°
18O(p,α)15N
=Blue color
Boron content reduction ~ 90%
~2-3 ppm of 11B
23Na(p,α)20Ne experiment
NRA 7Li(p,α)4He
Ep=1250keV, ~26µm Mylar
ΘNRA=150° ; sample tilt=0°

## Slide 39: LUNA Collaboration
D. Basak, T. Chillery, R. Gesue'*, M. Junker, F. Ferraro | INFN LNGS *and GSSI, Italy
R. Biasissi, C. Broggini, A. Caciolli, R. Menegazzo, D. Piatti, J. Skowronski | Università di Padova and INFN Padova, Italy
A. Formicola, C. Gustavino, M. Vagnoni* | INFN Roma 1 *and Università degli Studi della Campania, Italy
D. Bemmerer, A. Boeltzig, E. Masha | HZDR Dresden, Germany
L. Csedreki, Z. Elekes, Zs. Fülöp, Gy. Gyürky, T. Szücs | MTA-ATOMKI Debrecen, Hungary
M. Lugaro | Konkoly Observatory and ELTE University Budapest, Hungary
U. Battino, O. Straniero | INAF Osservatorio Astronomico di Collurania, Teramo, Italy
P. Corvisiero, P. Prati, M. Rossi, S. Zavatarelli | Università di Genova and INFN Genova, Italy
R. Depalo, A. Guglielmetti | Università di Milano and INFN Milano, Italy
A. Best, D. Dell'Aquila, A. Di Leva, D. Mercogliano, G. Imbriani, D. Rapagnani | Università di Napoli and INFN Napoli, Italy
F. Cavanna, P. Colombetti, G. Gervino | Università di Torino and INFN Torino, Italy
M. Aliotta, L. Barbieri, R. Bonnell, C. Bruno, A. Compagnucci, L. Dalla Vedova, T. Davinson, J. Marsh, D. Robb | University of Edinburgh, United Kingdom
G. Ciani | Università di Bari and INFN Bari, Italy
M. Campostrini, V. Rigato | INFN LNL, Italy

## Slide 40: Thank you for your attention