## Slide 1
Meeting of the EURO-LABS WP2.5.2 Collaboration May 15th, 2025 (Online)
Target manufacturing activities at INFN-LNL
J. Esposito, on behalf of INFN- Legnaro National labs (LNL) targets group- juan.esposito@lnl.infn.it
A quick review of techniques focused on different topics
“Target production” for nuclear physics (NP) experiments
“Target production” for applied NP (radioisotopes production)
“Quality Control techniques: nuclear targets characterization ”

## Slide 2: Target production at LNL Nuclear Physics (NP) studies

## Slide 3: Target production at LNL NP studies
Target production at LNL – Nuclear physics studies
Text
Targets for nuclear physics experiments typically are thin films of enriched isotopes obtained by various techniques:
- lamination (few mg/cm2)
- vacuum evaporation (few tens - few hundred ug/cm2)
There are different types of fabrication:
• self supporting
• with backing
• strip-targets
sandwich-target
• plunger – target

## Slide 4
Text
Self supporting target of 112Sn produced by cold rolling; the achieved thickness of 2.78 mg/cm2.
(e.g. in the picture a target used for an experiment at ANL USA (June 2023)
Target of 108Pd, thickness 1.3 mg/cm2, on Au backing of 3.8 mg/cm2 obtained by thermal evaporation (Thermal-based PVD) in vacuum (W crucible). The Au backing was previously prepared by rolling.
Thickness below the minimum stated in the literature (4 mg/cm2)
Adhesion improved by special heat treatment on the Au backing
Target production at LNL – Nuclear physics studies

## Slide 5
Text
Plunger-type target of 148Sm thickness 1 mg/cm2 attached to a 1.5 mg/cm2 backing of Ta. The target is stored under vacuum (4.5·10-7 mbar) to prevent oxidation of 148Sm.
64Ni/68Zn/64Ni - "Plunger"-type sandwich target consisting of a 2 mg/cm2 Zn core body, obtained by rolling and bonded on Plunger frame, on which a 0.4 mg/cm2 Ni film was evaporated on both sides. Subsequently "stretched" with a special cone.
Target production at LNL – Nuclear physics studies

## Slide 6: LNL Sputtering chamber and design
Characteristics:
3 sputtering source (50mm x 140mm)
2 sputtering source (150mm x 230mm)
Active gettering system (porous Ti /Ba/Al)
Optical emission plasma diagnostics for reactive processes (deposition of compound layes
Different power supply technologies: High-power Impulse Magnetron Sputtering (HiPIMS, DC, pulsed-DC, or RF)
2 different sample holder
Target production at LNL – Nuclear physics studies

## Slide 7
TaN 2.8*1018 atoms/cm2 deposited on 7.8*1017 atoms/cm2 of high purity Ta interlayer Tantalum substrate
LUNA solid target development by PVD magnetron sputtering technology
Ta
TiN 2.7*1018 atoms/cm2 deposited Tantalum substrate and Silicon substrate (for EBS analysis)
429 keV 15N resonance scan
of TaN and TiN
278 keV 14N resonance
scan of TaN
After an irradiation of 15 C
Analysis A. Compagnucci
Ti
Production and EBS characterization performed @ LNL (AN2000)
Low energy resonance scan and endurance test performed @ LNGS (LUNA400)
Target production at LNL – Nuclear physics studies
Targets preparation for LUNA experiments (Gran Sasso Laboratory): Nitrides (TanatN, ZrnatN, TinatN)
High-Z metals nitrides for reduction of neutrons production for LUNA-MV
TaN target produced by PVD technics using 14N enriched gas
EBS analyses

## Slide 8: Target production at LNL Applied NP studies (emerging radioisotopes production for thenanostics radiopharmaceuticals)

## Slide 9
Target production at LNL – Nuclear physics applications
Radioisotope of Interest
Dissolution
Extraction/
separation
Purification
Pure radioisotope
Radio-
pharmaceutical
preparation
Target activation
Target recovery
Target
preparation
Radiochemistry
process
Quality Control
Cyclotron irradiation
Nuclear physics studies
Contaminants
Cyclotron production cycle

## Slide 10
Target production at LNL – Nuclear physics applications
Target material to be irradiated
Often isotopically enriched material
very expensive how is it provided?(powder, crystal bar, foils..)
For production
For nuclear cross section
based on nuclear physics reaction for the production of the specific RN
Usually >150 µm
to exploit the optimal energy range to maximize production
1-10 µm (100s µg/cm2)
The information on the exact amount is mandatory
easily handled for safe radiochemistry process in hot-cell
easily handled for safety during the dismount after the irradiation
Selected backing material
Chemical inertness
High thermal conductivity
Mechanical strenght
Low activation under the beam
Material used as monitor foil (e.g., Al foil 25 µm thick)
Target system
thermo-mechanical strenght to withstand the thermal power deposited during the irradiation
Ø and thickness based on the cyclotron target station
Optimal thickness
Solid targets for medical application: requirements

## Slide 11
Advantages
Starting material powder
Efficiency 95-98% no losses of material
Low amount of starting material is needed
Thickness: 0.1-20 µm
Two targets are deposited simultaneously
Process duration 10-40 h
Requirements:
Metal substrates
Metal powder (irregular shape and small size <20 µm)
This deposition technique exploits the phenomenon of vibrational motion of metallic powder in a static electric field
High Energy Vibrational Powder Plating (HIVIPP)
For thin targets aimed at nuclear cross-section measurements
Target production at LNL – Nuclear physics applications
H. Skliarova, S. Cisternino, et al., Nuclear Instruments and Methods A, 2020
S. Cisternino, et al., Instruments, 2022
S. Cisternino, et al., Materials, 2023
HIVIPP apparatus @LNL
I. Sugai, Nuclear Instruments and Methods A, 1997

## Slide 12
Starting materials powder or foil
97% efficiency No loss of isotope-enriched material
Directly bonding of different materials (target and backing)
  protective thin layer in between instead of costly inert material backings
150 m - mm thickness pellet targets for production
Sintering of high melting point materials (metal or oxide)
Advantages respect to conventional sintering
  High heating rates (up to 1000 °C/min)
  Very short sintering times (min instead of hours)
Typical experimental conditions:
Voltage 5-10 V
Current intensity 103-104 A
Pressure 5-100 MPa
fast and versatile sintering technique used for several applications in different fields
Spark Plasma Sintering (SPS)
Advantages for cyclotron solid targets:
Target production at LNL – Nuclear physics applications
Components:
water-cooled vacuum chamber
vacuum system
vertical single-axis hydraulic press
specially designed water-cooled punch electrodes
AC generator
temperature and other sensors
PLC controlling all the sintering parameters
custom graphite punches and die
Dedicated SPS machine (TT_Sinter) tailored for targets manufacturing (for research)
Very fast process cycle
Customizable tooling
Easy to use and maintain
Affordability
Skliarova et al., J. Phys: Conf. Ser., 2020;
Sciacca et al., Molecules 2021;
Cisternino et al., NMB 2022
Cisternino et al., Ceramics International, 2025

## Slide 13: Spark Plasma Sintering (SPS): ZnO target example
12
SPS process
Main procedure steps
ZnO powder sintering
ZnO pellet-Au foil adhesion
Target (ZnO-Au/Au-Nb)
Metallurgical interface analysis – SEM
Cisternino et al.,Ceramics International,2025
Final results: ZnO target coin

## Slide 14
Target production at LNL – Nuclear physics applications
High Energy Vibrational Powder Plating (HIVIPP) for xs measurements targets
Skliarova et al., NIMA 2020;
Cisternino et al., Instruments 2022;
Cisternino et al., Materials 2023
Spark Plasma Sintering (SPS) for thick target >150 µm
Skliarova et al.,J.Phys:Conf.Ser.,2020;
Sciacca et al., Molecules 2021;
Cisternino et al., NMB 2022
Cisternino et al.,Ceramics International,2025
Magnetron sputtering (MS) for thin and thick targets
INFN patent WO/2019/053570, 2019
Skliarova et al., Instruments 2019;
Skliarova Molecules 2019;
Kotliarenko et al., Materials 2023
Some examples of tested targets

## Slide 15: Target production at LNL Quality Control (QC) techniques: nuclear targets characterization

## Slide 16
IBA facilities for nuclear target characterization @ LNL
-15° beam line at CN facility [a), b)]
EBS analysis
PIXE analysis
PIGE analysis
0° beam line (m-beam) at AN2000 facility [c)]
EBS analysis
PIXE analysis
60° beam line at AN2000 facility [d)]
EBS analysis
ERDA analysis
quantitative determination of composition
thickness measurements in terms of dose (at/cm2)
depth profiles analysis
non-destructive
High accuracy and resolution
c)
d)
b)
a)
Target characterization at LNL

## Slide 17
IBA facilities for nuclear target characterization @ LNL
Dedicated experiments in nuclear target analysis:
Deposition of Elements on Substrates (DES) involved in NUMEN project
Elastic backscattering spectrometry (EBS)
Characterization of HIVIPP targets for REMIX project (HIX) involved in LARAMED project
Elastic backscattering spectrometry (EBS)
Advances Nuclear Target (ANT)
involved in SALVIA project, LUNA collaboration (target development) and LNL target service (target characterization)
Elastic backscattering spectrometry (EBS)
Nuclear Reaction Analysis (NRA)
particle induced X-ray emission (PIXE)
particle induced -ray emission (PIGE)
Target characterization at LNL

## Slide 18
Target characterization at LNL

## Slide 19
Target characterization at LNL

## Slide 20
Massimo Loriggiola
Lorenzo Loriggiola
Matteo Campostrini
Valentino Rigato
Sara Carturan
Sara Cisternino
Alisa Kotliarenko
Gaja Piteo (PhD UNIPD)
Stefano Corradetti
Juan Esposito
EURO-LABS WP2.5.2 Collaboration meeting May 15th, 2025 (Online)
Thank you from target makers group @LNL