## Slide 1: Preliminary results May tests

## Slide 2: Setup
GC
CH4
4500 ppm
AIR
H2O
FLUX
H2O
VENT
Z5
P
PUMP
NEW
PIPE
New rotameter (less sensitve)
Pipe instead of Z3
No bubbler
Connection to pressurise Z5

## Slide 3: Setup
GC
CH4
4500 ppm
AIR
H2O
FLUX
H2O
VENT
Z5
P
PUMP
NEW
PIPE
Test scheme

## Slide 4: Setup
GC
CH4
4500 ppm
AIR
H2O
FLUX
H2O
VENT
Z5
P
PUMP
NEW
PIPE
Regeneration scheme

## Slide 5: Setup
GC
CH4
4500 ppm
AIR
H2O
FLUX
H2O
VENT
Z5
P
PUMP
NEW
PIPE
Put some pressure in the cartridge with only air

## Slide 6: Compatibility with previous tests
media BT B [ml] | media SAT B [ml] | concentration | # test
16.25 | 24.20 | 4509.0 | 3
9.74 | 11.52 | 2254.5 | 3
It seems ok

## Slide 7: Preliminary results
Chart: Measured CH4 concentration [ppm]
| 4509 | 1718.3803965866421 | 1261.6400672557254 | 857.78702432407533 | 2417.8508794525014
BT | 16.8543 | 9.7392 | 6.6295 | 3.64 | 12.4204
SAT | 23.9719 | 11.5164 | 7.7553 | 4.5647 | 15.4177
Correlation between CH4 concentration and total adsorbtion capacity
2 points are still at low statistics
The curve seems to not be linear
Problem with the point at lower concentration