## Slide 1
Development of drop-cast
PbS QD detectors – from
X-ray photoresistors to
proton detection
7th international workshop on new Photon-Detectors
PD 2025 - 3-5 December 2025 - Bologna, Italy
Marco Ruggieri (1)
Andrea Fabbri (1)
Luca Tortora (1)(3)
Matteo Rapisarda (2)
Mattia Scagliotti (2)
Francesca Pescosolido (2)
Antonio Valletta (2)
Muhammad Waqas (1)
Paolo Branchini (1)
INFN Roma Tre, Rome, Italy - (1)
CNR-IMM, Rome, Italy - (2)
Dep. Sciences, Roma Tre Univ., Rome, Italy (3)

## Slide 2
Outline
Introduction
PbS on Silicon
PbS on PEN
Conclusions
7th international workshop on new Photon-Detectors
Marco Ruggieri – INFN Roma Tre
  Solution-processable materials
  Quantum dots
  Detectors based on QDs
  From IR-Vis Devices
  Drop-Cast Photodetector
  EHD-Jet printed photodetector
…Preliminary!
  From Silicon to PEN
  Response to Vis Light
  Response to X-rays
  Response to Proton Beams

## Slide 3
Solution-processable materials
Introduction
7th international workshop on new Photon-Detectors
Marco Ruggieri – INFN Roma Tre
https://www.kromek.com/czt/
Hou, Bo, et al, Nature Reviews Electrical Engineering, 2024
https://www.ptwdosimetry.com
CdZnTe
Diamond
HPGe
Commercially available Semiconductors offer excellent performance and characteristics!
Solid State Semiconductor detectors
However…
Lots of research efforts on new materials
Solution-processable materials
Rigid, brittle
Expensive
HPGe needs Cryo
CZT needs High Bias
Perovskite
Organic Semic.
Quantum Dots
Inexpensive
Bendability
Low-power
OSC  Tissue Eq.
OSC are Low-Z
PVK, QD have High Sensitivity
Quantum Dots

## Slide 4
Introduction
Quantum Dots
7th international workshop on new Photon-Detectors
Marco Ruggieri – INFN Roma Tre
García de Arquer, F. Pelayo, et al. Science, 2021
Nanocrystal (2-20 nm) of semiconducting materials that exhibit quantum confinement effects
Colloidal Quantum Dot (QD)
Solution-processable materials
Size is tunable during synthesis
Size-dependant Optoelectr. Properties
High-Z Materials (PbS, CdTe, PVK…)
Efros, Alexander L., and Louis E. Brus. ACS nano 2021
Kagan, Cherie R., et al.
Science 2016

## Slide 5
Introduction
QD-based Detectors
7th international workshop on new Photon-Detectors
Marco Ruggieri – INFN Roma Tre
Liu, Jing, et al.
Nature Communications, 2023
Liu, Jingying, et al,
Advanced Materials, 2019
Davis, Brandon J., and Mark D. Hammig.
ACS Applied Nano Materials. 2021
Ankah, G. N., et al.
Organic Electronics, 2016
Spectrometry with PbSe QD solids
Org. Heterojunct. PbS QD Detector
Flexible printed PVK QD detector
Wide-band (IR-X) PbS QD photodiodes

## Slide 6
PbS on Silicon
From IR-Vis Devices
7th international workshop on new Photon-Detectors
Marco Ruggieri – INFN Roma Tre
García de Arquer, F. Pelayo, et al., Nature Reviews Materials, 2017

## Slide 7
PbS on Silicon
From IR-Vis Devices
7th international workshop on new Photon-Detectors
Marco Ruggieri – INFN Roma Tre
De Iacovo, Andrea, et al. Scientific report, 2016
Konstantatos,
Gerasimos, et al.
Nature 2006
Si
Au
Au
Si
Au
Au
Si
Au
Au
1.
2.
3.
Si
Au
Au
5.
PbS
Repeat until
Enough material
4.
PbS
But
MeOH
Drop
Casting
Butylamine
48h
Oxidation
Some first, old results (2006) – 10V
Low-Power (1V) PbS QD photocond. (2016)
Solution-Processed (QD + ligands + solvents)
Layer-by-layer deposition
Photoconductive gain emerges from defects
Stable in air @ RT
PbS QD IR-Vis Photoconductors
Ligand
Exchange
Shorter surface ligands promote charge-transfer between QDs  Conductivity increases with decreasing QD distance
Ligand Exchange

## Slide 8
PbS on Silicon
Drop-Cast Photodetector
7th international workshop on new Photon-Detectors
Marco Ruggieri – INFN Roma Tre
X-ray Tube
Silver Anode (22 keV )
Operated at 50kV
Dose rate controlled through Tube Current
Ref. Detector
Boron-doped Diamond
1 nC/Gy Linear Response
No Bias required
Clear Response under Hard X-Rays (1V Bias)
Linear Extr. Charge-Dose rate relation
Excellent Sensitivity:
Good Limit of Detection:
Photocurrent
Charge-Dose rate
I-V Plot
X-ray Response
Current to Dose Rate
No Saturation!
No Dosimetry but Information from Extracted Charge
Dosimetry?
Slowed down evaporation of solvent
From 2 to 4 cycles of deposition
Uniform coverage of contacts
Drop-Casting
Uniform topography (SEM)
Fissures and flaking
Presence of OA and But. (ATR-FTIR)
Surface Char.
Ruggieri, et al., ACS Applied Electronic Materials - 2023
X-Ray ON

## Slide 9
PbS on Silicon
EHD-J Printed Photodet.
7th international workshop on new Photon-Detectors
Marco Ruggieri – INFN Roma Tre
Electrohydrodynamic Jet
Printing
Ligand Exchange
1.
Droplet formation through High Voltage
Drop-on-Demand
Patterning capabilities
Improves carrier transport
Performed in air
Using TBAI
Tetrabutylammonium Iodide
2.

## Slide 10
PbS on Silicon
EHD-J Printed Photodet.
Stability
Thickness
Droplet shows coffee ring
Iodine exchange is not uniform
Surface Char.
Ref
QD
Tube Current
35uA
65uA
95uA
35uA
65uA
Diam. Current (pA)
QD Current (pA)
QD
Ref
Ref
QD
Diam. Current (pA)
QD Current (pA)
X-Ray Irradiation
LoD
Response to Vis
X-ray Response
Jet Printed with Iodine functionalisation
Fast, repeatable response under Hard X-Rays
Good Sensitivity:
Good Limit of Detection:
Fast, repeatble response to red laser
Transition Time
No sign of radiation damage
Limited stability in air (
X-ray Irradiation (60s & 30s pulses)
Sensitivity
Ruggieri, et al., ACS Applied Electronic Materials – 2025

## Slide 11
PbS on Silicon
Summing up on Silicon…
7th international workshop on new Photon-Detectors
Marco Ruggieri – INFN Roma Tre
Proof of Concept
Stable in air (>6 Months)
Printed (large-area?)
Unstable in air ( Weeks)
Drop-Cast Detector
EHD-Jet Printed Detector
EHD-Jet
Drop-Cast
Basiricò, Laura, et al. Advanced Materials Technologies 6.1 (2021): 2000475.
Most data from:
Basiricò et al. Advanced Materials Technologies, 2021

## Slide 12
PbS on PEN
From Silicon to PEN
7th international workshop on new Photon-Detectors
Marco Ruggieri – INFN Roma Tre
Current Objective
Fabrication of PbS QD photodetector on PEN
Photodetection of
X-ray Radiation
First test of response to proton beams
…Preliminary!

## Slide 13
PbS on PEN
From Silicon to PEN
7th international workshop on new Photon-Detectors
Marco Ruggieri – INFN Roma Tre
PEN
Au
Au
PEN
Au
Au
PEN
Au
Au
1.
2.
3.
Repeat until
Enough material
PEN
Au
Au
4.
Butylamine  MeOH  Oxid.
PbS
PEN
Au
Au
5.
PbS
PbS
PbS
Drop
Casting
Same procedure as on Si
Extremely random coverage
Samples hold little amount of material
Samples are always different!
Using the PbS on Silicon Recipe
Using Surface Tension to hold PbS Droplet
Casting PbS droplets until complete coverage
One final Ligand Exchange and MeOH
Improved coverage and thickness!
Improved Recipe for PEN
PatternedPEN
On Si
Recipe
Improved
Recipe

## Slide 14
PbS on PEN
Resp. to Vis Light
7th international workshop on new Photon-Detectors
Marco Ruggieri – INFN Roma Tre
Preliminary
Preliminary
Preliminary
Preliminary
Photoconductor behaviour
Typical
Low Power:
Benchmark using Vis Light Detection.
Better Response to Vis  Better Response to X-rays
On PEN - Photocurrent observed without bias – Still under Investigation!

## Slide 15
PbS on PEN
Resp. to X-rays
7th international workshop on new Photon-Detectors
Marco Ruggieri – INFN Roma Tre
Collected Charge
  Direct Photodetector Behaviour ()
  Linear I-V Char. In Dark and under X-rays
  Long Rise and Fall times
  Linear Charge-Rad. Intensity Characteristic
  No sign of radiation induced damage
X-Ray ON
X-ray Tube (Co anode )
However…
Tube
Current

## Slide 16
  RUN II
PbS on PEN
Resp. to Proton Beams
7th international workshop on new Photon-Detectors
Marco Ruggieri – INFN Roma Tre
  RUN I
The authors gratefully acknowledge Dr. Anna Bianchi (INFN-LNL) and the ATOMIQA project for providing valuable time during their concurrent experimental campaign
  Irradiated with constant beam of protons in TIFPA (Trento) Exp. Line
  No Bias!
  Linear with proton current
  Higher in Run II
  No failure of the detector
  Very
  Premilinary
Preliminary
Preliminary

## Slide 17
Conclusions
7th international workshop on new Photon-Detectors
Marco Ruggieri – INFN Roma Tre
Summing Up
In Conclusion
Future Objectives
Lead Sulfide QD-based detectors were fabricated and tested
Two Techniques: Drop-casting and EHD-Jet printing
Currently working to optimise transfer on plastic (PEN) substrates
First test with proton irradiation
PbS on Silicon offers high sensitivity and good stability
Still very slow!
Transfer to PEN is successful! Very similar characteristics
Proportional response to proton beam current variation
Characterisation on PEN still underway
Investigate proton detection capabilities
Radiation Hardness study

## Slide 18
Development of drop-cast PbS QD detectors – from X-ray photoresistors to proton detection
7th international workshop on new Photon-Detectors
PD 2025 - 3-5 December 2025 - Bologna, Italy
Marco Ruggieri (1)
Andrea Fabbri (1)
Luca Tortora (1)(3)
Matteo Rapisarda (2)
Mattia Scagliotti (2)
Francesca Pescosolido (2)
Antonio Valletta (2)
Muhammad Waqas (1)
Paolo Branchini (1)
INFN Roma Tre, Rome, Italy - (1)
CNR-IMM, Rome, Italy - (2)
Dep. Sciences, Roma Tre Univ., Rome, Italy (3)
Thank you!

## Slide 19
Development of drop-cast PbS QD detectors – from X-ray photoresistors to proton detection
7th international workshop on new Photon-Detectors
PD 2025 - 3-5 December 2025 - Bologna, Italy
Marco Ruggieri (1)
Andrea Fabbri (1)
Luca Tortora (1)(3)
Matteo Rapisarda (2)
Mattia Scagliotti (2)
Francesca Pescosolido (2)
Antonio Valletta (2)
Muhammad Waqas (1)
Paolo Branchini (1)
INFN Roma Tre, Rome, Italy - (1)
CNR-IMM, Rome, Italy - (2)
Dep. Sciences, Roma Tre Univ., Rome, Italy (3)
Backup

## Slide 20
Quantum Dots

## Slide 21
PbS on PEN
Resp. to Vis Light
Current (au)
Increasing light intensity
NO BIAS

## Slide 22
Drop-Cast PbS QD
Preliminary test of Proton Detection by PbS QD with an Epoxy conversion layer
SRIM Simulation
PbS on Si + Epoxy
Resp. to Proton Beams

## Slide 23
Detection near
Single shot
Electron beam
3 mm
Au
Au
QD
PbS on Si
Resp. to e Beams