## Slide 1
Dorothea Fonnesu - fonnesu@infn.it
INFN Legnaro National Laboratories
May 13, 2025
Surface Technology and Superconductivity Service
Collaboration meeting

## Slide 2: Outline
Nb3Sn/Cu state of the art at LNL
Nb3Sn activities for SuperMAD
New dedicated coating system
Currently ongoing
Next steps

## Slide 3: Nb3Sn/Cu state of the art at LNL
Optimized recipe:
  Low cathode power < 20 W
  Deposition pressure 2 x 10-2 mbar
  No annealing
  Deposition temperature 600 ºC – 650 ºC
  NbBL thickness = 30+ μm
NbBL thickness plays a major role:
  A thicker NbBL promotes the formation of the A15 phase (see Tc): accomodation effect
  30+ µm is the “saturation” thickness
650 °C
Nb3Sn
NbBL
D. Ford

## Slide 4: Nb3Sn/Cu state of the art at LNL
Comparison to LHC baseline: Q0 vs. Eacc @ 4.5 K
LHC cavities: Nb/Cu 400 MHz
QPR Nb3Sn/Nb bulk
G = 216 Ω
Equivalent to
Q0 ~ 9 x 109
@ 5 MV/m
@4.5 K
Quadrupole Resonator (QPR)
test of Nb3Sn/bulk Nb
coating according to optimized recipe
(O. Kugeler, S. Keckert)

## Slide 5
Nb3Sn activities for
WP1: Superconducting Materials
Reminder (Nb3Sn):
Q and B
Medium Performances at Very High B field
V and C
Direct Deposition via PVD
Easy Scalable Technology
Technology Readiness Level
Medium-High: Cavity prototypes already made
Conversion Power
DCMS deposition recipe with nominal Tc ready and successfully RF tested (QPR) Proceed with:
R&D on pulsed-MS deposition to improve material superconducting AC performances in high DC magnetic field
Parallel investigation of parameters toward improvement of current recipe, with goals: decreasing NbBL thickness, lowering Tdep

## Slide 6: New dedicated coating system
New sputtering system:
fully dedicated to pulsed-MS depositions
2” magnetron with commercial stoichiometric single Nb3Sn target
operated in DCMS: Tc = 17.5 K for Nb3Sn/Al3O2 substrate (*)  demonstrates we have good control over system  demonstrates reproducibility of DCMS recipe (4” system)
More results:
*M. Lazzari’s MSc thesis
(*)
Sn-rich islands observed on DCMS samples

## Slide 7: Currently ongoing
With new sputtering system being operational:
1x MSc student fully dedicated to it (E. Cremonesi)
deposition runs are resource- and time-consuming
  improve/assess pulsed-MS process robustness
  identify/confirm most influential parameters with minimal # of runs
   Tc and a oriented DOE: 9 runs with Tdep, f, p, P (NbBL thickness is intrinsic)
preparation of first batches of NbBLs (2 μm, 16 μm, 30 μm)
first run prepared, baking done and deposition starting today 🤩
NbBL-2 (2)
2x Al2O3
NbBL-2 (1)
NbBL-16 (1)
NbBL-30 (1)
NbBL-16 (2)
NbBL-30 (2)
NbBL-30 (3)
NbBL-16 (3)
NbBL-2 (3)
bulk Nb

## Slide 8: Next steps: 9 GHz haloscope
Workflow
Stripping of the SC layer
Persulphate etching
Plasma Electrolytic Polishing preparation
NbBL deposition
Nb3Sn deposition
Measurements
verified
Persulphate etched
PEP
Persulphate etched
PEP
E. Chyhyrynets

## Slide 9: Thank you!