## Slide 1
Cristian Pira - Dorothea Fonnesu
INFN Legnaro National Laboratories
July 01, 2025
Surface Technology and Superconductivity Service
Collaboration meeting

## Slide 2: Outline
Nb3Sn/Cu state of the art at LNL
Nb3Sn activities for SuperMAD
New dedicated coating system
Currently ongoing
Next steps

## Slide 3: Nb3Sn/Cu state of the art at LNL
Optimized recipe:
  Low cathode power < 20 W
  Deposition pressure 2 x 10-2 mbar
  No annealing
  Deposition temperature 600 ºC – 650 ºC
  NbBL thickness = 30+ μm
NbBL thickness plays a major role:
  A thicker NbBL promotes the formation of the A15 phase (see Tc): accomodation effect
  30+ µm is the “saturation” thickness
650 °C
Nb3Sn
NbBL
D. Ford

## Slide 4: Nb3Sn/Cu state of the art at LNL
Comparison to LHC baseline: Q0 vs. Eacc @ 4.5 K
LHC cavities: Nb/Cu 400 MHz
QPR Nb3Sn/Nb bulk
G = 216 Ω
Equivalent to
Q0 ~ 9 x 109
@ 5 MV/m
@4.5 K
Quadrupole Resonator (QPR)
test of Nb3Sn/bulk Nb
coating according to optimized recipe
(O. Kugeler, S. Keckert)

## Slide 5
Nb3Sn activities for
WP1: Superconducting Materials
Reminder (Nb3Sn):
Q and B
Medium Performances at Very High B field
V and C
Direct Deposition via PVD
Easy Scalable Technology
Technology Readiness Level
Medium-High: Cavity prototypes already made
Conversion Power
DCMS deposition recipe with nominal Tc ready and successfully RF tested (QPR) Proceed with:
R&D on pulsed-MS deposition to improve material superconducting AC performances in high DC magnetic field
Parallel investigation of parameters toward improvement of current recipe, with goals: decreasing NbBL thickness, lowering Tdep

## Slide 6: New dedicated coating system
New sputtering system:
fully dedicated to pulsed-MS depositions
2” magnetron with commercial stoichiometric single Nb3Sn target
operated in DCMS: Tc = 17.5 K for Nb3Sn/Al3O2 substrate (*)  demonstrates we have good control over system  demonstrates reproducibility of DCMS recipe (4” system)
More results:
*M. Lazzari’s MSc thesis
(*)
Sn-rich islands observed on DCMS samples

## Slide 7: Currently ongoing
With new sputtering system being operational:
1x MSc student fully dedicated to it (E. Cremonesi)
deposition runs are resource- and time-consuming
  improve/assess pulsed-MS process robustness
  identify/confirm most influential parameters with minimal # of runs
   Tc and a oriented DOE: 9 runs with Tdep, f, p, P (NbBL thickness is intrinsic)
preparation of first batches of NbBLs (2 μm, 16 μm, 30 μm)
first run prepared, baking done and deposition starting today 🤩
NbBL-2 (2)
2x Al2O3
NbBL-2 (1)
NbBL-16 (1)
NbBL-30 (1)
NbBL-16 (2)
NbBL-30 (2)
NbBL-30 (3)
NbBL-16 (3)
NbBL-2 (3)
bulk Nb

## Slide 8: Currently ongoing (update)
4 run done
Tc around 14-15 K
Coating set-up must be improved (several short cuts are limiting the productivity)
First coating presents lower film density compared to DC (preliminar)
Ion milling installed + FE-SEM: cross section characterization possible!

## Slide 9: Next steps: 9 GHz haloscope
Workflow
Stripping of the SC layer
Persulphate etching
Plasma Electrolytic Polishing preparation
NbBL deposition
Nb3Sn deposition
Measurements
verified
Persulphate etched
PEP
Persulphate etched
PEP
E. Chyhyrynets

## Slide 10: Next steps: 9 GHz haloscope (update)
Workflow
Stripping of the SC layer
Persulphate etching
Plasma Electrolytic Polishing preparation
NbBL deposition
Nb3Sn deposition
Measurements
verified
Peel off on the upper part
The cavity coating resist to HPR

## Slide 11: FLASH
Started a collaboration with FLASH group to define the Cu polishing of the large 100 MHz resonator
A small prototype in collaboration with University of Mainz will be built to test different solutions

## Slide 12: 2026 Activity
Continuation of the development of Nb₃Sn coatings via Pulsed MS
  Parameters explored: Pressure, Temperature, Pulse Frequency, Peak Power
Preparation of planar samples on sapphire for TO and RM3 and on Cu for RM3
Deposition of Nb₃Sn coating (DC-MS recipe) on 9 GHz haloscope cavity
Polishing of copper half-cells of reference cavity
First pulsed Nb₃Sn coating on reference cavity
Polishing test on FLASH cavity

## Slide 13: FTE e Budget 2026
Dettaglio richieste |  | 
Capitolo | Descrizione | Richiesta
Missioni | Trasferte ditte esterne per la fabbricazione di cavità e componenti meccanici | 1
Missioni | Missioni a Frascati, Roma, e Torino per misure | 3
Missioni | Partecipazione Thin Film Workshop in UK | 3 (SJ)
Consumo | Acidi e soluzioni chimiche per pulizia Cu | 3
Consumo | Lampade IR x portacampioni riscaldato Nb e Nb3Sn | 3
Consumo | Gasket CF per UHV | 2
Altri Cons | Gas puri per sputtering (Ar) | 2
Trasporti | Spese spedizione cavità e campioni STFC, CERN, Jlab, Fermilab | 2
Manutenzione | Pompe turbo sistema da sputtering | 5
SPServizi | Lavorazioni meccaniche varie (adattatori prototipo cavità, portacampioni, etc.) | 3
Inventario | Contributo acquisto Diffrattometro | 25
Budget per capitoli | 
Missioni | 1
Consumo | 2
Altri Cons | 2
Trasporti | 2
Manutenzione | 5
SPServizi | 3
Inventario | 25
TOTALE | 51
FTE |  | 
Nome | Qualifica | %
Cristian Pira | Primo Tecnologo | 30
Giorgio Keppel | Primo Tecnologo | 10
Eduard Chyhyrynets | Tecnologo | 30
Ezeaba Tochukwu Emmanuel | Dottorando | 40
Matteo Lazzari | Borsista | 50
Dal Ponte Matteo | Borsista | 70
Crnlovic Nikola | Borsista | 50
Stivanello Fabrizio | Tecnico | 65
TOTALE |  | 3,45 FTE

## Slide 14: Thank you!