## Slide 1: PHD Second Year Progress report Innovative holographic optical elements for modern optical instrumentation: CURRICULUM: Detectors, Lasers, and Optics Research Activity location: Observatory di Brera, Merate, Milan Student name: Dhiraj Gupta Supervisor: Andrea Bianco, Emilio Molinari 19/09/2025

## Slide 2
1. Introduction
2.Holographic Diffuser & Modelling
3. Lab work
(Diffuser fabrication & Reflection hologram)
5. Planning
6. Coursework and school
4. Conclusion

## Slide 3
Innovative Holographic Optical Elements for Modern Optical Instrumentation
The PhD thesis focuses on developing Volume Holographic Optical Elements (VHOEs). Holographic Optical Elements (HOEs) nowadays cover a relevant position in optics as they modify an optical wavefront depending on the recorded holographic pattern
The research aims to:
Enhance the Optical Systems: Developing Volume Holographic Optical Elements (VHOEs) with higher efficiency and broader functionality.
Simplify Optical Systems: Create compact, lightweight, and versatile optical systems using VHOEs.
Exploration of Applications: Apply VHOEs in spectroscopy, astronomical instrumentation, adaptive optics, and precise photometry.
VHOE Developments: (Diffuser)
  Adaptive optics: use in pyramid wavefront sensors to improve wavefront correction.
  Photometry: increasing precision in light measurement of Exoplanets.

## Slide 4
Adaptive optics (AO) corrects atmospheric distortion by measuring the incoming wavefront (with a sensor) in real time
The Pyramid Wavefront Sensor (PWFS) directs the wavefront onto a pyramid tip; with dynamic modulation, the beam is moved around the tip for sensitivity, but this requires precise alignment.
Scientific challenge & solution :
Challenge in AO: Dynamic modulation alignment sensitivity
Proposed Solution: Static modulation with a holographic diffuser stabilizes the wavefront, reducing alignment sensitivity
Exoplanet transit photometry measures a star’s brightness dip to find planets – it demands extremely high precision.
Challenge: In a small field of view, stable reference stars are scarce, limiting calibration accuracy.
Holographic Diffuser Benefit: By scattering light in a controlled way, diffusers can broaden the target’s light PSF without losing much light, allowing use of brighter reference stars and improving photometric stability.

## Slide 5
Holographic diffuser and requirement:
Conventional Diffuser:
  An optical component that scatters light for a softer, more even distribution.
Limitations
  Inefficient light use
  uncontrolled spread
  Inconsistent performance
  Not ideal for high-precision applications
Holographic diffusers
Uses a recorded interference pattern to scatter light.
Advantages:
  Enhanced light control and efficiency
  Wavelength-Selective Diffraction,
  Customized Angular Distribution,
  High Diffraction Efficiency
  Spectral Control
Holographic diffuser requirement by INAF Bologna:
Target angular diffusion ≈ 0.023°
Input beam: 5mm
Band: 0.9–1.1 μm (C ~ 1.025 μm )
Efficiency: ≥ 90%

## Slide 6
Modelling diffuser via speckle pattern and Mie scattering
Speckle recording:
coherent light + rough surface → speckle (granular interference).
Speckle size (speckle grain) → capturing on photopolymer → diffuser
Average Speckle size is approximated by
,
where f is focal length & a is aperture diameter
Mie scattering:
Speckle Size
Equivalent to Mie particle
Diffuser Angle behaviour for the Mie-speckle particle

## Slide 7
Wavelength (nm) | Speckle size |  | 
 | Angle(FWHM) for 21µm | Angle(FWHM) for 32 µm | Angle(FWHM) for 64 µm
625 | 1.2° | 0.60° | 0.240°
850 | 1.68° | 0.96° | 0.48°
950 | 1.80° | 1.20° | 0.48°
1025 | 2.04° | 1.32° | 0.48°
Mie scattering model results
Diffuser angles simulated via Mie scattering for different speckle sizes (set by aperture & focal length)
Diffusion angles extracted from BRDF curves using FWHM of the scattering peak (values in table)
Trend (bottom right plot): Diffusion angle decreases systematically with speckle size (21 µm > 32 µm > 64 µm).

## Slide 8: Holographic diffuser writing setup(Modified from VPHGs Setup):
Setup Modification
Repurposed one arm of the VHOE(VPHGs) recording setup for diffuser recording.
Added components to shape the speckle field and define the recording geometry.
Components
Master diffuser – seeds a controlled speckle field.
Variable iris (aperture 2–16 mm) – sets aperture size to control speckle grain.
Focusing lens (f = 100 mm) – images the speckle field at the recording plane.
Circular-aperture mask – defines beam footprint and suppresses edge scatter.
Fabrication procedure
Speckle calibration: vary iris → set grain size on substrate
Record: expose photopolymer at calibrated plane
Verify: phase-contrast microscope + Python analysis (speckle size)
Characterisation
Angle calculation: capturing the image and analyzing.
Efficiency: calculating the throughput.
Murphy, K., Toal, V., Naydenova, I., & Martin, S. (2018). Holographic beam-shaping diffractive diffusers fabricated by using controlled laser speckle. Optics Express, 26(7), 8916–8922

## Slide 9: Holographic diffusers fabrication Condition:
Diffuser | Material | Aperture Size mm | Average speckle size(μm) | Irradiance (μW/cm2) | Exposure time
T18 | Bayfol 16 μm | 6 | 21 | 500 | 690 sec
T19 | Bayfol 45μm | 4 | 21 | 500 | 960 sec
T20 | Bayfol 16 μm | 2 | 32 | 500 | 671 sec
T21 | Bayfol 45 μm | 6 | 32 | 500 | 1500 sec
T22 | Bayfol 16 μm | 4 | 64 | 200 | 1279 sec
T23 | Bayfol 45 μm | 2 | 64 | 200 | 2957 sec
T24 | Bayfol 70 μm | 6 | 21 | 700 | 1273 sec
T25 | Bayfol 70 μm | 4 | 32 | 500 | 2258sec
T26 | Bayfol 70 μm | 2 | 64 | 200 | 3730 sec
Parameters tested: – Aperture size: 6, 4, 2 mm → speckle sizes ≈ 21, 32, 64 µm – Film thicknesses: 16, 45, 70 µm – Irradiance levels: 3 values tested
Samples: T18–T26 → each = unique thickness–speckle–irradiance combination
Goal: Study how speckle grain and film thickness influence diffusion angle & efficiency
Monitoring: – Exposure tracked using 980 nm laser pointer – Exposure stopped when the transmission curve reached a plateau (nearly flat slope)
Plateau indicates speckle formation → exposure stopped here.

## Slide 10: Holographic diffuser fabrication: Speckle Calibration & Observation
Pre-exposure:
Captured speckle images using a Basler camera while varying the iris aperture (6, 4, 2 mm) at the diffuser plane in the setup.
Post-exposure :
Observed the recorded speckle pattern of the diffuser under an Olympus phase-contrast microscope.
Aperture size (mm) | Theoretical speckle size (µm) | Measured speckle size(µm) at diffuser plane | Measured speckle size(µm) in diffuser
6 | 21 | 23.98 | 14.39
4 | 32 | 29.12 | 22.40
2 | 64 | 50.66 | 45.08
100µm
50µm

## Slide 11
Collimated image
Diffused image T24
Set up for angle determination of diffuser:
Captured image
Diffused image T26

## Slide 12
Effect of aperture and thickness on diffuser angle
Three thicknesses (16, 45, 70 µm) and three apertures (6, 4, 2 mm) were designed and tested for diffusers
Same thickness (70 µm) with varying apertures shows that larger apertures give higher diffusion angles (T24 max, T26 min).
Same aperture (4 mm) with varying thicknesses yields similar angles, confirming that aperture dominates over thickness.

## Slide 13
Measured fractional throughput:
Throughput measurement on captured image while angle determination.
Same thickness(70 µm), varying apertures → efficiency varies with aperture.
Same aperture(4 mm), varying thicknesses → efficiency shows minor dependence on thickness.
In both cases, efficiency increases with wavelength but is lower at shorter wavelengths.
Overall, throughput is higher at longer wavelengths, with aperture having a stronger influence than thickness.

## Slide 14: Reflection Hologram for simulating the Laser Guide Star (LGS)system:
Goal: Record Cylindrical object hologram (L ≈ 24 mm, Ø ≈ 1 mm, 83.7° projection) → Simulate LGS for Ingot bench at INAF Padova.
Process: Expanded 532 nm laser → object & photopolymer plate illuminated from same side → volume reflection hologram.
Optimization: Painted capillary having weak scattering → replaced with a small wooden stick for stronger reflection.
Exposure: ~2 min 30 s @ 500 µW/cm² on 16 µm photopolymer film.
Holographic recording setup
Reconstruction Setup
Weak hologram (capillary): low scattering, faint replay
Strong hologram (stick): bright reflection, showing LGS behavior.
Side project

## Slide 15
Conclusion:
Developed and tested holographic diffusers (T18–T26) with varying speckle size, film thickness, and irradiance.
Confirmed inverse relation: smaller speckle → larger angular diffusion.
Efficiency trade-off observed: samples with higher angular spread showed lower throughput.
Successfully recorded a reflection hologram (INAF Padua ), achieving a bright, stable reconstructed image.

## Slide 16
Planning
Optimize diffuser fabrication against targets (core angle, diffused pattern, throughput/efficiency) and lock parameter recipes.
AO bench integration: implement the optimized diffuser on the adaptive-optics bench; verify PWFS modulation and stability.
On-sky demonstration (exoplanet photometry): deploy the optimized diffuser for a controlled on-sky test and collect performance data.
Consolidate methodology and results into a manuscript/technical report, image-driven quantification of holographic diffuser performance for adaptive optics.

## Slide 17
Coursework & school:
Coursework | Exam dates and credit | Total credits
Radio and Optical Interferometry: Lecturer: Fabrizio Massi & Lorenzo Busoni (INAF Arcetri) | 8/10/2024 2 credits | 12 credits
Laser Physics and Applications : Lecturer: Annalisa Volpe (Uniba) | 19/12/2024 2 credits | 
Advanced scientific programming in Matlab : Lecturer: Paolo Bardella (UniTo) | 09/05/2025 6 credits | 
Management of Scientific Projects : Lecturer: Maria Bergomi | 03/04/2025 2 credits | 
School | Dates
Scientific Communication in Astronomy Summer School in Bertinoro, Italy | 12/10/2025 to 17/10/2025

## Slide 18
Thank you For your Time