## Slide 1
Admission to second year
Technologies for fundamental research in phisycs and astrophisycs
Alberto Barci
A.Y. 2024-2025

## Slide 2
Development and Characterization of Innovative Additively Manufactured Metal Alloys for High and Ultra-High Temperature Applications
PhD Program: Tecnologie Per La Ricerca Fondamentale In Fisica E Astrofisica (TFPA)
CURRICULUM: Meccanica
UNIVERSITY/RESEARCH CENTRE: Università degli Studi di Padova (DFA) / INFN sezione di Padova
PhD STUDENT: Alberto Barci
SUPERVISOR: Prof. Massimo Pellizari
Dr. Pietro Rebesan

## Slide 3
PhD courses completed:
Analysis and Modelling of the Additive Manufacturing (12 hours)
Generative Design for Smart Additive Manufacturing (12 hours)
Coupled electrical-thermal-structural finite element analyses (10 hours)
Powder Flowability (course of DII department) (10 hours)
Summer school:
SEAMAC International Summer school: additive manufacturing, from powder to final parts with a smooth surface, 29.06 – 05.07.2025, Ljubljana
Advanced Course on "Metal Additive Manufacturing: Fundamentals, Modeling, Materials, and Implementation“, 22.09 – 26.09.2025, remotely
Additional activity:
Attendance -Phd Academic English – January-February 2025
Courses, exams and schools

## Slide 4
Research introduction
Context
Part of the HISOL_NEXT project (CSN V) for next-generation ISOL sources (SPES facility, INFN Legnaro).
Focus on additively manufactured refractory metals for very high-T applications (2000÷2200 °C).
Materials studied
Pure Tantalum (Ta)
Ta-10W alloy
Refractory High Entropy Alloy (RHEA) - TaWCrV
Objectives
Evaluate printability via LPBF.
Optimize process parameters (P, v, etc.).
Material characterization: physical, thermal, electrical, and mechanical properties evaluation

## Slide 5
Selective Production of Exotic Species
Proton Beam
Target
Transfer Line
Ione source
Radioactive Beam
PhD project context: SPES project
SPES building
Cyclotron
(a) CAD model section view of The SPES Target Ion Source (TIS) system; (b) magnification of the FEBIAD Ion Source of the system.

## Slide 6
Pure tungsten:
Current state of research / 1
https://doi.org/10.1016/j.jmatprotec.2003.11.051
https://doi.org/10.1007/s40195-018-0752-2
Literature:
Many examples of 3D printing of pure Ta by LPBF
Parameters:
Many examples of 3D printing of pure Ta by LPBF
Results:
Very high densities, up to 99.9%.
Gaps:
No research on thermal and electrical characterization
Pure tantalum:
Literature:
Many examples of 3D printing of pure W by LPBF
High Melting Temperature (3410°C)
High Thermal Conductivity (~174 W/m*K)
Brittleness at Room Temperature
Very difficult to print without cracks

## Slide 7
Properties:
Excellent corrosion/oxidation resistance
High mechanical strength
High-temperature stability; suitable for extreme enviroment
Ta-10W:
90 wt.% Ta, 10 wt.% W
Solid solution strengthening from W
Literature:
Only one study published as of 2025
RHEAs:
Multicomponent design (high configurational entropy)
Better radiation resistance (low embrittlement)
Our alloy TaWCrV:
Ta 35-40 %wt.
W 35-40 %wt.
Cr 12-17 %wt.
V 8-13 %wt.
Literature:
The composition was newly developed for this application
Few studies, mostly with low Ta/W content

## Slide 8
Layer thickness
Main parameters:
Laser power
Laser speed
Layer thickness
Hatch spacing
Ta block
Ta powder
Laser
3D Printing - LPBF
Main characteristics
Powder bed
Laser scanning
Layer-by-layer build
Solid part formation
Controlled environment
Eos M100 printer used in this research (left);
view of the interior (right)
Tantalum
Ta-10W

## Slide 9
Power | Speed
W | mm/s
95 – 125 | 100 - 350
Ta – The first LPBF samples
Cubes 8 mm side
It is the simplest geometry for controlling parameters
Measurement of relative density
Detection of defects (porosity)
Singles Scan Tracks (SST)
8 mm long
Single laser lines produced on solid blocks
Used to test if power & speed ensure stable melting
Help define the suitable process window
Best parameters from previous experiences
For both cubes and SSTs, the parameters were varied around these reference values.

## Slide 10
Figure: Cubes and Single Track (SST) Ta samples
Figure: SST Ta samples (SEM)
Ta – The first LPBF samples
No adhesion issues on the Cu platform.
SSTs: the tracks shape becomes irregular as laser power and scan speed increase + Balling

## Slide 11
Ed<290 J/mm3, RD=98.56 %
Ed>320 J/mm3, RD=98.81 %
Ed=290-320 J/mm3, RD=98.88 %
No porosity or defects on the top surface
Widespread porosity, probably due to the presence of impurities in the powder.
Maximum RD~98.8%
Ed: 293.33 J/mm3, Laser power: 110 W, Scanning speed: 250 mm/s, RD=98.88%
Ta – LOM and SEM analysis

## Slide 12
Build direction (BD)
VED: 271.60 J/mm3;
Laser power: 110 W;
Scan speed: 225 mm/s;
Relative density: 98.58%
VED: 289.96 J/mm3
Laser power: 120 W
Scan speed: 230 mm/s
Relative density: 98.55%
Ta samples - microstructure
Top surface
Examples of EBSD images of grains
https://doi.org/10.1016/j.ijrmhm.2022.105882

## Slide 13
The first printing attempts directly on the copper support were stopped after only about 20 layers.
The printing was successful by first creating a 1 mm layer of pure Tantalum and then printing the Ta-10W on top of it.
Ta-10W samples
Figure: Cubes and Single Track (SST) Ta-10W samples
Figure: SST Ta-10W samples (SEM)

## Slide 14
Ed<290 J/mm3, RD=94.4%
Ed>320 J/mm3, dr=93.32%
Ed=290-320 J/mm3, RD=96.79%
Surface:
Cracks
Porosity
Large pores and cracks, probably due to inadequate melting and cooling processes.
Maximum relative density ~97%
Energy density: 300.00 J/mm3; Laser power: 90 W; Scanning speed: 200 mm/s; RD: 96.52%
Ta-10W – LOM and SEM

## Slide 15
Second year activity
Conclusion of Metallographic Characterization of Tantalum
Optimization of Ta-10W parameters
Study of Mechanical Properties of Ta-10W
Study of Thermal and Electrical Properties of Ta-10W

## Slide 16
 | Year 1 |  |  |  | Year 2 |  |  |  | Year 3 |  |  | 
 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4
Bibliography research |  |  |  |  |  |  |  |  |  |  |  | 
Tantalum printing and characterization |  |  |  |  |  |  |  |  |  |  |  | 
Ta-10W printing optimization |  |  |  |  |  |  |  |  |  |  |  | 
Ta-10W thermal and electrical characterization |  |  |  |  |  |  |  |  |  |  |  | 
TaWCrV printing optimization |  |  |  |  |  |  |  |  |  |  |  | 
TaWCrV thermal and electrical characterization |  |  |  |  |  |  |  |  |  |  |  | 
Plan of activities

## Slide 17: Thank you for your attention