## Slide 1
PhD Program of National Interest in
“Technologies for fundamental research in Physics and Astrophysics”
Giacomo Voltan
Development, design and testing of metallic components for high-temperature nuclear physics applications produced using additive manufacturing technologies
Padova, 23/09/2025
Annual Report 2024/2025
Supervisor : Prof. Mattia Manzolaro
Co-supervisor: Dott. Michele Ballan

## Slide 2: The framework: SPES at LNL

## Slide 3: Research project and objectives
ISOL machine - TIS Complex
Cathode
Plasma Chamber (Ta/Mo)
Grid (Mo)
Outlet (Mo)
Anode
4x Cathode Centering Pins
(Ta, Al2O3)
3x Anode Support System
(Ta, Al2O3)
Housing
(Graphite)
Discharge Chamber
(Ta)
Extraction disks
(Ta)
Main Body (Ta)
Frontal Surface (Ta)
Flange (Ta)
FEBIAD Ion Source used for the production of Radioactive Ion Beams
ADIGE and ECR Ion Source (PIAVE)
Injection system used to produce Ion Beams from Solid Elements
Screw (Mo)
Oven body (Ta)
Crucible (Al2O3)
Heating Coil (W)
Insulators (Al2O3)
Oven head (AISI304)
Oven
Alignment system
Current connector
Heating rod

## Slide 4: Research project and objectives
Design of innovative anode-cathode interfaces
Investigate the influence of several factors on the FEBIAD performances exploiting LPBF advantages
Development of a new FEBIAD geometry through LPBF
Study the influence of the cathode surface finishing
Study the influence of the anode grid transparency
Evaluation of the possible improvements of using different materials
Injection system used to produce Ion Beams from Solid Elements
Development and validation of a Finite Element Model
Study the oven to identify its limitations, then develop a new design possibly using LPBF technology
Development of procedures for the high temperature characterization
Development a new oven design to improve its stability
Evaluation of innovative oven design possibly using new materials
Study of new experimental procedures to measure T<800°C
FEBIAD Ion Source used for the production of Radioactive Ion Beams

## Slide 5: Research project and objectives
Investigate the influence of several factors on the FEBIAD performances exploiting LPBF advantages
Design and development of innovative anode-cathode interfaces (e.g. conical, spherical)
Study the influence of the cathode surface finishing and anode grid transparency (new LPBF designs)
Evaluate the possible improvements of using different materials (e.g. TaW alloy)
Production and complete characterization of:
  The innovative LPBF FEBIAD geometry
  The new anode-cathode interfaces with standard FEBIAD geometry
(High temperature tests, thermionic emission tests and ionization efficiency measurements with stable elements)
Design and development of a new complete FEBIAD geometry through LPBF
2024-2025
2025-2026
2026-2027
Study the oven to identify its limitations, then develop a new design possibly using LPBF technology
Definition and validation of the oven Finite Element Model
Development of procedures for the high temperature characterization to identify the current design limitations
Improvement of the actual oven design
Evaluate innovative oven design possibly using new materials or LPBF technology (evaluation of operating temperature, potential reaction..)
Evaluate new experimental procedures to measure T<800 °C
Production and characterization of the new design
Possible production and characterization of the innovative geometry

## Slide 6: FEBIAD Ion Source
Design of innovative anode-cathode interface
First design: conical interface with 35° angle
Lateral Surface Temperature
Frontal Surface Temperature
Production by means of LPBF of the first prototype, ready for:
High temperature characterization
Thermionic emission measurement
Ionization efficiency tests with stable beams (noble gases)
High temperature characterization of the conical cathode

## Slide 7: The FEBIAD Ion Source
Influence of the cathode surface finishing
3D Optical Profiler Sensofar Neox
Sandblasted
Turned
Polished
Production of Standard LPBF cathodes and subsequent mechanical operation to have three different frontal surface finishing
Frontal Surface finishing characterization using an Optical Profiler
Study the parameters that can have an influence on the thermionic emission
Sandblasted
Turned
Polished

## Slide 8: The FEBIAD Ion Source
Influence of the anode grid transparency
Chart: Anode Drain Current
| 1708.4666666666665 | 1737.6333333333332 | 1764.6666666666667
Anode_33% | 0.83344 | 0.83828 | 0.84565
Anode_50% | 0.75567 | 0.76871 | 0.77644
(1) Transfer line
(2) Cathode
(3) Anode
(4) Probe
(5) Housing support
(6) Extraction chamber
(7) Support Box
(8) Insulators
150 V
150 V
-
-
-
-
-
-
-
-
-
-
-
-
-
-
i(t)
Transparency: 20%
Transparency: 33%
Transparency: 50%
Production of new grid geometries by means of LPBF with different transparency
Anode 33% during thermionic emission test

## Slide 9
The ECR Ion Source
Definition of a Finite Element Model
Chart: Crucible axis [mm]
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25
0 A | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20 | 20
0.25 A | 59.284 | 59.959 | 60.53 | 61.101 | 61.637 | 62.161 | 62.658 | 63.129 | 63.573 | 63.99 | 64.38 | 64.745 | 65.085 | 65.401 | 65.69 | 65.951 | 66.181 | 66.377 | 66.543 | 66.684 | 66.805 | 66.906 | 66.983 | 67.031 | 67.056 | 67.061
0.5 A | 254.03 | 259.84 | 264.75 | 269.67 | 274.22 | 278.64 | 282.83 | 286.79 | 290.5 | 293.97 | 297.19 | 300.18 | 302.96 | 305.5 | 307.79 | 309.8 | 311.51 | 312.9 | 313.98 | 314.85 | 315.55 | 316.1 | 316.47 | 316.6 | 316.55 | 316.44
0.75 A | 546.23 | 566.27 | 582.59 | 598.32 | 612.18 | 624.94 | 636.41 | 646.61 | 655.55 | 663.3 | 669.88 | 675.39 | 680 | 683.67 | 686.31 | 687.82 | 688.09 | 687.06 | 684.86 | 682.09 | 679.09 | 675.91 | 672.64 | 669.09 | 665.32 | 662.91
1 A | 798.05 | 841.76 | 875.39 | 906.07 | 931.48 | 953.53 | 972.23 | 987.84 | 1000.6 | 1010.6 | 1018.2 | 1023.6 | 1027.1 | 1028.7 | 1028.2 | 1025.4 | 1019.8 | 1011.4 | 1000.5 | 988.56 | 976.44 | 964.23 | 952.31 | 940.42 | 928.57 | 921.38
1.25 A | 1026.6 | 1104.1 | 1160.6 | 1209.8 | 1248.7 | 1281 | 1307.3 | 1328.3 | 1344.6 | 1356.9 | 1365.5 | 1370.8 | 1373.5 | 1373.5 | 1370.3 | 1363.2 | 1351.6 | 1335 | 1314.1 | 1291.6 | 1268.9 | 1246 | 1223.6 | 1201.4 | 1179.6 | 1166.6
1.5 A | 1253.1 | 1363.3 | 1437.5 | 1496.8 | 1539.9 | 1573.1 | 1598.7 | 1618.1 | 1632.7 | 1643.1 | 1649.7 | 1653.3 | 1654.6 | 1653.5 | 1649.1 | 1640.4 | 1626.1 | 1605.4 | 1578.7 | 1549.7 | 1520.2 | 1489.4 | 1458 | 1425.1 | 1390.8 | 1369.8
1.75 A | 1478.1 | 1611.8 | 1694.2 | 1755.8 | 1797.9 | 1829.3 | 1853.2 | 1871.2 | 1884.5 | 1893.8 | 1899.1 | 1901.4 | 1901.7 | 1899.6 | 1893.9 | 1883.3 | 1866.1 | 1841.1 | 1809 | 1774.2 | 1738.5 | 1700.7 | 1660.9 | 1617.9 | 1571.4 | 1541.7
2 A | 1704.7 | 1850.7 | 1937.4 | 2001.2 | 2044 | 2075.1 | 2098 | 2115 | 2127.2 | 2135.6 | 2139.8 | 2140.8 | 2140.3 | 2137.7 | 2131.2 | 2119.2 | 2099.4 | 2069.7 | 2030.8 | 1988.7 | 1946.1 | 1901.2 | 1853.6 | 1801.3 | 1743.5 | 1705
Thermal-electric simulation of the oven by means of ANSYS® MAPDL software
Temperature profile along the alumina crucible at different levels of supplied current
Chart: Current [A]
| 0 | 0.2 | 0.4 | 0.6 | 0.8 | 1 | 1.2 | 1.4 | 1.6 | 1.8 | 2
Model #1 | 0 | 0.65 | 2.05 | 4.05 | 6.63 | 9.73 | 13.25 | 17.31 | 21.76 | 26.71 | 32.34
Model #2 | 0 | 0.76 | 2.37 | 4.66 | 7.62 | 11.16 | 15.09 | 19.06 | 24.54 | 29.97 | 36.12
Datasheet | 0 | 5.7 | 10 | 13.6 | 20.3 | 29.7 | 31
Screw (Mo)
Oven body (Ta)
Crucible (Al2O3)
Heating Coil (W)
Insulators (Al2O3)
Oven head (AISI304)
Model #1
Model #2

## Slide 10
The ECR Ion Source
High temperature characterization
Observation Window
Observation Window
Endurance tests highlighted the instabilities of the oven and confirmed the strong gradient present in the crucible
Oven during high temperature test,
the red line identify the pyrometer spot
Chart: Time [seconds]
| 0 | 663 | 664 | 1101 | 1102 | 1689 | 1691 | 2171 | 2172 | 2761 | 2762 | 7404 | 7405 | 11292 | 11293 | 15152 | 15153 | 19034 | 19035 | 19477 | 19479 | 19900 | 19901 | 20290 | 20292 | 20769 | 20770 | 21632 | 21633 | 23309 | 23311 | 23405
FEM | 591.7174 | 591.7174 | 690.4449 | 690.4449 | 783.31 | 783.31 | 871.8579 | 871.8579 | 914.9958 | 914.9958 | 957.6338 | 957.6338 | 1042.1829 | 1042.1829 | 1127.0503 | 1127.0503 | 1213.7812 | 1213.7812 | 1127.0503 | 1127.0503 | 1042.1829 | 1042.1829 | 957.6338 | 957.6338 | 871.8579 | 871.8579 | 783.31 | 783.31 | 690.4449 | 690.4449 | 591.7174 | 591.7174
1.20A
1.50A
1.40A
1.30A
Redesign strongly recommended!

## Slide 11
Educational activities
Vacuum Technologies
Optimization Methods for Mechanical Design
Python for Numerical Heat Transfer Modelling and Building Physics
Physics, Technology and Applications of Linear Accelerators
Abroad period
Experimental campaign at ISOLDE (CERN)
School
Courses, exams and other training activities
COURSES
Expected in Fall 2026
Expected in 2026
Expected in Mar 2026
Completed in June 2025
Expected in Mar 2026
Ongoing
To be defined
OTHER
Co-supervisor of two Master’s Thesis
To be defended in Oct. 2025

## Slide 12
Thank you for your attention!