## Slide 1
Lodovico Ratti
Università di Pavia and INFN Pavia
(lodovico.ratti@unipv.it)
WP2 meeting
https://cern.zoom.us/j/6401428621
September 9, 2025
Online DCR measurements on CMOS SPADs

## Slide 2
150 nm CMOS technology
Available for characterization in single- and dual-layer configuration
Device under test: 150 nm CMOS SPAD
P+/N-well junction, isolated from substrate by deep n-well

## Slide 3
Neutron irradiation and test procedure
5 mm
5 mm
Three chips exposed to neutrons (0.5 to 3 MeV) in different steps up to a maximum fluence of 4.3x1010 1 MeV neutron equivalent cm-2
Relatively low flux: 3x106 1 MeV neutron equivalent cm-2s-1
Readout electronics biased in standard condition, SPADs biased at an excess voltage of 1.3 V
Irradiation and measurements (online and at the end of each step) performed at T=20°C
Time resolved measurements performed with a time resolution of 100 ms

## Slide 4
DUT
test board (bias, configuration, readout)
proton beam pipe
Test setup

## Slide 5
Online DCR measurements
72 pixels, 48 from array A1 and 24 from array A3, were monitored during irradiation  DCR was measured while the samples were being irradiated
Three chips, two single layer, one dual layer
Online DCR measurement procedure: of the 72 pixels
    9 pixels at a time are enabled for a Dt time window, then their single bit memories are read out in parallel and reset
    the previous operation is repeated Nr times for the same 9 pixels, resulting in an overall integration time Nr Dt, ensuring a sensitivity 1/Nr Dt
    the previous two steps are repeated for the other 63 pixels, 9 at a time
    with Dt=2 us, Nr=2500, sensitivity=200 Hz
    with the previous settings, we were able to measure the DCR of each of the 72 pixels every 100 ms
A similar approach can be replicated in the 110 nm test chip, where 6 pads for parallel readout of A1 and A3 arrays are available

## Slide 6
Time resolved DCR measurements
Online DCR measurements (100 ms time resolution) make it possible to study short-term annealing processes – to be taken into account when estimating damage based on fluence and non-ionizing energy loss (NIEL)
Significantly large set of events with pseudo-exponential recovery
150 s
F=8.10x109 cm-2
Single-layer, A1 subarray (75 mm pitch)

## Slide 7
Neutron-triggered RTS fluctuations
RTS fluctuations beginning a few tens to a few hundred of seconds after irradiation starts
bi-stable defect
mostly bi-stable defect, two seldom appearing additional levels