## Slide 1: HTS High Field Magnets for Future Energy Frontier Colliders
Francesco Mariani – ID 2118962
Ph.D in Accelerator Physics - 39° cycle
Sapienza University of Rome
Supervisor: Prof. Lucio Rossi
Co-Supervisor: Dott. Samuele Mariotto

## Slide 2: Table of contents
HTS for Future Colliders
Brandt Model Implementation
10T Dipole Demonstrator for FCC
Field Measurements of Racetrack Coils made at INFN-LASA
Next Steps
16T Dipole for Muon Collider

## Slide 3: HTS for Future Colliders
Higher energies can be obtained inside a collider either by increasing the bending radius of the machine or by enhancing the magnetic field.
Magnets exploiting High Temperature Supercondoctor (HTS) technology can achieve higher field values and allow to reduce the cryogenic power.
REBCO 1 is one of the most performant HTS materials in these terms.
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
HOWEVER…
REBCO superconductor is ceramic (so brittle) and anisotropic : it cannot be extruded in a filamentary structure!
This material needs to be deposited on flat substrate forming a tape-shaped conductor.
1 rare-earth barium copper oxide (REBCO, e.g., YBa₂Cu₃O₇–x)

## Slide 4: Screening Currents Magnetization
The high aspect ratio of REBCO tapes results in enhanced magnetization produced by the persistent currents flowing inside the superconductor to screen the external field.
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
Goal
Investigate screening current phenomenon by quantitative analysis and exploring mitigation strategies!
16
0
2
4
6
8
10
12
This phenomenon negatively affect the magnet performances :
  Hysteretic losses
  Field quality degradation
  Additional mechanical stresses
1 Comsol multiphysics. [Online]. Available: https://www.comsol.com
1

## Slide 5: Brandt Model
If , with the increase of the penetrates towards the center (Fig. a,b).
When :
  If has not yet fully penetrated, distributes in the region not yet saturated (Fig. c,d).
  If has fully penetrated, distributes in the central region, by pushing toward the edges (Fig. e,f).
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
1 E. H. Brandt and M. Indenbom, “Type-ii-superconductor strip with current in a perpendicular magnetic field” , Physical review B, vol. 48, no. 17, p. 12893, 1993.
2 Current density ) integrated along the tape thickness d (Figure inside the black box)
Brandt Model 1 describes how the distributes inside a single REBCO tape when immersed in uniform and perpendicular field.
Notes: The Brandt Model describes how the sheet current (Current density 𝑗 (𝐴/〖𝑚𝑚〗^2) integrated along the tape thickness d ) distributes inside a single REBCO tape when immersed in uniform and perpendicular field. It can be briefly described as follows:
If the transport current is zero and an external field is present, a screening current (𝐼_𝑠𝑐𝑟𝑒𝑒𝑛) originates inside it (starting from the edges) to cancel the inner perpendicular field (Fig.a)
As the field increases (Fig. b) , 𝐼_𝑠𝑐𝑟𝑒𝑒𝑛 penetrates towards the center of the tape thus reducing the zero-field region.
If a transport current 𝐼_𝑡 flows along the tape, we need to distinguish between 2 scenarios:
If 𝐼_𝑠𝑐𝑟𝑒𝑒𝑛 has not yet fully penetrated inside the tape (Fig.c) , then 𝐼_𝑡 will distribute in the region not yet saturated (Fig. d);
Whereas if 𝐼_𝑠𝑐𝑟𝑒𝑒𝑛 has fully penetrated (Fig. e) , then 𝐼_𝑡 will distribute in the central region of the tape by pushing 𝐼_𝑠𝑐𝑟𝑒𝑒𝑛 towards the edges and so reducing its intensity (Fig. f).

## Slide 6: Brandt Model for Magnet Design
1 tape
10736 tapes
uniform
non uniform
tape
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
The model considers only a single tape, whereas the dipole magnet is made of thousands of tapes.
The model assumes a single value of in which the tape is immersed.
Iterative solution needs to be performed to consider how each tape is affected by the current distribution of the others.
averaged along each tape is taken as the uniform field in which the tape is immersed.
Notes: Implementing this model in MATLAB for the calculation of the current distribution over a magnet cross section is not straightforward:
- First, because magnets are composed by not one but thousands of tapes interacting between each other. For this reason, iterative solution needs to be performed to consider how each tape is affected by the current distribution of the others.
In addition, the model assumes a single value of 𝑩_┴ in which the tape is immersed, but the field produced by a magnet is non-uniform in the coil region. So, to apply the model, we must average the field along each tape.

## Slide 7: MATLAB code initialization
The magnetic flux density value B is calculated in each quadrature point.
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
2= quadrature point
Inside each block of the magnet, a grid of quadrature points is built.
A uniform current distribution is supposed to flow inside the magnet (i.e. same value of for each ).
1 MathWorks. 1994-2023 the mathworks, inc. [Online]. Available: https://matlab.mathworks.com
1
2
quadrature point qp

## Slide 8: New current distribution
For each the value of critical sheet current density is calculated taking into account both the intensity and the direction of .
For each tape the mean critical sheet current density is calculated :
,
New sheet current density for each by the following formula :
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani

## Slide 9: Iterative Process
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
1= field orientation respect the tape surface
The new value of obtained by the Brandt formula will generate a new field map producing a new sheet current distribution .
The process must be iterated several times until convergence is achieved.
Iteration n
current distribution
Field map over the coils cross-section
Biot-Savart
current distribution
obtained for each tape
Brandt
Does it converge?
Yes
No
-1
1
0
N.B. No time-dependent phenomena
Notes: By the iterative process schematized on the right the solution is reached.
Indeed, the new value of 𝑠ℎ𝑒𝑒𝑡 𝑐𝑢𝑟𝑟𝑒𝑛𝑡 𝑑𝑒𝑛𝑠𝑖𝑡𝑦 𝐽_𝑛 obtained by the Brandt formula will generate a new field map producing a new sheet current distribution 𝐽_(𝑛+1).The process must be iterated several times until convergence is achieved.
the code, actually, cannot simulate time dependent phenomena. It means that in principle it is more suitable for the design of steady state magnets instead of ramped magnets.

## Slide 10: Code Validation by comparison with FEM software
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
16T Dipole for Muon Collider
(steady state)
  10T dipole demonstrator for FCC (ramped)

## Slide 11: Muon Collider
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
REQUIREMENTS | 
 | (with iron)
REQUIREMENTS | 
EM and MEC design considering effects produced by screening currents.
GOAL
Collider Ring Dipoles
featuring:
Highest field possible to have a compact ring.
Large aperture for shielding against beam induced heat.
(10 km-long ring, C.o.M of 10 TeV)

## Slide 12: Comparison: ROXIE-MATLAB
ROXIE
MATLAB
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
First numerical validation of field and margin using before adding complex effect.
1
1 S. Russenschuck. Roxie. [Online]. Available: https://espace.cern.ch/roxie
Notes: Before considering screening currents , a first numerical validation of field and margin using〖 𝐽〗_𝑢𝑛𝑖𝑓 had been performed.
The comparison with results obtained by ROXIE (a FEM software developed by CERN) shows good agreement between the two tools, ensuring that any possible deviation that could arise considering screening currents are not attributable to the wrong implementation of the basic equations or to the wrong integration of the grid points.

## Slide 13: Validation by COMSOL
(MATLAB)
(COMSOL)
N.B. Iron yoke not considered
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
2° numerical validation considering and comparing results with COMSOL.
1 Thinkbook Lenovo: RAM (16 GB), Processor (AMD Ryzen 5 5600 with Radeon Graphics, 2.3 GHz), 6 core
1

## Slide 14: Mechanical Study: Lorentz Forces
Homogenized coils ()
Infinitely rigid structure
Frictionless contact between coils and structure
Layers bonded together
Only Lorentz forces (no forces for cooling contraction)
Goal: evaluate how screening currents affect the stress analysis.
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani

## Slide 15: Mechanical Study: Stresses
Radial stress
Azimuthal stress
Transverse Compressive Stress
> 400 MPa2
Transverse Tensile Stress
10-100 MPa1
Parallel Compressive Stress
< 100 MPa2
Parallel Tensile Stress
> 700 MPa1
(MPa)
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
= 22 Mpa
= - 197 MPa
= 17 Mpa
= -261 MPa
Next Study Step:
Stress management
Radial compressive stress
needs to be reduced!
1 H. Maeda and Y. Yanagisawa, "Recent Developments in High-Temperature Superconducting Magnet Technology (Review)," doi: 10.1109/TASC.2013.2287707
2 Superconductor Business Development Division Fujikura Ltd., “Introduction of Fujikura re-based high temperature superconductor,” Fujikura Global, Koto City, Tokyo, Japan, Tech. Rep., Jul. 2024. [Online]. Available: https://www.fujikura.co.jp/eng/products/newbusiness/

## Slide 16: FCC-hh
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
Next generation Hadron Collider proposed at CERN.
Designed for 100 TeV center-of-mass energy.
90 km circular tunnel planned near Geneva.
Requires high-field superconducting dipole magnets (14 T).
Key challenge: use of HTS materials in ramped-magnet!
INFN-CERN agreement within HFM program foresees the construction of a 10 T (with no iron contribution) HTS dipole demonstrator.
Preliminary target

## Slide 17: 10T HTS Dipole Demonstrator
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
REQUIREMENTS | 
(geometric) | 
REQUIREMENTS | 
ROXIE
COMSOL
COMSOL
MATLAB
EM design considering

## Slide 18: Field Measurements on Racetrack Coils
GOAL
Coil system must be designed to enhance the screening current effects.
Parametric simulations to identify the best layout.
comparing the measurements with the simulated results for further validation.
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani

## Slide 19: Output Example ()
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani

## Slide 20
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
The best configuration, also considering the ease in construction, is:
STAND ALONE | 
STAND ALONE | 
Hall probe

## Slide 21: Next Steps
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
winding
assembly
test of magnet performances
comparison

## Slide 22
Timeline
Analytical Brandt Model Implementation in MATLAB
1° year
Further code validation by comparison with experimental results through field measurements on Racetrack coils
3° year
Code validation by COMSOL developing the 16T Muon Collider HTS dipole and the 10T FCC HTS dipole demonstrator
2° year
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
Notes: .

## Slide 23: Thank you for the attention!
HTS High Field Magnets for Future Energy Frontier Colliders
Francesco Mariani

## Slide 24: References
Papers:
Images:
Slides:
  https://github.com/pietro-nardelli/sapienza-ppt-template [Attribution-NonCommercial-ShareAlike 4.0 International (CC BY-NC-SA 4.0)]
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani

## Slide 25: Backup Slides

## Slide 26: Brandt Model Implementation
HTS High Field Magnets for Future Energy Frontier Colliders – Francesco Mariani
1 = self field contribution VS external field contribution
N.B. the parameter g if , while if
…
3
1
2
where
the values of for each tape must be obtained (and )
,
,