## Slide 1
Funded by the European Union (EU). Views and opinions expressed are however those of the author only and do not necessarily reflect those of the EU or European Research Executive Agency (REA). Neither the EU nor the REA can be held responsible for them.
Development of Superconducting Magnets for the Future
Muon Collider
Daniel Novelli
Ph.D. in Accelerator Physics
Final Seminar XXXVIII cycle
12 November 2025
Supervisors:
Stefania Farinon
Barbara Caiffi
Tutor:
Lucio Rossi

## Slide 2: Why a Muon Collider?
The Muon Collider is a very promising post-LHC high physics facility:
  200 times heavier than electron ( m=105.7 MeV/c2 ,me=0.511 MeV/c2 ) → 109 times less radiation loss.
  elementary particle: all COM energy available for the collision, contrary to hadron machines.
BUT ecays in 2.2 in rest frame:
IMCC (Internation Muon Collider Collaboration) aims at studying the feasibility of a 10 km, 10 TeV center of mass energy Muon Collider, as indicated by the European Strategy for Particle Physics.
must be produced, accelerated and collided ASAP
decay products must be shielded to avoid damage to the machine or radiation
Notes: The energy at which the proton collider cross-section equals that of a muon collider. The dashed line assumes comparable Feynman amplitudes for the muon and the proton production processes. A factor of ten enhancement of the proton production amplitude squared, possibly due to QCD production, is considered in the continuous line

## Slide 3: Why a Muon Collider?
IMCC (Internation Muon Collider Collaboration) aims at studying the feasibility of a 10 km, 10 TeV center of mass energy Muon Collider, as indicated by the European Strategy for Particle Physics.
must be produced, accelerated and collided ASAP
decay products must be shielded to avoid damage to the machine or radiation
J.P. Delahaye et al., Muon colliders,
arXiv:1901.06150 [physics.acc-ph].
Physics?
Muon collisions in the range of 14 TeV
have comparable discovery potential to hadron (proton) collisions in the range of 100 TeV
The Muon Collider is a very promising post-LHC high physics facility:
  200 times heavier than electron ( m=105.7 MeV/c2 ,me=0.511 MeV/c2 ) → 109 times less radiation loss.
  elementary particle: all COM energy available for the collision, contrary to hadron machines.
BUT ecays in 2.2 in rest frame:
Comparable Feynman amplitudes for the muon and the proton production processes.
A factor of ten enhancement of the proton production amplitude squared,
possibly due to QCD production, is considered.

## Slide 4: Why a Muon Collider?
IMCC (Internation Muon Collider Collaboration) aims at studying the feasibility of a 10 km, 10 TeV center of mass energy Muon Collider, as indicated by the European Strategy for Particle Physics.
must be produced, accelerated and collided ASAP
decay products must be shielded to avoid damage to the machine or radiation
K. R. Long et al, Nature Physics, v.17, p.289, 2021.
Sustainability?
A 10 TeV muon collider
can provide the highest integrated luminosity
per unit of energy consumption.
The Muon Collider is a very promising post-LHC high physics facility:
  200 times heavier than electron ( m=105.7 MeV/c2 ,me=0.511 MeV/c2 ) → 109 times less radiation loss.
  elementary particle: all COM energy available for the collision, contrary to hadron machines.
BUT ecays in 2.2 in rest frame:
Collider size comparison
D. Schulte, The muon collider, IPAC2022, Bangkok, Thailand.

## Slide 5: Why a Muon Collider?
IMCC (Internation Muon Collider Collaboration) aims at studying the feasibility of a 10 km, 10 TeV center of mass energy Muon Collider, as indicated by the European Strategy for Particle Physics.
must be produced, accelerated and collided ASAP
decay products must be shielded to avoid damage to the machine or radiation
D. Neuffer and V. Shiltsev 2018 JINST 13 T10003
Affordability?
Its size is competitive because it is compact.
A 10 TeV muon collider making use of the LHC infrastructure could be the most cost-effective energy frontier collider
The Muon Collider is a very promising post-LHC high physics facility:
  200 times heavier than electron ( m=105.7 MeV/c2 ,me=0.511 MeV/c2 ) → 109 times less radiation loss.
  elementary particle: all COM energy available for the collision, contrary to hadron machines.
BUT ecays in 2.2 in rest frame:
Collider size comparison
D. Schulte, The muon collider, IPAC2022, Bangkok, Thailand.

## Slide 6: Why a Muon Collider?
Main stages of a muon collider complex
Purpose:
Evaluate realistic performance targets for the collider magnets, in close collaboration with studies of beam physics, cryogenics, and energy storage.
Produce a credible and affordable design study (contain costs, energy efficiency, sustainable operation).
Magnets:
Dipoles
Quadrupoles
Sextupoles
Combined Dip + Quad
Combined Dip + Sext

## Slide 7: Collider Magnets Requirements
3 TeV collider (5 km ring):
Close to state of the art
11T/150mm (Nb3Sn)
600 magnets, 5 m length
Operating temperature: 4.5 K
10+ TeV collider (10 km ring):
HTS magnets, R&D is required
16T/150mm (ReBCO, hybrid)
1200 magnets, 5 m length
Operating temperature: 4.5…20 K
High field dipoles to minimize collider ring size and maximize luminosity.
Beam loss protection
High-energy electrons and positrons arising from muon decay and striking the collider ring magnets can cause radiation damage and unwanted heat load.
Shielding
Large aperture
Muon decay
Dip + Quad combined-function
Circular magnet aperture, 4.5 K
Dimensions (130x130) mm
Tungsten = (40x40) mm

## Slide 8
Allowed area
Forbidden area
Allowed area
Forbidden area
Allowed area
Forbidden area
Allowed area
Forbidden area
Allowed area
Forbidden area
Allowed area
Forbidden area
Main assumptions:
– Cos-theta cross section in sector coil approx.
– Budget: 400 kEUR/m for each magnet.
– These plots apply to ARC magnets. For the IR quadrupoles, a double budget is assumed.
– SC cost: 2500 EUR/kg (aspirational value).
– Max. coil width: 80 mm
– Max. stress: 400 MPa
– Protection: MI or NI
– Tungsten screen: 3 cm at 20K, increasing to 4 cm if below 20K.
– HTS as baseline for the 10 TeV, NbTi and Nb3Sn as options for the 3 TeV.
– Filling factor = 0.011 (Roebel cable)
ANALYTICAL STUDY
Limit curves are introduced by mechanical challenges (stress limit), critical current density (margin limit) and stored magnetic energy (quench protection), depending on the superconducting material.
HTS arc A-B and A-G plots
Notes: This is an innovative approach, useful for interfacing the needs of beam dynamics with the technological limits (of today and the near future) related to superconducting magnets.
Could provide an immediate feedback capable of analyzing many possible configurations in a single plot.

## Slide 9: Combined-Function Magnets
Beam physics requirements
Dip + Quad :
8 T, 100 T/m, aperture of 310 mm (FF)
8 T, 320 T/m, aperture of 130 mm (ARC)
4 T, 240 T/m, aperture of 170 mm (Corr.)
4 T, 330 T/m, aperture of 130 mm (Corr.)
Dip + Sext :
14 T, 7100 T/m2, aperture of 130 mm (ARC)
4 T, 11555 T/m2, aperture of 170 mm (Corr.)
Nested Configurations
Asymmetric Coils
Quad inside Dip
Dip inside Quad
Asym. Dip
Asym. Quad
Problem of the neutrino flux:
Notes: Purpose:
Evaluate realistic performance targets for the collider magnets, in close collaboration with studies of beam physics, cryogenics, and energy storage.
Produce a credible and affordable design study (contain costs, energy efficiency, sustainable operation).

## Slide 10
a1_quad
w_quad
w_dip
A Python-ANSYS interface was developed to run FEM configurations capable of providing the electromagnetic performance of various designs.
Loops were implemented by varying the temperature, a1_quad and w_quad. For each fixed value, the maximum w_dip was calculated using a cost model, and an optimization code for electromagnetic performance was executed. This code aimed to maximize the current density while staying within stress and margin limits.
Python-Ansys Interface
Electromagnetic optimization
Fixed geometry
Mechanical optimization
Cost model
Change geometry
For each temperature:

## Slide 11
w_dip
w_quad
Current density
Optimization (1%)
Optimize J_quad​ and J_dip​ to be close to the critical current density:
….
while not ( 0.99 < f < 1.01 ):
…..
→ ANSYS input (a1, w_quad, J_quad, w_dip, J_dip)
Run ANSYS
ANSYS output →
f = J_c (B_peak) / J
if f > 1: J=J*1.01
else: J = J*0.99
…..
…..
the optimization acts on J_quad and J_dip
with corrections of 1%,
and the cycle closes when either
J_quad or J_dip is within 1% of J_c
Limitations on stress and cost are still missing
Only EM optimization
Method: B-G plot at 4.5K

## Slide 12
Chart: Gradient [T/m]
| 196.66692 | 164.01513 | 142.37194 | 128.22597999999999 | 116.85381 | 108.48817 | 100.74382 | 93.680881999999997
w_quad=10mm | 8.7624 | 12.8845 | 15.8254 | 18.1884 | 20.3397 | 21.9954 | 23.6469 | 24.962
w_quad=20mm | 8.6179 | 12.691 | 15.4943 | 17.8753 | 20.0047 | 21.7123 | 23.3549 | 24.7758
w_quad=30mm | 8.486 | 12.4244 | 15.2232 | 17.5711 | 19.6635 | 21.3661 | 22.9663 | 24.3751
w_quad=40mm | 8.3249 | 12.0514 | 14.8888 | 17.2671 | 19.329 | 21.0997 | 22.5924 | 24.0893
w_quad=50mm | 8.0976 | 11.8841 | 14.6303 | 17.0466 | 19.0072 | 20.8447 | 22.3246 | 23.7028
w_quad=60mm | 7.8859 | 11.5245 | 14.313 | 16.6119 | 18.7678 | 20.4148 | 21.9644 | 23.4211
w_quad=70mm | 7.6968 | 11.3159 | 14.1243 | 16.4023 | 18.4585 | 20.1714 | 21.7076 | 23.0556
w_quad=80mm | 7.5309 | 11.0653 | 13.7617 | 16.1232 | 18.1558 | 19.9266 | 21.3606 | 22.792
Current density
Optimization (1%)
Optimize J_quad​ and J_dip​ to be close to the critical current density:
….
while not ( 0.99 < f < 1.01 ):
…..
→ ANSYS input (a1, w_quad, J_quad, w_dip, J_dip)
Run ANSYS
ANSYS output →
f = J_c (B_peak) / J
if f > 1: J=J*1.01
else: J = J*0.99
…..
…..
the optimization acts on J_quad and J_dip
with corrections of 1%,
and the cycle closes when either
J_quad or J_dip is within 1% of J_c
Limitations on stress and cost are still missing
Only EM optimization
Method: B-G plot at 4.5K
Increasing
Increasing

## Slide 13
EM and Stress optimization
Midplane pressure
Optimization (1%)
Optimize (decrease) J_quad​ and J_dip​ to not exceed the maximum stress (400 MPa)
…..
while not ( 0.99 < f < 1.01 ):
…..
read the J from 1% optimization
→ ANSYS input (a1, w_quad, J_quad, w_dip, J_dip)
Run ANSYS
ANSYS output →
if stress > 400:
f = 400/stress
J=J*
…..
…..
the optimization acts on J_quad and J_dip
with quadratic dependence of J on stress,
and the cycle closes when the stress is below
400 MPa on both the dipole and the quadrupole.
Limitation on cost is still missing
Method: B-G plot at 4.5K

## Slide 14
EM, Stress and Cost optimization
Chart: 
| 108.48817 | 190.70204000000001 | 258.54275999999999 | 305.21280999999999 | 347.07609000000002 | 392.33798000000002 | 426.81304 | 481.05939999999998
a1=25mm, T=4.5K | 21.9954 | 19.9533 | 17.5878 | 15.1191 | 12.4368 | 9.798 | 6.9049 | 3.4961
a1=50mm, T=4.5K | 17.9425 | 15.4509 | 12.9332 | 10.3704 | 7.5264 | 4.0514
a1=75mm, T=4.5K | 14.2376 | 11.8742 | 9.2632 | 6.3305 | 2.7034
a1=100mm, T=4.5K | 11.9483 | 9.257 | 6.3572 | 2.7452
Method: B-G plot at 4.5K
Cost
Optimization
The dipole coil width (w_dip) can be computed if the aperture radius (a1_quad) and the quadrupole coil width (w_quad) are known.
…..
for a1_quad in range(25,151,25):
…..
for w_quad in range(10, 81, 10):
w_dip = round(cost_model(a1_quad,w_quad),0)
…..
…..
…..
The cost value for the structures and iron is taken from HL-LHC, while the cost of the superconducting material (ReBCO) is based on the aspirational value of 2500 EUR/kg.
Maximum budget for each magnet: 400 kEUR/m
  The cost model saves one point for each curve with the same aperture.

## Slide 15
EM, Stress and Cost optimization
Chart: 
| 108.48817 | 190.70204000000001 | 258.54275999999999 | 305.21280999999999 | 347.07609000000002 | 392.33798000000002 | 426.81304 | 481.05939999999998
a1=25mm, T=4.5K | 21.9954 | 19.9533 | 17.5878 | 15.1191 | 12.4368 | 9.798 | 6.9049 | 3.4961
a1=50mm, T=4.5K | 17.9425 | 15.4509 | 12.9332 | 10.3704 | 7.5264 | 4.0514
a1=75mm, T=4.5K | 14.2376 | 11.8742 | 9.2632 | 6.3305 | 2.7034
a1=100mm, T=4.5K | 11.9483 | 9.257 | 6.3572 | 2.7452
Cost
Optimization
The dipole coil width (w_dip) can be computed if the aperture radius (a1_quad) and the quadrupole coil width (w_quad) are known.
…..
for a1_quad in range(25,151,25):
…..
for w_quad in range(10, 81, 10):
w_dip = round(cost_model(a1_quad,w_quad),0)
…..
…..
…..
The cost value for the structures and iron is taken from HL-LHC, while the cost of the superconducting material (ReBCO) is based on the aspirational value of 2500 EUR/kg.
Maximum budget for each magnet: 400 kEUR/m
  The cost model saves one point for each curve with the same aperture.
Method: B-G plot at 4.5K
  For different costs, we will have different limit curves, but not different points. Each point is EM- and stress-optimized using FEM code;
the selection of the maximum point on each dotted curve depends on the cost.

## Slide 16
Each curve of a different color corresponds to a different magnet aperture.
For a fixed aperture, the area under the curve is the allowed area for identifying a target design, while the area above the curve is the prohibited area where some maximum limit (stress, margin, quench protection or cost) will be exceeded.
8 T, 320 T/m, aperture of 130 mm (ARC)
Results: B-G plot at 4.5K
For example:
Green area = allowed area
Red area = forbidden area
The same method can be applied for sextupole – dipole combined function magnets, which are essential in the arc and in the chromaticity correction and matching sections

## Slide 17
Limits of Combined–Function Magnets
Dip + Quad B–G plots
Dip + Sext B–G2 plots

## Slide 18
Specific design for this configuration:
4 layers, canted cos-theta (two double-pancakes):
  - first two layers = B2
  last two layers = B1+B2
Nb3Sn cable used for the MQXF magnets of HL-LHC.
Aperture of 130 mm.
Ansys model to evaluate the performance @ 4.2 K.
Winding test to prove the configuration feasibility
One of the most effective technologies available today is Nb3Sn cables, while R&D is still required for HTS.
What performance can be achieved with a quad + dip magnet using this cable?
How far are we from meeting the beam optics requirements?
Removing the constraint of having the quadrupole inside and the dipole outside, the study revealed that the best configuration is having a quadrupole inside and a combined function outside with B1[T] / (B2[T/m]*Raperture ) = 1.4, that means with a stronger dipolar component.
Quad
Dip+Quad
Layer 1
Layer 2
Layer 3
Layer 4
Raperture= 65 mm | [T] | [T/m] | [T]
Simulation | 3.97 | 157.80 | 14.34
Design Target | 8 | 320 | 
Raperture= 65 mm |  |  | 
Simulation | 3.97 | 157.80 | 14.34
Design Target | 8 | 320 | 
With the technology available today, only up to half of the required performance can be achieved.
MQXF cable
Practical studies

## Slide 19
Analytical and
numerical study
3D model
3D printing
Winding test
The winding test was successfully executed.
The large aperture facilitate the winding process.
The winding was stopped after the first turn in order to save the cable for other tests, as each turn should be identical to the others.
Conclusion: the windability of this magnet has been proved for a CCT geometry.
Layer 3, combined function
Layer 1, quadrupole
Feasibility Study

## Slide 20
The limit plots are provided and discussed using both analytical and FEM approaches, serving as a starting point for defining possible beam optics that are also compatible with current technological constraints.
      B-G plots:
        Combined dipole + quadrupole magnets
      B-G2 plots:
        Combined dipole + sextupole magnets
These plots represent a powerful method for identifying new design targets for each magnet type. The allowed area does not imply that a magnet there is feasible, but that—based on analytical calculations and numerical simulations using simplified models—it is worth exploring a detailed design study within that region.
This work enable the comparison of a wide range of electromagnetic configurations within a single plot, providing a comprehensive view of the trade-offs between aperture and electromagnetic performances. Although these plots were developed in the framework of the Muon Collider, the methodology itself is general. By adjusting the underlying assumptions, it can be readily extended to any other accelerator project.
Summary and conclusions
A-B plots: Dipoles
A-G plots: Quadrupoles
A-G2 plots: Sextupoles

## Slide 21
Funded by the European Union (EU). Views and opinions expressed are however those of the author only and do not necessarily reflect those of the EU or European Research Executive Agency (REA). Neither the EU nor the REA can be held responsible for them.
Ph.D. in Accelerator Physics
Final Seminar XXXVIII cycle
12 November 2025
Thank you
For your attention
Daniel Novelli

## Slide 22
We implemented a FEM model for a sector dipole in ANSYS.
We implemented a Python code able to work with Ansys software
to run FEM simulations with the same inputs as the analytical study.
In the comparison, the FEM curves are always more restricting than the analytical ones
since they take the maximum pressure on the midplane instead of an average over the coil width.
FEM Crosscheck for Stress Curves

## Slide 23
We implemented a FEM model for a sector quadrupole in ANSYS.
We implemented a Python code able to work with Ansys software
to run FEM simulations with the same inputs as the analytical study.
In the comparison, the FEM curves are always more restricting than the analytical ones
since they take the maximum pressure on the midplane instead of an average over the coil width.
FEM Crosscheck for Stress Curves

## Slide 24
The A - G2 plots of the sextupole standalone corresponds to the points on the x-axis of the combined function B - G2 plots.
Sextupole Standalone

## Slide 25
Nb3Sn is limited by peak stress and operating margin
NbTi is intrinsically limited by the which doesn’t allow to reach high field
Dip. A-B Plots with LTS technologies

## Slide 26
Nb3Sn is limited by peak stress and operating margin
NbTi is intrinsically limited by the which doesn’t allow to reach high field
Quad. A-B Plots with LTS technologies

## Slide 27
Quad. A-B Plots with LTS technologies
The curves shown in the plots are the limit curves,
i.e., for each aperture value the strictest limit is taken, excluding the limit for insulated magnets.
reduction
Baseline:
400 kEUR/m
for each magnet
A reduction of operating temperature will result in wider design A-B range
reduction

## Slide 28
Summary of cost assumptions:
We use the ReBCO’s aspirational cost 2500 EUR/kg
  Today’s price is around 8000 EUR/kg
The starting budget of 175 kEUR/m is taken from the FCC cost model
Cryogenic, protection and shielding costs are not taken into account.
Summary of technical assumptions:
Single sector coil
Maximum allowed stress: 400 MPa
Fujikura Tape, Roebel cable
Non-insulated or Metal-insulated cable
Maximum coil width: 80 mm
HTS dipole – A-B Plots behavior
Cost reduction
Cost reduction
Cost reduction

## Slide 29
HTS dipole – A-B Plots behavior
Summary of cost assumptions:
We use the ReBCO’s aspirational cost 2500 EUR/kg
  Today’s price is around 8000 EUR/kg
The starting budget of 175 kEUR/m is taken from the FCC cost model
Cryogenic, protection and shielding costs are not taken into account.
Summary of technical assumptions:
Single sector coil
Maximum allowed stress: 400 MPa
Fujikura Tape, Roebel cable
Non-insulated or Metal-insulated cable
Maximum coil width: 80 mm
Cost
reduction
Cost
reduction
Cost
reduction

## Slide 30
Quad into dipole:
(ReBCO @20 K)
Dipole into quad:
(ReBCO @20 K)
Arc:
Combined function magnets: B1, B1+B2 and B1+B3
B ≈ 8…16 T; G ≈ 320 T/m; G’ ≈ 7100 T/m2
Aperture ≈ 130 mm
Final focus:
Combined function magnets: B1, B2, B1+B2 , B1+B3
B ≈ 4…16 T; G ≈ 100…300 T/m; G’ ≈ 12000 T/m2
Aperture ≈ 120…300 mm
The quadrupole into dipole configuration is the most efficient one, in accordance with US-MAP. Additionally, for combined function magnets in the muon collider, quadrupoles are generally required to be stronger than dipoles.
These two configurations are NOT realistic.
Combined: Nested Configuration