## Slide 1
PICOSEC Micromegas gaseous detectors
for precise timing and developments
towards applicable detector
Francesco Guerra
Supervisors: M. Lisowska, F. Brunbauer & E. Oliveri
October 17th, 2025

## Slide 2
Outline
  PICOSEC project
    Motivation
    Detector concept
    Developments towards applicable detector
  Single photoelectron measurements
    Detector assembling and testing
    General waveform analysis
    Code improvements
  Measurements with particle beam
    DRD1 test beam
    Signal analysis
    Robust photocathodes
    Large area prototype
  Summary & Conclusions
Francesco Guerra | 26 August 2025

## Slide 3: PICOSEC project
Francesco Guerra | 26 August 2025

## Slide 4
Gaseous detectors: cost effective, large area coverage, high rate resistance
Motivation
  Future high energy physics experiments will go for higher luminosity and precision measurements
   Highly precise timing detectors are required
Mitigation of pile-up
Precise ToF measurements
Francesco Guerra | 26 August 2025

## Slide 5
Standard Micromegas
Detector concept
PICOSEC Micromegas
Stochastic nature of ionization
 Time jitter of a few ns
σt ≈ 1.5 ns
Photoelectrons produced synchronous in space and time
σt ≈ O(10) ps
Early pre-amplification
Francesco Guerra | 26 August 2025
  J. Bortfeldt et al., NIM A 903 (2018) 317
  I. Giomataris et al., NIM A 376 (1996) 29-35

## Slide 6
Developments towards applicable detector
Single channel prototypes
Robust photocathodes
Large area prototypes
Scalable electronics
1 inch
DLC
Ti
B4C
Ageing studies - CsI
QE
10 cm
10 cm
Francesco Guerra | 26 August 2025
  A. Utrobičić et al., JINST 18 (2023) C07012
  M. Lisowska, PhD dissertation

## Slide 7: Single photoelectron measurements
Francesco Guerra | 26 August 2025

## Slide 8
Single photoelectron measurements
DUT
HV
Amplifier
Scope
UV LED
LV
Characterise the detector
Extract the average n. of PE produced per particle
Electron peak
Ion tail
Francesco Guerra | 26 August 2025

## Slide 9
Detector assembling and testing
Outer board
PEEK insert
Spacer
Radiator with photocathode
Housing
Quartz window
Flange
MM board
Francesco Guerra | 26 August 2025
  M.L.V. Fernandez, Summer student presentation

## Slide 10
General waveform analysis
Peak amplitude
Pre-trigger region
Polya distribution fit
Francesco Guerra | 26 August 2025

## Slide 11
Code improvements
Filtered analysis
Multi-peak recognition
Better noise rejection
Extracting easily general waveform properties (e.g. ion-tail end)
Code parallelization
57 min per run  11 min per run
Integrating over the entire waveform
Francesco Guerra | 26 August 2025

## Slide 12: Measurements with particle beam
Francesco Guerra | 26 August 2025

## Slide 13
DRD1 test beam
Particle beam @ CERN SPS H4 beamline
We have tested:
Single-channel prototypes
  Different resistivities
  Different photocathodes
Parallel plate prototypes
Different gas mixtures
PICOSEC as photon detector
Multi-channel prototypes
  Medium granularity
  100-channel double layer DLC MM
uRGroove PICOSEC (USTC)
PIMENT (Saclay)
Francesco Guerra | 26 August 2025

## Slide 14
Signal analysis
20%
tREF
20%
tDUT
CsI 3 nm
A: 275V
C: 440V
Preliminary
Timewalk correction
REF
DUT
  A. Utrobičić et al., NIM A 1072 (2024) 170127
  M. Lisowska, PhD dissertation

## Slide 15
Robust photocathodes
Various thicknesses of CsI, Ti and B₄C were evaluated to identify the optimal choice for application.
Preliminary
Preliminary
Preliminary
Francesco Guerra | 26 August 2025
The thinner, the better
Produced at the MPT workshop

## Slide 16
Large area prototype
24
Double layer DLC MM
23
34
33
Scope
Amp.
Amp.
Amp.
Amp.
10 mm
10 mm
Analysed configuration:
10 | 9 | 8 | 7 | 6 | 5 | 4 | 3 | 2 | 1
20 | 19 | 18 | 17 | 16 | 15 | 14 | 13 | 12 | 11
30 | 29 | 28 | 27 | 26 | 25 | 24 | 23 | 22 | 21
40 | 39 | 38 | 37 | 36 | 35 | 34 | 33 | 32 | 31
50 | 49 | 48 | 47 | 46 | 45 | 44 | 43 | 42 | 41
60 | 59 | 58 | 57 | 56 | 55 | 54 | 53 | 52 | 51
70 | 69 | 68 | 67 | 66 | 65 | 64 | 63 | 62 | 61
80 | 79 | 78 | 77 | 76 | 75 | 74 | 73 | 72 | 71
90 | 89 | 88 | 87 | 86 | 85 | 84 | 83 | 82 | 81
100 | 99 | 98 | 97 | 96 | 95 | 94 | 93 | 92 | 91
100 mm
100 mm
Marta Lisowska & Francesco Guerra | 6 October 2025
Photocathode: Ti 2.4 nm
Voltages: -550/275 V

## Slide 17
Large area prototype
24
34
23
33
24
34
23
33
First studying the pad one by one and then merging them together
Marta Lisowska & Francesco Guerra | 6 October 2025

## Slide 18
Single pad analysis
24
34
23
24
34
23
Marta Lisowska & Francesco Guerra | 6 October 2025
Pad center estimation from e-peak charge distribution
Timewalk correction for fully contained events
Time resolution for single pads evaluated as RMS of corrected SAT distribution
PAD | RMSSAT (ps)
23 | 39
24 | 38
33 | 39
34 | 41
Time resolution for fully-contained events
Fully contained

## Slide 19
Correlated spurious signals
Marta Lisowska & Francesco Guerra | 6 October 2025
Looking at SAT distribution
Events correlated in time even 15 mm distant from pad center

## Slide 20
Correlated spurious signals
Marta Lisowska & Francesco Guerra | 6 October 2025
Cutting geometrically and looking at SAT distribution
SAT in the center of pad 23

## Slide 21
Correlated spurious signals
Marta Lisowska & Francesco Guerra | 6 October 2025
Standard
Spurious
High frequency related (capacitive coupling)
Amplitudes ratio depends on distance
Possible time correlation with distance
This effect could be used to enhance spatial reconstruction capabilities of the detector
Adjacent
Diagonal
WORK IN PROGRESS…

## Slide 22
Combining different pads
Marta Lisowska & Francesco Guerra | 6 October 2025
Cutting on SAT to exclude spurious signals
Merging infos from different pads using eventID
Using a charge weighted algorithm to reconstruct particle hit position
Correcting SAT on the full set of events recorded by each pad

## Slide 23
Combining different pads
Marta Lisowska & Francesco Guerra | 6 October 2025
Combining corrected SAT from different pads
24
23
34
33
Selected area
Estimated time resolution for this detector:
45 ± 3 ps

## Slide 24: Summary & Conclusions
Francesco Guerra | 26 August 2025

## Slide 25
Summary & Conclusions
  Progress up to now:
    Improved analysis code for faster processing and better noise rejection
    Tested different photocathodes for time resolution (RMS):
      Ti: ~35 ps
      B₄C: ~50 ps
      CsI: ~12 ps
    Multipad prototype achieved 45 ± 3 ps over a selected area
  Future perspectives:
    Fine tuning of filtered analysis parameters
    Perform a more systematic study of photocathodes
    Investigate correlated spurious signals in detail
    Explore optimized methods for combining SAT from different pads (e.g. machine learning approaches)
Francesco Guerra | 26 August 2025

## Slide 26: Thank you for your attention!
Francesco Guerra | 26 August 2025

## Slide 27: Backup slides
Francesco Guerra | 26 August 2025

## Slide 28
PICOSEC for ENUBET: PIMENT
Francesco Guerra | 26 August 2025
ENUBET (Enhanced NeUtrino BEams from kaon Tagging) project aims at building a monitored neutrino: - timing at the ENUBET tagger for single MIP detection (<50 ps) - timing of e⁻ and 𝛾 showers in an electromagnetic calorimeter (∼10 ps) - instrumentation of the hadron dump for muon monitor - time tagging at the neutrino detector

## Slide 29
Waveform analysis: SNR problem
Polya distribution fit
Triggering higher  biasing results
Triggering lower  picking up noise
Francesco Guerra | 26 August 2025

## Slide 30
Time walk correction
Earlier pre-amplification  Bigger avalanche  Reduced signal arrival time
Francesco Guerra | 26 August 2025
  J. Bortfeldt et al., NIM A 993 (2021) 165049

## Slide 31
Test beam analysis
Francesco Guerra | 26 August 2025

## Slide 32
CsI photocathode
Francesco Guerra | 26 August 2025

## Slide 33
Ti photocathode
Francesco Guerra | 26 August 2025

## Slide 34
B4C photocathode
Francesco Guerra | 26 August 2025

## Slide 35
Double layer DLC MM
Double layer DLC MM
Photocathode: Ti 2.4 nm
Pre-amplification gap: 180 μm
Anode voltage: 275 V
Cathode voltage: 550 V
Charge is being evacuated vertically instead of horizontally
Achieve higher rate capability
Preserve protection against discharges
Francesco Guerra | 26 August 2025

## Slide 36
Rise time behaviour
Marta Lisowska & Francesco Guerra | 6 October 2025
Are we correcting SAT for some real avalanche dynamics or for something else?
Are there any other timing techniques alternative to CFD that will not suffer from changing rise time ?

## Slide 37: Old run from July 2022
Probably is not a problem coming from the resistive layer because in this run the multipad analysed was metallic
Adjacent
Diagonal

## Slide 38: Timewalk correction
What is the correct timewalk parametrization to use? Is there some geometrical effect?
Looking only at the pad
Looking only at the center of the pad
Looking at all* the events recorded on the pad
*after cutting on the SAT values to get rid of crosstalk

## Slide 39: SAT over the pad

## Slide 40: SAT over the pad
Even after timewalk correction the problem is still there
On pad 23 is difficult to see it because of the scale, but it’s there

## Slide 41: Combining different pads
RMS weighted
SAT combined using:
Max e-peak charge
E-peak charge weighted