## Slide 1
Solid state detectors
a brief working principles overview
Piero Giubilato – V Scuola Nazionale Legnaro – 15 Apr 2013

## Slide 2
1
Solid state detectors – overview
A bit of history
CCDs, CMOs practical detectors
Some detector properties
7
6
Basic solid state
Extrinsic semiconductors
2
4
PN junction
5
3
Intrinsic semiconductors

## Slide 3
Solid state detectors – history
1
Actually, film is a solid state detector
Silver Halides
Pixel
50 ISO
0.5 um
100 ISO
1 um
200 ISO
3 um

## Slide 4
Solid state detectors – history: silver halides
2
γ
e-
hν
Ag X
Ag Br
Ag Cl
Ag I
AgV- + hν → AgV + e-
AgI+ + e- → AgI
Frenkel defects
Ideal lattice
1.16 eV formation
0.05 eV mobility
Silver halides

## Slide 5
Solid state detectors – history: the dark side of the moon
3
Luna 3 - 1959
Film main limits:
It doesn’t generate an electric signal
It is single use, you need a lot of it!
Need mechanics.
The dark side of the Moon, first shot
Yenisey camera system

## Slide 6
Basics – crystals
1
Si lattice, TEAM microscope
Si ore
Si lattice, diamond cubic

## Slide 7
Basics – density of states function
2
MC = equivalent minima
mde = (m*1m*2m*3)1/3
m*x = effective mass
h = Planck constant
The density of states function describes the bands energy levels structure defined by the physical properties of the crystal.

## Slide 8
Basics – electron wave equation
3
Schrodinger equation in 1D, time-independent potential (non relativistic)
Variables separation to split space-dependent and time-dependent parts
cost
space
time
This depends upon the material lattice properties for an electron moving inside a crystal

## Slide 9
Basics – electron wave equation meaning
4
is complex, no direct physical meaning:
1
But the associated probability density function (Bohr) gives the chances of finding an electron at a given position and time :
2
Since represents the probability density function, for a single particle it musts hold the boundary condition:
3

## Slide 10
Basics – Fermi-Dirac distribution
5
EF = Fermi level (µ)
K = Boltzmann constant
T = temperature (kelvin)
Fermi-Dirac statistics describes semi-integer spin particles (which obey to Pauli exclusion principle) distribution in a system respect to their energy.

## Slide 11
Basics – semiconductor outlook
6
f(E) gives the probability
that a state is occupied
T = 0
T > 0
T > 0
N(E) gives where
Available states are
Electrons live inside the lattice

## Slide 12
Semiconductors – some naming conventions
Nc effective conduction states density [1/cm3]
1
n0 negative carriers densities [1/cm3]
Ex energy levels in eV
fF is the Fermi-Dirac probability distribution
gx(E) is the density of states
Nv effective valence states density [1/cm3]
p0 positive carriers densities [1/cm3]
T > 0
How many?

## Slide 13
Intrinsic – and quantities
2
Fermi-Dirac
probability
function
Density of quantum states in conduction band
Electrons in
conduction
band
Fermi-Dirac
probability
function
Holes in
valence
band
Density of
quantum states
in valence
band
The lattice structure defines the density of quantum states function g(E), which describes the bands structure, while Fermi-Dirac statistics describes the states occupation.

## Slide 14
Intrinsic – carrier densities and at equilibrium
3
Electrons/dE in conduction band
Holes/dE in valence band
Integrating aover the respective energy bands returns the total number of electron/holes in the conduction/valence band respectively.
Permitted energy levels overlaps forming bands
Total electrons in conduction band
Total holes in valence band

## Slide 15
Intrinsic – expression of and
4
Within 5% as long as
Let use Boltzmann approximation to express
Let also recall the form of and
Effective electron/hole mass. Accounts for interactions inside the lattice, both with ions and with other carriers.

## Slide 16
Intrinsic – calculating
5
States density in band
Fermi dist.
Set
Effective states density
Gamma function
at 300k

## Slide 17
Intrinsic – calculating
6
States density in band
Fermi dist.
Set
Effective states density
Gamma function
at 300k

## Slide 18
Intrinsic – some material dependent values
7
Material | Nc | Nv |  | 
Si | 2.8 × 1019 cm-3 | 1.04× 1019 cm-3 | 1.08 | 0.56
GaAs | 4.7 × 1017 cm-3 | 7.0 × 1018 cm-3 | 0.067 | 0.48
Ge | 1.04 × 1019 cm-3 | 6.0 × 1018 cm-3 | 0.55 | 0.37
Material | Nc | Nv |  | 
Si | 2.8 × 1019 cm-3 | 1.04× 1019 cm-3 | 1.08 | 0.56
GaAs | 4.7 × 1017 cm-3 | 7.0 × 1018 cm-3 | 0.067 | 0.48
Ge | 1.04 × 1019 cm-3 | 6.0 × 1018 cm-3 | 0.55 | 0.37

## Slide 19
Intrinsic – in intrinsic semiconductors
8
These expressions for aare valid for an intrinsic semiconductor at thermal and electric equilibrium.
Material | ni | Eg
Si | 1.5 × 1010 cm-3 | 1.12 eV
GaAs | 1.8 × 106 cm-3 | 1.43 eV
Ge | 2.4 × 1013 cm-3 | 0.67 eV
At equilibrium,
Bandgap energy

## Slide 20
Intrinsic – in intrinsic semiconductors
9
Plot versus temperature for different semiconductors.
1018
1017
1016
1015
1014
1013
1012
1011
1010
109
108
107
106
-20
27
100
200
500
1000
0
1500
Ge
Si
GaAs
[1/cm3]
[Celsius]

## Slide 21
Intrinsic – validity range of calculations
10
The range of validity of the Boltzmann approximation we used sets the limits within the derived values of and are valid.
Within 5% for
The value (≈ 1.24x10-20 J/K = ≈ 0.074 eV at 300K) means that:
3kT
3kT
Validity range for EF
being not to close (3kT) to Ec or Ev
Ec-EF > 3kT : ND < 1.6  1018 cm–3
EF-Ev > 3kT. NA < 9.1  1017 cm–3

## Slide 22
Intrinsic – position of EF in intrinsic semiconductors
11
To calculate the position of within the bandgap, let recall that in an intrinsic semiconductor at equilibrium:
Midgap energy
In words: EF shifts respect the bandgap middle in order to maintain the number of electrons and holes balanced ( and both depend on the density of respective state function!)

## Slide 23
Intrinsic – position of EF in intrinsic silicon
12
As an example, we calculate the position of in silicon at 300 K. Effective carriers masses in silicon are:
Silicon bandgap is about 1.12 eV: in many cases we can therefore approximate EF for silicon (at room temperature) being at 560 meV
silicon

## Slide 24
Extrinsic – material doping
1
After discussing the properties of an intrinsic semiconductor, we now consider the effect of adding impurities of different materials to the semiconductor lattice
Nd Donor impurities density [1/cm3]
nd extrinsic negative carriers densities [1/cm3]
Na acceptor impurities density [1/cm3]
pa extrinsic positive carriers density [1/cm3]

## Slide 25
Let focus on two classes of materials: material with 5 electrons in the outermost shell (group V elements) and materials with 3 electrons in the outermost shell (group III elements).
Extrinsic – silicon lattice with added impurities (doping)
2

## Slide 26
Doped silicon at T > 0
Both thermally generated and dopant introduced carriers are available for conduction
Pure silicon at T > 0
Appearance of thermally generated electrons and holes carriers
Extrinsic – qualitative impurities and temperature effect
3
Two major effects have to be considered at first: the change of the lattice properties due to the impurities introduction and the effect of temperature on the introduced electron/holes. At T = 0 nothing so exciting happens!
Pure silicon at T = 0
No free carriers (in an ideal lattice)
Doped silicon at T = 0
Impurities electrons/holes are bound to their atom, and cannot contribute to conduction.

## Slide 27
Extrinsic – impurities intrinsic energy levels
4
Both electrons from donor materials and holes from acceptor materials sits in well defined energy levels, Ed and Ea. IMPORTANT: Ed and Ea are single, well defined levels as long as the densities of impurities Nd and Na are small enough such that there is no interaction between the impurities carriers themselves
nd electrons = Nd @ T = 0
pa holes = Na @ T = 0
Electrons are rendered in gray as they are in electrical equilibrium as long as they sit on their original energy level Ed. They CANNOT act as carriers in this condition.
Holes are rendered in gray as they are in electrical equilibrium as long as they sit on their original energy level Ea. They CANNOT act as carriers in this condition.

## Slide 28
Extrinsic – impurities ionization
5
Electrons in excess from donor materials and holes from acceptor materials have a binding energy which must be overridden before the become available carriers.
nd electrons
Ionized donors
Nd+ = Nd - nd
Thermally generated electrons and holes
pa holes
Ionized acceptors
Na+ = Na - pa

## Slide 29
Extrinsic – impurities ionization energy
6
Applying first quantization rules (Bohr’s atom model) it is possible to derive with good precision the ionization energy for the electrons.
Dopant | Ionization Energy [eV] | 
 | In Si | In Ge
Intrinsic | 1.12 | 0.67
Phosphorous | 0.045 | 0.0120
Arsenic | 0.049 | 0.0127
Boron | 0.045 | 0.0104
Aluminum | 0.060 | 0.0102
Gallium | 0.065 | 0.0110
Forces balance
Kinetic energy
Potential energy
Total energy
Momentum
quantization
Radius
quantization
Bohr radius

## Slide 30
Extrinsic – donors/acceptors probability function
7
Donors and acceptors from dopant impurities densities are described by the very same Fermi-Dirac probability distribution.
Ionized donors
Ionized acceptors
Electrons in the energy level Ed
Holes in the energy level Ea
Donors
density
Acceptors
density
We are actually interested in the ionized donors/acceptors, as they are carriers which become available for conduction

## Slide 31
Extrinsic – ionized donors/acceptors at room temperature
8
At room temperature (T = 300) acceptor/donors are mostly ionized, i.e. actually available as free carriers populating the valence/conduction band.
Boltzmann approx.
2.8×1019 cm3
2×1016 cm3
-0.045 eV
At room temperature 99.6% of the donors electrons are ionized, and therefore contribute to conduction. The same happens for holes.

## Slide 32
Extrinsic – deriving and from doping levels
9
T = 300 k
Nd = 1016 cm-3
Na=0 cm-3
ni=1.5×1010 cm-3
Calculate carriers densities at thermal equilibrium with:
Minority carriers decrease! Electrons redistribution among energy bands
Complete ionization

## Slide 33
Extrinsic – balance visualized
10
Visualizing previous example: in such a case we are “adding” only donors, so we will have electrons at the donors energy level, but no acceptors.
Thermally
generated electrons and holes
nd electrons
Ionized donors
Nd+ = Nd - nd
}
donors Eg ≈ 0.045 eV
A few donor annihilate some intrinsic holes
decreases!

## Slide 34
Extrinsic – doping moves the Fermi energy level
11
Added impurities change the lattice properties, shifting the Fermi energy level respect its position in a pure semiconductor.

## Slide 35
Extrinsic – doping moves the Fermi energy level
12
Added impurities change the lattice properties, shifting the Fermi energy level respect its position in a pure semiconductor.

## Slide 36
Extrinsic – position of EF in doped semiconductors
13
The position of within the bandgap changes with doping. Calling back equations derived for carriers concentration at thermal equilibrium:
If ,
If ,
n
p

## Slide 37
Extrinsic – assumption behind our model
14
Degenerate semiconductors: if the donors/acceptors density is too large, there is interaction between donor carriers, which hence distribute themselves indo band levels. The approximation of a single energy level for impurities is therefore no valid anymore.
No more one single level, but a bands filled semi-continuum
No more one single level, but a bands filled semi-continuum

## Slide 38
Extrinsic – material doping overview
15
By doping the material by adding donors (electrons with V group material) and/or acceptors (holes with III group materials) the carriers densities will change, , but at equilibrium it will hold:
Thermally
generated electrons and holes
nd electrons
pa holes
Ionized donors
Nd+ = Nd - nd
Ionized acceptors
Na+ = Na - pa
}
donors Eg ≈ 0.045 eV in Si
}
acceptors Eg ≈ 0.045 eV in Si
A few donor annihilate some intrinsic carriers

## Slide 39
Extrinsic – balance at equilibrium
16
nd electrons
pa holes
Ionized donors
Nd+ = Nd - nd
Ionized acceptors
Na- = Na - pa
Charge neutrality:
Complete ionization:
Carriers balance:
Holes left by ionized donors (e- promoted in c-band)
e- left by ionized acceptors (holes promoted in v-band)

## Slide 40
Extrinsic – balance is temperature dependent
17
strognly depends on T: i.e. using the previous value for ND = 1016
Extrinsic
Intrinsic
Partial ionization

## Slide 41
PN Junction – depletion
Exposed lattice ions due to ionized carriers
Let start with one p doped and one n doped semiconductor regions.
Fermi levels are shifted from the intrinsic position accordingly to the doping levels
1

## Slide 42
PN Junction – depletion
By mating the two regions, the Fermi level uniforms through the material.
The Fermi level is constant across the whole material
2

## Slide 43
At equilibrium the diffusion due to carrier density is balanced by the electric field due to “uncovered” ions in the lattice. Carriers can move, lattice ions cannot!
PN Junction – depletion
3
The equilibrium is actually reached through free carriers redistribution
E
Be aware: carriers mutually screen their charge, they DO NOT annihilate physically (holes DO NOT exist as physical particles!)

## Slide 44
PN Junction – energy levels
4
25 mV
Vbi
Mating two differently doped semiconductor regions forces the Fermi energy level to uniform across the resulting body, as the system must stay in thermal equilibrium.

## Slide 45
PN Junction – carriers
5
In a thermal equilibrium system, EF is constant
Majority carriers
Minority
carriers
Majority carriers
Minority
carriers
p
EF
n
EF
p
EF
n
EF
EC
EV
EI
EC
EI
EF
EF
EV

## Slide 46
p
n
Depletion region
p
n
Direct bias
E = 0
p
n
Reverse bias
Depletion region
E
E
PN Junction – depletion
6

## Slide 47
1969 at AT&T Bell Labs by Willard Boyle and George E. Smith. They were working on a semiconductor bubble memory, and called their design 'Charge "Bubble" Devices'.
2009 Physics Nobel prize
Detectors – the Cahrge Coupled Device
1

## Slide 48
γ
E
+V
_
+
The CCD basic building block is a MOS capacitor
Insulator
Gate
-V
Capacitor
Detectors – CCD detection 1
2

## Slide 49
By shaping the potential is possible to trap and move the collected charge
-V
-V
+V
Detectors – CCD detection 2
3

## Slide 50
Detectors – CCD readout 1D
4

## Slide 51
Detectors – CCD readout 2D
5

## Slide 52
Full frame
Needs mechanical shutter to shield pixel from light during readout
Frame transfer
It is formed by two CCDs: the shielded is used as a storage frame. Expensive!
Interline
Sensitive and shielded storage regions alternate by column. Low fill factor
Detectors – CCD 2D array implementations
6

## Slide 53
+
_
All clocks and different voltages have to be generated outside the chip.
Detectors – CCD feeding
7

## Slide 54
γ
_
+
E
Detectors – The CMOS active pixel 1
OFF
OFF
OFF
Accumulates the generated charge into the collection node
Integrate
Active electronic elements are embedded into each detection element
8

## Slide 55
ON
OFF
Reset
The stored charge is drained through the reset node
OFF
Detectors – The CMOS active pixel 2
OFF
ON
ON
The stored charge modulates a current into the periphery. Each cell is address by MOS switches.
Read
9

## Slide 56
20 μm
20 μm
Clocked comparator with current threshold
Clocked current amplifier
“Digital” pixel
Analog 3T pixel
Detectors – The CMOS active pixel 2
10

## Slide 57
All this digital electronic is embedded into the chip itself
Detectors – readout layout
OFF
ON
ON
Integrate
OFF
OFF
OFF
Read
ON
OFF
Reset
11

## Slide 58
Digital level clocking and power supply.
Detectors –CMOS feeding
12

## Slide 59
Requires special process
More external components
More power hungry
Low noise (no in-electronic)
Higher resolution
100% fill-factor for FF
More noisy
Less dynamic range
Lower resolution (maybe)
Uses standard CMOS process
Camera-on-a-chip capable
Low power design available
CMOS
CMOS
Detectors –CMOS and CCD compared
13

## Slide 60
Sensitive
area
Detectors – Fill factor
Which parts of the device screen the incoming radiation actually depends on the radiation type and energy.
In case of visible photons we can use microlenses to increase the fill factor
14

## Slide 61
The global sensitivity is the quantum efficency multiplied by the fill-factor
Detectors – quantum efficiency in photons detection
15

## Slide 62
To reduce the amount of material incoming radiation pass through before reaching the depleted region, it is possible to thin and illuminate the device from the back.
Detectors – back illumination
16

## Slide 63
Thermal energy is enough to promote carriers into the conduction band, even without external light.
Thermally promoted electron: noise
Detectors – thermal noise
e-/p/s
Temperature (k)
~ factor 2 every 6k
17